Table 1. Qualitative and quantitative characteristics of coumarone-indene-containing raw materials
	Component
	Structural formula
	Content [wt. %]

	
	
	Fraction
140-190 °С
	Fraction
140-200 °С

	Methylbenzene
(toluene)
	

	4,44
	7,34

	Ethylbenzene
	

	1,98
	–

	1,4-Dimethylbenzene
(p-xylene) 
	

	27,61
	39,40

	1,3-Dimethylbenzene
(m-xylene)
	

	
	

	1,2-Dimethylbenzene
(o-xylene)
	

	5,15
	8,26

	Methylbenzene (toluene)
	

	1,46
	–

	Ethenylbenzene
(styrene)
	

	18,13
	3,86

	1-Methyl-2-ethylbenzene
	

	–
	2,11



Continuation of table 1
	1,3,5-Trimethylbenzene
 (mesitylene)
	

	0,33
	–

	2,3-Dimethyloctane
	

	3,81
	–

	1,2,4-trimethylbenzene
(pseudocumene)
	

	4,31
	2,69

	2,3-Benzofuran
(coumarone)
	

	1,65
	2,69

	Benzocyclopentadiene
(indene)
	

	22,15
	27,24

	1,2,4,5-Tetramethylbenzene
(durene)
	

	–
	1,11

	Naphthalene
(naphthalin)
	

	2,08
	3,54

	Other hydrocarbons1 and unidentified compounds
	–
	6,90
	1,76

	Total
	–
	100,00
	100,00

	Quantity of resin-forming2 components [wt. %]
	–
	41,93
	33,79

	The content of styrene in
resin-forming2 components [wt. %]
	–
	43,23
	11,42


Continuation of table 1
	The content of coumarone in resin-forming2 components [wt. %]
	–
	3,94
	7,96

	The content of indene in the resin-forming2 components [wt. %]
	–
	52,83
	80,62


1 – components, the content of which in all samples did not exceed 1.0% wt.
2 – styrene, coumarone, indene.
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