A dispersion-corrected DFT calculations on encapsulation of Favipiravir drug used as antiviral against COVID-19 into carbon-, boron-, and aluminum-nitride nanotubes for optimal drug delivery systems combined with molecular docking simulations

Roqaya Albarakati1, Ohoud Al-Qurashi2, Zaki Safi3, Nuha Wazzan1‡

1King Abdulaziz University, Chemistry Department, Faculty of Science, P.O. Box 4280, Jeddah 21589, Saudi Arabia.

2Department of Chemistry, Faculty of Science, University of Jeddah, Jeddah, Saudi Arabia

3Department of Chemistry, Faculty of Science, Al Azhar University-Gaza, P.O. Box 1277, Gaza, Palestine.

‡Corresponding author: nwazzan@kau.edu.sa (Nuha Wazzan)

Supplementary Data (SD)

Contents

Supplementary tables	2

Table SD 1: Comparison between some important geometrical parameters of the optimized FAV forms calculated at CPCM/B3LYP/6-31G(d,p( in water medium. Note: for more clarifications bond lengths and angles are represented in molecular structures.	2

Table SD 2: Relative total energies ∆E (in kJ/mol), electronic parameters (in eV), and dipole moments DM (in Debye) of FAV forms in gas and water at B3LYP-D with 6-31G(d,p) level of theory.	3

Table SD 3: BSSE energies, binding energies corrected/uncorrected with BSSE, and relative binding energies corrected with BSSE (in kJ/mol), difference (∆)  and recovery time (τ) at 298.15 K (in sec) computed at the B3LYP-D with 6-31G(d,p) level of theory.	3

Table SD 4: Thermodynamic parameters (in kJ/mol) of ES at CPCM/B3LYP-D/6-31G(d,p).	4

Supplementary figures	5

Figure SD 1: The linear relationship between the energy gaps and global hardness values as calculated at the CPCM/B3LYP-D/6-31G(d,p) level of theory.	5

Cartesian coordinates of optimized geometries of FAV forms at CPCM/B3LYP/6-31G(d,p) level of theory.	5

K2	5

E3	5

E1	6

E2	6

K1	7

# Supplementary tables

## Table SD 1: Comparison between some important geometrical parameters of the optimized FAV forms calculated at CPCM/B3LYP/6-31G(d,p( in water medium. Note: for more clarifications bond lengths and angles are represented on molecular structures.

| E2 |  | K2 |  | E3 |  |
| --- | --- | --- | --- | --- | --- |
| K1 |  |  | E1 |  |  |
| Bond length/angle | E1 | E2 | E3 | K1 | K2 |
| O9−H14 | 0.972 | 0.972 | 1.001 | − | − |
| N6−H14 | − | − | − | 1.015 | 1.015 |
| N6-C2 | 1.338 | 1.333 | 1.341 | 1.407 | 1.392 |
| C=O | 1.340 | 1.349 | 1.331 | 1.226 | 1.239 |
| C-F | 1.341 | 1.343 | 1.343 | 1.342 | 1.343 |
| N5-C2-O9 | 117◦ | 117◦ | 116.86◦ | 117◦ | 117◦ |
| N10-C8-O13 | 123.7◦ | 123◦ | 123.5◦ | 123.4 | 124 |

A close look at the structures, both E1 and E3 are the same structure in which E1 form has the O-H cis to the N atom of pyrazine ring, while it is a trans for E3 form with a distance of 0.972 and 1.001 Å, respectively. However, the five forms of FAV are different in the terminal amine (NH2) and carbonyl (C=O) groups, in which the structure of K1 and E3 (E1) are tautomers to each other, and they have the C=O at the right side with a value of N-C-O angle about 124°. Whereas the two other forms K2 and E2 are tautomers to each other and have the NH2 in the right side with a value of N-C-O angle of 124° and 123° , respectively. Moreover, the movement of the H atom between the N and O atomic sites through the keto-enol tautomerism could result in significant changes. For instance, the O-H bond length of E2 form is 0.971 Å while it increases to 1.001 Å for E3 form. Whereas the N-H which are fixed at 1.015 Å. Besides, the bond lengths in E3 form, N-C and C=O are 1.341 and 1.331 Å, while those of K1 form are 1.407 and 1.226 Å, respectively. Likewise, the bond lengths of C=O and N-C in E2 form are 1.349 and 1.333 Å, but those for the K2 form become shorter for C=O by 0.11 (1.239 Å) and longer for N-C (1.392 Å). Also, the angle of N-C-O of K1/K2 (120°) is greater than E3/E2 (116.8°). Furthermore, for all tautomers the C-F length is fixed at 1.343 Å.

## Table SD 2: Relative total energies ∆E (in kJ/mol), electronic parameters (in eV), and dipole moments DM (in Debye) of FAV forms in gas and water at B3LYP-D with 6-31G(d,p) level of theory.

| Medium | form | ∆E | EHOMO | ELUMO | Eg | DM | η |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Gas | E3 | 0.000 (0.000)[1] | −6.792 | −2.317 | 4.475 | 4.545 | 2.238 |
|  | E1 | 40.987 | −6.818 | −2.220 | 4.597 | 2.447 | 2.281 |
|  | K2 | 50.417 | −6.719 | −2.669 | 4.050 | 5.909 | 2.009 |
|  | E2 | 50.739 | −6.888 | −2.176 | 4.713 | 5.581 | 2.338 |
|  | K1 | 66.422 | −6.463 | −2.639 | 3.824 | 5.320 | 1.897 |
| Water | E3 | 0.000 (0.000)[1] | −6.778 | −2.261 | 4.517 | 4.545 | 2.259 |
|  | K2 | 23.955 | −6.506 | −2.531 | 3.975 | 8.070 | 1.987 |
|  | E1 | 33.924 | −6.861 | −2.166 | 4.696 | 3.454 | 2.348 |
|  | E2 | 36.510 | −7.009 | −2.151 | 4.858 | 7.476 | 2.410 |
|  | K1 | 36.930 | −6.416 | −2.544 | 3.872 | 7.649 | 1.921 |

## Table SD 3: BSSE energies, binding energies corrected/uncorrected with BSSE, and relative binding energies corrected with BSSE (in kJ/mol), difference (∆)  and recovery time (τ) at 298.15 K (in sec) computed at the B3LYP-D with 6-31G(d,p) level of theory.

|  | System | EBSSE | Binding energy |  | 1∆ | Corrected relative binding energy with BSSE (∆EbindBSSE) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Uncorrected with BSSE (Ebind) | Corrected with BSSE (EbindBSSE) |  |  |
| Gas | K2/AlNNT | 0.03393 | −273.801 | −184.724 | 89.077 | 0.000 |
|  | E3/AlNNT | 0.03028 | −230.999 | −151.503 | 79.496 | 33.221 |
|  | K2/BNNT | 0.03841 | −224.890 | −124.014 | 100.876 | 60.710 |
|  | E3/BNNT | 0.03762 | −197.108 | −98.324 | 98.784 | 86.400 |
|  | K2/CNT | 0.03086 | −176.900 | −95.855 | 81.044 | 88.868 |
|  | E3/CNT | 0.02876 | −143.888 | −68.367 | 75.521 | 116.357 |
| Aqueous | K2/AlNNT | 0.036 | −402.292 | −308.821 | 93.471 | 0.000 |
|  | E3/AlNNT | 0.0310 | −249.157 | −167.611 | 81.546 | 141.210 |
|  | K2/BNNT | 0.0385 | −221.878 | −120.750 | 101.128 | 188.071 |
|  | E3/BNNT | 0.038 | −195.351 | −96.316 | 99.035 | 212.505 |
|  | K2/CNT | 0.0313 | −175.268 | −93.094 | 82.174 | 215.727 |
|  | E3/CNT | 0.0287 | −143.009 | −67.572 | 75.44 | 241.249 |
| 1∆=EbindBSSE-Ebind |  |  |  |  |  |  |

## Table SD 4: Thermodynamic parameters (in kJ/mol) of ES at CPCM/B3LYP-D/6-31G(d,p).

| System | ∆Hbind | ∆Gbind | ∆Sbind |
| --- | --- | --- | --- |
| K2/AlNNT | −903.311 | −834.757 | −0.230 |
| E3/AlNNT | −849.764 | −790.604 | −0.198 |
| K2/BNNT | −797.848 | −733.654 | −0.215 |
| E3/BNNT | −782.895 | −716.649 | −0.222 |
| K2/CNT | −840.567 | −770.217 | −0.236 |
| E3/CNT | −821.141 | −752.999 | −0.229 |

# Supplementary figures

## Figure SD 1: The linear relationship between the energy gaps and global hardness values as calculated at the CPCM/B3LYP-D/6-31G(d,p) level of theory.

# Cartesian coordinates of optimized geometries of FAV forms at CPCM/B3LYP/6-31G(d,p) level of theory.

## K2 form

| Atom | X | Y | Z |
| --- | --- | --- | --- |
| C | -2.144904 | 0.785396 | 0.000011 |
| C | 0.242361 | 1.277484 | 0.000024 |
| C | 0.426593 | -0.180897 | -0.000027 |
| C | 1.803859 | -0.823563 | -0.000038 |
| C | -1.836925 | -0.548198 | -0.000045 |
| F | -2.823784 | -1.459154 | -0.000074 |
| N | -0.591908 | -1.014683 | -0.000057 |
| N | -1.099646 | 1.648523 | 0.000051 |
| N | 2.839614 | 0.041684 | -0.000040 |
| O | 1.124932 | 2.147623 | 0.000095 |
| O | 0 1.927277 | -2.047870 | 0.000062 |
| H | 3.777075 | -0.332102 | 0.000060 |
| H | 2.663253 | 1.042283 | -0.000011 |
| H | -1.276804 | 2.648356 | 0.000102 |
| H | -3.149469 | 1.185830 | 0.000034 |

## E3 form

| Atom | X | Y | Z |
| --- | --- | --- | --- |
| C | 2.092683 | 0.874117 | 0.000051 |
| C | -0.156089 | 1.258295 | 0.000077 |
| C | -0.389206 | -0.138489 | -0.000048 |
| C | 1.839333 | -0.503516 | -0.000036 |
| C | -1.785970 | -0.662119 | -0.000266 |
| F | 2.870497 | -1.361567 | -0.000075 |
| N | -1.922433 | -1.993436 | 0.000301 |
| N | 0.631641 | -1.008986 | -0.000072 |
| N | 1.092307 | 1.748462 | 0.000072 |
| O | -1.150376 | 2.144107 | 0.000099 |
| O | -2.752159 | 0.130950 | -0.000229 |
| H | -1.105190 | -2.586464 | 0.000420 |
| H | -2.844819 | -2.402532 | 0.000344 |
| H | -1.990873 | 1.600185 | 0.000128 |
| H | 3.111575 | 1.250454 | 0.000060 |

## E1 form

| Atom | X | Y | Z |
| --- | --- | --- | --- |
| C | 2.120916 | 0.792749 | -0.000345 |
| C | -0.120602 | 1.279848 | -0.000008 |
| C | -0.436895 | -0.099193 | 0.000301 |
| C | -1.846261 | -0.640520 | 0.000740 |
| C | 1.795056 | -0.563824 | -0.000034 |
| F | 2.773358 | -1.481301 | -0.000066 |
| N | 0.559800 | -0.998871 | 0.000259 |
| N | 1.149705 | 1.700826 | -0.000321 |
| N | -1.911881 | -1.991402 | 0.000200 |
| O | -1.073122 | 2.222967 | 0.000067 |
| O | -2.835372 | 0.091736 | -0.000368 |
| H | -1.071636 | -2.549419 | -0.000224 |
| H | -2.817088 | -2.435220 | -0.000894 |
| H | -0.612769 | 3.080119 | -0.000139 |
| H | 3.152569 | 1.130372 | -0.000627 |

## E2 form

| Atom | X | Y | Z |
| --- | --- | --- | --- |
| C | 2.105686 | 0.870063 | -0.000046 |
| C | -0.152068 | 1.209282 | 0.000052 |
| C | -0.396216 | -0.183763 | 0.000025 |
| C | 1.855898 | -0.502678 | -0.000077 |
| C | -1.753832 | -0.868078 | 0.000060 |
| F | 2.891362 | -1.357471 | -0.000135 |
| N | 0.653187 | -1.018889 | -0.000040 |
| N | 1.080408 | 1.718041 | 0.000017 |
| N | -2.841454 | -0.065477 | -0.000175 |
| O | -1.175676 | 2.088583 | 0.000094 |
| O | -1.826318 | -2.095673 | 0.000287 |
| H | -3.749070 | -0.506613 | -0.000174 |
| H | -2.772563 | 0.941351 | -0.000332 |
| H | 3.115011 | 1.268949 | -0.000076 |
| H | -0.801479 | 2.985578 | 0.000060 |

## K1 form

| Atom | X | Y | Z |
| --- | --- | --- | --- |
| C | 2.178707 | 0.668307 | -0.000070 |
| C | -0.175428 | 1.378590 | 0.000057 |
| C | -0.472467 | -0.064664 | 0.000036 |
| C | 1.759699 | -0.634592 | -0.000069 |
| C | -1.900472 | -0.562702 | 0.000034 |
| F | 2.658116 | -1.632616 | -0.000131 |
| N | 0.475429 | -0.980602 | -0.000016 |
| N | 1.212392 | 1.616076 | -0.000010 |
| N | -2.008540 | -1.912262 | 0.000493 |
| O | -0.953929 | 2.326731 | 0.000071 |
| O | -2.870286 | 0.194412 | -0.000325 |
| H | -1.187745 | -2.497931 | 0.000199 |
| H | -2.928125 | -2.325090 | -0.000059 |
| H | 3.215135 | 0.978842 | -0.000113 |
| H | 1.476207 | 2.596456 | -0.000007 |

References

1.	Antonov, L., Favipiravir tautomerism: a theoretical insight. Theoretical Chemistry Accounts, 2020. 139(8): p. 1-7.