Synthesis, structural characterization and Hirshfeld surface analysis of 
3-acetylpyridinium and 4-acetylpyridinium picrate crystals

Loganathan Guganathan 1 • Chellakarungu Balakrishnan 2 • Palusamy Suppuraj2
Venkataraman Balasubramanian 3*

1 Department of Physics, Annamalai University, Annamalainagar-608002, Tamil Nadu, India.

2 Department of Chemistry, Erode Sengunthar Engineering College, Erode - 638057, Tamil Nadu, India.

3 Department of Physics, Sona College of Technology, Salem-636005, Tamil Nadu, India.

Supplementary Figures

Fig. S1 3D space-filling view along b-axis (a) ladder like architecture for (I) and (b) layered 	architecture for (II)

Fig. S2 FT-IR spectra for (I) and (II)

Fig. S3 Percentage contributions to the Hirshfeld surface areas for the various close 	intermolecular contacts for (I) and (II)

Supplementary Tables

Table S1. Selected bond lengths (Å), angles and Torsion angles (°) for (I).

Table S2. Selected bond lengths (Å), angles and Torsion angles (°) for (II).

Fig. S1 3D space-filling view along b-axis (a) ladder like architecture for (I) and (b) layered architecture for (II)

b

a

Fig. S2 FT-IR spectra

I

II

Fig. S3 Percentage contributions to the Hirshfeld surface areas for the various close intermolecular contacts for (I) and (II)

Table S1. Selected bond lengths (Å), angles and Torsion angles (°) for (I).

| Bond lengths (Å) |  |  |  |
| --- | --- | --- | --- |
| O1-C2 | 1.212(2) | O6-N3 | 1.222(2) |
| O3-N2 | 1.229(2) | O8-N4 | 1.187(2) |
| O5-N3 | 1.224(2) | N1-C4 | 1.334(2) |
| O7-N4 | 1.214(2) | N2-C9 | 1.459(2) |
| N1-C5 | 1.336(2) | N4-C13 | 1.458(2) |
| N3-C11 | 1.4476(19) | C1-C2 | 1.491(3) |
| C2-C3 | 1.501(2) | C3-C4 | 1.385(2) |
| C3-C7 | 1.392(2) | C5-C6 | 1.372(3) |
| C8-C13 | 1.441(2) | C6-C7 | 1.382(3) |
| C11-C12 | 1.380(2) | C8-C9 | 1.452(2) |
| C12-C13 | 1.382(2) | C9-C10 | 1.364(2) |
| O2-C8 | 1.2527(19) | C10-C11 | 1.393(2) |
| O4-N2 | 1.214(2) |  |  |
| Bond angles (°) |  |  |  |
| C5-N1-C4 | 122.56(14) | C11-N3-O5 | 117.94(15) |
| C9-N2-O3 | 118.00(15) | O8-N4-O7 | 119.94(18) |
| O6-N3-O5 | 122.97(15) | C13-N4-O8 | 120.88(17) |
| C11-N3-O6 | 119.08(15) | C3-C2-O1 | 118.88(16) |
| C13-N4-O7 | 119.13(16) | C4-C3-C2 | 118.08(15) |
| C1-C2-O1 | 122.86(17) | C7-C3-C4 | 118.19(15) |
| C3-C2-C1 | 118.25(16) | C7-C6-C5 | 119.15(16) |
| C7-C3-C2 | 123.73(14) | C6-C7-C3 | 120.08(15) |
| C3-C4-N1 | 120.03(15) | C13-C8-O2 | 126.64(15) |
| C6-C5-N1 | 119.92(16) | C8-C9-N2 | 117.39(13) |
| C9-C8-O2 | 121.68(15) | C10-C9-C8 | 125.58(15) |
| C13-C8-C9 | 111.64(13) | C11-C10-C9 | 117.93(15) |
| C10-C9-N2 | 117.03(14) | C10-C11-N3 | 119.21(15) |
| C12-C11-N3 | 119.13(15) | C12-C11-C10 | 121.63(14) |
| C12-C13-N4 | 116.12(14) | C13-C12-C11 | 119.28(15) |
| O4-N2-O3 | 123.17(17) | C8-C13-N4 | 119.97(14) |
| C9-N2-O4 | 118.82(16) | C12-C13-C8 | 123.91(14) |
| Torsion angles (°) |  |  |  |
| O1-C2-C3-C4 | -4.9(2) | O1-C2-C3-C7 | 175.60(17) |
| O2-C8-C9-N2 | 2.82(19) | O2-C8-C9-C10 | -177.22(17) |
| O2-C8-C13-N4 | -3.7(2) | O2-C8-C13-C12 | 176.94(18) |
| O3-N2-C9-C8 | 50.15(18) | O3-N2-C9-C10 | -129.81(16) |
| O4-N2-C9-C8 | -131.12(18) | O4-N2-C9-C10 | 48.9(2) |
| O5-N3-C11-C10 | 12.5(2) | O5-N3-C11-C12 | -165.54(18) |
| O6-N3-C11-C10 | -168.50(17) | O6-N3-C11-C12 | 13.5(2) |
| O7-N4-C13-C8 | 166.3(2) | O7-N4-C13-C12 | -14.3(3) |
| O8-N4-C13-C8 | -11.3(3) | O8-N4-C13-C12 | 168.1(3) |
| N1-C4-C3-C2 | -178.85(15) | N1-C4-C3-C7 | 0.72(19) |
| N1-C5-C6-C7 | 0.4(2) | N2-C9-C8-C13 | -179.13(15) |
| N2-C9-C10-C11 | 178.76(15) | N3-C11-C10-C9 | -176.26(15) |
| N3-C11-C12-C13 | 176.07(15) | N4-C13-C8-C9 | 178.34(16) |
| N4-C13-C12-C11 | -177.79(15) | C1-C2-C3-C4 | 174.09(18) |
| C1-C2-C3-C7 | -5.4(2) | C2-C3-C7-C6 | -178.86(18) |
| C3-C7-C6-C5 | -2.1(2) | C8-C9-C10-C11 | -1.20(19) |
| C8-C13-C12-C11 | 1.57(19) | C9-C10-C11-C12 | 1.69(19) |
| C10-C11-C12-C13 | -1.89(19) |  |  |

Symmetry transformations used to generate equivalent atoms:

Table S2. Selected bond lengths (Å), angles and Torsion angles (°) for (II).

| Bond lengths (Å) |  |  |  |
| --- | --- | --- | --- |
| O1-C2 | 1.213(2) | O2-C8 | 1.2444(19) |
| O3-N2 | 1.205(2) | O4-N2 | 1.194(2) |
| O5-N3 | 1.214(2) | O6-N3 | 1.222(2) |
| O7-N4 | 1.223(2) | O8-N4 | 1.204(2) |
| N1-C6 | 1.324(2) | N1-C5 | 1.340(2) |
| N3-C11 | 1.450(2) | N2-C9 | 1.460(2) |
| C1-C2 | 1.477(3) | N4-C13 | 1.465(2) |
| C2-C3 | 1.519(2) | C3-C4 | 1.387(2) |
| C3-C7 | 1.390(2) | C4-C5 | 1.372(2) |
| C6-C7 | 1.382(2) | C8-C9 | 1.446(2) |
| C8-C13 | 1.447(2) | C9-C10 | 1.378(2) |
| C10-C11 | 1.383(2) | C12-C13 | 1.363(2) |
| C11-C12 | 1.381(2) |  |  |
| Bond angles (°) |  |  |  |
| C6-N1-C5 | 122.41(14) | O4-N2-O3 | 120.70(17) |
| O4-N2-C9 | 118.45(17) | O3-N2-C9 | 120.83(16) |
| O5-N3-O6 | 122.96(16) | O5-N3-C11 | 118.11(17) |
| O6-N3-C11 | 118.87(17) | O8-N4-O7 | 123.03(18) |
| O8-N4-C13 | 119.51(18) | O7-N4-C13 | 117.46(16) |
| O1-C2-C1 | 122.83(16) | O1-C2-C3 | 118.19(17) |
| C1-C2-C3 | 118.97(16) | C4-C3-C7 | 119.08(14) |
| C4-C3-C2 | 118.43(14) | C7-C3-C2 | 122.48(15) |
| C5-C4-C3 | 119.66(15) | N1-C5-C4 | 119.69(15) |
| N1-C6-C7 | 120.34(14) | C6-C7-C3 | 118.81(15) |
| O2-C8-C9 | 126.02(15) | O2-C8-C13 | 121.73(15) |
| C9-C8-C13 | 112.22(13) | C10-C9-C8 | 123.37(15) |
| C10-C9-N2 | 116.94(15) | C8-C9-N2 | 119.69(14) |
| C9-C10-C11 | 119.28(15) | C12-C11-C10 | 121.65(14) |
| C12-C11-N3 | 118.96(15) | C10-C11-N3 | 119.38(16) |
| C13-C12-C11 | 118.56(15) | C12-C13-C8 | 124.80(15) |
| C12-C13-N4 | 116.58(15) | C8-C13-N4 | 118.54(14) |
| Torsion angles (°) |  |  |  |
| O1-C2-C3-C4 | -16.4(3) | C1-C2-C3-C4 | 164.10(18) |
| O1-C2-C3-C7 | 162.36(18) | C1-C2-C3-C7 | -17.1(3) |
| C7-C3-C4-C5 | 0.0(3) | C2-C3-C4-C5 | 178.79(16) |
| C6-N1-C5-C4 | 0.3(3) | C3-C4-C5-N1 | -0.3(3) |
| C5-N1-C6-C7 | 0.1(3) | N1-C6-C7-C3 | -0.4(3) |
| C4-C3-C7-C6 | 0.4(2) | C2-C3-C7-C6 | -178.38(16) |
| O2-C8-C9-C10 | 174.68(19) | C13-C8-C9-C10 | -3.1(2) |
| O2-C8-C9-N2 | -5.0(3) | C13-C8-C9-N2 | 177.18(17) |
| O4-N2-C9-C10 | 1.8(3) | O3-N2-C9-C10 | 179.9(2) |
| O4-N2-C9-C8 | -178.5(3) | O3-N2-C9-C8 | -0.4(3) |
| C8-C9-C10-C11 | 0.8(3) | N2-C9-C10-C11 | -179.51(16) |
| C9-C10-C11-C12 | 1.2(3) | C9-C10-C11-N3 | -177.84(15) |
| O5-N3-C11-C12 | -178.60(19) | O6-N3-C11-C12 | -1.2(3) |
| O5-N3-C11-C10 | 0.5(3) | O6-N3-C11-C10 | 177.92(17) |
| C10-C11-C12-C13 | -0.5(3) | N3-C11-C12-C13 | 178.58(15) |
| C11-C12-C13-C8 | -2.4(3) | C11-C12-C13-N4 | -179.02(16) |
| O2-C8-C13-C12 | -173.95(18) | C9-C8-C13-C12 | 4.0(2) |
| O2-C8-C13-N4 | 2.6(3) | C9-C8-C13-N4 | -179.42(16) |
| O8-N4-C13-C12 | -149.9(2) | O7-N4-C13-C12 | 30.4(3) |
| O8-N4-C13-C8 | 33.2(3) | O7-N4-C13-C8 | -146.4(2) |

Symmetry transformations used to generate equivalent atoms: