Supplementary material

Table S1. Results of test of significance of factors and interaction for the model (⊍ = 0.05)

|  |  | Total carbohydrates model |  | Phenolic compounds model |  |
| --- | --- | --- | --- | --- | --- |
| Factor (coded) | Factors | p - value |  | p - value |  |
| A | Time | 0.1742 | not significant | < 0.0001 | significant |
| B | Sulfuric acid | < 0.0001 | significant | < 0.0001 | significant |
| C | Temperature | < 0.0001 | significant | < 0.0001 | significant |
| AB | _ | 0.6453 | not significant | < 0.0001 | significant |
| AC | _ | 0.0366 | not significant | < 0.0001 | significant |
| BC | _ | < 0.0001 | significant | < 0.0001 | significant |
| A2 | _ | < 0.0001 | significant | 0.0128 | significant |
| B2 | _ | < 0.0001 | significant | < 0.0001 | significant |
| C2 | _ | < 0.0001 | significant | < 0.0001 | not significant |
| ABC | _ | _ | _ | 0.0749 | significant |
| Model | _ | < 0.0001 | significant | < 0.0001 | significant |
| Lack of fit | _ | 0.3542 | Not significant | 0.4745 | not significant |
| R2 | _ | 0.9849 |  | 0.9754 |  |
| Adjusted R2 | _ | 0.9814 |  | 0.9688 |  |

S1. Confocal analysis methodology

Structural changes between untreated and hydrolyzed GP were appraised by a confocal laser scanning microscopy (CLSM). For CLSM, representative samples of untreated and hydrolyzed GP for all conditions were taken respectively. Particularly, for CLSM the samples were incubated with 2 markers in the dark for 30 minutes at room temperature. The markers used were safranin O at 1% w/v for lignin staining (green) ʎ emission/excitation 546/ 590 nm and Congo red for holocellulose. Then, the samples were centrifuged and washed with PBS 1X, and mounted for visualization on a fluorodish plate. The samples were visualized in three fluorescence channels using the FV1000 confocal laser microscope (Olympus, Japan), and then the images were analyzed (including the relative fluorescence unit (RFU) quantification) using the FV10 Olympus var 0.2c software.

Treatment 7

(120 min,15 %v/v H2SO4, 95°C)

Untreated Grape Pomace

1410±341 UFR

Treatment 8

(240 min,15 %v/v H2SO4, 95°C)

1359±161 UFR

Treatment 1

(120 min, 5 %v/v H2SO4, 65°C)

1894±144 UFR

1315±376 UFR

2044±178 UFR

1619±387 UFR

1416±57 UFR

1451±113 UFR

H

E

B

A

F

G

C

D

D

c

Figure S1. Confocal images for untreated grape pomace and treated grape pomace for treatment number 1,7 y 8. a-d) lignin (green colour) and e-h) cellulose (red colour)