Supplementary Information

Surface-Immobilized Cross-linked Cationic Polyelectrolyte Enables CO2 Reduction with Metal Cation-free Acidic Electrolyte

AUTHORS: Hai-Gang Qin, Yun-Fan Du, Yi-Yang Bai, Fu-Zhi Li, Hao Wang, Jian-Zhao Peng, Jun Gu *

AFFILIATION:

Department of Chemistry, Southern University of Science and Technology, Shenzhen, Guangdong 518055, China.

Corresponding author E-mail: guj6@sustech.edu.cn

SIMULATION SECTION

The one-dimensional stationary GMPNP simulation was done with COMSOL Multiphysics version 6.0. The General Form PDE module within COMSOL was used to build the size dependent Nernst Planck equation and the Poisson equation. Geometry of the simulation domain, partial differential equations, boundary conditions, mesh and solver for the finite element analysis are specified below. All parameters and coefficients used in the simulation are listed in Table S1.

Geometry

The geometry of simulation is shown in Figure S9a. The geometry is one-dimensional and consists of two domains. Domain 1 is x∈[0,Lp], corresponding to the polymer layer. Domain 2 is x∈(Lp,Ltot], corresponding to the diffusion layer out of the polymer layer. The thickness of the layer of c-PDDA on Ag MDE was around 1 μm based on the amount of polymer loaded onto the Ag MDE. Therefore, Lp was fixed at 1 μm in most simulations unless otherwise specified. Considering that radius of the Ag MDE (r0) is 12.5 μm, the effective thickness of the diffusion layer on this Ag MDE is π4r0,1 namely 9.8 μm. Therefore, Ltot was fixed at 9.8 μm in all simulations.

Size dependent Nernst Planck equations

Figure S9b shows the governing equations and boundary conditions used in the simulations. The size dependent Nernst Planck equation was given by:

∂Ci∂t=-∇∙Ji+Ri														(S1)

where the ∇ operator stands for d/dx, Ci is the concentration of solution specie i (i = H+, OTf-, and OH-), Ji is the flux of specie i and Ri is the production rate of specie i in homogeneous reactions. Ji was given by:

Ji=-DiCi∇(lnγiCi)-DiCiziFRT∇φ										(S2)

In this equation, Di, Ci and zi are the diffusion coefficient, concentration and charge of species i, respectively. φ is the potential, F is the Faradaic constant, R is the gas constant, T is the temperature (298 K). γi is the activity coefficient. The diffusion coefficients in the polymer layer (Domain 1) were set to 1/10 of the values in water (Domain 2) for each species, which is a commonly used assumption.2 γi in Equation S2 is given by:3

γi=11-Vp-NAi=1Nai3Ci														(S3)

In this equation, NA is the Avogadro’s number (6.023×1023 mol−1). ai is the effective solvated diameter of the species i. Vp is the volume fraction occupied by the polymer. Vp was set to 0 in the region out of the polymer layer (Domain 2). We observed that the volume of a layer of c-PDDA on a glass slide swelled to 2.8 times of the initial volume of this polymer layer when it was immersed in water (see “Measurements of charge density of c-PDDA” in the Methods Section in the main text for the procedure of the measurement). Therefore, Vp was set to 1/2.8 = 0.36 in the polymer layer (Domain 1). Then, Equation S2 is rewritten as:

Ji=-Di∇Ci-DiCiziFRT∇φ-DiCiNAai3∇Ci1-Vp-NAai3Ci								(S4)

The reversible reaction between H+ and OH− was considered in the simulation:

H2O kw1⇌kw2 H++OH- 														(S5)

where kw1 is the rate constant of water dissociation, kw2 is the rate constant of neutralization reaction. Thus, the Ri in Equation S1 is given by:

ROTf− = 0																(S6)

RH+ = ROH− = kw1 – kw2CH+COH−											(S7)

Boundary conditions of the size dependent Nernst Planck equations

OHP is defined as the origin of x axis. The left boundary condition (x = 0) of size dependent Nernst Planck equation is the flux Ji, which is built in COMSOL using the Flux/Source boundary. For OTf- and OH-, Ji is given by:

JClO4-, x=0=JOH-, x=0=0 												(S8)

For specie H+, Ji is given by:

JH+, x=0=jH+F 															(S9)

where jH+ is the current density of H+ reduction, The reduction current is defined as negative current. We assume H+ + e- → H* (Volmer step) is the rate determining step of H+ reduction, and this step is irreversible. Thus, the current density can be described as:

jH+=-Fk0CH+,x=0exp[-βFRT(φM-φ0'-φx=0)]							(S10)

In this equation, k0 is the standard rate constant and φ0’ is the formal potential of the rate determining step. β is the transfer coefficient. The term ‘−φx=0’ is introduced for the Frumkin correction. φ0’ is defined as:1

φ0'=φ0+RTFlnγH+														(S11)

In this equation, φ0 is the standard reduction potential of the rate determining step. γH+ is the activity coefficient of H+ according to Equation S3. We assume k0, β and φ0 are constants. Then, Equation S10 can be rewritten as:

jH+=-AγH+βCH+,x=0exp[-βFRT(φM-φx=0)]								(S12)

In this equation, A is a constant expressed as:

A=Fk0exp[βFRTφ0]														(S13)

The values of A and β were taken from our previous work on the GMPNP simulation of Ag rotating disk electrode.4

The right boundary (x = Ltot) condition is the concentration of species i in bulk solution, which is built in COMSOL using the Dirichlet Boundary Condition. Ci,x=Ltot is given by:

CH+,x=Ltot = 0.01 M														(S14)

COH−,x=Ltot = 10−12 M														(S15)

COTf−,x=Ltot = 0.01 M														(S16)

Poisson equation

The Poisson equation is utilized to model the electric field generated from the charged specie, which is built in COMSOL using the General Form PDE module. In the polymer layer (Domain 1), the Poisson equation is given by:

∇2φ=-FziCi+ρpε0εr														(S17)

Out of polymer layer (Domain 2), the Poisson equation is given by:

∇2φ=-FziCiε0εr															(S18)

In above equations, ρp is the charge density carried by the polymer layer, ε0 is the permittivity of vacuum and εr is the relative permittivity. The relative permittivity of water was used in both domains. The effect of the polymer on the relative permittivity was not considered in our simulation.

Boundary condition of Poisson equation

The left boundary (x = 0) condition of Poisson equation is the surface excess charge density of the cathode, which is built in COMSOL using the Flux/Source boundary. The surface charge density of the cathode σ is given by:

σ=-ε0εrφx=0-φMd 														(S19)

In this equation, φx=0 is the potential at OHP, φM is the potential at electrode, d is the thickness of Stern layer, which was set to 0.4 nm.

The right boundary (x = Ltot) is the potential of bulk solution, which is built in COMSOL using the Dirichlet Boundary Condition. The φx=Ltot is given by:

φx=Ltot = 0 V																(S20)

All potential values used in the simulation is on PZC scale. The PZC of polycrystalline Ag was reported to be -0.55 V vs SHE in acidic solution without specifically adsorbed anions.5 The simulated potential values were converted to SHE scale by subtracting 0.55 V.

Mesh and solver

The distribution type of mesh is set as predefined, the number of elements is 100000, the element ratio is 0.9999, and the exponential growth rate in reverse direction is selected. The coupled equations were solved with a commercial solver (COMSOL 6.0) utilizing a MUMPS solver with a non-linear automatic Newton method. The solution was converged when a relative tolerance of 0.001 was reached. Further increasing the relative tolerance resulted in a difference in the results of less than 1%.

Figure S1. (a, c) Survey XPS and (b,d) N 1s XPS spectra of (a, b) PDDA decorated Ag NPs and (c, d) c-PDDA decorated Ag NPs before (orange curves) and after (blue curves) CO2 electroreduction experiments. I element was detected in the as-prepared c-PDDA decorated Ag NPs, which was introduced from 1,6-diiodohexane. I element existed in the form of I- ions and were exchanged by SO42- ions during electrolysis in 0.1 M H2SO4, as indicated by that S element was detected in the c-PDDA decorated Ag NPs after electrolysis. The intensity of Ag peaks of c-PDDA decorated Ag NPs decreased drastically after electrolysis. This does not indicate the leaching of Ag, since ICP-MS measurement showed that Ag was not dissolved in the electrolyte. This observation can be ascribed to that the thickness of c-PDDA layer increased when the catalyst was immersed in water. The thicker layer of polymer inhibited the photoelectrons generated by Ag from being detected.

Figure S2. Procedure of the preparation of c-PDDA decorated catalyst.

Figure S3. Characterizations of the copolymer of DADMACl and DAMA. (a) Survey XPS spectrum. (b) N 1s XPS spectrum. The spectrum is deconvoluted into two peaks corresponding to tertiary amine sites (orange) and quaternary ammonium sites (blue). (c) 1H-NMR spectrum. The broadened peaks indicate the formation of polymer. Peaks with the chemical shift of 5~6 corresponding to CH2=CH- moieties disappeared, and peaks with the chemical shift of 1.2~1.7 corresponding to CH2 at the γ site of N (peak a) and CH at the β site of N appeared, confirming the polymerization reaction. (d) The distribution of molecular weight (MW) determined by GPC with water as the mobile phase. Mp, Mn, Mw and PDI represent peak MW, number averaged MW, weight averaged MW and polymer dispersity index, respectively.

Figure S4. (a, b) HAADF-STEM images of Ag NPs decorated by c-PDDA. (c-f) EDS mapping of the region in panel (b). (c) Ag channel, (d) N channel, (e) C channel and (f) merging of the three channels. The sample was peeled off from a piece of GDE and dispersed in ethanol with sonification. Carbon particles on the GDE were peeled off together with the catalyst. Therefore, Ag element and N element appear in the same region while C element appears in a larger region, as indicated in panel (f).

Figure S5. Chronopotentiometry curves of (a) c-PDDA decorated Ag NPs in 0.1 M H2SO4 and (b) bare Ag NPs in 0.1 M H2SO4 + 0.4 M K2SO4. The total current density was -200 mA·cm-2.

Figure S6. Characterizations of GDE with Ag NPs after CO2 electroreduction with 0.1 M H2SO4 + 0.4 M K2SO4 as the electrolyte. XRD patterns of (a) Ag/GDE after electrolysis and (b) bare GDE. The orange and blue vertical lines indicate the standard diffraction peaks of face-centered-cubic Ag (JCPDS card no. 04-0783) and monoclinic KHCO3 (JCPDS card no. 12-0292), respectively. (c) SEM image and (d-f) the corresponding EDS mapping images of the cross-section of Ag/GDE after electrolysis. Panels (d)-(f) show the distribution of C, Ag and K elements, respectively.

Figure S7. Characterizations of In NPs. (a) TEM image. (b) HAADF-STEM image. (c) XRD pattern. The vertical lines indicate the standard diffraction pattern of tetragonal In (JCPDS No. 05-0642).

Figure S8. Faradaic efficiency and electrode potential of CO2 reduction on c-PDDA decorated Ag NPs with 1 M H2SO4 as the electrolyte.

Figure S9. Faradaic efficiency and electrode potential of (a) bare Ag NPs and (b) bare In NPs by feeding CO2 and with 0.1 M H2SO4 as the electrolyte.

Figure S10. Schematic of the GMPNP simulation. (a) Geometry. (b) Governing equations and boundary conditions.

Figure S11. Simulated polarization curves of H+ reduction of Ag electrode covered by polymer layer with different ρp (unit: C·cm-3) in 10 mM HOTf. (b) is the magnification of (a).

Figure S12. Simulated pH profiles at -1.8 V vs SHE. Solid curves: Ag electrode covered by polymer layer with different ρp (unit: C·cm-3) in 10 mM HOTf. Dashed grey curve: bare Ag electrode in 10 mM HOTf + 40 mM KOTf.

Figure S13. Simulated effects of the thickness of polymer layer (Lp) on the properties of Ag electrode in 10 mM HOTf. (a) The migration rate of H+ at 2 μm from the OHP. (b) Plots of the electric field strength in Stern layer based on the electrode potential.

Table S1. Parameters and coefficients used in the GMPNP simulations.

| Parameter | Explanation | Value | Unit | Reference |
| --- | --- | --- | --- | --- |
| DH+ | Diffusion coefficient of H+ in water | 9.311×10−9 | m2·s−1 | 6 |
| DK+ | Diffusion coefficient of K+ in water | 1.957×10−9 | m2·s−1 | 6 |
| DOH− | Diffusion coefficient of OH- in water | 5.273×10−9 | m2·s−1 | 6 |
| DOTf− | Diffusion coefficient of OTf- in water | 0.863×10−9 | m2·s−1 | 7 |
| zH+ | Number of charges carried by H+ | +1 | 1 |  |
| zK+ | Number of charges carried by K+ | +1 | 1 |  |
| zOH− | Number of charges carried by OH- | −1 | 1 |  |
| zOTf− | Number of charges carried by OTf- | −1 | 1 |  |
| aH+ | Effective solvated size of H+ | 5.6×10−10 | m | 6 |
| aK+ | Effective solvated size of K+ | 6.62×10−10 | m | 6 |
| aOH− | Effective solvated size of OH- | 6×10−10 | m | 6 |
| aOTf− | Effective solvated size of OTf- | 6×10−10 | m | 7 |
| Vp | Volume fraction of polymer | 0.36 | 1 |  |
| Lp | Thickness of polymer layer | 1×10−6 | m |  |
| Ltot | Total length for simulation | 9.8×10−6 | m |  |

Figure S1 (continued). Parameters and coefficients used in the GMPNP simulations.

| Parameter | Explanation | Value | SI unit | Reference |
| --- | --- | --- | --- | --- |
| F | Faraday’s constant | 96485 | C·mol−1 |  |
| R | Gas constant | 8.314 | J·mol−1·K−1 |  |
| T | Temperature | 298.15 | K |  |
| NA | Avogadro’s number | 6.0221×1023 | mol−1 |  |
| kw1 | Rate constant of water dissociation | 0.0204 | mol·m−3·s−1 | 6 |
| kw2 | Rate constant of neutralization | 2.4×106 | mol−1·m3·s−1 | 6 |
| ε0 | Permittivity of vacuum | 8.8542×10−12 | F·m−1 | 6 |
| εr | Relative permittivity of water | 80.1 | 1 | 6 |
| d | Thickness of Stern layer | 4×10−10 | m | 6 |
| A | Pre-factor in Equation S12 | 5×10−9 | m·s−1 | 4 |
| β | Electron transfer coefficient | 0.42 | 1 | 4 |

REFERENCES

1	Bard, A. J. & Faulkner, L. R. Electrochemical methods: fundamentals and applications. 2nd. edn, (John Wiley & Sons, Inc., 2001).

2	Xu, Y. et al. Self-Cleaning CO2 Reduction Systems: Unsteady Electrochemical Forcing Enables Stability. ACS Energy Lett. 6, 809-815, (2021).

3	Wang, H., Thiele, A. & Pilon, L. Simulations of Cyclic Voltammetry for Electric Double Layers in Asymmetric Electrolytes: A Generalized Modified Poisson–Nernst–Planck Model. J. Phys. Chem. C 117, 18286-18297, (2013).

4	Qin, H.-G. et al. Quantitative Understanding of Cation Effects on the Electrochemical Reduction of CO2 and H+ in Acidic Solution. ACS Catal. 13, 916-926, (2023).

5	Bode, D. D., Andersen, T. N. & Eyring, H. Anion and pH effects on the potentials of zero charge of gold and silver electrodes. J. Phys. Chem. 71, 792-797, (1967).

6	Bohra, D., Chaudhry, J. H., Burdyny, T., Pidko, E. A. & Smith, W. A. Modeling the electrical double layer to understand the reaction environment in a CO2 electrocatalytic system. Energy Environ. Sci. 12, 3380-3389, (2019).

7	Vanýsek, P. Ionic conductivity and diffusion at infinite dilution, in Handbook of Chemistry and Physics. (CRC Press, 1992).