Supplementary Information (SI)

Enhancement in ionic conductivity of liquid crystals by graphene/metal-oxide-nanocomposite

M. Khodaee1, N. Dalir2, F. Feghhi3, N. Ansari3, M. Mohammadimasoudi4, A. Goudarzi4

, A. Faghih Nasiri1, M. Kolahdouz1*, S. M. Mohseni5**

1 School of Electrical and Computer Engineering, College of Engineering, University of Tehran, Tehran, Iran

2 Department of Renewable Energy, Interdisciplinary Science and Technology, Tarbiat Modares University, Tehran, Iran

3 Department of Physics, Alzahra University, Tehran, Iran

4 Nano-bio-photonics Lab, Faculty of New Sciences and Technologies, University of Tehran, Tehran, Iran

5 Department of Physics, Shahid Beheshti University, Evin, Tehran, Iran

Table 1S. The process of quantitative changes related to impedance value

| sample | Slope of impedance value in the part (I), (MΩ/Hz) Measured in the frequency range of (0.1Hz-1Hz) | quasi-constant impedance value in part (II), (MΩ) | Slope of impedance value in part (III), (MΩ/kHz) Measured in the frequency range of (1kHz-6.3kHz) |
| --- | --- | --- | --- |
| Pure E7 | -4.03 | 3.16 | -0.23 |
| 1 w% sample | -7.077 | 1.85 | -0.17 |
| 0.01 w% sample | -5.83 | 1.56 | -0.17 |
| 0.001 w% sample | -3.937 | 0.92 | -0.1 |
| 0.0001 w% sample | -3.301 | 0.64 | -0.071 |

The changes in slopes and impedance values in the first three parts have shown in table (1S). In part III, the decrease in the slopes of 1 w%, 0.01 w%, 0.001 w%, and 0.0001 w% samples compared to pure E7 are 35.29%, 35.29%, 56.52%, and 69.56%, respectively. In part I, we are facing a different trend. The response slopes for 1 w% and 0.01 w% samples increase compared to the pure E7. The increases are 75.6% and 44.66% for 1 w% and 0.01 w% samples, respectively. Therefore, at the frequency of 0.25 Hz, the impedance values of these two samples exceed the value of pure E7 response, and at the final frequency of 100mHz, the impedance values for 1 w% and 0.01 w% samples and pure E7 are 9.2 MΩ, 8.15 MΩ, and 7.34 MΩ, respectively. We have also examined suspension with a higher concentration of GMN dopant, in which both the frequency of overtaking of the response and the magnitude of the low-frequency impedance compared to pure E7 increase significantly above these values. Albeit, we did not find it necessary to present this result. At the opposite point, the response of 0.001 w% and 0.0001 w% samples are different, and their slopes are reduced compared to the pure E7 sample. The values of these slope reductions for 0.001 w% and 0.0001 w% samples are equal to 2.3% and 18.09%, and at the frequency of 100 mHz, the impedance values for them are 5.34 MΩ and 4.29 MΩ, respectively.

Warburg Impedance

The generalized finite-length Warburg impedance  is expressed by the following expression[1]:

With the two parameters and as follow:

where R is the gas constant, T absolute temperature, NA Avogadro’s constant, F the Faraday constant, A the electrode area of the test cell, ns the concentration of mobile ions on the surface, D the effective diffusion coefficient of mobile ions, δn the thickness of the Nernst diffusion layer, Wsr Warburg coefficient in bulk and Wsc Warburg coefficient in double layer.

References

[1]	G. J. Sprokel, “Resistivity, permittivity and the electrode space charge of nematic liquid crystals,” Mol. Cryst. Liq. Cryst., vol. 22, no. 3–4, pp. 249–260, 1973.