Supporting Information

# Fast response MSM photodetector based on 2D Ruddlesden Popper Perovskite layer

Parsa Darman, Amin Yaghoobi, Sara Darbari*1

1 Nano-Sensors and Detectors Lab., and Nano Plasmo-photonic Research Group, Faculty of Electrical and Computer   Engineering, Tarbiat Modares University, Tehran, Iran.

* s.darbari@modares.ac.ir

| 50 µm (d) 0.018 molar 50 µm (d) 0.018 molar | 50 µm (c) 0.026 molar 50 µm (c) 0.026 molar | 50 µm (b) 0.039 molar | 50 µm (a) 0.057 molar |
| --- | --- | --- | --- |
| 50 µm (h) 3.9 mmolar 50 µm (h) 3.9 mmolar | 50 µm (g) 5.7 mmolar | (f) 8.4 mmolar 50 µm (f) 8.4 mmolar 50 µm | 50 µm (e) 0.012 molar |
|  |  | 500 nm (i) 0.057 molar |  |

Figure S1. (a-h) Optical microscopy images of RPP layers, hot cast by RPP/DMF solution of (a) 0.057 molar, (b) 0.039 molar, (c) 0.026 molar, (d) 0.018 molar, (e) 8.4 mmolar, (f) 5.7 mmolar, (g) 3.89 mmolar, (h) 1.2 mmolar. (i) Cross section SEM image of RPP layer corresponding to 0.057 molar. (j, k) PL spectra of of RPP layers, hot cast by RPP/DMF precursors of (j) 0.057 molar to 0.018 molar, and (k) 12 mmolar to 3.89 mmolar. (l) Absorption spectra of hot cast (BA)2PbI4 layers with RPP/DMF precursor molarities of 0.057 molar to 0.018 molar.

Figure S2. The current-voltage characteristics of the fabricated Au/RPP/Au photodetector, in response to power density of 4 mW/cm2 and wavelength of 520 nm. The inset shows the current in logarithmic scale.

Figure S3. Optoelectrical characteristics of Al/(BA)2PbI4/Al photodetector with RPP layer thickness of 800 nm. (a-f) The current voltage characterization in the dark and under illumination of green (520 nm), blue (450 nm), and UV (400 nm) light with optical power of (a) 6 mW/cm2 (b) 4 mW/cm2 (c) 2 mW/cm2 (d) 1.5 mW/cm2 (e) 1 mW/cm2 (f) 0.5 mW/cm2. (g-i) The current voltage characterization of the device under illuminations of (g) UV (400 nm) (h) blue light (450 nm) (i) green (520 nm) light with optical power in range of 0.5 mW/cm2 and 6 mW/cm2. (j) The photocurrent of (g-i) for every power of light source at 15 V bias under green (520 nm), blue (450 nm), and UV (400 nm) illuminations.

Figure S4. Optoelectrical characteristics of Al/(BA)2PbI4/Al photodetector with RPP layer thickness of 300 nm. (a-d) The current voltage characterization in the dark and under illuminations of green (520 nm), blue (450 nm), and UV (400 nm) light with optical power of (a) 6 mW/cm2 (b) 4 mW/cm2 (c) 2 mW/cm2 (d) 1 mW/cm2. (e-g) The current voltage characterization of the device under illuminations of (e) UV (400 nm) (f) blue light (450 nm) (g) green (520 nm) light with optical power in range of 0.5 mW/cm2 and 6 mW/cm2. (h) The photocurrent of (e-g) for every power of light source at 15 V bias under green (520 nm), blue (450 nm), and UV (400 nm) illuminations.

Table S1. X-ray diffraction data of the (BA)2PbI4 perovskites.

| Position (2θ) | Counts | FWHM (2θ) | d-spacing (A) |
| --- | --- | --- | --- |
| 7.52 | 164587 | 0.1226 | 13.62 |
| 14.96 | 11526 | 0.1308 | 6.86 |
| 22.47 | 18068 | 0.1408 | 4.58 |
| 30.09 | 32567 | 0.1508 | 3.44 |
| 37.84 | 10902 | 0.1639 | 2.75 |