Table 1 | Optimization of reaction conditions for C-H/C-S activation reactiona

| Entry | Thioether Source | [Pd] (mol%) | [Cu] (mol%) | Yieldb (%) |
| --- | --- | --- | --- | --- |
| 1 | 1a | Herrmann’s Cat. (5) | None | 45 |
| 2 | 1a | Herrmann’s Cat. (5) | CuI (20) | 78 |
| 3 | 1a | Pd2(dba)3 (5) | CuI (20) | 91 (85)c |
| 4 | 1a | Pd(MeCN)2Cl2 (10) | CuI (20) | 80 |
| 5 | 1a | Pd(PtBu3)2 (10) | CuI (20) | 72 |
| 6 | 1a | Pd2(dba)3 (2) | CuI (20) | 98 |
| 7 | 1a | Pd2(dba)3 (0.5) | CuI (20) | 93 |
| 8 | 1b | Pd2(dba)3 (5) | CuI (20) | 45 |
| 9 | 1b | Pd(MeCN)2Cl2 (10) | CuI (20) | 77 |
| 10 | 1b | Pd(PtBu3)2 (10) | CuI (20) | 88 (86)c |
| 11 | 1b | Pd(PtBu3)2 (5) | CuI (20) | 37 |

aReaction conditions: 1a or 1b (1.0 equiv, 0.20 mmol), 2 (1.0 equiv, 0.20 mmol), [Pd] (4-10 mol%), [Cu] (20 mol%), dcype ([Pd]: [P] = 1: 2), KOtBu (1a, 5.0 equiv; 1b, 3.0 equiv), toluene (2.0 mL), 24 h under nitrogen atmosphere. bYields were determined by GC using anthracene as an internal standard. cIsolated yields.

Table 2 | Optimization of C–H/C–S polycondensation reaction conditionsa

| Entry | [Pd] (mol%) | Solvent | Mn/Mw (kg/mol)b | Ɖb | Yield (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | Pd2(dba)3 (10) | Toluene | 16.5/27.4 | 1.66 | 68 |
| 2 | Herrmann’s Cat. (10) | Toluene | 15.9/33.2 | 2.09 | 96 |
| 3 | Pd(PhCN)2Cl2 (20) | Toluene | 24.3/46.9 | 1.93 | 96 |
| 4 | Pd(MeCN)2Cl2 (20) | Toluene | 51.6/97.0 | 1.88 | 98 |
| 5 | Pd(MeCN)2Cl2 (10) | Toluene | 33.0/78.9 | 2.39 | 96 |
| 6 | Pd(MeCN)2Cl2 (5) | Toluene | 12.4/24.9 | 2.01 | 88 |
| 7 | Pd(MeCN)2Cl2 (20) | o-Xylene | 6.0/11.4 | 1.90 | 40 |
| 8 | Pd(MeCN)2Cl2 (20) | Chlorobenzene | 4.0/7.4 | 1.85 | 27 |
| 9c | Pd(MeCN)2Cl2 (20) | Toluene | 6.0/10.8 | 1.80 | 53 |
| 10d | Pd(MeCN)2Cl2 (20) | Toluene | 5.3/9.3 | 1.75 | 41 |
| 11e | Pd(MeCN)2Cl2 (20) | Toluene | 20.0/46.8 | 2.34 | 92 |

aReaction conditions: E1 (1.0 equiv; 0.20 mmol), N1 (1.0 equiv; 0.20 mmol), [Pd] (5-20 mol%), CuI (40 mol%), dcype ([Pd]: [P] = 1: 2), KOtBu (3.0 equiv), toluene (1.0 mL), 48 h under nitrogen atmosphere. bMn, Mw, and Ɖ were determined with GPC at 150 ℃ in 1,2,4-trichlorobenzene against a polystyrene standard. cReaction concentration of 0.1 M. dReaction concentration of 0.05 M. eReaction time of 24 h.