Tab S1. Physicochemical characteristics of sp-MSNs and MSNs (mean ± SD; n=3).

|  | sp-MSNs | MSNs |
| --- | --- | --- |
| Particle size (nm) | 87.7 ± 0.2 | 92.4 ± 2.2 |
| PDI | 0.146 ± 0.010 | 0.118 ± 0.118 |

Tab S2. Pore structure parameters of sp-MSNs and MSNs.

|  | BET Surface Area (m2/g) | Pore Diameter (nm) | Pore Volume (cm3/g) |
| --- | --- | --- | --- |
| sp-MSNs | 743.78 | 5.44 | 1.01 |
| MSNs | 572.99 | 8.00 | 1.15 |

Fig. S1 Transmission electron microscopy images of sp-MSNs (A) and MSNs (B).

Fig. S2 The N2 adsorption/desorption isotherms of sp-MSNs (A) and MSNs (C), and the pore size distributions of sp-MSNs (B) and MSNs (D).

Fig. S3 The levodopa and curcumin release profiles of binary-drug loaded lf-protocells in neutral or acidic medium.

Fig. S4 Hemolysis activity of MSNs, protocells, lf-protocells at different concentrations.

Fig. S5 The cell viability of MSNs and lf-protocells at different concentrations.

Fig. S6 The effects of rotenone induction on the expressions of apoptosis related proteins and PD related proteins in SH-SY5Y cells through western blot analysis.

- Expression of apoptosis related proteins in rotenone group. (B) Expression of PD related proteins in rotenone group. The expression levels of Bax, Cleaved Caspase-3, PARP, α-syn were increased, while the expression levels of Bcl-2, Caspase-3 and TH were significantly decreased by the rotenone treatment compared with control.

Fig. S7 Effects of drug loaded lf-protocells on Rot-induced cytotoxicity determined by MTT .

Treatments with drug loaded lf-protocells protected against 4 μM Rot induced cellular toxicity in SH-SY5Y cells. (mean ± SD; n=3. *** P < 0.001 compared with the 4μM Rot group. ** P < 0.01 compared with the 4μM Rot group. # P < 0.05 compared between two groups.) Cells were exposed for 24 h and cell viability was determined by MTT assay. Rot: rotenone; C: curcumin; L: levodopa; L/C: levodopa and curcumin; Lf-Pro: lf-protocells.

Fig. S8 Ultra High Resolution Microscope images of bEnd.3 cells incubated with RBITC/Calcein-protocells or RBITC/Calcein-lf-protocells after 4 h incubation at 37 ℃.