Phosphorus removal in denitrifying woodchip bioreactors varies by wood type and water chemistry

Ana Paula Sanchez Bustamante Bailon†, Andrew Margenot†, Richard A. C. Cooke‡, and Laura E. Christianson†*

† Department of Crop Sciences, University of Illinois at Urbana-Champaign, AW-101 Turner Hall, 1103 S. Goodwin Ave., Urbana, IL 61801, USA;

‡ Department of Agricultural and Biological Engineering, University of Illinois at Urbana-Champaign, 1304 W. Pennsylvania Ave., Urbana, IL 61801, USA.

* Corresponding author: LEChris@illinois.edu; Ph. 1-217-244-6173

Supporting Information

Pages: 3

Figures: 2

Tables: 1

Fig. S1 Seven woodchip types sieved to the 6.3-13 mm particle size range for use in 72-h phosphorus sorption batch tests

Fig. S2 Potassium (a), sodium (b), and sulfur (c) concentrations for six treatments tested during 72-h batch tests (n = 1). Test # in the legend refers to the test numbers in Table 1. t = 0 was set at 0.01 h due to the logarithmic x-axis. Note the y-axis breaks in each panel

Table S1 Physical characteristics and nutrient content of seven woodchips used in 72-h batch tests (C, carbon; N, nitrogen; P, phosphorus)

| Common name | Scientific name | Source | Bulk Density | Total porosity | ------------- Nutrient content --------- |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | C | N | P | C:N Ratio |
|  |  |  | kg/m3 | % | -------------- % ------------ |  |  |  |
| Poplar | Populus spp. | Lumber | 142 | 73 | 48.3 | 0.20 | < 0.010 | 241 |
| White oak | Quercus alba | Live branches | 191 | 74 | 47.0 | 0.39 | 0.035 | 121 |
| Hickory | Carya spp. | Lumber | 271 | 68 | 48.5 | < 0.20 | < 0.010 | 242 |
| Cypress | Taxodium distichum | Deadfall, live branches | 184 | 76 | 48.5 | 0.35 | 0.031 | 139 |
| Field bioreactor | Unknown, contractor sourced | Commercial woodchips | 227 | 68 | 47. 8 | 0.30 | 0.011 | 161 |
| Cedar | Cedrus spp. | Commercial woodchips | 152 | 69 | 49.9 | < 0.20 | 0.010 | 249 |
| Maple | Acer spp. | Commercial woodchips | 202 | 74 | 48.5 | 0.28 | 0.026 | 173 |