Supporting information

MOF-derived Fe2O3/MoSe2 Heterostructure for Promoted Electrocatalytic Nitrogen Fixation

Liming Huang1,2, ‡, * · Leiming Tao2, ‡,* · Kui Pang2,3 · Shuying He2 · GuanHua Zhu2 · LinHai Duan2 · Chenglin Wen2 · Changlin Yu2 · Hongbing Ji1,*

1 School of Chemistry and Chemical Engineering, Guangxi University, Nanning, 530003, China

2 Guangdong Provincial Key Laboratory of Petrochemical Equipment Fault Diagnosis, School of Science, Guangdong University of Petrochemical Technology, Maoming, Guangdong, 525000, China

3 Engineering Research Center for Nanomaterials, Henan University, Henan, 475001, China

‡ Liming Huang and Leiming Tao contributed equally to this work.

* Authors to whom correspondence should be addressed.

Electronic addresses: jihb@mail.sysu.edu.cn; leimingtao@foxmail.com.

## Determination of NH3

The concentration of generated ammonia was quantitatively determined by the indophenol blue method. Specifically, 2 ml of electrolyte solution was firstly taken from the cathode chamber, and then 2 ml of NaOH (1 M) mixed solution of salicylic acid (5 wt%) and sodium citrate (5 wt%), 1 ml of NaClO solution (0.05 M), 0.2 ml sodium nitroferricyanide (C5FeN6Na2O·2H2O) solution (1 wt%). After standing for 2 h in a dark light environment at room temperature, the absorbance of the solution at λ = 655 nm was measured with a UV-Vis spectrophotometer. Concentration-absorbance curves were calibrated using standard NH4Cl solutions at different concentrations (0.1, 0.2, 0.3, 0.4, 0.5 and 0.8 μg/mL) in 0.1 M H2SO4. The fitted curve (y = 0.3958 x - 0.00636, R2 = 0.997) shows a good linear relationship between absorbance values and NH3 concentration.

The NH3 yield was calculated by the following formula:

NH3 Yield rate = (cNH3V) / (tm)

The Faradaic efficiency was calculated as follows:

Faradaic efficiency = (3F cNH3V) / 17Q

where cNH3 is the measured NH3 concentration, V is the volume of electrolyte in the cathode compartment, t is the reduction reaction time (2 h), and m is the catalyst loading on the carbon cloth. F is Faraday's constant (96485 C mol-1) and Q is the total charge passing through the electrode.

## Determination of N2H4

The intermediate N2H4 during NRR was estimated by the method of Watt and Chrisp, first, by mixing dimethylaminobenzaldehyde (5.99 g), HCl (30 mL) and C2H5OH (300 mL) as a chromogenic reagent. Remove 5 mL of electrolyte and mix with the colour developer (5 mL) prepared above. After stirring at room temperature for 20 minutes, the absorbance of the resulting solution was measured at 455 nm, and the N2H4 yield was estimated from a standard curve.

## Details of Density Functional Theory (DFT) Calculations

All the density functional theory (DFT) calculations were performed using the Vienna ab-initio simulation package (VASP). The description of the exchange correlation adopted the generalized gradient approximation (GGA) of the Perdew, Burke, and Ernzerhof form. The plane wave energy cutoff was set to 400 eV. The generalized gradient approximation (GGA) with the Perdew-Burke-Ernzerhof (PBE) exchange-correlation functional. The Brillouin zone was sampled at the Gamma point with the 2 × 2 × 1 k-point meshes for Fe2O3, MoSe2 and Fe2O3/MoSe2 surfaces. The energy and force criterion for convergence of the electron density was set at 10-5 eV and 0.03 eV/Å, respectively. The vacuum space along the z-direction was set to 15 Å to avoid interactions between adjacent images.

Figure S1. Synthesis process of Fe2O3/MoSe2 heterostructure.

Figure S2. XRD pattern of as-synthesized Fe2O3.

Figure S3. XRD pattern of as-synthesized MoSe2.

Figure S4. SEM images of (a) Fe2O3 and (b) MoSe2.

Figure S5. EDX spectra of Fe2O3/MoSe2.

Figure S6. (a) UV-Vis absorption spectra of indophenol assays with NH4Cl after incubated for 2 h at ambient conditions. (b) Calibration curve used for calculation of NH3 concentrations.

Figure S7. (a) UV-Vis absorption spectra of N2H4 assays after incubated for 20 min at ambient conditions. (b) Calibration curve used for calculation of N2H4 concentrations.

Figure S8. (a) UV-Vis spectra of the electrolytes (stained with the chemical indicator based on the method of Watt and Chrisp) after 2 h electrocatalysis on Fe2O3/MoSe2 at various potentials, and (b) corresponding N2H4 concentrations in the electrolytes.

Figure S9. CV curves of (a) Fe2O3, (b) MoSe2, and (c) Fe2O3/MoSe2 at various scan rates, and corresponding (d) plots of current density differences (Δj/2) vs. scan rate at 0.45 V vs. RHE.

Figure S10. Electrochemical impendence spectra of Fe2O3, MoSe2 and Fe2O3/MoSe2.

Figure S11. UV-Vis absorption spectra of working electrolytes after 2 h of electrolysis in N2-saturated solution and Ar-saturated solutions on Fe2O3/MoSe2 at -0.5 V, N2-saturated solution on Fe2O3/MoSe2 at open circuit, and N2-saturated solution on pristine CC at -0.5 V.

Figure S12. 1H NMR measurements using 14N2, 15N2 and Ar as feed gases.

Figure S13. UV-Vis absorption spectra of working electrolytes on Fe2O3/MoSe2 (each for 2 h of NRR electrolysis at -0.5 V) for seven cycles.

Figure S14. Morphologies and XRD pattern of Fe2O3/MoSe2 after stability test.

Figure S15. Optimized atomic configuration of Fe2O3/MoSe2 (color notation: purple-Mo, green-Se, blue-O, yellow-Fe).

Figure S16. (a, b) High resolution XPS spectra of MoSe2 and Fe2O3/MoSe2: (a) Mo 3d, (b) Se 3d. (c, d) High resolution XPS spectra of Fe2O3 and Fe2O3/MoSe2: (c) Fe 2p, (d) O 1s.

Table S1. The comparison of Fe2O3/MoSe2 catalyst with the representative reported catalysts for electrochemical NRR in aqueous solutions.

| Catalyst | Electrolyte | NH3 yield rate (μgh-1 mgmat-1) | Faraday Efficiency (%) | Ref. |
| --- | --- | --- | --- | --- |
| Fe2O3/MoSe2 | 0.05 M H2SO4 | 55.52 | 9.6 | This work |
| AuSA/np-MoSe2 | 0.1 M Na2SO4 | 30.83 | 37.82 | [[1]] |
| Fe2(MoO4)3 | 0.1 M Na2SO4 | 7.5 | 1.0 | [[2]] |
| Vo-MoO2/C | 0.1M Na2SO4 | 9.75 | 3.24 | [[3]] |
| Cu2-xS/MoS2 | 0.1 M HCl | 22.1 | 6.06 | [[4]] |
| FeMoO4 | 0.1M Na2SO4 | 17.51 | 10.5 | [[5]] |
| Fe SAs/MoS2 | 0.1 M K2SO4 | 8.63 | 18.8 | [[6]] |
| Au-Fe3O4 | 0.1 M KOH | 21.42 | 10.54 | [[7]] |
| 1T′-MoS2/Ti3C2 | 0.1 M Na2SO4 | 31.96 | 30.75 | [[8]] |
| Nb2O5/C-800 | 0.1 M HCl | 29.1 | 11.5 | [[9]] |
| MoS2/rGO | 0.5 M Li2ClO4 | 24.82 | 4.58 | [[10]] |
| V4C3Tx | 0.1 M KOH | 21.29 | 8.04 | [[11]] |
| CoS/S-MAs (Ti3C2Tx MXene) | 0.1 M Na2SO4 | 12.4 | 27.05 | [[12]] |
| Ru SAs/Ti3C2O | 0.1 M HCl | 27.56 | 23.3 | [[13]] |

1.	Chen D, Luo M, Ning S, Lan J, Peng W, Lu Y R, Chan T STan Y (2022) Single‐Atom Gold Isolated Onto Nanoporous MoSe2 for Boosting Electrochemical Nitrogen Reduction. Small 18:2104043.

2.	Chen C, Liu YYao Y (2020) Ammonia synthesis via electrochemical nitrogen reduction reaction on iron molybdate under ambient conditions. European Journal of Inorganic Chemistry 2020:3236-3241.

3.	Du Y, He Z, Ma F, Jiang Y, Wan J, Wu GLiu Y (2021) Anionic Biopolymer assisted preparation of MoO2@C Heterostructure nanoparticles with oxygen vacancies for ambient electrocatalytic ammonia synthesis. Inorganic Chemistry 60:4116-4123.

4.	Jiang T, Li L, Li L, Liu Y, Zhang D, Zhang D, Li H, Mao BShi W (2021) Ultra-thin shelled Cu2-xS/MoS2 quantum dots for enhanced electrocatalytic nitrogen reduction. Chemical Engineering Journal 426:130650.

5.	Wu J, Wang Z, Li S, Niu S, Zhang Y, Hu J, Zhao JXu P (2020) FeMoO4 nanorods for efficient ambient electrochemical nitrogen reduction. Chemical Communications 56:6834-6837.

6.	Su H, Chen L, Chen Y, Si R, Wu Y, Wu X, Geng Z, Zhang WZeng J (2020) Single atoms of iron on MoS2 nanosheets for N2 electroreduction into ammonia. Angewandte Chemie 132:20591-20596.

7.	Zhang J, Ji Y, Wang P, Shao Q, Li YHuang X (2020) Adsorbing and activating N2 on heterogeneous Au–Fe3O4 nanoparticles for N2 fixation. Advanced Functional Materials 30:1906579.

8.	Chen X, Zhang S, Qian X, Liang Z, Xue Y, Zhang X, Tian J, Han YShao M (2022) Enabling efficient electrocatalytic conversion of N2 to NH3 by Ti3C2 MXene loaded with semi-metallic 1T′-MoS2 nanosheets. Applied Catalysis B: Environmental 310:121277.

9.	Zhang M, Yin H, Jin F, Liu J, Ji X, Du A, Yang WLiu Z (2022) Vacancy engineering of oxidized Nb2CTx MXenes for a biased nitrogen fixation. Green Energy & Environment

10.	Li Y, Li J, Huang J, Chen J, Kong Y, Yang B, Li Z, Lei L, Chai GWen Z (2021) Boosting electroreduction kinetics of nitrogen to ammonia via tuning electron distribution of single‐atomic iron sites. Angewandte Chemie 133:9160-9167.

11.	Du C-F, Yang L, Tang K, Fang W, Zhao X, Liang Q, Liu X, Yu H, Qi WYan Q (2021) Ni nanoparticles/V4C3Tx MXene heterostructures for electrocatalytic nitrogen fixation. Materials Chemistry Frontiers 5:2338-2346.

12.	Li Q, Song T, Wang Z, Wang X, Zhou X, Wang QYang Y (2021) A General Strategy toward Metal Sulfide Nanoparticles Confined in a Sulfur‐Doped Ti3C2Tx MXene 3D Porous Aerogel for Efficient Ambient N2 Electroreduction. Small 17:2103305.

13.	Chen G, Ding M, Zhang K, Shen Z, Wang Y, Ma J, Wang A, Li YXu H (2022) Single‐Atomic Ruthenium Active Sites on Ti3C2 MXene with Oxygen‐Terminated Surface Synchronize Enhanced Activity and Selectivity for Electrocatalytic Nitrogen Reduction to Ammonia. ChemSusChem 15:e202102352.