Supplementary Materials for

Automated and Intelligent Synthesis of Oxygen-Producing Catalysts from Martian Meteorites by Robotic AI-Chemist

Qing Zhu1,†, Yan Huang1,†, Donglai Zhou1,†, Luyuan Zhao1,†, Lulu Guo1, Ruyu Yang1, Zixu Sun1, Man Luo1, Fei Zhang2, Hengyu Xiao1, Xinsheng Tang2, Xuchun Zhang2, Tao Song2, Xiang Li2, Baochen Chong2, Junyi Zhou2, Yihan Zhang2, Baicheng Zhang1, Jiaqi Cao1, Guozhen Zhang1,5, Song Wang1, Guilin Ye3, Wanjun Zhang3, Haitao Zhao4, Shuang Cong2, Huirong Li1, Weiwei Shang2,*, Jun Jiang1,5*, Yi Luo1,5*

1 Hefei National Research Center for Physical Sciences at the Microscale, School of Chemistry and Materials Science, University of Science and Technology of China, Hefi 230026, China

2 School of Information Science and Technology, University of Science and Technology of China, Hefei 230026, China

3 Hefei JiShu Quantum Technology Co. Ltd., Hefei 230026, China

4 Materials Interfaces Center, Shenzhen Institute of Advanced Technology, Chinese Academy of Sciences, Shenzhen 518055, China

5 Hefei National Laboratory, Hefei 230088, China

* Corresponding authors. E-mails: wwshang@ustc.edu.cn; jiangj1@ustc.edu.cn; yiluo@ustc.edu.cn)

† Equally contributed to this work.

The standard operating procedures of AI-Chemist for electrochemical measurements

Supplementary Fig. 1. The AI-chemist operation flow chart of electrocatalytic oxygen evolution performance characterization.

First, the robot initializes the operation, including detecting whether the communication of each device node is connected and detecting the pose of the marker fixed to the workstation. After the marker is detected, the robotic manipulator will automatically calculate the current poses and make error compensation for the base pose of the robotic manipulator. The calculation and compensation process is as follows:

- The robot acquires the pose of the ArUco marker fixed to electrochemical workstation  by means of the camera, specifically, the pixel coordinates of the center of the marker in the image based on the RGB image, after which the actual pose are obtained according to the depth image, and then calculates the pose of the marker represented in the coordinate system of the robotic manipulator using equation

where  is the camera's pose relative to the robot coordinate system, obtained in advance by hand-eye calibration.

- To further improve locating accuracy, the robot moves again so that the marker is in the center of the camera's field of view and computes the current pose.  Thus the measurement error is compensated by multiple locating.

After relocating the electrochemical workstation, the robot will load the pre-recorded structured information of the electrochemical workstation , which are operating poses represented in the marker coordinate system of the electrochemical workstation. The operating poses of the manipulator in the current environment after error compensation for subsequent trajectory planning can be calculated based on equation:

Supplementary Fig. 2. Description of the robot coordinate system.

Then, after obtaining the error-compensated operating poses, the robot performs trajectory planning according to a pre-defined operational flow, including the sequence of operating poses, the planning method, velocity and acceleration for reaching the next operating pose, and gripper control commands. The following illustrates the trajectory planning method used (take the mth operating pose as an example):

- Obtain the m-1th trajectory  from  to  by trajectory planning according to the planning method, velocity and acceleration in the pre-defined operation flow information. Similarly the mth trajectory   can be derived.

- Calculate the distance  between  and  by:

In which  is the translation part of  and  is the translation part of . The distance  from  and  is calculated in the same way.

- Access the maximum permissible radius  of the transition segment trajectory  between  and  using:

- Calculate the actual radius  of the smooth transition segment through

Where  is the transition radius factor defined in the operational flow information.

- Make a ball with  as the center of the ball and  as the radius and find the intersection pose of the ball with  and , denoted as   and , and note the velocity of  at  and  at  as , , the acceleration as ,  respectively.

- Plan the transition segment trajectory  based on fifth-order Bezier curve:

where  is a Bernstein polynomial and the control point  is computed as follows:

- Acquire the final value of  by minimizing the following equation:

Where  and  is the velocity and acceleration of  at  separately. And the initial value of  can be obtained by solving equation (7).

- Interpolate the transition segment trajectory based on the  and inserting it between  and , and the final trajectory from  to is obtained.

Based on the planned trajectory and gripper control instructions, the robot will perform the following operations: (Supplementary Fig. 3c) pick up the pneumatic gripper, use the pneumatic gripper to grip the carbon paper and place it on the substrate; (Supplementary Fig. 3d) put back the pneumatic gripper and move the substrate to the drip station; (Supplementary Fig. 3e) place the test tube rack holding vials with test sample on the drip station for sample preparation and wait for the sample to dry; (Supplementary Fig. 3f) move the substrate to the electrochemical reaction cell and start the electrochemical reaction by sending a message to the electrochemical workstation.

Supplementary Fig. 3. a, b The RGB and depth images of electrochemical workstation and c-f, AI-chemist operation flows for the working electrode preparation.

In the above process, the robot detects and feeds back the execution status in real-time and deals with exceptions (including lacking carbon paper, not resetting substrate, collision, locating error out of threshold, and gripping failure). When collisions occur, the location error exceeds the threshold or fails to grasp the object, the robot will plan and executes a recovery process by incorporating the currently implemented processes, the current pose of the robot, and gripping status, and monitors the situation in real-time during this process to enable dynamic adjustment of the recovery process.

Supplementary Fig. 4. The specimen images of selected meteorites for OER catalyst preparation.

Supplementary Fig. 5. The petrography and mineralogy identification chart of Aletai meteorite in Meteoritical Bulletin Database (MBD).

Supplementary Fig. 6. The petrography and mineralogy identification chart of NWA8171 meteorite in Meteoritical Bulletin Database (MBD).

Supplementary Fig. 7. The petrography and mineralogy identification chart of NWA13669 meteorite in Meteoritical Bulletin Database (MBD).

Supplementary Fig. 8. The petrography and mineralogy identification chart of NWA12564 meteorite in Meteoritical Bulletin Database (MBD).

Supplementary Fig. 9. The petrography and mineralogy identification chart of Hassi Messaoud 001 meteorite in Meteoritical Bulletin Database (MBD).

Supplementary Fig. 10. a, Schematic diagram of operating principle and b, device graphics of the laboratory self-developed LIBS setup. The beam generated from an Nd:YAG pulsed laser is focused onto the meteorites surface using a focusing lens, and the atomic radiation emitted from the meteorites is transmitted to an echelle spectrometer through an optical fiber. The spectrometer disperses the atomized radiation into spectral emission wavelengths and imaged by an attached CCD camera. The delay generator between the laser and the camera controls the start of data acquisition so that the camera captures the image signal of the plasma when the atomic emission wavelengths are most prominent. After camera exposure, the spectral data is sent to a computer for automatic data processing, analysis and display.

Supplementary Fig. 11. Temperature versus time curve for the MD simulation.

Supplementary Fig. 12. Energy versus time curve for the MD simulation.

Supplementary Fig. 13. Distance distribution between metals for metal hydroxyl oxides.

Supplementary Fig. 14. Distance distribution between metals and oxygen for metal hydroxyl oxides.

Supplementary Fig. 15. GUI of the ratio transformation software.

Supplementary Fig. 16. The electrochemical experiment results and comparison of catalysts prepared from a single meteorite feedstock. a, Linear sweep voltammetry (LSV) curves collected at the sweep rate of 5 mV/s in 1 M KOH electrolyte and b, corresponding Tafel plots for the anodic water oxidation derived from the LSV data in a to evaluate the reaction kinetics. c, The electrochemical impedance spectra (EIS). d, The extracted Helmholtz double layer capacitance (Cdl) to evaluate the electrocatalytically active surface areas (ECSA).

Supplementary Fig. 17. The electrochemical experiment report of sample No. 197 with the best local performance. a, Cyclic voltammetry (CV) voltammogram curves. b, Linear sweep voltammetry (LSV) curves collected at the sweep rate of 5 mV/s in 1 M KOH electrolyte and c, corresponding Tafel plots for the anodic water oxidation derived from the LSV data in b to evaluate the reaction kinetics. d, The electrochemical impedance spectra (EIS). e, The electrocatalytically active surface areas (ECSA) calculated based on the cyclic voltammetry (CV) voltammogram within the non-Faradaic region. f, The extracted Helmholtz double layer capacitance (Cdl) from the slope of linear regression between the current density differences (∆j/2 = (ja-jc)/2) in the middle of potential window of CV curves versus the scan rates in e.

Supplementary Fig. 18. The electrochemical experiment report of sample Exp-guided OPT. a, Cyclic voltammetry (CV) voltammogram curves. b, Linear sweep voltammetry (LSV) curves collected at the sweep rate of 5 mV/s in 1 M KOH electrolyte and c, corresponding Tafel plots for the anodic water oxidation derived from the LSV data in b to evaluate the reaction kinetics. d, The electrochemical impedance spectra (EIS). e, The electrocatalytically active surface areas (ECSA) calculated based on the cyclic voltammetry (CV) voltammogram within the non-Faradaic region. f, The extracted Helmholtz double layer capacitance (Cdl) from the slope of linear regression between the current density differences (∆j/2 = (ja-jc)/2) in the middle of potential window of CV curves versus the scan rates in e.

Supplementary Fig. 19. The electrochemical experiment report of sample Model-guided OPT. a, Cyclic voltammetry (CV) voltammogram curves. b, Linear sweep voltammetry (LSV) curves collected at the sweep rate of 5 mV/s in 1 M KOH electrolyte and c, corresponding Tafel plots for the anodic water oxidation derived from the LSV data in b to evaluate the reaction kinetics. d, The electrochemical impedance spectra (EIS). e, The electrocatalytically active surface areas (ECSA) calculated based on the cyclic voltammetry (CV) voltammogram within the non-Faradaic region. f, The extracted Helmholtz double layer capacitance (Cdl) from the slope of linear regression between the current density differences (∆j/2 = (ja-jc)/2) in the middle of potential window of CV curves versus the scan rates in e.

Supplementary Fig. 20. a, Cyclic voltammetry (CV) voltammogram curve of carbon paper electrode in CO2-saturated 2.8 M Mg(ClO4)2 electrolyte containing 2 mM Fe(CN)64-/Fe(CN)63- using platinum mesh as counter electrode and Ag wire as the reference. b, Linear sweep voltammetry (LSV) curves of Model-guided OPT collected at the sweep rate of 5 mV/s in CO2-saturated 2.8 M Mg(ClO4)2 electrolyte at 23°C and −37°C, respectively.

According to Supplementary Fig. 20a, we measured that the electrode potential of Ag wire (at V=0) is 0.283V lower than Fe(CN)64-/Fe(CN)63-, and it is known that the Fe(CN)64-/Fe(CN)63- redox potential is 0.71 V vs. RHE, therefore, we can deduce that the reference potential of Ag wire is 0.427V vs. RHE. When the OER test is completed, the LSV curve can be converted into coordinates corresponding to the RHE unit (Supplementary Fig. 20b).

Supplementary Table 1. Concentration of metal ions in the prepared feedstocks solution.

| Serial number | Fe (mmol/L&ppm) | Mn (mmol/L&ppm) | Ni (mmol/L&ppm) | Ca (mmol/L&ppm) | Mg (mmol/L&ppm) | Al (mmol/L&ppm) | Total (ppm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Aletai | 3.303/184.47 | 0 | 0.328/19.266 | 0.0055/0.221 | 0.00155/0.0377 | 0.00149/0.0403 | 204.035 |
| NWA 8171 | 1.379/77.076 | 0.0288/1.584 | 0 | 0.1374/5.508 | 5.167/125.55 | 0.02/0.54 | 210.258 |
| NWA 13669 | 2.401/134.09 | 0.0521/2.864 | 0 | 0.7697/30.851 | 1.306/31.734 | 0.0803/3.1264 | 202.666 |
| NWA 12564 | 0.9698/54.164 | 0.0132/0.726 | 0 | 1.417/56.7985 | 0.744/18.0675 | 2.759/74.415 | 204.171 |
| Hassi Messaoud 001 | 2.238/124.965 | 0.0541/2.974 | 0 | 1.142/45.7605 | 1.438/34.9425 | 0.0779/2.1015 | 210.744 |

Supplementary Table 2. DFT calculations of three catalytic properties for metal hydroxyl oxides, the three catalytic properties represent the free energy change of hydroxyl adsorption, the difference between GO* and GOH* and the charge transfer during hydroxyl adsorption the activate site metal, respectively.

| Metal | GOH* / eV | GO*-OH* / eV | Δq / e |
| --- | --- | --- | --- |
| Fe-Fe | 0.7107 | 1.9195 | 0.1126 |
| Mn-Fe | 0.7345 | 1.8561 | 0.0308 |
| Mn-Mn | 1.0939 | 1.5368 | 0.0434 |
| Mn-Al | 1.2549 | 2.8057 | 0.0118 |
| Al-Fe | 0.9291 | 1.9519 | 0.0424 |
| Al-Al | 1.6181 | 2.5402 | 0.0126 |
| Al-Ni | 0.7211 | 1.9942 | 0.0318 |
| Ca-Fe | 0.7342 | 1.9184 | 0.0913 |
| Ca-Mn | 1.2655 | 1.3841 | 0.0477 |
| Ca-Al | 1.4790 | 2.6778 | 0.0180 |
| Ca-Ca | 3.0012 | 2.3938 | 0.01494 |
| Ca-Mg | 2.7184 | 2.4405 | -0.0130 |
| Ca-Ni | 1.4518 | 2.1166 | 0.0386 |
| Mg-Fe | 0.9151 | 1.9725 | 0.0201 |
| Mg-Mn | 1.29339 | 1.53339 | 0.0309 |
| Mg-Al | 1.57015 | 2.57572 | 0.0216 |
| Mg-Mg | 2.65895 | 2.43158 | -0.0141 |
| Mg-Ni | 1.47536 | 2.13782 | 0.0362 |
| Ni-Fe | 0.780184 | 1.92284 | 0.0785 |
| Ni-Mn | 1.2645 | 1.47608 | 0.0147 |
| Ni-Ni | 1.17646 | 2.16916 | 0.0314 |