Supporting Information

Targeting Nano-regulator based on Metal-Organic Frameworks for Enhanced Immunotherapy of Bone Metastatic Prostate Cancer

Shu Huang1, Jun Yuan1, Yong Xie1, Kai Qing1, Zeya Shi1, Guanyu Chen1, Jie Gao1, Haoxiang Tan1 and Wenhu Zhou1, 2, 3*

1. Department of Orthopedics, Hunan Provincial People’s Hospital (The first-affiliated hospital of Hunan normal university), Changsha 410005, China

2. Xiangya School of Pharmaceutical Sciences, Central South University, Changsha, Hunan, 410013, China

3. Hunan Provincial Key Laboratory of the Research and Development of Novel Pharmaceutical Preparations, Changsha Medical University, Changsha, China

E-mail: zhouwenhuyaoji@163.com

Table S1. The effect of the weight ratio between PA and Fe3+ on the MOF formation (n = 3).

| PA (mg/mL) | Fe3+ (mg/mL) | Volume ratio | Size (nm) | PDI |
| --- | --- | --- | --- | --- |
| 2 2 2 2 | 0.5 0.5 0.5 0.5 | 1:3 1:2 2:1 3:1 | 452±3.3 146±1.5 376±2.9 570±4.7 | 0.283±0.035 0.155±0.001 0.257±0.003 0.543±0.063 |

Table S2. Effect of MTO feeding concentration on MTO@PA/Fe3+ MOF formation (n = 3).

| MTO (mg/mL) | Entrapment Efficiency (%) | Drug loading (%) | Size (nm) | PDI |
| --- | --- | --- | --- | --- |
| 0.1 0.125 0.2 0.25 | 73% 85% 78% 76% | 22% 30% 25% 24% | 252±2.9 135±1.3 235±2.4 292±2.8 | 0.310±0.002 0.148±0.001 0.239±0.028 0.298±0.015 |