Supplementary information

Terbium-Based Dual-Ligand Metal Organic Framework by Diffusion Method for Selective and Sensitive Detection of Danofloxacin in Aqueous Medium

Gurdeep Singh a, Deepika a,Sanjay Kumar b, Rajpal Verma a,c, Ashok Kumar Malik a *

a Department of Chemistry, Punjabi University, Patiala-147002, Punjab, India

b Department of Chemistry, Multani Mal Modi College, Patiala-147001, Punjab, India

cDepartment of Chemistry, Dr. B. R. Ambedkar Govt. College Dabwali, Sirsa, Haryana, India

*Corresponding author: malik_chem2002@yahoo.co.uk (A.K.M.)

| NAME | NOMENCLATURE | STRUCTURE | USE |
| --- | --- | --- | --- |
| Danofloxacin (DANO) CAS No. 119478-55-6 Chemical Formula: C19H20FN3O3 Mol. Wt. 357.37 | 7-[(1′s,4′s)-5′-Methyl-2′,5′ diazabicyclo[2.2.1]hept-2′-yl]-1-cyclopropyl-6-fluoro-1,4-dihydro-4-oxo-3- quinoline carboxylic acid |  | veterinary use |
| Ciprofloxacin (CIPRO) CAS No. 86483-48-9 Chemical Formula: C17H18FN3O3 Mol. Wt. 331.35 | 1-Cyclopropyl-6-fluoro-1,4-dihydro-4-oxo- 7-(1-piperazinyl)-3-quinoline carboxylic acid |  | Human and veterinary use |
| Norfloxacin (NOR) CAS No. 70458-96-7 Chemical Formula: C16H18FN3O3 Mol. Wt. 319.33 | 1-Ethyl-6-fluoro-1,4-dihydro-4-oxo-7-(1- piperazinyl)-3quinoline carboxylic acid |  | Human and veterinary use |
| Levofloxacin (LEVO) CAS No. 100986-85-4 Chemical Formula: C18H20FN3O4 Mol. Wt. 361.37 | S-isomer of racemic ofloxacin |  | Human use |
| Ofloxacin (OFLO) CAS No. 83380-47-6 Chemical Formula: C18H20FN3O4 Mol. Wt. 361.37 | (±)-9-Fluoro-2,3-dihydro-3-methyl-10-(4 methyl-1-piperazinyl)-7-oxo-7 H-pyrido [1,2,3-de]-1,4-benzoxazine-6-carboxylic acid |  | Human and veterinary use |

Table S1. Nomenclature, structure, and use of FQs.

Figure S1. Energy-dispersive X-ray (EDX) spectra of TBP.

Figure S2. Fluorescence emission spectra (excitation wavelength (λex) from 323 to 383 nm) of TBP in aqueous solution.

Figure S3. 3D bar graph of fluorescence spectra for TBP dispersed in an aqueous solution containing different FQs when excited at 353 nm.

Figure S4. Schematic illustration of hydrogen bonding between TBP and DANO.

Figure S5. Schematic depiction of electron transfer between DANO and TBP (fluorescence turn-on mechanism)