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[bookmark: _Hlk103261716]Figure S1. Antibacterial activity of ZnO symbol sample against: (a) P. aeruginosa, (b) S. aureus 
Table S1. Antibacterial activity of ZnO NPs samples against: (a) P. aeruginosa, (b) S. aureus
	Bacterial strains
	Diameters of the zones of inhibition for the tested bacteria (mm)

	
	DMSO
	ZnO
	ZPS25
	ZPS50
	ZPS75

	P. aeruginosa
	0
	21
	31
	42
	37

	S. aureus
	0
	16
	35
	39
	36


Table S2. Cytotoxic activity against KB human cancer cell line of ZPS50
	No.
	Concentration (g/mL)
	Inhibition (%)

	1
	256
	81

	2
	64
	79

	3
	16
	11

	4
	4
	0

	5
	IC50
	43.53±2.98
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Figure S2. Anticancer activity of various concentrations of ZPS50 against KB
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