Supplementary materials

GREEN SYNTHESIS OF ZnO DOPED PIPER CHAUDOCANUM LEAF EXTRACT BY CO-PRECIPITATION METHOD: CHARACTERIZATION, ANTIBACTERIAL AND ANTICANCER ACTIVITY

Truong Thi Thao1, Khieu Thi Tam1*

## 1Faculty of Chemistry, TNU-University of Sciences, Tan Thinh Ward, Thai Nguyen city, Vietnam

*Corresponding author: Khieu Thi Tam (tamkt@tnus.edu.vn)

†Present address: Faculty of Chemistry, TNU-University of Sciences, Tan Thinh Ward, Thai Nguyen city, Vietnam

Figure S1. Antibacterial activity of ZnO symbol sample against: (a) P. aeruginosa, (b) S. aureus

Table S1. Antibacterial activity of ZnO NPs samples against: (a) P. aeruginosa, (b) S. aureus

| Bacterial strains | Diameters of the zones of inhibition for the tested bacteria (mm) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | DMSO | ZnO | ZPS25 | ZPS50 | ZPS75 |
| P. aeruginosa | 0 | 21 | 31 | 42 | 37 |
| S. aureus | 0 | 16 | 35 | 39 | 36 |

Table S2. Cytotoxic activity against KB human cancer cell line of ZPS50

| No. | Concentration (g/mL) | Inhibition (%) |
| --- | --- | --- |
| 1 | 256 | 81 |
| 2 | 64 | 79 |
| 3 | 16 | 11 |
| 4 | 4 | 0 |
| 5 | IC50 | 43.53±2.98 |

Figure S2. Anticancer activity of various concentrations of ZPS50 against KB