Amorphous nanoparticles: the essence of clay

Katsuhiro Tsukimura*1, Kazuko Manpuku1, Youko Miyoshi1, Tetsuich Takagi1, Masaya Suzuki1 & Shin-ichiro Wada2

1Institute for Geo-Resources and Environment, AIST (National Institute of Advanced Industrial Science and Technology), Tsukuba, Ibaraki 305-8567, Japan

2Faculty of Agriculture, Kyusyu University, Fukuoka, Fukuoka 819-0395, Japan

| Sample description | Specific surface area / (m2/g) | Plasticity index / (per cent) |
| --- | --- | --- |
| 100% kaolinite – 0% bentonite | 18.1 (3.5) | 7.8 (1.6) |
| 95% kaolinite – 5% Bentonite | 38.7 (3.5) | 13.7 (1.3) |
| 90% kaolinite – 10% Bentonite | 56.8 (2.8) | 20.0 (1.8) |
| 95% kaolinite – 15% Bentonite | 77.4 (2.4) | 27.2 (2.3) |
| 100% Illite – 0% Bentonite | 35.5 (4.1) | 6.1 (2.0) |
| 95% Illite – 5% Bentonite | 54.5 (4.0) | 11.2 (0.4) |
| 90% Illite – 10% Bentonite | 75.7 (1.7) | 21.9 (0.7) |
| 85% Illite – 15% Bentonite | 95.5 (4.6) | 34.3 (1.9) |

Supplementary Table S1. Laboratory-altered cay mixtures parameters. Data are taken from Reference S1. Values in parentheses represent the estimated errors.

| No. | Soil description | Specific surface area / (m2/g) | Plasticity index/ (per cent) |
| --- | --- | --- | --- |
| 1 | Topsoil from new Business Building Area OSU Campus, Stillwater, Oklahoma | 91.8 (4.3) | 28.1 (1.8) |
| 2 | Sandy Clay from bottom of drilled piers, new Business Building, OSU Campus, Stillwater, Oklahoma | 46.0 (3.6) | 13.6 (1.4) |
| 3 | Permian clay chunk sample from base course pit overburden, Ingalls, Oklahoma | 132.2 (0.8) | 43.8 (2.3) |
| 4 | Caliche spoil from borrow pit, Concho County, Texas | 71.0 (1.3) | 14.2 (2.1) |
| 5 | Stiff clay with trace of organic matter, Nowata, Oklahoma | 188.4 (6.2) | 50.3 (1.3) |
| 6 | Stiff silty clay, Nowata, Oklahoma | 218.5 (7.3) | 70.1 (2.2) |
| 7 | Calcareous silty soil, Panhandle A. and M. College, Oklahoma | 67.8 (1.9) | 19.4 (1.7) |
| 8 | Fine loess, Salina, Kansas | 138.5 (2.7) | 42.9 (1.9) |
| 9 | Stiff clay, Massard, Arkansas | 136.1 (2.3) | 44.1 (1.1) |
| 10 | Loess with trace of organic matter, Ulysses, Kansas | 95.8 (4.6) | 27.7 (1.9) |
| 11 | Laurentian clay with traces of very fine mica flakes | 96.0 (0.6) | 31.8 (1.9) |

Supplementary Table S2. Natural soil clay parameters. Data are taken from Reference S1. Values in parentheses represent the estimated errors.

Supplementary References

S1. LeFever E. W. J. Soil plasticity dependency on surface area. Doctor of Philosophy Ph.D Thesis, Oklahoma State University (1966).