Supporting Information

for

Biodegradable trimethyl chitosan nanofiber mats as bioabsorbable dressings for wound closure and healing

Alexandru Anisiei1, Bianca-Iustina Andreica1, Liliana Mititelu-Tartau2, Corneliu G. Coman2, Rostyslav Bilyy3, Galyna Bila3, Irina Rosca1, Andreea-Isabela Sandu1, Evžen Amler4, Luminita Marin1*

1“Petru Poni” Institute of Macromolecular Chemistry of Romanian Academy, Iasi, Romania

2“Grigore T. Popa” University of Medicine and Pharmacy, Iasi, Romania

3Lectinotest R&D, Mechamichna Str 2, 79022, Ukraine

4Research and Development Department Inocure, Prague, Czech Republic

*lmarin@icmpp.ro

Content

Synthesis of N, N, N-trimethyl chitosan

Figure S1. 1H-NMR spectrum of TMC and determination of the quaternization degree-TMC

Figure S2. FTIR spectrum of TMC

Figure S3. 1H-NMR spectrum of residual PEO

Figure S4. FTIR spectra of NCT and NC fibers

Figure S5. 1H-NMR spectra of NCT and NC fibers and TMC

Figure S6. POM images of the NCT fibers and TMC

Figure S7. Histograms of the fibers’ alignment assigned by Image J

Figure S8. Diameter distribution histograms of the fibers determined from SEM images

Figure S9. The kinetics of water vapor sorption uptake

Figure S10. Optical microscopy images of liver structure in rats treated with the studied fibers

Figure S11. Optical microscopy images of kidney structure in rats treated with the studied fibers Table S1. Fiber mats morphological parameters

Table S2. Parameters of the dynamic water sorption

Table S3. RBC, Hb, and Ht values in rats treated with the studied fibers

Table S4. Percentage values of components of leukocyte formula of rats treated with the studied fibers

Table S5. Serum levels of GPT, GOT, and LDH of rats treated with the studied fibers

Table S6. Effects of TMC-NCT nanofiber administration on blood urea and creatinine values in rats treated with the studied fibers

Table S7. Values of the serum complement activity and peripheral blood PMN phagocytosis capacity (NBT %) of rats treated with the studied fibers

Synthesis of N, N, N-trimethyl chitosan (TMC) was done in two steps, as follows. (i) 1 g of chitosan, 3 mL formic acid, 4 mL 37% formaldehyde, and 18 mL H2O were added into a 100 mL round-bottom flask were, and kept under reflux, at 70 ℃ with continuous stirring for 5 days, when it turned into a homogeneous, viscous liquid of dark-yellow colour. The pH of the media was then adjusted to 12 with 1M NaOH, and the formed gel was separated by filtration under reduced pressure and washed with distilled water. The gel was then dissolved in acidic water (HCl, pH 4), filtered, and lyophilized. (ii) 250 mg of the previously obtained product (N,N-Dimethylchitosan) was dissolved in 40 mL distilled water, and then the pH was adjusted to 11 with 1M NaOH. The obtained gel was washed by filtration with distilled water and three times with acetone. Further, the gel was poured into a 100 mL round-bottom flask and 50 mL N-methyl-2-pyrrolidone was added, along with 2 mL iodomethane. The reaction mixture was kept under magnetic stirring, at 40 ℃, for 3 days, and then it was precipitated in a mixture of diethyl ether/ethanol (1/1, v/v). The solid was separated by filtration, washed with diethyl ether, and dried under vacuum overnight. For the exchange of I- with Cl-, the obtained product was dissolved in 40 mL 10% NaCl and kept under stirring for 24 hours. The final product was obtained by precipitation in diethyl ether/ethanol (1/1, v/v), filtration, washing with diethyl ether, and drying under vacuum overnight.

Figure S1. 1H-NMR spectrum of TMC (400 MHz, D2O, ppm): δ = 2.04 (H7), 2.8 (H2), 2.93 (H8), 3.32 (H9), 3.72-4.1 (H3-H6), 4.1-4.5 (H2′-H6′), 5.02-5.46 (H1′).

Determination of the quaternization degree-TMC (DQ)

The degree of quaternization (DQ%) and of dimethylation (DDM%) of TMC were determined from the following equations:

DQ (%) = [(CH3)3/(H1) x 1/9] x100

DDM (%) = [(CH3)2/(H1) x 1/6] x100

Where (CH3)3 represents the integral corresponding to the hydrogens of trimethyl groups at 3.32 ppm, (CH3)2 represents the integral corresponding to the hydrogens of dimethyl groups at 2.93 ppm and (H1) represents the integral of the H1, between 5.4-5.46 ppm. Applying these equations, the values of DQ and DDM were found: DQ = 61.33% and DDM = 17.33%

Figure S2. FTIR spectrum of TMC (ATR, cm-1): 3733-2997 (υOH, υNH), 2932, 2887 (υC-H), 1657 (υC=o amide), 1562 (υN-H), 1480 (δN+(CH3)3), 1151 (υC-O-C).

Figure S3. 1H-NMR spectrum recorded on the residuum extracted from the ethanol used to remove PEO from the ternary fibers. The spectrum was recorded in D2O/AcOH to simulate the same conditions as for the nanofibers, and it shows the bands characteristic for PEO and the absence of the bands characteristic for chitosan and TMC, proving that only PEO was removed by washing with ethanol.

TMC: 3736-2994 (υOH, υNH), 2928, 2883 (υC-H), 1659 (υC=O amide), 1563 (υN-H), 1481 (δCH3), 1156 (υC-O-C), 1100, 1038 (υC-O amide).

NCT3: 3668-2995 (υOH, υNH), 2919, 2875 (υC-H), 1650 (υC=O amide), 1594 (υN-H), 1461 (δCH3), 1152 (υC-OC), 1094, 1028 (υC-O).

NCT7: 3667-2996 (υOH, υNH), 2922, 2871 (υC-H), 1630 (υC=o amide), 1590 (υN-H), 1461(δCH3), 1152 (υC-OC), 1091, 1034 (υC-O amide).

NCT19: 3668-2995 (υOH, υNH), 2922, 2873 (υC-H), 1649 (υC=O amide), 1596 (υN-H), 1461(δCH3), 1152 (υC-O-C), 1090, 1034 (υC-O amide).

NC: 3675-3229 (υOH, υNH), 2924, 2858 (υC-H), 1669 (υC=O amide), 1600 (υN-H), 1158 (υC-O-C), 1080, 1032 (υC-O amide)

Figure S4. FTIR spectra of NCT and NC fibers

TMC: δ = 3.03 (H8), 3.08 (H2), 3.35 (H9), 3.76-4.2 (H3-H6), 4.2-4.7 (H2′-H6′), 5.44-5.51 (H1′)

NCT3: δ = 3.03 (H8), 3.14 (H2), 3.31 (H9), 3.58 – 4.01 (H3-H6), 4.2-4.5 (H2′ -H6′)

NCT7: δ = 3.03 (H8), 3.15 (H2), 3.32 (H9), 3.58 – 4.01 (H3-H6), 4.2-4.5 (H2′ -H6′)

NCT19: δ = 3.03 (H8), 3.14 (H2), 3.31 (H9), 3.57 – 4.02 (H3-H6), 4.2-4.5 (H2′ -H6′)

NC: δ = 1.93, 2.05 (H7), 3.11 (H2), 3.71 – 3.87 (H3-H6)

Figure S5. 1H-NMR spectra of the studied NCT and NC fibers and TMC, recorded in D2O/AcOH

| - TMC |  |
| --- | --- |
| - NC | - NCT19 |
| - NCT7 | - NCT3 |

Figure S6. POM images of the NCT fibers and TMC (scale bar: 20 m)

| - NC | - NCT19 |
| --- | --- |
| - NCT7 | - NCT 3 |

Figure S7. Histograms of the fibers’ alignment assigned by Image J

| - NC | - NCT19 |
| --- | --- |
| - NCT7 | - NCT3 |

Figure S8. Diameter distribution histograms of the fibers determined from SEM images

- NC

- NCT19

- NCT7

- NCT3

Figure S9. The kinetics of water vapor sorption uptake (blue colour was used for the steps of increasing the humidity; red colour was used for the mass increase of the sample in response to the increase of humidity

.

Figure S10. Optical microscopy images of liver structure in rats from the control (A); NCT3 (B); NCT7 (C); and NCT19 (D) groups. H&E x 50 stains.

Figure S11. Optical microscopy images of kidney structure in rats from the control (A); NCT3 (B); NCT7 (C); and NCT19 (D) groups. H&E x 200 stain

Table S1. Fiber mats morphological parameters

|  | NC | NCT3 | NCT7 | NCT19 |
| --- | --- | --- | --- | --- |
| Diameter Mean (µm) | 0.171944 | 0.153577 | 0.158247 | 0.193082 |
| Diameter SD (µm) | 0.033644 | 0.031823 | 0.064791 | 0.033896 |
| Mean Inter-fiber Pore Area (µm2) | 51.69674 | 12.10142 | 7.282158 | 28.53398 |
| Inter-fiber pore Area SD (µm2) | 61.69834 | 13.63104 | 9.193949 | 40.95672 |
| Min. Pore Area (µm2) | 0.207469 | 0.099585 | 0.099585 | 0.099585 |
| Max. Pore Area (µm2) | 257.2614 | 93.84232 | 70.87137 | 246.083 |
| Percent Porosity (%) | 52.05 | 28.88 | 21.96 | 38.74 |

Table S2. Parameters of the dynamic water sorption (A = BET surface area; W= maximum water uptake)

| SAMPLE | A, m2 (BET) | Max water uptake (%) | Average pore size (nm) |
| --- | --- | --- | --- |
| NC | 301.6 | 28.5 | 1.89 |
| NCT19 | 284.1 | 41.9 | 2.95 |
| NCT7 | 287.1 | 45.4 | 3.16 |
| NCT3 | 247.6 | 40.3 | 3.26 |

Table S3. RBC, Hb, and Ht values expressed as the arithmetic mean ± S.D. of the average for 5 rats per lot

|  | Moment of determination | RBC (mil/μl) | SD | Hb (g/ml) | SD | Ht (%) | SD |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Control | 24 hours | 8.49 | 2.31 | 12.16 | 4.33 | 45.07 | 11.11 |
|  | 7 days | 8.67 | 2.53 | 11.63 | 3.88 | 45.45 | 10.93 |
| NCT3 | 24 hours | 8.54 | 2.38 | 11.49 | 3.47 | 44.83 | 10.35 |
|  | 7 days | 8.51 | 2.26 | 11.58 | 3.93 | 45.14 | 10.67 |
| NCT7 | 24 hours | 8.43 | 2.67 | 11.84 | 3.41 | 44.48 | 10.53 |
|  | 7 days | 8.48 | 2.16 | 12.22 | 4.16 | 44.56 | 11.22 |
| NCT19 | 24 hours | 8.62 | 3.26 | 12.14 | 4.31 | 45.27 | 10.31 |
|  | 7 days | 8.56 | 2.33 | 11.56 | 3.67 | 44.53 | 10.55 |

Table S4. Percentage values of components of leukocyte formula expressed arithmetic mean ± S.D. of the average for 5 rats per lot

|  | Moment of determination | Leukocyte formula (%) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | PMN | SD | Ly | SD | E | SD | M | SD | B | SD |
| Blank | 24 hours | 27.1 | 8.16 | 69 | 13.17 | 0.3 | 0.01 | 3.4 | 0.1 | 0.2 | 0.01 |
|  | 7 days | 27.3 | 8.41 | 68.7 | 13.33 | 0.3 | 0.03 | 3.5 | 0.1 | 0.2 | 0.03 |
| NCT3 | 24 hours | 26.8 | 7.29 | 69.3 | 12.67 | 0.4 | 0.03 | 3.3 | 0.05 | 0.2 | 0.01 |
|  | 7 days | 27.2 | 7.55 | 68.8 | 13.25 | 0.3 | 0.03 | 3.5 | 0.05 | 0.2 | 0.01 |
| NCT7 | 24 hours | 27.4 | 7.67 | 68.6 | 12.83 | 0.3 | 0.01 | 3.5 | 0.1 | 0.2 | 0.01 |
|  | 7 days | 27.6 | 8.43 | 68.5 | 12.55 | 0.3 | 0.01 | 3.4 | 0.05 | 0.2 | 0.03 |
| NCT19 | 24 hours | 26.9 | 7.33 | 68.9 | 13.41 | 0.4 | 0.03 | 3.6 | 0.1 | 0.2 | 0.01 |
|  | 7 days | 27.5 | 8.17 | 68.6 | 12.88 | 0.3 | 0.05 | 3.4 | 0.1 | 0.2 | 0.01 |

Table S5. Serum levels of GPT, GOT, and LDH expressed as the arithmetic mean ± S.D. of the average for 5 rats per lot.

|  | Moment of determination | GPT (U/l) | SD | GOT (U/l) | SD | LDH (U/l) | SD |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Blank | 24 hours | 47.65 | 11.88 | 124.12 | 27.93 | 1279.25 | 135.51 |
|  | 7 days | 47.34 | 13.26 | 125.64 | 28.51 | 1283.54 | 131.16 |
| NCT3 | 24 hours | 46.76 | 12.79 | 122.38 | 29.25 | 1280.39 | 134.39 |
|  | 7 days | 47.55 | 11.33 | 124.82 | 28.67 | 1285.46 | 136.88 |
| NCT7 | 24 hours | 46.39 | 12.67 | 123.46 | 28.79 | 1294.32 | 135.43 |
|  | 7 days | 46.64 | 14.55 | 121.65 | 30.16 | 1289.27 | 132.27 |
| NCT19 | 24 hours | 47.48 | 13.39 | 125.76 | 29.75 | 1298.16 | 137.55 |
|  | 7 days | 48.16 | 15.22 | 123.53 | 29.33 | 1287.43 | 135.67 |

Table S6. Effects of TMC-NCT nanofiber administration on blood urea and creatinine values. Values are represented as the arithmetic mean ± S.D. of the average for 5 animals per lot.

|  | Moment of determination | Urea (mg/dl) | SD | Creatinine (mg/dl) | SD |
| --- | --- | --- | --- | --- | --- |
| Blank | 24 hours | 42.67 | 14.26 | 0.16 | 0.03 |
|  | 7 days | 43.56 | 15.79 | 0.15 | 0.03 |
| NCT3 | 24 hours | 43.48 | 14.33 | 0.15 | 0.03 |
|  | 7 days | 42.33 | 13.45 | 0.16 | 0.01 |
| NCT7 | 24 hours | 42.27 | 13.83 | 0.15 | 0.03 |
|  | 7 days | 44.72 | 15.22 | 0.16 | 0.05 |
| NCT19 | 24 hours | 43.38 | 14.67 | 0.17 | 0.03 |
|  | 7 days | 43.46 | 15.16 | 0.15 | 0.01 |

Table S7. Values of the serum complement activity and peripheral blood PMN phagocytosis capacity (NBT %), expressed as the arithmetic mean ± S.D. of the average for 5 animals per lot

|  | Moment of determination | Complement (UCH50) | SD | NBT (%) | SD |
| --- | --- | --- | --- | --- | --- |
| Blank | 24 hours | 54.45 | 14.43 | 14.21 | 5.26 |
|  | 7 days | 53.76 | 14.88 | 14.42 | 4.43 |
| NCT3 | 24 hours | 53.39 | 15.26 | 14.78 | 4.51 |
|  | 7 days | 55.12 | 14.51 | 14.64 | 3.38 |
| NCT7 | 24 hours | 54.34 | 15.43 | 14.53 | 4.67 |
|  | 7 days | 53.61 | 16.51 | 14.19 | 3.88 |
| NCT19 | 24 hours | 54.46 | 15.38 | 14.12 | 5.26 |
|  | 7 days | 55.73 | 15.67 | 14.75 | 4.38 |

Table S8. Wound closure (%)

| day | G | G-SFT | NCT7 |
| --- | --- | --- | --- |
| 22 | -19±15 | -22.5±9 | -49.57±0 |