Supplemental information

Integration of AIEgens into Covalent Organic Frameworks for Pyroptosis and Ferroptosis Primed Cancer Immunotherapy

Liang Zhang1,2,4,5, An Song1,5, Qi-Chao Yang1, Shu-Jin Li1, Shuo Wang1, Shu-Cheng Wan1, Jianwei Sun2, Ryan T. K. Kwok2, Jacky W. Y. Lam2,*, Hexiang Deng4,*, Ben Zhong Tang2,3,*, Zhi-Jun Sun1,*

11The State Key Laboratory Breeding Base of Basic Science of Stomatology (Hubei-MOST) & Key Laboratory of Oral Biomedicine Ministry of Education, School and Hospital of Stomatology, Wuhan University, Wuhan 430079, China.

2 Department of Chemistry, and The Hong Kong Branch of Chinese National Engineering Research Center for Tissue Restoration and Reconstruction, The Hong Kong University of Science and Technology, Clear Water Bay, Kowloon, Hong Kong, 999077, China.

3 Shenzhen Institute of Aggregate Science and Technology, School of Science and Engineering, The Chinese University of Hong Kong, Shenzhen, Guangdong 518172, China.

4 Key Laboratory of Biomedical Polymers-Ministry of Education, College of Chemistry and Molecular Sciences, Wuhan University, Luojiashan, Wuhan 430072, China.

5These authors contributed equally: Liang Zhang, An Song.

*Email: chjacky@ust.hk; hdeng@whu.edu.cn; tangbenz@cuhk.edu.cn; sunzj@whu.edu.cn

Experimental Section

Chemicals: The organic solvent was procured from Adamas-beta®, while 2,7-dichloro-dihydrofluorescein diacetate (DCFH-DA) and N1,N1'-(1,4-phenylene)bis(N1-(4-aminophenyl)-benzene-1,4-diamine) (M-TPA) were obtained from Jilin Chinese Academy of Sciences-Yanshen Technology Co., Ltd. Puromycin, fetal bovine serum (FBS), penicillin/streptomycin (PS), and RPMI-1640 medium were sourced from Thermo Fisher (MA, USA). The CCK8 was acquired from Dojindo Laboratories (Japan), while the anti-mouse PD-1 mAb (CD279) was procured from BioXcell (NH, USA).

Instruments: Fluorescence spectra were obtained using Cary Eclipse Fluorescence Spectrophotometer (Agilent Technologies). UV-vis absorption spectra were obtained using Cary 300 UV-vis Spectrophotometer (Agilent Technologies). Size distribution and zeta potential were detected by using Zetasizer Nano-ZS90 (Malvern). XPS was recorded by Thermal Fisher ESCALAB 250Xi. ICP measurements were performed on a THERMO Intrepid XSP Radial ICP-AES instrument.

Synthesis of COF@PEG sample: These COF samples were well dispersed into PBS solution using F-127 as PEG gens. Typically, 100 mg of COF samples and 200 mg F-127 were dispersed in 100 ml PBS and then sonicated via an 1800 W ultrasonic cell shredder (JY99-IIDN, from Ningbo Scientz Biotechnology Co., Ltd, www.scientz.com) for 24 h. The resulting mixture was centrifuged at 1500 rpm for 30 min to discard un-isolated nanoparticles and then centrifuged at 10000 rpm for 20 min to obtain the isolated COF@PEG samples.

FT-IR spectra for ligands and COFs: All IR spectra were recorded on a Thermo Nicolet iS10 IR spectroscopy made by Thermo fisher, and samples were tableted and utilized KBr background. The wavelength range is 3800 to 500 cm-1. The successful formation of imine linkage was evidenced by the emergence of a 1620 to 1622 cm-1 peak in the Fourier transform infrared (FT-IR) spectrum, representing the telescopic vibration of the imine bond (νC=N).

X-ray Photoelectron Spectrometer (XPS) measurement of the molecular chromophores and their corresponding COFs: X-ray Photoelectron Spectrometer (XPS) was carried out on a Thermo Fisher ESCALAB 250Xi spectrometer, with the ion source of Al Kα, and samples were prepared in tablet for the test. The XPS spectra reflected the change in the chemical environment of nitrogen before and after the conversion to COFs. New N 1s peaks were observed at 398.9 eV, indicating the successful formation of imine bonds.

UV-Vis diffuse reflectance spectra for ligands and COFs: UV-vis DRS of COFs were performed on a PerkinElmer Lambda 750 S spectroscopy using BaSO4 as background. Band gap calculations were based on the Kubleka-Munk theory. The optical absorption coefficient (α) was calculated from reflectance data according to the Kubelka-Munk equation that F(R) = α = (1-R)2/2R, in which R is the percentage of reflected light. The incident photon energy (hν) and the optical band gap energy (Eg) are related to the transformed Kubelka-Munk function, [F(R)hν]2 = A(hν-Eg), where Eg is the band gap energy, A is the constant depending on transition probability, and intercept of [F(R)hν]2 vs hν is Eg. In comparison to the corresponding molecular building blocks, these COFs exhibited smaller band gaps.

N2 adsorptions analysis of these COFs: N2 adsorptions isotherms were measured on a Quantachrome Autosorb-IQ2 automatic volumetric instrument in a liquid nitrogen bath (77 K). Ultra-high purity grade N2 was used for the adsorption experiments. The BET surface area analysis was performed by plotting x/v(1 - x) vs x, where x = P/P0 (P0 = 1 bar) and v is the volume of nitrogen adsorbed per gram of COF at standard temperature and pressure (STP), where satisfactory correlation coefficients and positive C constant were observed. The slope ([c - 1]/vmc) and y-intercept (1/vmc) of the linear region between the dashed lines give the monolayer capacity, vm, that is then used to calculate the surface area from A = vmσ0NAV, where σ0 is the cross-section area of the adsorbate at liquid density (16.2 Å2 for nitrogen) and NAV is Avogadro’s number. The surface areas of these COFs range from 780 to 870 m2 g-1.

Determine the crystal structure of these COFs: Powder X-ray diffraction (PXRD) characterization was performed on a Smart lab diffractometer (Rigaku) with filtered Cu Kα radiation. Molecular models of COF-818 and COF-919 were generated with the Materials Studio (ver. 8.0) suite of programs. Pawley refinement was performed using Reflex, a software package for crystal determination from the PXRD pattern. Unit cell dimension was set to the theoretical parameters. The Pawley refinement was performed to optimize the lattice parameters iteratively until the Rwp and Rp value converges and the overlay of the observed with refined profiles shows good agreement. The lattice models were then fully optimized using MS Forcite molecular dynamics module method for each COF model. We performed Pawley refinement using the Reflex Plus module of the Material Studio, which showcases good agreement with the experimental PXRD patterns, with (Rwp, Rp) values of (1.11%, 0.85%) for COF-818, (Rwp, Rp) values of (0.58%, 0.47%) for COF-919 with Pawley refined cell parameters of a = 28.03 Å, b = 22.59 Å, c = 3.72 Å and α = β = γ = 90°, for COF-818, a = 27.39 Å, b = 21.73 Å, c = 3.91 Å, α = β = γ = 90° for COF-919.

DFT calculations: The specific process conformational search is to use ORCA5.0.3 package1, and the first excited state geometry optimization was conducted under the wB97X-D3/def2SVP level2-3.

Cellular iron assay: The intracellular ferrous iron (Fe2+) level was determined using an iron assay kit, as per the manufacturer's instructions. Briefly, cells were seeded onto a plate with 5 × 106 cells per plate, collected, and washed in ice-cold phosphate buffer solution. Next, 100-200 μl of lysate was added, and the mixture was centrifuged at 4 °C. The supernatant was then treated with an iron reducer and incubated at 60℃ for 60 min. Subsequently, 30 μl of the iron probe was added, and the solution was mixed thoroughly using a horizontal shaker and incubated at 25 °C for 30 min. Finally, the 550 nm absorbance peak was measured using a microplate reader.

Mitochondrial morphology assays: After washing with PBS three times, 4T1 cells were fixed in 4% paraformaldehyde solution for 1 hour, and the mitochondrial morphology was analyzed by TEM. The cells were fixed in 0.1 M sodium cacodylate buffer solution (pH 7.4) with 2.5% glutaraldehyde, followed by postfixation in 2% aqueous osmium tetroxide and dehydration in an ethanol/propylene oxide mixture. The cells were then embedded in Epon solution for 24 h at 60 °C (Merck, Darmstadt, Germany). Prior to TEM analysis, the cells were cut into ultra-thin sections, stained with 0.5% uranyl acetate for 30 min, and then further stained with 3% lead citrate for 7 min.

References

1  Neese, F. et al. Electronic structure and spectroscopy of novel copper chromophores in biology. Konstanz: University of Konstanz; 1997.

2  Chai, J.-D. & Head-Gordon, M. et al. Systematic optimization of long-range corrected hybrid density functionals. J. Chem. Phys. 128, 084106-084130 (2008).

3  Grimme S. et al. A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. J. Chem. Phys. 132, 154104-154123 (2010).

Fig. S1. Space-filling models of COF-818 from the top view.

Fig. S2. Space-filling models of COF-919 from the top view.

Fig. S3. Connolly surface of COF-818, carbon, hydrogen and nitrogen atoms are represented as grey, white, and blue spheres, respectively.

Fig. S4. Solvent surface of COF-818, carbon, hydrogen and nitrogen atoms are represented as grey, white, and blue spheres, respectively.

Fig. S5. Connolly surface of COF-919, carbon, hydrogen and nitrogen atoms are represented as grey, white, and blue spheres, respectively.

Fig. S6. Solvent surface of COF-919, carbon, hydrogen and nitrogen atoms are represented as grey, white, and blue spheres, respectively.

Table S1. Crystallographic Information of Modeled COFs.

|  | COF-818 | COF-919 |
| --- | --- | --- |
| Space group | Cmmm | Cmmm |
| a (Å) | 28.03 | 27.39 |
| b (Å) | 22.59 | 21.73 |
| c (Å) | 3.72 | 3.91 |
| Rp (%) | 1.11 | 0.58 |
| Rwp(%) | 0.85 | 0.47 |
| α (˚) β(˚) γ(˚) | 90 90 90 | 90 90 90 |

Table S2. Atomic parameters of COF-818

| Atomic parameters of COF-818 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | x (Å) | y (Å) | z (Å) | Atom | x (Å) | y (Å) | z (Å) |
| C1 | 0.32594 | 0.34581 | -0.04425 | C32 | 0.47669 | 0.55476 | 0.02905 |
| C2 | 0.30363 | 0.29411 | -0.06502 | C33 | 0.67003 | 0.34052 | -0.07718 |
| C3 | 0.7659 | 0.65991 | -0.00925 | C34 | 0.69191 | 0.28797 | -0.08823 |
| C4 | 0.30425 | 0.39753 | -0.0125 | C35 | 0.23611 | 0.66352 | 0.10739 |
| C5 | 0.25664 | 0.29161 | -0.0541 | C36 | 0.69276 | 0.39166 | -0.0508 |
| N6 | 0.80966 | 0.77384 | -0.02624 | C37 | 0.73909 | 0.28431 | -0.07152 |
| C7 | 0.02409 | 0.95247 | 0.23996 | N38 | 0.19385 | 0.77867 | 0.10378 |
| C8 | 0.90446 | 0.89009 | -0.10583 | C39 | 0.97703 | 0.95271 | 0.22266 |
| C9 | 0.88125 | 0.83352 | -0.10004 | C40 | 0.10133 | 0.89555 | -0.03713 |
| C10 | 0.19134 | 0.12332 | -0.12048 | C41 | 0.12494 | 0.84087 | -0.01118 |
| C11 | 0.88098 | 0.94214 | -0.03975 | C42 | 0.80467 | 0.11398 | -0.12374 |
| C12 | 0.83421 | 0.82837 | -0.02832 | C43 | 0.12247 | 0.94566 | 0.05546 |
| C13 | 0.76643 | 0.76982 | 0.01273 | C44 | 0.17061 | 0.83436 | 0.1044 |
| C14 | 0.66797 | 0.44742 | -0.03214 | C45 | 0.23732 | 0.77212 | 0.15368 |
| C15 | 0.62081 | 0.44737 | -0.02267 | C46 | 0.33038 | 0.45176 | 0.01471 |
| C16 | 0.52285 | 0.44784 | 0.0058 | C47 | 0.37757 | 0.45054 | 0.01009 |
| C17 | 0.67314 | 0.65925 | 0.02844 | C48 | 0.47577 | 0.4483 | 0.01524 |
| C18 | 0.69572 | 0.71146 | 0.03246 | C49 | 0.32932 | 0.66027 | 0.13999 |
| C19 | 0.23236 | 0.34311 | -0.0236 | C50 | 0.30739 | 0.71228 | 0.16082 |
| C20 | 0.69499 | 0.60708 | 0.00595 | C51 | 0.76435 | 0.33554 | -0.04586 |
| C21 | 0.74266 | 0.71294 | 0.01267 | C52 | 0.30655 | 0.60959 | 0.10268 |
| N22 | 0.19095 | 0.2281 | -0.03032 | C53 | 0.26026 | 0.71503 | 0.1435 |
| C23 | 0.9745 | 0.04987 | -0.23757 | N54 | 0.80463 | 0.21921 | -0.03568 |
| C24 | 0.10073 | 0.11085 | 0.07441 | C55 | 0.0242 | 0.05139 | -0.22782 |
| C25 | 0.12327 | 0.16579 | 0.05734 | C56 | 0.89824 | 0.10517 | 0.05556 |
| C26 | 0.81611 | 0.88067 | 0.02845 | C57 | 0.87405 | 0.15862 | 0.04873 |
| C27 | 0.12219 | 0.0601 | -0.00522 | C58 | 0.19317 | 0.8828 | 0.20501 |
| C28 | 0.1685 | 0.17227 | -0.03637 | C59 | 0.87707 | 0.05438 | -0.02823 |
| C29 | 0.23412 | 0.23453 | -0.06755 | C60 | 0.82766 | 0.16346 | -0.03906 |
| C30 | 0.33153 | 0.55461 | 0.07254 | C61 | 0.76114 | 0.22632 | -0.07806 |
| C31 | 0.37873 | 0.55465 | 0.06648 | C62 | 0.66909 | 0.55174 | -0.00251 |

Table S2. Atomic parameters of COF-818

| Atomic parameters of COF-818 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | x (Å) | y (Å) | z (Å) | Atom | x (Å) | y (Å) | z (Å) |
| C63 | 0.62192 | 0.55281 | 0.00645 | H98 | 0.398 | 0.59825 | 0.08733 |
| C64 | 0.52378 | 0.5543 | 0.01943 | H99 | 0.45821 | 0.59904 | 0.03875 |
| C65 | 0.0492 | 0.00345 | 0.00701 | H100 | 0.67192 | 0.24497 | -0.11178 |
| C66 | 0.5973 | 0.50035 | -0.00317 | H101 | 0.19767 | 0.66501 | 0.09413 |
| C67 | 0.54738 | 0.50084 | 0.00758 | H102 | 0.95677 | 0.91824 | 0.37899 |
| C68 | 0.9518 | 7.3E-4 | -0.01352 | H103 | 0.06487 | 0.89627 | -0.13581 |
| C69 | 0.40223 | 0.5023 | 0.03543 | H104 | 0.10729 | 0.79769 | -0.08596 |
| C70 | 0.45216 | 0.50177 | 0.02691 | H105 | 0.76724 | 0.11673 | -0.19358 |
| C71 | 0.30876 | 0.50348 | 1.04574 | H106 | 0.25943 | 0.81247 | 0.2088 |
| C72 | 0.25922 | 0.61054 | 1.08778 | H107 | 0.39612 | 0.40647 | -0.01482 |
| C73 | 0.25714 | 0.39856 | 0.99729 | H108 | 0.45627 | 0.40475 | 0.01345 |
| C74 | 0.69077 | 0.49929 | 0.97867 | H109 | 0.32722 | 0.75525 | 0.19324 |
| C75 | 0.74212 | 0.60678 | 0.98764 | H110 | 0.80275 | 0.3329 | -0.03293 |
| C76 | 0.74261 | 0.38988 | 0.96394 | H111 | 0.04452 | 0.08586 | -0.38362 |
| C77 | 0.82788 | 0.06009 | 0.87695 | H112 | 0.93553 | 0.10512 | 0.13177 |
| C78 | 0.16723 | 0.06615 | 0.89045 | H113 | 0.89177 | 0.20205 | 0.11689 |
| C79 | 0.17047 | 0.93753 | 1.18913 | H114 | 0.22967 | 0.87904 | 0.30004 |
| C80 | 0.83668 | 0.92967 | 1.02444 | H115 | 0.74023 | 0.18452 | -0.12174 |
| N81 | 0.90284 | 0.99922 | -0.02694 | H116 | 0.60329 | 0.59695 | 0.02178 |
| N82 | 1.09818 | 1.00316 | 0.01892 | H117 | 0.54328 | 0.59785 | 0.02122 |
| H83 | 0.32316 | 0.25081 | -0.09234 | H118 | 0.23986 | 0.56713 | 1.05926 |
| H84 | 0.80434 | 0.65991 | -0.02465 | H119 | 0.23852 | 0.4426 | 1.02145 |
| H85 | 0.04483 | 0.91944 | 0.40362 | H120 | 0.76268 | 0.43287 | 0.98312 |
| H86 | 0.94221 | 0.89194 | -0.16493 | H121 | 0.18546 | 0.02362 | 0.81076 |
| H87 | 0.90076 | 0.79089 | -0.15431 | H122 | 0.19072 | 0.97746 | 1.28585 |
| H88 | 0.22851 | 0.12633 | -0.19823 | H123 | 0.81199 | 0.96706 | 1.08668 |
| H89 | 0.74527 | 0.8116 | 0.049 | H124 | 0.36441 | 0.34639 | -0.05355 |
| H90 | 0.60156 | 0.40365 | -0.03099 | H125 | 0.36776 | 0.65912 | 0.15416 |
| H91 | 0.54134 | 0.40356 | -0.00346 | H126 | 0.27027 | 0.50362 | 1.0492 |
| H92 | 0.67629 | 0.75494 | 0.05225 | H127 | 0.76107 | 0.5629 | 0.97014 |
| H93 | 0.1939 | 0.34155 | -0.01533 | H128 | 0.82335 | 0.03973 | 0.59727 |
| H94 | 0.95294 | 0.08239 | -0.39828 | H129 | 0.81138 | 0.02858 | 1.07836 |
| H95 | 0.06367 | 0.10901 | 0.15689 | H130 | 0.6347 | 0.65881 | 0.04431 |
| H96 | 0.10432 | 0.20844 | 0.12259 | H131 | 0.63159 | 0.34182 | -0.09036 |
| H97 | 0.25462 | 0.19242 | -0.11286 | H132 | 0.72925 | 0.49936 | 0.97191 |

Table S3. Atomic parameters of COF-919

| Atomic parameters of COF-919 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | x (Å) | y (Å) | z (Å) | Atom | x (Å) | y (Å) | z (Å) |
| N1 | 0.32594 | 0.34581 | -0.04425 | C37 | 0.73909 | 0.28431 | -0.07152 |
| C2 | 0.30363 | 0.29411 | -0.06502 | N38 | 0.19385 | 0.77867 | 0.10378 |
| C3 | 0.7659 | 0.65991 | -0.00925 | C39 | 0.97703 | 0.95271 | 0.22266 |
| C4 | 0.30425 | 0.39753 | -0.0125 | C40 | 0.10133 | 0.89555 | -0.03713 |
| C5 | 0.25664 | 0.29161 | -0.0541 | C41 | 0.12494 | 0.84087 | -0.01118 |
| N6 | 0.80966 | 0.77384 | -0.02624 | C42 | 0.80467 | 0.11398 | -0.12374 |
| C7 | 0.02409 | 0.95247 | 0.23996 | C43 | 0.12247 | 0.94566 | 0.05546 |
| C8 | 0.90446 | 0.89009 | -0.10583 | C44 | 0.17061 | 0.83436 | 0.1044 |
| C9 | 0.88125 | 0.83352 | -0.10004 | C45 | 0.23732 | 0.77212 | 0.15368 |
| C10 | 0.19134 | 0.12332 | -0.12048 | C46 | 0.33038 | 0.45176 | 0.01471 |
| C11 | 0.88098 | 0.94214 | -0.03975 | C47 | 0.37757 | 0.45054 | 0.01009 |
| C12 | 0.83421 | 0.82837 | -0.02832 | C48 | 0.47577 | 0.4483 | 0.01524 |
| C13 | 0.76643 | 0.76982 | 0.01273 | N49 | 0.32932 | 0.66027 | 0.13999 |
| C14 | 0.66797 | 0.44742 | -0.03214 | C50 | 0.30739 | 0.71228 | 0.16082 |
| C15 | 0.62081 | 0.44737 | -0.02267 | C51 | 0.76435 | 0.33554 | -0.04586 |
| C16 | 0.52285 | 0.44784 | 0.0058 | C52 | 0.30655 | 0.60959 | 0.10268 |
| N17 | 0.67314 | 0.65925 | 0.02844 | C53 | 0.26026 | 0.71503 | 0.1435 |
| C18 | 0.69572 | 0.71146 | 0.03246 | N54 | 0.80463 | 0.21921 | -0.03568 |
| C19 | 0.23236 | 0.34311 | -0.0236 | C55 | 0.0242 | 0.05139 | -0.22782 |
| C20 | 0.69499 | 0.60708 | 0.00595 | C56 | 0.89824 | 0.10517 | 0.05556 |
| C21 | 0.74266 | 0.71294 | 0.01267 | C57 | 0.87405 | 0.15862 | 0.04873 |
| N22 | 0.19095 | 0.2281 | -0.03032 | C58 | 0.19317 | 0.8828 | 0.20501 |
| C23 | 0.9745 | 0.04987 | -0.23757 | C59 | 0.87707 | 0.05438 | -0.02823 |
| C24 | 0.10073 | 0.11085 | 0.07441 | C60 | 0.82766 | 0.16346 | -0.03906 |
| C25 | 0.12327 | 0.16579 | 0.05734 | C61 | 0.76114 | 0.22632 | -0.07806 |
| C26 | 0.81611 | 0.88067 | 0.02845 | C62 | 0.66909 | 0.55174 | -0.00251 |
| C27 | 0.12219 | 0.0601 | -0.00522 | C63 | 0.62192 | 0.55281 | 0.00645 |
| C28 | 0.1685 | 0.17227 | -0.03637 | C64 | 0.52378 | 0.5543 | 0.01943 |
| C29 | 0.23412 | 0.23453 | -0.06755 | C65 | 0.0492 | 0.00345 | 0.00701 |
| C30 | 0.33153 | 0.55461 | 0.07254 | C66 | 0.5973 | 0.50035 | -0.00317 |
| C31 | 0.37873 | 0.55465 | 0.06648 | C67 | 0.54738 | 0.50084 | 0.00758 |
| C32 | 0.47669 | 0.55476 | 0.02905 | C68 | 0.9518 | 7.3E-4 | -0.01352 |
| N33 | 0.67003 | 0.34052 | -0.07718 | C69 | 0.40223 | 0.5023 | 0.03543 |
| C34 | 0.69191 | 0.28797 | -0.08823 | C70 | 0.45216 | 0.50177 | 0.02691 |
| C35 | 0.23611 | 0.66352 | 0.10739 | N71 | 0.30876 | 0.50348 | 1.04574 |
| C36 | 0.69276 | 0.39166 | -0.0508 | C72 | 0.25922 | 0.61054 | 1.08778 |

Table S3. Atomic parameters of COF-919

| Atomic parameters of COF-919 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | x (Å) | y (Å) | z (Å) | Atom | x (Å) | y (Å) | z (Å) |
| C73 | 0.25714 | 0.39856 | 0.99729 | H100 | 0.398 | 0.59825 | 0.08733 |
| N74 | 0.69077 | 0.49929 | 0.97867 | H101 | 0.45821 | 0.59904 | 0.03875 |
| C75 | 0.74212 | 0.60678 | 0.98764 | H102 | 0.67192 | 0.24497 | -0.11178 |
| C76 | 0.74261 | 0.38988 | 0.96394 | H103 | 0.19767 | 0.66501 | 0.09413 |
| C77 | 0.82788 | 0.06009 | 0.87695 | H104 | 0.95677 | 0.91824 | 0.37899 |
| C78 | 0.16723 | 0.06615 | 0.89045 | H105 | 0.06487 | 0.89627 | -0.13581 |
| C79 | 0.17047 | 0.93753 | 1.18913 | H106 | 0.10729 | 0.79769 | -0.08596 |
| C80 | 0.83668 | 0.92967 | 1.02444 | H107 | 0.76724 | 0.11673 | -0.19358 |
| N81 | 0.90284 | 0.99922 | -0.02694 | H108 | 0.25943 | 0.81247 | 0.2088 |
| N82 | 1.09818 | 1.00316 | 0.01892 | H109 | 0.39612 | 0.40647 | -0.01482 |
| H83 | 0.32316 | 0.25081 | -0.09234 | H110 | 0.45627 | 0.40475 | 0.01345 |
| H84 | 0.80434 | 0.65991 | -0.02465 | H111 | 0.32722 | 0.75525 | 0.19324 |
| H85 | 0.04483 | 0.91944 | 0.40362 | H112 | 0.80275 | 0.3329 | -0.03293 |
| H86 | 0.94221 | 0.89194 | -0.16493 | H113 | 0.04452 | 0.08586 | -0.38362 |
| H87 | 0.90076 | 0.79089 | -0.15431 | H114 | 0.93553 | 0.10512 | 0.13177 |
| H88 | 0.22851 | 0.12633 | -0.19823 | H115 | 0.89177 | 0.20205 | 0.11689 |
| H89 | 0.74527 | 0.8116 | 0.049 | H116 | 0.22967 | 0.87904 | 0.30004 |
| H90 | 0.60156 | 0.40365 | -0.03099 | H117 | 0.74023 | 0.18452 | -0.12174 |
| H91 | 0.54134 | 0.40356 | -0.00346 | H118 | 0.60329 | 0.59695 | 0.02178 |
| H92 | 0.63571 | 0.65882 | 0.0439 | H119 | 0.54328 | 0.59785 | 0.02122 |
| H93 | 0.67629 | 0.75494 | 0.05225 | H120 | 0.23986 | 0.56713 | 1.05926 |
| H94 | 0.1939 | 0.34155 | -0.01533 | H121 | 0.23852 | 0.4426 | 1.02145 |
| H95 | 0.95294 | 0.08239 | -0.39828 | H122 | 0.76268 | 0.43287 | 0.98312 |
| H96 | 0.06367 | 0.10901 | 0.15689 | H123 | 0.18546 | 0.02362 | 0.81076 |
| H97 | 0.10432 | 0.20844 | 0.12259 | H124 | 0.19072 | 0.97746 | 1.28585 |
| H98 | 0.77847 | 0.88459 | 0.08802 | H125 | 0.81199 | 0.96706 | 1.08668 |
| H99 | 0.25462 | 0.19242 | -0.11286 |  |  |  |  |

Fig. S7. Aggregation-caused quenching (ACQ) effects of M-TPA, (A) photo luminescence spectrum with different water fractions. (B) ACQ curve of M-TPA.

Fig. S8. BET surface area was calculated for COF-818 and COF-919, based on nitrogen adsorption isotherm at 77 K. (A) and (B) pore size distribution of COF-818 and COF-919, (C) to (F) plot shows good fitting to the BET model.

Fig. S9. Light absorbance property of monomers.

Fig. S10. Intracellular uptake of COF-919 in 4T1 cells, detected by confocal microscopy.

Fig. S11. Cytotoxicity of COF-818 and COF-919 at different concentrations under 660 nm or 808 nm laser irradiation.

Fig. S12. Representative H&E staining of major organs of differently treated mice,

including hearts, livers, spleens, lungs, and kidneys, scale bar = 50 μm.

Fig. S13. Representative 4-HNE and Ki67 images of tumor tissues under different treatments, scale bar = 50 μm.

Fig. S14. Quantification and representative immunohistochemical images of CD8, Granzyme B, and cleaved caspase-3 under different treatments, scale bar = 50 μm.

Fig. S15. Gating strategy of DC cells in draining lymph nodes (DLN).

Fig. S16. Gating strategy of myeloid-derived suppressor cells (MDSCs) in spleen.

Fig. S17. Gating strategy of memory T cells.

Fig. S18. Gating strategy of Treg cells in draining lymph nodes (DLN).