Supplementary Material

A Appendix. Plasma reactions

The elementary reactions for argon1 are shown in Table A1.

Table A1. Elementary Argon plasma reactions

| Index | Reaction | Type | ΔE (eV) | Constant |
| --- | --- | --- | --- | --- |
| 1 | e+Ar→e+Ar | Elastic collision | 0 |  |
| 2 | e+Ar→2e+Ar+ | Direct ionization | 15.8 |  |
| 3 | e+Ar→e+Ar* | Excitation | 11.4 |  |
| 4 | e+Ar→e+Ar | Excitation | 13.1 |  |
| 5 | e+Ar*→2e+Ar+ | Stepwise ionization | 4.4 |  |
| 6 | 2Ar*→e+Ar*+Ar+ | Penning ionization |  | 6.2x10-10cm3s-1 |
| 7 | Ar*→hv+Ar | Radiation |  | 1.0x107s-1 |

Figure A1 shows the corresponding cross-section profiles with respect to electron energy.

Figure A1. Electron cross sections for plasma reactions used in the model. Curve labels correspond to indices of corresponding processes in Table 1.

B Appendix. Model validation

We validate our model by comparing our non-pulsed DCM results with those reported by Costin et al.2, also based on fluid model. Using the same geometry and discharge operating condition, we model the chamber as a cylinder with both radius and height equal to 26.95 mm, which carries argon gas at temperature of 3500 K and pressure of 20 mTorr (Fig. B1a). A constant potential of -550 V is applied to the lower target cathode of radius 16.5 mm; elsewhere, all other boundaries are grounded. Concentric magnets are positioned below the cathode, and they generate a magnetic field with field strength of 750 G on the cathode surface at the radial location of 9.5 mm, which focuses electrons as a spotlight about 6 mm away at radial position of 9.35 mm (Fig. B1a). Taking cross sections at radial position of 9.35 mm, we compare the electron density (ne) and argon ion density (ni) with Costin et al.2 and found good agreement in the results, with peak values of 2.5x1016 m-3 at z-location of 5 mm, as shown in Fig. B1b.

Figure B1. (a) Modelled electron density distribution in indicated chamber geometry and discharge operating conditions. (b) Comparison between electron density (ne) and argon ion density (ni) along the z direction at radial position r = 9.35 mm with reported results from Costin et al.2, also based on fluid model.

References

1	Rafatov, I., Bogdanov, E. A. & Kudryavtsev, A. A. On the accuracy and reliability of different fluid models of the direct current glow discharge. Phys. Plasmas 19, 033502, doi:10.1063/1.3688875 (2012).

2	Costin, C., Marques, L., Popa, G. & Gousset, G. Two-dimensional fluid approach to the dc magnetron discharge. Plasma Sources Sci. Technol. 14, 168, doi:10.1088/0963-0252/14/1/018 (2005).