Cellulose based fluorescent macromolecular sensors and their ability in 2, 4, 6-trinitrophenol detection

Xinyue Jiao, Heyi Li, and Xinjian Cheng*

School of Chemistry and Environmental Engineering, Wuhan Institute of Technology, Wuhan, 430073, China. E-mail: chxj606@163.com

Contents

1. Synthesis of reference small molecules……………………………………………..1

2. Characterization of small fluorescent probe molecules………………………...…..2

2.1. FTIR analysis……………………………………………………...…...………2

2.2. 1H NMR analysis……………………………………………………………….3

2.3. HR-MS analysis………...…………………………………………………..….5

2.4. SEM analysis………………………………………………….………………..5

3.Fluorescence spectra of AC 4……………………………………………………….7

4. UV-vis absorption analysis of CS 3, CS 4 and CS 5………...……………………..7

5. XPS of cellulose and its derivatives………………………………………….……..8

6. Structural formula of aromatic and aromatic nitro compounds………...…….….....8

7. Photographs……………………………………………………………………..…..9

1. Synthesis of small fluorescent probe molecules

1.1. Synthesis of compound AC 2

Add 4-bromo-1,8-naphthalic anhydride (5 g) and n-butylamine (1.6 g) to a 100 mL three-necked flask containing anhydrous ethanol solvent. The mixture was heated to reflux at 75°C under nitrogen for 8 hours, and the reaction was followed by TLC. After cooling to room temperature, the mixture was purified on a silica gel column (EA: PE = 1: 10). 1H NMR (400 MHz, CDCl3, ppm): 0.977-1.712 (s, H-7, 8, 9); 4.173 (s, H-6); 7.850-8.650 (s, H-1, 2, 3, 4, 5).

1.2. Synthesis of compound AC 3

Under N2 atmosphere, AC 2 (1 g), 2-Mercaptobenzothiazole (0.7 g) and potassium carbonate (0.7 g) were suspended in dry N,N–dimethylformamide (DMF) and stirred at 120℃ for 8 hours. After the reaction was completed, the mixture was cooled, and DMF was evaporated under vacuum, the crude product was extracted with chloroform (50 mL×2), and dried over anhydrous sodium sulfate, then the residue mixture was purified on a silica gel column (EA: PE = 1: 10).1H NMR (400 MHz, DMSO-d6, ppm): 0.935-1.645 (s, H-7, 8, 9); 4.069 (s, H-6); 7.358-8.746 (s, H-1, 2, 3, 4, 5, 10, 11, 12, 13).

1.3. Synthesis of compound AC 4

AC 2 (0.5 g) and solid KOH powder were added to the solvent DMSO (20 mL) containing the nucleophile benzothiazole-2-ylamine (0.3 g), stirred at room temperature for 2 hours, then heated to 90℃, and reacted for 12 hours under a nitrogen atmosphere. The reaction was followed by TLC throughout the process. After the completion of the reaction, the mixture was washed with water and then purified on a silica gel column (Acetone: PE = 1: 5).1H NMR (400 MHz, DMSO-d6, ppm): 0.914-1.638 (s, H-7, 8, 9); 4.048 (s, H-6); 7.202-8.458 (s, H-1, 2, 3, 4, 5, 10, 11, 12, 13).

1.4. Synthesis of compound AC 5

The substitution reaction of AC 2 was carried out in the same way, and the residue was purified by silica gel column chromatography using EA:PE as eluent to obtain a yellow solid.

2. Characterization of small fluorescent probe molecules

2.1. FTIR analysis

It can be seen from Fig. S1a that the presence of the naphthalene ring is indicated by the absorption peaks at 1582 cm-1 and 780 cm-1, and the characteristic peak of the C-Br bond of naphthalimide is at 521 cm-1. Due to the C-H stretching vibration on n-butylamine, AC 2 has characteristic peaks of saturated hydrocarbon groups at 2955 cm-1 and 2864 cm-1. When Bromine is replaced, the C-Br bond disappears, and a new characteristic peak of 1656 cm-1 appears, which is considered to be caused by C=N vibration. This peak can also be seen in the AC 4 spectrum. But the difference is that AC 4 exhibits N-H vibration at 3424 cm-1. Therefore, it was confirmed that the substitution reaction on the naphthalimide has been successfully performed.

Fig. S1. FT-IR spectra of (a)AC 1, AC 2, AC 3, AC 4 and (b)CS 4, CS 5

2.2. 1H NMR analysis

1H NMR was used to further determine the structure of the small molecule. The result is shown in Fig. S2-4. The 1H NMR spectra of CS 4 and CS 5 are shown in Fig S5-6.

Fig. S2. 1H NMR spectrum of AC 2 in CDCl3

Fig. S3. 1H NMR spectrum of AC 3 in DMSO-d6

Fig. S4. 1H NMR spectrum of AC 4 in DMSO-d6

2.3. HR-MS analysis

The high-resolution mass spectrum is shown in Fig. S5, which further proves that the naphthalimide small molecule probe was successfully synthesized.

Fig. S5. HR-MS spectrum of (a) AC 4

2.4. SEM analysis

Fig. S6. SEM micrograph of modified cellulose derivatives (a) CS 4, (b) CS 5. The scale bars for samples are 1 µm

3. Fluorescence spectra of AC 4

Because the fluorescence intensity of AC 3 is too weak, we chose the small molecule probe AC 4 as the reference object for fluorescence spectrum analysis. In order to study the effect of different pH conditions on it, B-R buffer solution was used to verify the stability of the sensor by measuring the absorbance at different pH values. The small molecule AC 4 was dissolved in acetonitrile (CH3CN), and buffer solutions (1.81-11.98) of different pH (CH3CN: B-R = 1:1) were added. It can be seen from Fig. S9a that when the pH is 11.98, the absorbance of the small molecule sensor AC 4 changes, but there is no significant change in the pH range of 1.81-11.71, indicating that it is still available in a wider pH range.

Fluorescence spectroscopy technology is used to study the ability of sensor AC 4 to recognize nitro compounds. Fig. S9b shows that under an excitation wavelength of 365 nm, AC 4 shows a fluorescence emission peak at 502 nm. After adding 7 equivalents of nitro compounds, TNP caused significant fluorescence quenching, and other nitro compounds showed no obvious fluorescence changes. The photo inserted in the Fig. S14b shows that this change in fluorescence quenching can be seen with the naked eye under ultraviolet light, and there is no obvious change in other aromatic nitro compounds. The results show that the sensor has a good ability to recognize TNP and can be used to distinguish TNP from other nitro compounds.

The recognition effect of the sensor and TNP was further studied by fluorescence titration experiment. As shown in Fig. S9c, as the TNP concentration increases from 0 equivalent to 20 equivalents, the fluorescence gradually decreases. Under the ultraviolet light, the gradual disappearance can be seen with the naked eye, and the result of TNP titration can be directly seen with the naked eye under natural light (Fig. S14). Therefore, the small molecule sensor AC 4 has the ability to specifically recognize TNP.

Fig. S7. (a) Fluorescence spectra of AC 4 at different pH (1.81-11.98). (b) Fluorescence intensity (λex = 365 nm) change of AC 4 (10-5 mol/L) in CH3CN after addition of nitro compounds (7 equivalent of sensor). Insert: photograph of blank sample with TNP under fluorescence. (c) Fluorescence intensity changes of sensors with different equiv of TNP (from 0 to 20 equiv), when λex = 365 nm

4. UV-vis absorption analysis of CS 3, CS 4 and CS 5

Fig. S8. UV-vis absorption of (a) CS 3, (b) CS 4, and (c) CS 5 (2mg/mL) in DMSO after addition of nitro compounds (2 equivalent of sensor). Insert: photograph of 4-NP and TNP with blank sample under natural light

5. XPS of cellulose and its derivatives

Table S1. Distribution of XPS spectra for cellulose derivatives.

| Entry | C | O | N | Br | S |
| --- | --- | --- | --- | --- | --- |
| CS |  |  |  |  |  |
| CS 1 |  |  |  |  |  |
| CS 2 |  |  |  |  |  |
| CS 3 |  |  |  |  |  |
| CS 4 |  |  |  |  |  |
| CS 5 |  |  |  |  |  |

6. Structural formula of aromatic and aromatic nitro compounds

Fig. S9. Structural formula and corresponding abbreviations of all aromatic and aromatic nitro compounds used in the experiment

7. Photographs

Fig. S10. Photographs of all macromolecular sensors recognizing nitro compounds from left to right, (a) photographs of CS 3 in DMSO under UV light, (b) photographs of CS 4 in mixed solvent (glycerol: ethanol=3:4) under UV light, (c) photographs of CS 5 in DMSO under UV light, (d) photographs of CS 3 in DMSO under natural light, (e) photographs of CS 4 in mixed solvent (glycerol: ethanol =3: 4) under natural light, (f) photographs of CS 5 in DMSO under natural light

Fig. S11. Photograph of all macromolecular sensors with different concentration of 4-NP or TNP from 1 equivalent to 10 equivalents. The left is under UV light, the right is under natural light. (a) CS 3 with TNP under UV light. (b) CS 4 with 4-NP under UV light. (c) CS 4 with TNP under UV light. (d) CS 5 with TNP under UV light. (e) CS 3 with TNP under natural light. (f) CS 4 with 4-NP under natural light. (g) CS 4 with TNP under natural light. (h) CS 5 with TNP under natural light

Fig. S12. Photographs of small sensors recognizing nitro compounds from left to right, (a) photographs of AC 3 in CH3CN under UV light, (b) photographs of AC 4 in CH3CN under UV light. Photograph of AC 3 with different concentration of TNP from 1 equivalent to 20 equivalents under (c) UV light, (d) natural light