Table 2 Key thermodynamic data of TGA curves of WCS, DWCS, CDWCS and PCDWCS

	Samples
	WCS
	DWCS
	CDWCS
	PCDWCS

	Onset decomposition temperature/℃
	301.0
	291.5
	290.2
	292.8

	End decomposition temperature/℃
	356.3
	360.3
	336.0
	333.4

	Rate of mass loss/%
	46.6
	50.8
	31.5
	30.9


