Preparation of magnetized carrageenan-metformin as a new bio-inspired heterogeneous nanocatalyst for the synthesis of dihydropyrano[2,3-c]pyrazoles

Forouzan Heydari1, Mohsen Bakhtiarian1, Mohammad Mehdi Khodaei1,2*

1Department of Organic Chemistry, Razi University, 67149-67346 Kermanshah, Iran

2Nanoscience and Nanotechnology Research Center (NNRC), Razi University, 67149-67346 Kermanshah, Iran

| Content | Page |
| --- | --- |
| Fig. S1. 1H-NMR Spectrum of 6-amino-3-methyl-4-phenethyl-1,4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6g). | 2 |
| Fig. S2. 13C-NMR Spectrum of 6-amino-3-methyl-4-phenethyl-1,4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6g). | 3 |
| Fig. S3. 1H-NMR Spectrum of 6-amino-3-methyl-4-(naphthalen-1-yl)-1,4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6i). | 4 |
| Fig. S4. 13C-NMR Spectrum of 6-amino-3-methyl-4-(naphthalen-1-yl)-1,4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6i). | 5 |
| Fig. S5. 1H-NMR Spectrum of 6-amino-3-methyl-4-phenyl-1,4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6j). | 6 |
| Fig. S6. 13C-NMR Spectrum of 6-amino-3-methyl-4-phenyl-1,4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6j). | 7 |
| Calculation of number of active sites, turnover number (TON), and turnover frequency (TOF) | 8 |
| Fig. S7. EDX of reused catalyst after 5 run. | 9 |

Fig. S1. 1H-NMR Spectrum of 6-amino-3-methyl-4-phenethyl-1,4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6g).

Fig. S2. 13C-NMR Spectrum of 5-amino-1, 3-diphenyl-1H-pyrazole-4-carbonitrile (6g).

Fig. S3. 1H-NMR Spectrum of 6-amino-3-methyl-4-(naphthalen-1-yl)-1, 4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6i).

Fig. S4. 13C-NMR Spectrum of 6-amino-3-methyl-4-(naphthalen-1-yl)-1, 4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6i).

Fig. S5. 1H-NMR Spectrum of 6-amino-3-methyl-4-phenyl-1, 4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6j).

Fig. S6. 13C-NMR Spectrum of 6-amino-3-methyl-4-phenyl-1, 4-dihydropyrano[2,3-c]pyrazole-5-carbonitrile (6j).

Calculation of number of active sites, turnover number (TON), and turnover frequency (TOF)

The effectiveness of a catalyst is defined by turnover number (TON) parameter.

TON=Yield ×mole of reactantsmole% of catalyst

TOF=TONTime (h)

- From titration the amount of acid sites will be = 0.76 mmol/g and amount of basic sites will be 0.56 mmol/g.

- Hence, the amount of active sites will be 1.32 mmol/g.

- Since we used 0.03 g of Carr-Met-MNPs under optimized conditions, the amount of active sites will be 0.0396 mmol.

- The mol% of sulfonic acid groups will be: (0.0396/0.0396 +1) × 100 = 3.8 mol%, where 1 is the mmol of limiting reactant.

For the model reaction:

TON=94×43.8=98.94

TOF=98.940.25=395.8

Using this method, TON and TOF were calculated for all reactions and the results are collected in Table 3.

Fig. S7. EDX of reused catalyst after 5 run.