Supporting Information

Citric acid cross-linked regenerated bacterial cellulose as biodegradable and biocompatible film for food packaging

Qingqing Yu1, Luyu Yang1, Shujun Wang2, Lei Zhang1*, and Dongping Sun1*

1Institute of Chemicobiology and Functional Materials, School of Chemistry and Chemical Engineering, Nanjing University of Science and Technology, 200 Xiao Ling Wei, Nanjing 210094, China.

2Department of Blood Transfusion, Jinling Hospital, Nanjing University School of Medicine, Nanjing 210002, China

*Corresponding author, E-mail:

leizhang@njust.edu.cn (Lei Zhang);

sundpe301@163.com (Dongping Sun).

Fig. S1. XPS spectrogram of CA15%-RC.

Fig. S2. SEM image of the surface of the RC, CA5%-RC, CA10%-RC, CA15%-RC, and CA20%-RC.

Fig. S3. Comparing the degradation time of CA15%-RC and other degradable materials previously reported.

Fig. S4. Combustion experiment of CA15%-RC shows it is ignitable.

Table S1. The O2 permeability and water vapor permeability of RC, CA5%-RC, CA10%-RC, CA15%-RC, and CA20%-RC.

| Samples | RC | CA5%-RC | CA10%-RC | CA15%-RC | CA20%-RC* |
| --- | --- | --- | --- | --- | --- |
| O2 permeability (m3.m/m2.s.Pa) |  | 1.71E-17 | 1.29E-17 | 2.13E-17 |  |
| water vapor permeability (g m-2 day-1) | 1698 | 1630 | 1624 | 1687 | 1646 |

*The O2 permeability of RC and CA20%-RC sample was not successful due to the smallest tensile strain.

Fig. S5. Stress - strain curve of CA15%-RC.

Fig. S6. CA15%-RC can be used to make a water balloon without any water leakage.

Fig. S7. Bar chart showing the hemolysis rates of RC, CA5%-RC, CA10%-RC, CA15%-RC, and CA20%-RC.