Supporting Information

Nanostructured Ce/CeO2-rGO: Highly Sensitive and Selective Electrochemical Hydrogen Sulphide Sensor

Shivsharan M. Malia,Shankar S. Narwadea, Balaji B. Mulikac,Vijay S. Sapnera,Shubham J. Annadateaand Bhaskar R. Satheab*

Figure S1: The SEM of Ce/CeO2 NPs:

S2: FTIR spectrum:

Figure. S2:  FTIR spectra of Ce/CeO2nanoparticles.

The FTIR spectra of Ce/CeO2 obtained using KBr pellet method, are shown in Figure. The band at 3500 cm−1 corresponds to δ (OH) vibration. Absorption peaks corresponding (1500-600 cm-1) to residual water and hydroxyl groups are usually detected in the FTIR spectrum of as prepared CeO2 nanoparticles regardless of the synthesis method [1, 2]. Large absorption band around 421 cm-1 is due to the υ(O–Ce–O) vibration.

FigureS3: Linearity data at Ce/CeO2-rGO for different H2S concentrations:

FigureS3: Linearity data at Ce/CeO2-rGO for different H2S concentrations between 1 ppm to 5 ppm.

FigureS4: Linearity data at Ce/CeO2-rGO for different H2S concentrations Error bar between 1 ppm to 5 ppm (a) and (b) graph.

Table S1: Comparative study of electrochemical H2S sensing

| Sr.no. | Modified Electrodes | Type | LOD (µM) | Ref. |
| --- | --- | --- | --- | --- |
| 1 | magnetic CNT/Co/MoS2 | Amperometry | 0.12 μM | 3 |
| 2 | Ti3C2 TxMXene | Amperometry | 0.016 μM | 4 |
| 3 | Cu2O − CuO@AuNIs ODH | Amperometry | 0.7 μM | 5 |
| 4 | GO/MB/Ag-NPs/GCE | DPV | 23.88 μM | 6 |
| 5 | PDMS/ITO | Amperometry | 0.17μM | 7 |
| 6 | ABFC/GO/GCE | DPV | 0.32 µM | 8 |
| 7 | Ce/CeO2-rGO | LSV | 1 ppm | Present work |

References:

- D.W. Wheeler, I. Khan, Vib. Spectrosc.70, 200 (2014).

- G. Jayakumar, A. A. Irudayaraj,  A. D. Raj,  Applied Physics A,125, 742 (2019)

- C. Li, D. Zhang, J. Wang, P. Hu, Z. Jiang, Anal. Chim.Acta. 975, 61 (2017).

- X. Liu, L. He, P. Li, X. Li, P. Zhang, ChemElectroChem.8,3658 (2021).

- M. Asif, A. Aziz, G. Ashraf, Z. Wang, J. Wang, M.Azeem, X. Chen, F. Xiao, H. Liu, ACS Appl. Mater. Interfaces.10, 36675 (2018).

- H. Shang, H. Xu, C. Wang, C. Chen, C. Wang, L. Jin, Y. Du, J. Nanopart. Res. 22, 1 (2020).

- S. Wang, X. Liu, M. Zhang, Anal. Chem. 89, 5382 (2017).

- K. Manibalan, V. Mani, P. C. Chang, C. H. Huang, S. T. Huang, K. Marchlewicz, S. Neethirajan, Biosens. Bioelectron. 96, 233 (2017).