Electronic Supplementary Information (ESI)

18-Crown-6 based supramolecular structure, hydrogen bonding behaviour and its nonlinear optical properties

Chellakarungu Balakrishnan1,2 • Muniyasamy Manonmani1 • Govindarajan Vinitha3 • 
Subbiah Meenakshisundaram1*

1 Department of Chemistry, Annamalai University, Annamalainagar - 608002, Tamil Nadu, India

2 Department of Chemistry, Erode Sengunthar Engineering College, Erode - 638057, Tamil Nadu, India.

3 Division of Physics, School of Advanced Science, VIT Chennai, Chennai - 600127, Tamil Nadu, India

| Title | Figure |
| --- | --- |
| FT-IR spectrum of (18C6).2(5ATIPA).2(H2O) | S1 |
| Percentage contributions to the Hirshfeld surface areas for the various close intermolecular contacts | S2 |

| Title | Table |
| --- | --- |
| Selected bond lengths [Å], angles [°] and torsion angles [°] for (18C6).2(5ATIPA).2(H2O) | S1 |

Fig. S1 FT-IR spectrum of (18C6).2(5ATIPA).2(H2O)

Fig. S2 Percentage contributions to the Hirshfeld surface areas for the various close intermolecular contacts.

Table S1. Selected bond lengths [Å], angles [°] and torsion angles [°] for (18C6).2(5ATIPA).2(H2O)

| Bond length [Å] |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| C(1)-C(2) | 1.41(5) | C(5)-C(6) | 1.34(5) | C(10)-O(7) |  | 1.45(6) |
| C(1)-C(6) | 1.52(5) | C(5)-I(2) | 2.15(4) | C(10)-C(11) |  | 1.51(2) |
| C(1)-I(3) | 2.07(4) | C(6)-C(7) | 1.49(5) | C(11)-O(6) |  | 1.34(6) |
| C(2)-N(1) | 1.34(5) | C(7)-O(4) | 1.16(4) | C(12)-O(6) |  | 1.41(6) |
| C(2)-C(3) | 1.43(5) | C(7)-O(3) | 1.38(4) | C(12)-C(13) |  | 1.51(2) |
| C(3)-C(4) | 1.34(5) | C(8)-O(2) | 1.11(4) | C(13)-O(5) |  | 1.44(2) |
| C(3)-I(1) | 2.15(3) | C(8)-O(1) | 1.39(4) | C(14)-O(5) |  | 1.44(2) |
| C(4)-C(5) | 1.36(5) | C(9)-C(14)#1 | 1.46(8) | - |  | - |
| C(4)-C(8) | 1.55(5) | C(9)-O(7) | 1.47(6) | - |  | - |
| Bond Angles [°] |  |  |  |  |  |  |
| C(2)-C(1)-C(6) | 120(4) | C(5)-C(4)-C(8) | 123(3) | O(2)-C(8)-C(4) |  | 126(4) |
| C(2)-C(1)-I(3) | 120(3) | C(6)-C(5)-C(4) | 126(4) | O(1)-C(8)-C(4) |  | 113(3) |
| C(6)-C(1)-I(3) | 119(3) | C(6)-C(5)-I(2) | 117(3) | C(14)#1-C(9)-O(7) |  | 114(5) |
| N(1)-C(2)-C(1) | 118(3) | C(4)-C(5)-I(2) | 116(3) | O(7)-C(10)-C(11) |  | 105(4) |
| N(1)-C(2)-C(3) | 127(3) | C(5)-C(6)-C(7) | 128(3) | O(6)-C(11)-C(10) |  | 109(4) |
| C(1)-C(2)-C(3) | 114(3) | C(5)-C(6)-C(1) | 115(3) | O(6)-C(12)-C(13) |  | 128(5) |
| C(4)-C(3)-C(2) | 126(3) | C(7)-C(6)-C(1) | 117(3) | O(5)-C(13)-C(12) |  | 97(4) |
| C(4)-C(3)-I(1) | 120(3) | O(4)-C(7)-O(3) | 124(3) | O(5)-C(14)-C(9)#1 |  | 105(5) |
| C(2)-C(3)-I(1) | 112(2) | O(4)-C(7)-C(6) | 124(3) | C(13)-O(5)-C(14) |  | 102(4) |
| C(3)-C(4)-C(5) | 117(3) | O(3)-C(7)-C(6) | 112(3) | C(11)-O(6)-C(12) |  | 111(4) |
| C(3)-C(4)-C(8) | 119(3) | O(2)-C(8)-O(1) | 121(3) | C(10)-O(7)-C(9) |  | 114(4) |
| Torsion Angles (°) |  |  |  |  |  |  |
| C(6)-C(1)-C(2)-N(1) |  | 178(4) | C(2)-C(1)-C(6)-C(5) |  | 9(6) |  |
| I(3)-C(1)-C(2)-N(1) |  | 2(6) | I(3)-C(1)-C(6)-C(5) |  | -175(3) |  |
| C(6)-C(1)-C(2)-C(3) |  | -10(6) | C(2)-C(1)-C(6)-C(7) |  | -178(4) |  |
| I(3)-C(1)-C(2)-C(3) |  | 173(3) | I(3)-C(1)-C(6)-C(7) |  | -1(4) |  |
| N(1)-C(2)-C(3)-C(4) |  | -177(4) | C(5)-C(6)-C(7)-O(4) |  | 67(5) |  |
| C(1)-C(2)-C(3)-C(4) |  | 12(6) | C(1)-C(6)-C(7)-O(4) |  | -106(4) |  |
| N(1)-C(2)-C(3)-I(1) |  | -11(5) | C(5)-C(6)-C(7)-O(3) |  | -111(4) |  |
| C(1)-C(2)-C(3)-I(1) |  | 178(3) | C(1)-C(6)-C(7)-O(3) |  | 76(4) |  |
| C(2)-C(3)-C(4)-C(5) |  | -11(6) | C(3)-C(4)-C(8)-O(2) |  | 74(5) |  |
| I(1)-C(3)-C(4)-C(5) |  | -176(3) | C(5)-C(4)-C(8)-O(2) |  | -96(5) |  |
| C(2)-C(3)-C(4)-C(8) |  | 179(4) | C(3)-C(4)-C(8)-O(1) |  | -98(4) |  |
| I(1)-C(3)-C(4)-C(8) |  | 14(5) | C(5)-C(4)-C(8)-O(1) |  | 92(4) |  |
| C(3)-C(4)-C(5)-C(6) |  | 9(6) | O(7)-C(10)-C(11)-O(6) |  | 68(6) |  |
| C(8)-C(4)-C(5)-C(6) |  | 179(4) | O(6)-C(12)-C(13)-O(5) |  | -58(8) |  |
| C(3)-C(4)-C(5)-I(2) |  | 178(3) | C(12)-C(13)-O(5)-C(14) |  | -104(5) |  |
| C(8)-C(4)-C(5)-I(2) |  | -12(5) | C(9)#1-C(14)-O(5)-C(13) |  | -163(4) |  |
| C(4)-C(5)-C(6)-C(7) |  | 179(4) | C(10)-C(11)-O(6)-C(12) |  | -170(4) |  |
| I(2)-C(5)-C(6)-C(7) |  | 10(5) | C(13)-C(12)-O(6)-C(11) |  | 167(6) |  |
| C(4)-C(5)-C(6)-C(1) |  | -8(6) | C(11)-C(10)-O(7)-C(9) |  | 171(5) |  |
| I(2)-C(5)-C(6)-C(1) |  | -177(3) | C(14)#1-C(9)-O(7)-C(10) |  | 172(5) |  |

Symmetry transformations used to generate equivalent atoms: #1 -x+1,-y+1,-z+1