Interface Engineering induced NiFe/Ni-Mo-S@CC Heterostructure as Enhanced Bifunctional Electrocatalysts for Overall Water Splitting

Zhangquan Gong, Wentao Cheng, Zheng Fang, Na Li, Yanmin Qin, Xing Wang*, Haifeng Bao*

School of Materials Science and Engineering, Key Laboratory for New Textile Materials and Applications of Hubei Province, State Key Laboratory of New Textile Materials and Advanced Processing Technologies, Wuhan Textile University, 430200 Wuhan, China

*Corresponding author E-mail: wx@wtu.edu.cn, baohaifeng@wtu.edu.cn

Fig. S1. EDS elemental mapping images of Ni-Mo-S@CC.

Fig. S2. The water and bubble contact angle of NiFe/Ni-Mo-S@CC.

Fig. S3. XPS full spectrum of (a) Ni-Mo-S@CC, (b) Ni/Ni-Mo-S@CC,

(c) Fe/Ni-Mo-S@CC samples, (d) NiFe/Ni-Mo-S@CC,.

Fig. S4. LSV curve of Ni/Ni-Mo-S@CC under reverse scan.

Fig. S5. CV curves of (a) Ni-Mo-S@CC, (b) Fe/Ni-Mo-S@CC, (c) Ni/Ni-Mo-S@CC, (d) NiFe/Ni-Mo-S@CC, (e) NiFe@CC taken at various scan rates of 80, 100, 120, 140, 160, 180 and 200 mV/s.

Fig. S6. LSV curves of NiFe/Ni-Mo-S@CC before and after 24 h stability test.

Potential change from 1.47 to 1.50 V at 100 mA cm-2

Fig. S7. Time-dependent current density curves for Ni-Mo-S@CC‖Ni-Mo-S@CC cell and corresponding polarization curves before and after stability test.

Table S1. The comparison of OER activity data for various catalysts.

| Catalyst electrodes | Support | η (mV) | Durability (h) | Reference |
| --- | --- | --- | --- | --- |
| NiFe/Ni-Mo-S@CC | CC | 161 (η10) | 24 | This work |
| CoFeNx HNAs/NF | Ni foam | 256 (η10) | 40 | [1] |
| S-doped Ni4Mo/CF | Cu foam | 140 (η10) | 60 | [2] |
| Co-Ni3S2 | Ni foam | 228 (η10) | / | [3] |
| Co(OH)2/NiMo CA@CC | CC | 267 (η10) | 24 | [4] |
| Co-W-B-P/CF | Cu foam | 280 (η10) | / | [5] |
| CNTs@NiP2/NbP | Ni foam | 248.2 (η20) | 32 | [6] |
| MoS2/Co9S8/Ni3S2/Ni | Ni foam | 166 (η10) | / | [7] |
| MoO3/Ni–NiO | CC | 347 (η100) | 10 | [8] |
| Au/Ni3S2/NF | Ni foam | 230 (η10) | 60 | [9] |
| Co2P/CoP@Co@NCNT | NCNT | 256 (η10) | 50 | [10] |
| CoFe2O4/CoO | / | 246 (η10) | / | [11] |
| CC/MOF-CoSe2@MoSe2 | CC | 183.8 (η10) | 24 | [12] |

Table S2. The comparison of HER activity data for various catalysts.

| Catalyst electrodes | Support | η (mV) | Durability (h) |  | Reference |
| --- | --- | --- | --- | --- | --- |
| NiFe/Ni-Mo-S@CC | CC | 72 (η10) | 24 | This work |  |
| CoFeNx HNAs/NF | Ni foam | 200 (η10) | 40 | [1] |  |
| S-doped Ni4Mo/CF | Cu foam | 128 (η10) | 60 | [2] |  |
| Co-Ni3S2 | Ni foam | 102 (η20) | / | [3] |  |
| Co(OH)2/NiMo CA@CC | CC | 30 (η10) | 24 | [4] |  |
| Co-W-B-P/CF | Cu foam | 65 (η10) | / | [5] |  |
| CNTs@NiP2/NbP | Ni foam | 137 (η20) | 32 | [6] |  |
| MoS2/Co9S8/Ni3S2/Ni | Ni foam | 113 (η10) | / | [7] |  |
| MoO3/Ni–NiO | CC | 62 (η10) | 20 | [8] |  |
| Au/Ni3S2/NF | Ni foam | 97 (η10) | 60 | [9] |  |
| Co2P/CoP@Co@NCNT | NCNT | 118 (η10) | 50 | [10] |  |
| CoFe2O4/CoO | / | 164 (η10) | / | [11] |  |
| CC/MOF-CoSe2@MoSe2 | CC | 109.9 (η10) | 24 | [12] |  |

Table S3. The comparison for overall water splitting of NiFe/Ni-Mo-S@CC with the electrocatalysts reported in 1 M KOH (V10-cell voltage at 10 mA cm-2).

| Catalyst electrodes | Support | V10 (V) | Durability (h) | Reference |
| --- | --- | --- | --- | --- |
| NiFe/Ni-Mo-S@CC | CC | 1.50 | 24 | This work |
| CoFeNx HNAs/NF | Ni foam | 1.592 | 40 | [1] |
| S-doped Ni4Mo/CF | Cu foam | 1.595 | 60 | [2] |
| Co-Ni3S2 | Ni foam | 1.54 | 25 | [3] |
| Co(OH)2/NiMo CA@CC | CC | 1.52 | 30 | [4] |
| Co-W-B-P/CF | Cu foam | 1.57 | 48 | [5] |
| CNTs@NiP2/NbP | Ni foam | 1.51 | 50 | [6] |
| MoS2/Co9S8/Ni3S2/Ni | Ni foam | 1.54 | 24 | [7] |
| MoO3/Ni–NiO | CC | 1.55 | 20 | [8] |
| Au/Ni3S2/NF | Ni foam | 1.52 | 60 | [9] |
| Co2P/CoP@Co@NCNT | NCNT | 1.60 | 12 | [10] |
| CoFe2O4/CoO | / | 1.614 | ∼60 | [11] |
| CC/MOF-CoSe2@MoSe2 | CC | 1.53 | 24 | [12] |

References

[1] D. Li, Y. Xing, R. Yang, T. Wen, D. Jiang, W. Shi, S. Yuan, Holey Cobalt-Iron Nitride Nanosheet Arrays as High-Performance Bifunctional Electrocatalysts for Overall Water Splitting, ACS Appl Mater Interfaces, 12 (2020) 29253-29263.

[2] S. Feng, J. Wang, W. Wang, X. Wang, Y. Zhang, Chenchen, A. Ju, J. Pan, R. Xu, The Ni‐Mo‐S Catalyst @Copper Foams with Excellent Stability and 1.5 V Drive Electrolytic Water, Advanced Materials Interfaces, 8 (2021) 2100500.

[3] C. Jin, P. Zhai, Y. Wei, Q. Chen, X. Wang, W. Yang, J. Xiao, Q. He, Q. Liu, Y. Gong, Ni(OH)2 Templated Synthesis of Ultrathin Ni3S2 Nanosheets as Bifunctional Electrocatalyst for Overall Water Splitting, Small, 17 (2021) 2102097.

[4] Q. Zhang, W. Xiao, W.H. Guo, Y.X. Yang, J.L. Lei, H.Q. Luo, N.B. Li, Macroporous Array Induced Multiscale Modulation at the Surface/Interface of Co(OH)2/NiMo Self‐Supporting Electrode for Effective Overall Water Splitting, Advanced Functional Materials, 31 (2021) 2102117.

[5] G. Hu, W. Fu, Y. Lin, Y. Yue, M. Wang, P. Liu, Y. Li, J. Li, L. Wei, X. Zhao, Y. Wei, Highly Efficient Nanoflower-like Bifunctional Electrocatalyst Co-W-B-P/CF for Overall Water Splitting, ACS Applied Energy Materials, 5 (2022) 4259-4269.

[6] S. Singh, D.C. Nguyen, N.H. Kim, J.H. Lee, Interface engineering induced electrocatalytic behavior in core-shelled CNTs@NiP2/NbP heterostructure for highly efficient overall water splitting, Chemical Engineering Journal, 442 (2022) 136120.

[7] Y. Yang, H. Yao, Z. Yu, S.M. Islam, H. He, M. Yuan, Y. Yue, K. Xu, W. Hao, G. Sun, H. Li, S. Ma, P. Zapol, M.G. Kanatzidis, Hierarchical Nanoassembly of MoS2/Co9S8/Ni3S2/Ni as a Highly Efficient Electrocatalyst for Overall Water Splitting in a Wide pH Range, J Am Chem Soc, 141 (2019) 10417-10430.

[8] X. Li, Y. Wang, J. Wang, Y. Da, J. Zhang, L. Li, C. Zhong, Y. Deng, X. Han, W. Hu, Sequential Electrodeposition of Bifunctional Catalytically Active Structures in MoO3/Ni-NiO Composite Electrocatalysts for Selective Hydrogen and Oxygen Evolution, Adv Mater, 32 (2020) 2003414.

[9] H. Liu, J. Cheng, W. He, Y. Li, J. Mao, X. Zheng, C. Chen, C. Cui, Q. Hao, Interfacial electronic modulation of Ni3S2 nanosheet arrays decorated with Au nanoparticles boosts overall water splitting, Applied Catalysis B: Environmental, 304 (2022) 120935.

[10] Z. Lu, Y. Cao, J. Xie, J. Hu, K. Wang, D. Jia, Construction of Co2P/CoP@Co@NCNT rich-interface to synergistically promote overall water splitting, Chemical Engineering Journal, 430 (2022) 132877.

[11] K. Srinivas, Y. Chen, Z. Su, B. Yu, M. Karpuraranjith, F. Ma, X. Wang, W. Zhang, D. Yang, Heterostructural CoFe2O4/CoO nanoparticles-embedded carbon nanotubes network for boosted overall water-splitting performance, Electrochimica Acta, 404 (2022) 139745.

[12] S.J. Patil, N.R. Chodankar, S.K. Hwang, P.A. Shinde, G. Seeta Rama Raju, K. Shanmugam Ranjith, Y.S. Huh, Y.K. Han, Co-metal–organic framework derived CoSe2@MoSe2 core–shell structure on carbon cloth as an efficient bifunctional catalyst for overall water splitting, Chemical Engineering Journal, 429 (2022) 132379.