Supplementary Materials

- Table S1. Selected bond lengths (A˚), angles (°) and Hydrogen-bond geometry for [Cd(maa)2(vim)2H2O]·H2O complex

- Table S2. Comparison of Langmuir and Freundlich isotherm constants

- Fig. S1. Langmuir adsorption isotherm of Cd(II)-IIP

- Fig. S2. Freundlich adsorption isotherm of Cd(II)-IIP

- Langmuir isotherm

- Freundlich isotherm

Table S1. Selected bond lengths (A˚), angles (°) and Hydrogen-bond geometry for [Cd(maa)2(vim)2H2O]·H2O complex

| Geometric parameters (Å, º) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| N1-Cd1 | 2.289 (3) | O1-Cd1 | 2.524(2) | O2-Cd1 |  | 2.373(3) |  |
| Cd-O3W | 2.334(4) | Cd1-N1i | 2.289 (3) | Cd1-O2i |  | 2.373 (3) |  |
| Cd1—O1i | 2.524 (2) |  |  |  |  |  |  |
| N1-Cd1-O3 | 84.89(7) | N1-Cd1-O2 | 100.15(11) | N1-Cd1-O1 |  | 89.92 (10) |  |
| O3-Cd1-O2 | 139.35(6) | O3-Cd1-O1 | 87.39 (5) |  | O2-Cd1-O1 |  | 52.60(8) |  |
| N1i-Cd1-O3 | 84.89(7) | N1i-Cd1-O2 | 87.65 (11) |  | N1-Cd1-O2i |  | 87.66(11) |  |
| N1i-Cd1-O2i | 100.15(11) | N1-Cd1-N1i | 169.77 (14) |  | N1i-Cd1-O2i |  | 100.15(11) |  |
| O3-Cd1-O2i | 139.35(6) | O2-Cd1-O2i | 81.30(12) |  | N1i-Cd1-O1 |  | 89.61(10) |  |
| O2i-Cd1-O1 | 132.56(8) | N1-Cd1-O1i | 8961(10) |  | N1i-Cd1-O1i |  | 89.92(10) |  |
| O3-Cd1-O1i | 87.39(5) | O2-Cd1-O1i | 132.56(8) |  | O2i-Cd1-O1i |  | 52.60(8) |  |
| (i)−x+1/2,−y+1,z |  |  |  |  |  |  |  |
| Hydrogen-bond geometry (Å, º) |  |  |  |  |  |  |  |
| D-H· · ·A | D-H | H···A | D···A | D-H···A |  |  |  |
| C5—H5···O1i | 0.93 | 2.39 | 3.260 (4) | 157 |  |  |  |
| O3—H3···O1ii | 0.82 (2) | 1.91(2) | 2.732 (2) | 179(4) |  |  |  |
| O4—H4···O2 iii | 0.84 (2) | 2.01 (2) | 2.787 (4) | 154(4) |  |  |  |
| (i)−x+1/2,−y+1,z; (ii)−x+1,−y+1, −z+1;(iii) x−1/2, y,−z+1. |  |  |  |  |  |  |  |

Table S2. Comparison of Langmuir and Freundlich isotherm constants

| Langmuir |  |  |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Qexp | Qmax | b | R2 |  | Kf | n | R2 |
| （mg/g） | （mg/g） |  |  |  |  |  |  |
| 43.0 | 75.2 | 0.005 | 0.3761 |  | 1.28 | 1.37 | 0.9534 |

Fig. S1. Langmuir adsorption isotherm of Cd(II)-IIP

Fig. S2. Freundlich adsorption isotherm of Cd(II)-IIP

Langmuir isotherm

Langmuir adsorption isotherm assumes that the maximum adsorption corresponds to a saturated monolayer of solute molecules on the adsorbent surface, having no interaction with molecules adsorbed from lateral sides. The linear form of Langmuir isotherm is given as:

CeQe=CeQmax+1Qmax .  b									(4)

Where Qe is the equilibrium metal ion concentration on the adsorbent (mg/g), Ce the equilibrium metal ion concentration in the solution (mg/L), Qmax is the maximum adsorption amount of the adsorbent (mg/g), and b is the Langmuir adsorption constant (L/mg).

Freundlich isotherm

Freundlich isotherm is mostly used to explain the heterogeneous systems and is given by the equation.

lnQe=lnKf+1nlnCe 								(5)

Where Ce is the equilibrium concentration in mg/L, Qe is the amount of adsorbent adsorbed in mg/g, Kf and n are constants of Freundlich. Kf shows adsorption capacity while n is the adsorption intensity.