Supporting Information
Improved mechanical, optical, and electrical properties of chitosan films with the synergistic reinforcing effect of carbon nanotubes and reduced graphene oxide for potential optoelectronic applications
Jesús Roldán González-Martínez1, Aurora Guadalupe Magallanes-Vallejo2, Ana Bertha López-Oyama 3,4*, Tomás Jesús Madera-Santana5, Karely Anaya-Garza3*, Eugenio Rodríguez-González2, Felipe Barfusson-Domínguez6, Rogelio Gámez-Corrales6
1DIFUS. Universidad de Sonora, Rosales y Transversal 83000 Hermosillo, Sonora, México

2 Cicata-IPN. Km 14.5 Carr. Puerto Industrial. 89600. Altamira, Tamaulipas, México

3DIQM. Universidad de Sonora, Rosales y Transversal 83000 Hermosillo, Sonora, México

4 Conacyt-Cicata Km. 14.5 Carretera Puerto Industrial. 89600. Altamira, Tamaulipas, México

5CIAD, A.C., Carr. Gustavo E. Astiazarán Rosas No. 46, Col. La Victoria, C.P. 83304, Hermosillo, Sonora, México.

6Departamento de Física, Universidad de Sonora, Rosales y Transversal, 83000 Hermosillo, Sonora, México

*Corresponding author: ablopezoy@conacyt.mx (López-Oyama, Ana Bertha) and karely.anaya@unison.mx (Anaya-Garza, Karely)

1. Supporting Figures and Tables
1.1. Figures
	
	
	CNT
	rGO
	CNT/rGO

	CSL
	[image: image1.png]15:51 ul 4G @)

< Floy Editar ()

BEERRER:: ::
l QO





	[image: image2.png]15:51 ull 4G @)

< Hoy Editar (&)

ERERRER: :::
d QO





	[image: image3.png]15:51 all 4G @)

Hoy .
< i Editar (&)

ERERRER: :::
n o





	[image: image4.png]15:51 all 4G @)

Hoy .
< i Editar (&)

ERERRER: :::
n o






	CSM
	[image: image5.png]15:51 ull 4G @)

< Hoy Editar (&)

ERERRER: :::
d QO





	[image: image6.png]15:51 ull 4G @)

< Hoy Editar (&)

ERERRER: :::
d QO





	[image: image7.png]15:51 ull 4G @)

< Hoy Editar (&)

ERERRER: :::
d QO





	[image: image8.png]15:51 al 4G @)

Hoy .
< i Editar ()

ERENRER: :::
n o






	CSH
	[image: image9.png]15:51 ull 4G @)

< 3% Editar ()

ERERREN: :::
n o





	[image: image10.png]15:51 al 4G @)

< Hﬂi Editar ()

RRRTA:E s
M Q





	[image: image11.png]15:51 ul 4G @

< Hloy Editar ()

BEENRAR: ::
d O





	[image: image12.png]15:51 ul 4G @)

< Floy Editar ()

BEERRER:: ::
l QO






	Fig. S1 Photographs of the as-prepared chitosan films and their composites.


	
[image: image13.emf]4000 3500 3000 2500 2000 1500 1000 500

Transmittance (%)

Wavenumber (cm

-1

)

 

 

 

CH

2

 

O-H

C-O-C

 

C=O

C-OH

 

(a)


	
[image: image14.emf]2900 2800 2700 2600 2500 2400 2300

 

 

 

P

22

P

12

+P

21

   

 

 

Raman shift (cm

-1

)

Intensity (a.u.)

(b) 

P

11



	Fig. S2 (a) FTIR spectra of graphene oxide (red line) and rGO (black line) and (b) Raman spectra of the rGO with the inner components that indicate a reduction of the oxygen-containing groups.


	
[image: image15.emf]24 25 26 27 28

2



 (degree)

 

 

 

      CNT

 

 

Intensity (a. u.)

(002)

cCSL

cCSM

 

cCSH

(101)

(a)


	
[image: image16.emf]25.0 25.5 26.0 26.5 27.0 27.5 28.0

2



 (degree)

 

 

 

 

 

(002)

(b)

eCSH

eCSM

rGO

Intensity (a. u.)

eCSL



	Fig. S3 Enlarged comparison of the (002) plane of (a) CNT-chitosan films and (b) rGO-chitosan films.


	
[image: image17.emf]1000 800 600 400 200 0

N1s

C1s

O1s

 

Intensity (a. u.)

Binding energy (eV)

mCSM

eCSM

cCSM

 

CSM

 

 

 

 



	Fig. S4 XPS survey spectrum and high resolution of CSM, cCSM, eCSM, and mCSM films.


	
[image: image18.emf]0.00 0.01 0.02 0.03 0.04 0.05

0

40

80

120

 

 

Strees (MPa)

Strain (mm)

 CSL

 cCSL

 eCSL

 mCSL

(a)



	
[image: image19.emf]0.000 0.022 0.044 0.066 0.088 0.110

0

20

40

60

80

100

 

 

Strain 

(

MPa

)

Strain (mm)

 CSM

 cCSM

 eCSM

 mCSM

(b)



	
[image: image20.emf]0.0000 0.0375 0.0750

0

20

40

60

80

 

 

Stress strain (MPa)

Strain (mm)

 CSH

 cCSH

 eCSH

 mCSH

(c)



	Fig. S5 Strain-stress curves extracted from the mechanical test of (a) LCS, (b) MCS, and (c) HCS and its composites.

	


[image: image21.png]



	Fig. S6 Flexible (a) and electrically conductive (b) composite film fabricated with low-molecular-weight chitosan and carbon nanotubes via cast-solvent technique.



1.2. Tables
Table S1 Labels of the formulations.

	Sample
	Label

	Chitosan low-molecular weight
	CSL

	Chitosan medium-molecular weight
	CSM

	Chitosan high-molecular weight
	CSH

	Chitosan low-molecular weight/MWCNT
	cCSL

	Chitosan medium-molecular weight/MWCNT
	cCSM

	Chitosan high-molecular weight/MWCNT
	cCSH

	Chitosan low-molecular weight/rGO
	eCSL

	Chitosan medium-molecular weight/rGO
	eCSM

	Chitosan high-molecular weight/rGO
	eCSH

	Chitosan low-molecular weight/MWCNT/rGO
	mCSL

	Chitosan medium-molecular weight/MWCNT/rGO
	mCSM

	Chitosan high-molecular weight/MWCNT/rGO
	mCSH


_1740928393.bin

_1740928567.bin

_1740928717.bin

_1741003738.bin

_1740928664.bin

_1740928462.bin

_1740927278.bin

_1740927402.bin

