Supplementary information

Understanding fluoride adsorption from groundwater by alumina modified with alum using PHREEQC surface complexation model

Francis Adu-Boahenea; Patrick Boakye*b,e; Frank Ofori Agyemangc; Jolly Kanjuad,e, Sampson Oduro‑Kwartenga

a Department of Civil Engineering (Regional Water and Environmental Sanitation Centre, Kumasi), Kwame Nkrumah University of Science and Technology, PMB, Kumasi, Ghana.

b,e Department of Chemical Engineering, Kwame Nkrumah University of Science and Technology, PMB, Kumasi, Ghana.

c Department of Materials Engineering, Kwame Nkrumah University of Science and Technology, PMB, Kumasi, Ghana.

dDepartment of Behavioural Science, Kwame Nkrumah University of Science and Technology, PMB, Kumasi, Ghana.

eElectrophysiology Laboratory, Institute of Computation and Neuroscience, Apemso Kumasi, Ghana.

- Kinetic studies

Table S 1. Results obtained from Kinetic studies at initial concentration of 1 mg/L

| Pseudo-First Order, 1 mg/L |  |  |  |  |
| --- | --- | --- | --- | --- |
| Adsorbents | qexp | qcal | K1 | R2 |
| A1 | 0.58 | 0.5725 | 0.0322 | 0.9377 |
| A2 | 0.86 | 0.8147 | 0.3675 | 0.3799 |
| A3 | 0.74 | 0.7042 | 0.1985 | 0.5388 |
| Pseudo- Second Order |  |  |  |  |
| Adsorbent | qexp | qcal | K2 | R2 |
| A1 | 0.58 | 0.6998 | 0.0463 | 0.8967 |
| A2 | 0.86 | 0.8514 | 0.9089 | 0.7530 |
| A3 | 0.74 | 0.7520 | 2.8281 | 0.8408 |
| Intraparticle Diffusion Model |  |  |  |  |
| Adsorbent | C | Kp | R2 |  |
| A1 | 0.0584 | 0.0445 | 0.7444 |  |
| A2 | 0.7141 | 0.0130 | 0.6307 |  |
| A3 | 0.5358 | 0.0194 | 0.6816 |  |

Table S 2. Results obtained from Kinetic studies at initial concentration of 10 mg/L

| Pseudo-First Order, 10 mg/L |  |  |  |  |
| --- | --- | --- | --- | --- |
| Adsorbents | qexp | qcal | K1 | R2 |
| A1 | 4.05 | 4.0237 | 0.1040 | 0.9066 |
| A2 | 4.30 | 4.1474 | 0.4775 | 0.3171 |
| A3 | 4.20 | 4.0187 | 0.3830 | 0.4621 |
| Pseudo- Second Order |  |  |  |  |
| Adsorbent | qexp | qcal | K2 | R2 |
| A1 | 4.05 | 4.4610 | 0.0321 | 0.8587 |
| A2 | 4.30 | 4.2746 | 0.2952 | 0.7565 |
| A3 | 4.20 | 4.1818 | 0.2061 | 0.8205 |
| Intraparticle Diffusion Model |  |  |  |  |
| Adsorbent | C | Kp | R2 |  |
| A1 | 2.2576 | 0.1783 | 0.4844 |  |
| A2 | 3.8029 | 0.0462 | 0.7091 |  |
| A3 | 3.5544 | 0.0601 | 0.7165 |  |

Table S 3. Results obtained from Kinetic studies at initial concentration of 15 mg/L

| Pseudo-First Order, 15 mg/L |  |  |  |  |
| --- | --- | --- | --- | --- |
| Adsorbents | qexp | qcal | K1 | R2 |
| A1 | 3.25 | 3.1107 | 0.2347 | 0.7263 |
| A2 | 8.23 | 7.6052 | 0.2237 | 0.3507 |
| A3 | 6.69 | 6.3432 | 0.1656 | 0.5005 |
| Pseudo- Second Order |  |  |  |  |
| Adsorbent | qexp | qcal | K2 | R2 |
| A1 | 3.25 | 3.2894 | 0.1371 | 0.9370 |
| A2 | 8.23 | 8.2014 | 0.0435 | 0.7265 |
| A3 | 6.69 | 6.7757 | 0.0442 | 0.7614 |
| Intraparticle Diffusion Model |  |  |  |  |
| Adsorbent | C | Kp | R2 |  |
| A1 | 2.5234 | 0.0679 | 0.6224 |  |
| A2 | 5.7423 | 0.2289 | 0.7283 |  |
| A3 | 4.6159 | 0.1907 | 0.6087 |  |

Table S 4. Results obtained from Kinetic studies at initial concentration of 30 mg/L

| Pseudo-First Order, 30 mg/L |  |  |  |  |
| --- | --- | --- | --- | --- |
| Adsorbents | qexp | qcal | K1 | R2 |
| A1 | 5.95 | 5.4483 | 0.1277 | 0.5319 |
| A2 | 7.85 | 7.6076 | 0.0858 | 0.9447 |
| A3 | 7.05 | 7.1844 | 0.1655 | 0.9280 |
| Pseudo- Second Order |  |  |  |  |
| Adsorbent | qexp | qcal | K2 | R2 |
| A1 | 5.95 | 5.8358 | 0.0977 | 0.7494 |
| A2 | 7.85 | 8.3617 | 0.06156 | 0.9414 |
| A3 | 7.05 | 7.7324 | 0.0878 | 0.9371 |
| Intraparticle Diffusion Model |  |  |  |  |
| Adsorbent | C | Kp | R2 |  |
| A1 | 3.6154 | 0.1925 | 0.6271 |  |
| A2 | 4.0141 | 0.3484 | 0.6186 |  |
| A3 | 5.1458 | 0.2229 | 0.5904 |  |

* Corresponding Author:

Email: patrickboakye@knust.edu.gh

Phone: +233 244109589