Supplemental Materials for

Molecular Mimicry and Assemblies of Asymmetric Organic Semiconductors

Craig P. Yu1, Shohei Kumagai1, Michitsuna Tsutsumi1, Tadanori Kurosawa1, Hiroyuki Ishii2, Go Watanabe3, Daisuke Hashizume4, Hiroki Sugiura5, Yukio Tani5, Toshihiro Ise5, Tetsuya Watanabe5, Hiroyasu Sato6, Jun Takeya1,7,8, and Toshihiro Okamoto1,7,9

1Material Innovation Research Center (MIRC) and Department of Advanced Materials Science, Graduate School of Frontier Sciences, The University of Tokyo, 5-1-5 Kashiwanoha, Kashiwa, Chiba 277-8561, Japan

2Department of Applied Physics, Faculty of Pure and Applied Sciences, University of Tsukuba, 1-1-1 Tennodai, Tsukuba, Ibaraki 305-8573, Japan

3Department of Physics, School of Science, Kitasato University, 1-15-1 Kitasato, Minami-ku, Sagamihara, Kanagawa 252-0373, Japan.

4RIKEN Center for Emergent Matter Science (CEMS), 2-1 Hirosawa, Wako, Saitama 351-0198, Japan

5FUJIFILM Corp., 577 Ushijima, Kaisei-machi, Ashigarakami-gun, Kanagawa 258-8577, Japan

6Rigaku Corp., 3-9-12 Matsubara-cho, Akishima, Tokyo 196-8666, Japan

7National Institute of Advanced Industrial Science and Technology (AIST)-University of Tokyo Advanced Operando-Measurement Technology Open Innovation Laboratory (OPERANDO-OIL), AIST, 5-1-5 Kashiwanoha, Kashiwa, Chiba 277-8561, Japan

8International Center for Materials Nanoarchitectonics (MANA), National Institute for Materials Science (NIMS), 1-1 Namiki, Tsukuba 205-0044, Japan

9PRESTO, JST, 4-1-8 Honcho, Kawaguchi, Saitama 332-0012, Japan

*Corresponding Author:

Toshihiro Okamoto, tokamoto@k.u-tokyo.ac.jp

Table of Contents

1.	1H and 13C NMR Spectra	3

2.	Fundamental Properties	8

Thermal Properties	8

Electrochemical Measurements	9

Solubility	10

3.	X-Ray Crystallography	11

Temperature-Variant Powder X-Ray Diffractions (PXRD)	12

X-Ray Diffraction of Edge-Casted Thin-Films	13

4.	OFET Performance Evaluations	15

5.	Single-Crystalline Thin-Films	16

6.	Large-Area Single-Crystalline Thin Film	17

# 1H and 13C NMR Spectra

Supplementary Fig. 1 1H NMR of N-(4-methoxybenzyl)-2-phenylethan-1-amine in CDCl3.

Supplementary Fig. 2 1H NMR of compound 2 in TCE-d2 at 100 ˚C.

Supplementary Fig. 3 1H NMR of compound PhC2–BQQDI–C5 in TCE-d2 at 100 ˚C.

Supplementary Fig. 6 1H NMR of compound PhC2–BQQDI–C6 in TCE-d2 at 100 ˚C.

Supplementary Fig. 7 1H NMR of compound PhC2–BQQDI–C7 in TCE-d2 at 100 ˚C.

# Fundamental Properties

## Thermal Properties

Supplementary Fig. 8 TG-DTA plots of a PhC2–BQQDI–C5, b PhC2–BQQDI–C6, and c PhC2–BQQDI–C7.

Supplementary Fig. 9 DSC plots of a PhC2–BQQDI–C5, b PhC2–BQQDI–C6, and c PhC2–BQQDI–C7.

## Electrochemical Measurements

Supplementary Fig. 10 Cyclic voltammograms of PhC2–BQQDI–Cn, where E0/−1 and E−1/−2 attribute to the half-wave reduction potentials corresponding to the first and second redox reactions, respectively (vs. Fc/Fc+). ELUMO (vs. vacuum level) is estimated from E0/−1: ELUMO = −4.8 – E0/−1.

## Solubility

Supplementary Table 1 Solubility of PhC2–BQQDI, C8–BQQDI, and PhC2–BQQDI–Cn.

| Compound | Solubility (wt%) |
| --- | --- |
| PhC2–BQQDI | < 0.0007 |
| C8–BQQDI | 0.019 |
| PhC2–BQQDI–C5 | 0.0015 |
| PhC2–BQQDI–C6 | 0.0016 |
| PhC2–BQQDI–C7 | 0.0023 |

# X-Ray Crystallography

Supplementary Table 2 Single-crystal data of PhC2–BQQDI–Cn

|  | PhC2–BQQDI–C5 | PhC2–BQQDI–C6 | PhC2–BQQDI–C7 |
| --- | --- | --- | --- |
| Formula | C35H26N4O4 | C36H28N4O4 | C37H30N4O4 |
| MW | 566.60 | 580.62 | 594.65 |
| Temperature (K) | 298 | 298 | 293 |
| Crystal System | Monoclinic | Monoclinic | Monoclinic |
| Space Group | Pn | Pn | Pn |
| a (Å) | 7.7195(2) | 7.8191(2) | 7.8265(5) |
| b (Å) | 4.98810(10) | 4.96240(10) | 4.9428(4) |
| c (Å) | 35.0076(10) | 35.6599(11) | 35.626(3) |
| α (˚) | 90 | 90 | 90 |
| β (˚) | 91.243(6) | 92.408(7) | 92.355(7) |
| γ (˚) | 90 | 90 | 90 |
| V (Å3) | 1347.67(6) | 1382.44(6) | 1377.01(18) |
| Z | 2 | 2 | 2 |
| Dx (g cm-3) | 1.396 | 1.395 | 1.434 |
| µ (mm) | 0.753 | 0.747 | 0.763 |
| Refined Parameters | 389 | 397 | 452 |
| GOF on F2 | 1.196 | 1.013 | 1.593 |
| R1 [I > 2σ(I)] | 0.0642 | 0.0643 | 0.1282 |
| wR2 (all data) | 0.1888 | 0.1823 | 0.3751 |
| Δρmin, max (e Å–3) | -0.47, 0.74 | -0.25, -0.25 | -0.56, 0.48 |

## Temperature-Variant Powder X-Ray Diffractions (PXRD)

Supplementary Fig. 11 Temperature-variant PXRD plots of PhC2–BQQDI–C5.

## X-Ray Diffraction of Edge-Casted Thin-Films

The X-ray irradiation was set perpendicular and parallel to the thin film for in-plane and out-of-plane diffractions, respectively.

Supplementary Fig. 12 In-plane and out-of-plane thin-film XRD of PhC2–BQQDI–C5.

Supplementary Fig. 13 Out-of-plane thin-film XRD of PhC2–BQQDI–C6.

Supplementary Fig. 14 In-plane and out-of-plane thin-film XRD of PhC2–BQQDI–C7.

# OFET Performance Evaluations

Supplementary Fig. 15 Transfer characteristics, output curves, and gate voltage-dependent µe of PhC2–BQQDI–C5 in six different devices.

Supplementary Fig. 16 Transfer characteristics, output curves, and gate voltage-dependent µe of a PhC2–BQQDI–C6, and b PhC2–BQQDI–C6.

# Single-Crystalline Thin-Films

Supplementary Fig. 17 Polarized optical microscopic images of single-crystalline thin films of a PhC2–BQQDI–C5, b PhC2–BQQDI–C6, and c PhC2–BQQDI–C7, fabricated at the best temperatures of 115˚C, 110˚C, and 90˚C, respectively (scale bar = 0.5 mm).

# Large-Area Single-Crystalline Thin Film

Supplementary Fig. 18 Polarized optical microscopic images of large-area single-crystalline thin films of PhC2–BQQDI–C5.

Supplementary Fig. 19 Gate voltage (VG) dependent saturated µe (µsat) of large-area single-crystalline thin film of PhC2–BQQDI–C5 with their corresponding angle (˚) relative to the printing direction.