Enhancing the electrical conductivity and strength of PET by single-wall carbon nanotube film coating

Wu-Tong Dinga,b, Xin-Yu Jiaoa,b, Yi-Ming Zhaoa,b, Xin-Yang Suna,b, An-Ping Wu, Yu- An-Ping Wua, Tian Dingc*, Peng-Xiang Houa,b*, Chang Liua,b*

a Shenyang National Laboratory for Materials Science, Institute of Metal Research, Chinese Academy of Sciences, Shenyang 110016, China

b School of Materials Science and Engineering, University of Science and Technology of China, Hefei 230026, China

c State Key Laboratory of Advanced Processing and Recycling of Non-ferrous Metals, Lanzhou University of Technology, Lanzhou, Gansu 730050, PR China

*e-mail: cliu@imr.ac.cn; pxhou@imr.ac.cn; dingyt@lut.edu.cn

Fig. S1. SEM image of the cross section of SWCNT/PET-240-10 film.

Fig. S2. (a) Low magnification and (b) high magnification TEM images of the SWCNT film

Fig. S3. D mode and G mode Raman spectra of the SWCNT/PET-240-10 film after hot pressing

Fig. S4. Optical images of (a) SWCNT/PEEK and (b) SWCNT/PAI films; SEM images of (b) SWCNT/PEEK and (c) SWCNT/PAI films

Fig. S5. Typical stress-strain curves of PET and SWCNT/PET-240-10 film.

Fig. S6. SEM image of the SWCNT/PET-240-5 film.

Fig. S7. SEM image of the SWCNT/PET-240-15 film.

Fig. S8. SEM image of the SWCNT/PET-235-10 film.

Figure S9. Optical images of SWCNT/PET films bend at different angles.

Table S1. Mechanical performance of PET and SWCNT/PET films hot-pressed at different temperatures and times

|  | Temperature (℃) | Time (min) | Young’s modulus (GPa) | Tensile strength (MPa) |
| --- | --- | --- | --- | --- |
| PET |  |  | 3.3 | 119 |
| SWCNT/PET | 240 | 5 | 3.4 | 124 |
| SWCNT/PET | 240 | 10 | 4.6 | 148 |
| SWCNT/PET | 240 | 15 | 3.6 | 127 |
| SWCNT/PET | 235 | 10 | 3.8 | 115 |

Table S2. Electricity performance of PET and SWCNT/PET films hot-pressed at different temperatures and times

| Sample | Surface resistance(Ω)/Sheet resistance(Ω/□) |
| --- | --- |
| PET | >1016 |
| SWCNT/PET-240-5 | 120 |
| SWCNT/PET-240-10 | 128 |
| SWCNT/PET-240-15 | 133 |
| SWCNT/PET-235-10 | 130 |

Supplementary Note 1

We measured the thickness of SWCNT films using a Step profiler. The as-collected SWCNT films were dry transferred onto the surface of a silicon wafer for the measurement. Five points of the SWCNT films were randomly selected for each sample and the averaged value obtained was used as the mean film thickness.

Supplementary Note 2

The Young’s moduli were calculated based on the initial elastic stage in the static tensile strengths of sample using the formula of E=σ/ε. For example, Fig. S5 is a typical stress-strain curve of the SWCNT/PET-240-10 composite film[1, 2]. The slope of this linear segment is the Young's modulus of the sample. As shown in Fig. S5 the Young's modulus of the SWCNT/PET-240-10 composite film is thus calculated to be ~4.6 GPa.

References:

[1] Jiang Q, Wang X, Zhu Y, Hui D, Qiu Y. (2014) Mechanical, electrical and thermal properties of aligned carbon nanotube/polyimide composites. Composites Part B: Engineering. 56, 408.http://doi.org/10.1016/j.compositesb.2013.08.064.

[2] Liu X, Liu W, Xia Q, Feng J, Qiu Y, Xu F. (2019) Highly tough and strain sensitive plasma functionalized carbon nanotube/epoxy composites. Composites Part A: Applied Science and Manufacturing. 121, 123.http://doi.org/10.1016/j.compositesa.2019.03.015.