Supporting Information

A multi-response sensor based on a bat-like Zn(II) coordination polymer: synthesis, structure and ‘turn off’ sensing of TC, Fe3+ and AA in aqueous system

Ya-Tong Zhang 1 · Ai Wang* 1,2 · Si-Si Feng 1,2· Cai-Xia Yuan 1· Li-Ping Lu* 1

1 Institute of Molecular Science, Key Laboratory of Chemical Biology and Molecular Engineering of the Education Ministry, Shanxi University, Taiyuan, Shanxi 030006, People’s Republic of China.

2 Key Laboratory of Materials for Energy Conversion and Storage of Shanxi Province; Shanxi University, Taiyuan, Shanxi 030006, People’s Republic of China.

*Corresponding authors, E-mail: luliping@sxu.edu.cn; aiwang@sxu.edu.cn.

Content

Table S1 Selected bond lengths (Å) and bond angles (º) for Zn-CP

Table S2 Comparison of various complexes sensor for detecting TC, Fe3+ and AA

Table S3 ICP results of Zn-CP@Fe3+

Table S4 Quantum yield results of Zn-CP before and after adding TC, Fe3+ and AA

Table S5 Lifetime for Zn-CP before and after adding TC, Fe3+ and AA

Table S6 The resonance energy transfer efficiency of Zn-CP (E = 1 – τ1/τ0, where τ1 and τ0 are the fluorescence lifetime of TC / Fe3+ / AA in the presence and absence of Zn-CP)

Fig. S1 IR spectrum of Zn-CP

Fig. S2 PXRD patterns of Zn-CP (black was simulation, purple was experimental, orange was recycled and green was heated at 95ºC)

Fig. S3 TGA diagram of Zn-CP

Fig. S4 The PXRD patterns of Zn-CP in different pH

Fig. S5 Interference experiments of Zn-CP for (a) TC detection in the presence of different antibiotics; (b) AA detection in the presence of different biological small molecules; (c) Fe3+ detection in the presence of different ions

Fig. S6 Infrared spectra of Zn-CP before and after soaking in TC/Fe3+/AA solution

Fig. S7 PXRD patterns of Zn-CP before and after soaking in TC/Fe3+/AA solution

Fig. S8 The color change of Zn-CP after adding 0.1 mM Fe3+

Fig. S9 The color change of Zn-CP@Fe3+ and FeCl3 after adding 0.3 mM NaSCN

Fig. S10 UV-vis spectra of Zn-CP, TC, Fe3+ and AA in the aqueous solution

Fig. S11 The emission of Zn-CP and the absorption spectra of TC, Fe3+ and AA

Fig. S12 The photoluminescence decay times of Zn-CP before and after loading in TC, Fe3+ and AA

Table S1 Selected bond lengths (Å) and bond angles (°) for Zn-CP

| Bond | Å | Bond | Å |
| --- | --- | --- | --- |
| Zn1—O1 | 1.979 (19) | Zn1—O1i | 1.979 (19) |
| Zn1—N3ii | 1.996 (2) | Zn1—N3iii | 1.996 (2) |
| Angle | (º) | Angle | (º) |
| O1—Zn1—O1i | 106.04 (12) | N3ii—Zn1—N3iii | 123.23 (14) |
| O1i—Zn1—N3ii | 104.94 (8) | O1—Zn1—N3iii | 104.94 (8) |
| O1i—Zn1—N3iii | 108.31 (9) | O1—Zn1—N3ii | 108.31 (9) |
| Symmetry codes: (i) -x+1, y, -z+2; (ii) x, y+1, z+1; (iii) -x+1, y+1, -z+1. |  |  |  |

Table S2 Comparison of various complexes sensor for detecting TC, Fe3+ and AA

| No. | Complex | Analyte | Detection range | LOD (nM) | Media | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Zn-CP | TC | 0–2.5 μM | 4.42 | H2O | This work |
| 2 | gC3N4−CdS | TC | 0.01–0.25 μM | 5.3 | Na2SO4 | S1 |
| 3 | Atta-CDs-Eu | TC | 0–20 μM | 8.7 | H2O | S2 |
| 4 | Laponite-Eu-Cit | TC | 0–7 μM | 9.5 | H2O | S3 |
| 5 | [Cd(L)(SA)]n | TC | 0–0.5 μM | 33 | H2O | S4 |
| 6 | Eu-MOF | TC | 0–140 μM | 39.8 | H2O | S5 |
| 7 | [Cd(L)(chdc)⋅(H2O)]n | TC | 0–1.7 μM | 76 | H2O | S4 |
| 8 | Eu3+/NH2-MIL-53(Al) | TC | 0.5–60 μM | 0.16×103 | Tris–HCl | S6 |
| 9 | In-sbdc | TC | -- | 0.28×103 | Tris–HCl | S7 |
| 10 | Ag NCs | TC | 1.12–230 μM | 0.47×103 | BR buffer | S8 |
| 11 | NH2-MIL-53(Al) | TC | 1.5–70 μM | 0.92×103 | Tris–HCl | S6 |
| 12 | ND-MS/GCE | TC | 5–180 μM | 2×103 | PBS buffer | S9 |
| 13 | Zn-CP | Fe3+ | 0–3.5 μM | 3.49 | H2O | This work |
| 14 | 1 | Fe3+ | -- | 40 | H2O | S10 |
| 15 | [Cd2.5(L1)(Htbip)(tbip)2]n | Fe3+ | 0–18 mM | 180 | H2O | S11 |
| 16 | Compound 1 | Fe3+ | 0–0.6 mM | 270 | H2O | S12 |
| 17 | Cd-CP | Fe3+ | 0–0.1 mM | 310 | H2O | S13 |
| 18 | RhB@DiCH3MOF-5 | Fe3+ | 1–10 μM | 360 | NaAc-HAc | S14 |
| 19 | Eu(PDCA)2(H2O)6 | Fe3+ | -- | 490 | H2O | S15 |
| 19 | [Zn(cpp)2(H2O)2]·H2O | Fe3+ | 0–25 μM | 498 | H2O | S16 |
| 20 | {[Cd(L2)0.5(1,4-chdc)]⋅H2O}n | Fe3+ | 0–0.24 μM | 790 | H2O | S11 |
| 21 | [Cd(L)(chdc)⋅(H2O)]n | Fe3+ | 0–55 μM | 880 | H2O | S4 |
| 22 | 1@PVDF | Fe3+ | -- | 1.1×103 | H2O | S10 |
| 23 | [Cd(L)(SA)]n | Fe3+ | 0–55 μM | 1.2×103 | H2O | S4 |
| 24 | GOQs | Fe3+ | 0–500 μM | 1.49×103 | H2O | S17 |
| 25 | Zn-CP | Fe3+ | 0–0.3 mM | 2.4×103 | H2O | S13 |
| 26 | {[Tb(Cmdcp)(H2O)3]2(NO3)2·5H2O}n | Fe3+ | 0–1.5 mM | 4×103 | H2O | S18 |
| 27 | ([Eu(L)(H2O)3]ClH2O)n | Fe3+ | 0–0.15 mM | 5×103 | H2O | S19 |
| 28 | [Co(4-dptb)(5-NIP)] | Fe3+ | 10–1000 μM | 5.84×103 | Na2SO4 | S20 |
| 29 | [Zn2(NO3)2(4,4’-bpy)2(TBA)] | Fe3+ | 0.1–0.3 mM | 7.18×103 | H2O | S21 |
| 30 | {[Eu2(TBrTA)3(H2O)8]2H2O}n | Fe3+ | 0–2 mM | 3.02×104 | EtOH | S22 |
| 31 | Eu HDSs | AA | 0.1–5 μM | 1.46 | EtOH | S23 |
| 32 | GOQs | AA | 0–300 μM | 1.62 | H2O | S17 |
| 33 | [CdL(H2O)] | AA | 0.03–0.22 μM | 4.3 | H2O | S24 |
| 34 | C3F7-azo+/RGO | AA | 0.04–6.01 μM | 8 | K3Fe(CN)6 | S25 |
| 35 | AuCN | AA | 0.1–10 μM | 22 | pH=3 | S26 |
| 36 | MOF-Cd-abtz | AA | 0.1–140 μM | 75 | H2O | S27 |
| 37 | Zn-CP | AA | 0–25 μM | 380 | H2O | This work |
| 38 | [Ni(HL)(bpe)1.5(H2O)] | AA | 2–10 μM | 1.23×103 | H2O | S28 |
| 39 | Compound 1 | AA | 0.1–0.9 μM | 2.9×103 | H2O | S12 |
| 40 | RhB@DiCH3MOF-5 | AA | 1–25 μM | 3.1×104 | NaAc-HAc | S14 |
| 41 | {(H3O)[Eu(SBDB)(H2O)2]}n | AA | 0–0.1 mM | 5×103 | H2O | S29 |
| 42 | {[Tb(Cmdcp)(H2O)3]2(NO3)2·5H2O}n | AA | 0.1–5 μM | 5.9×103 | H2O | S18 |

Table S3 ICP results of Zn-CP@Fe3+

| Concentration of ions | Fe3+ ions | Zn2+ ions |
| --- | --- | --- |
| Sample(Zn-CP@Fe3+) | 1.346 mg/L | 0.884 mg/L |

Table S4 Quantum yield results of Zn-CP before and after adding TC, Fe3+ and AA

| Sample | Zn-CP | Zn-CP@TC | Zn-CP@Fe3+ | Zn-CP@AA |
| --- | --- | --- | --- | --- |
| Quantum yield | 5.11% | 3.35% | 1.21% | 3.52% |

Table S5 Lifetime for Zn-CP before and after adding TC, Fe3+ and AA

| Sample | τ1 (ns) | Rel1 % | τ2 (ns) | Rel2 % | τ (ns) |
| --- | --- | --- | --- | --- | --- |
| Zn-CP | 0.31 | 65.47 | 3.49 | 34.53 | 1.41 |
| Zn-CP@TC | 0.35 | 74.97 | 2.07 | 25.03 | 0.78 |
| Zn-CP@Fe3+ | 0.29 | 83.23 | 2.32 | 16.77 | 0.63 |
| Zn-CP@AA | 0.34 | 71.19 | 2.5 | 28.81 | 0.96 |

Table S6. The resonance energy transfer efficiency of Zn-CP (E = 1 – τ1/τ0, where τ1 and τ0 are the fluorescence lifetime of TC / Fe3+ / AA in the presence and absence of Zn-CP)

| Fluorescence lifetime / ns | τ0 | τ1 | Resonance energy transfer efficiency (E) |
| --- | --- | --- | --- |
| Zn-CP | 1.41 |  |  |
| Zn-CP@TC |  | 0.78 | 44.68% |
| Zn-CP@Fe3+ |  | 0.63 | 55.32% |
| Zn-CP@AA |  | 0.96 | 31.91% |

Fig. S1 IR spectrum of Zn-CP

Fig. S2 PXRD patterns of Zn-CP (black was simulation, purple was experimental, orange was recycled and green was heated at 95ºC)

Fig. S3 TGA diagram of Zn-CP

Fig. S4 The PXRD patterns of Zn-CP in different pH

Fig. S5 Interference experiments of Zn-CP for (a) TC detection in the presence of different antibiotics; (b) AA detection in the presence of different biological small molecules; (c) Fe3+ detection in the presence of different ions

Fig. S6 Infrared spectra of Zn-CP before and after soaking in TC/Fe3+/AA solution

Fig. S7 PXRD patterns of Zn-CP before and after soaking in TC/Fe3+/AA solution

Fig.S8 The color change of Zn-CP after adding 0.1 mM Fe3+

Fig. S9 The color change of Zn-CP@Fe3+ and FeCl3 after adding 0.3 mM NaSCN

Fig. S10 UV-vis spectra of Zn-CP, TC, Fe3+ and AA in the aqueous solution

Fig. S11 The emission of Zn-CP and the absorption spectra of TC, Fe3+ and AA

Fig. S12 The photoluminescence decay times of Zn-CP before and after loading in TC, Fe3+ and AA

References

[S1] Y. Liu, K. Yan, and J. Zhang, (2016) ACS Appl Mater Interfaces, 8,28255-28264.

[S2] L. Jia, R. Chen, J. Xu, L. Zhang, X. Chen, N. Bi, J. Gou, and T. Zhao, (2021) J Hazard Mater, 413,125296.

[S3] J. Xu, S. Guo, L. Jia, T. Zhu, X. Chen, and T. Zhao, (2021) Chemical Engineering Journal, 416.

[S4] Q.-L. Cao, R.-T. Wang, J.-Y. Duan, and G.-Y. Dong, (2022) Journal of Solid State Chemistry, 307.

[S5] Z. Gan, X. Hu, X. Xu, W. Zhang, X. Zou, J. Shi, K. Zheng, and M. Arslan, (2021) Food Chem, 354,129501.

[S6] J. Chen, Y. Xu, S. Li, F. Xu, and Q. Zhang, (2021) RSC Adv, 11,2397-2404.

[S7] Q. Liu, D. Ning, W.J. Li, X.M. Du, Q. Wang, Y. Li, and W.J. Ruan, (2019) Analyst, 144,1916-1922.

[S8] Y. Zhang, M. Lv, P. Gao, G. Zhang, L. Shi, M. Yuan, and S. Shuang, (2021) Sensors and Actuators B: Chemical, 326.

[S9] W.S. Fernandes-Junior, L.F. Zaccarin, G.G. Oliveira, P.R. de Oliveira, C. Kalinke, J.A. Bonacin, J. Prakash, B.C. Janegitz, and S.K. Srivastava, (2021) Journal of Sensors, 2021,1-10.

[S10] Y. Zhang, L. Gao, S. Ma, and T. Hu, (2022) Spectrochim Acta A Mol Biomol Spectrosc, 267,120525.

[S11] Q.-L. Cao, L. Fu, and G.-H. Cui, (2022) Journal of Solid State Chemistry, 313.

[S12] R. Dalapati, and S. Biswas, (2019) Chem Asian J, 14,2822-2830.

[S13] R.-D. Wang, W.-Q. Zhang, S. Zhou, J. Tang, M. He, S. Zhang, L. Du, and Q.-H. Zhao, (2022) Journal of Molecular Liquids, 355.

[S14] L. Guo, Y. Liu, R. Kong, G. Chen, Z. Liu, F. Qu, L. Xia, and W. Tan, (2019) Anal Chem, 91,12453-12460.

[S15] Y.J. Kong, G.Z. Hou, Z.N. Gong, F.T. Zhao, and L.J. Han, (2022) RSC Adv, 12,8435-8442.

[S16] Y. Wang, Y.-H. Su, S.-M. Gong, J.-R. Wang, R.-S. Zhou, W.-Z. Jiao, and J.-F. Song, (2022) Journal of Solid State Chemistry, 308.

[S17] L. Zhu, D. Li, H. Lu, S. Zhang, and H. Gao, (2022) Int J Biol Macromol, 194,254-263.

[S18] K.Y. Wu, L. Qin, C. Fan, S.L. Cai, T.T. Zhang, W.H. Chen, X.Y. Tang, and J.X. Chen, (2019) Dalton Trans, 48,8911-8919.

[S19] C.-B. Yang, C.-B. Jiang, M.-Y. Zhang, X. Chen, P. Zou, R.-W. Yang, H.-B. Rao, and G.-T. Wang, (2020) Polyhedron, 175.

[S20] Y. Wang, J.-X. Ma, Y. Zhang, N. Xu, and X.-L. Wang, (2021) Crystal Growth & Design, 21,4390-4397.

[S21] X. Zhang, X. Zhuang, N. Zhang, C. Ge, X. Luo, J. Li, J. Wu, Q. Yang, and R. Liu, (2019) CrystEngComm, 21,1948-1955.

[S22] J.A. Smith, M.A. Singh-Wilmot, K.P. Carter, C.L. Cahill, and J.A. Ridenour, (2020) New Journal of Chemistry, 44,12317-12330.

[S23] A. Li, J. Zhang, S. Sun, E. Ding, F. Chen, S. He, T. Li, S. Liu, and B. Wang, (2019) Sensors and Actuators B: Chemical, 296.

[S24] Y.-N. Wang, S.-D. Wang, L.-L. Yang, Y.-F. Zhao, and Q.-F. Yang, (2020) Journal of Solid State Chemistry, 289.

[S25] S. Wu, H. Wang, B. Zhao, T. Cao, J. Ma, L. Liu, and Z. Tong, (2022) Talanta, 237,122986.

[S26] H. Meng, D. Yang, Y. Tu, and J. Yan, (2017) Talanta, 165,346-350.

[S27] C. Guo, Q. Jin, Y. Wang, B. Ding, Y. Li, J. Huo, and X. Zhao, (2016) Sensors and Actuators B: Chemical, 234,184-191.

[S28] Y.-N. Wang, S.-D. Wang, Y. Fan, L. Yu, R.-H. Zha, L.-J. Liu, L.-M. Wen, X.-P. Chang, H.-Q. Liu, and G.-D. Zou, (2022) Journal of Luminescence, 243.

[S29] Y.-Y. Yuan, S.-L. Yang, C.-X. Zhang, and Q.-L. Wang, (2018) CrystEngComm, 20,6989-6994.