Supplementary Information

Enabling giant thermopower by heterostructure engineering of hydrated vanadium pentoxide for zinc ion thermoelectrochemical cells

Zhiwei Li, Yinghong Xu, Langyuan Wu, Jiaxin Cui, Hui Dou, Xiaogang Zhang*

Jiangsu Key Laboratory of Electrochemical Energy Storage Technologies, College of Material Science and Technology, Nanjing University of Aeronautics and Astronautics, Nanjing 211106, China

Correspondence to X. Z. (azhangxg@nuaa.edu.cn)

Supplementary Fig. 1 Energy barrier for ions diffusion in V2O5@rGO.

Supplementary Fig. 2 FESEM image of V2O5@rGO-1.5.

Supplementary Fig. 3 FESEM images of a V2O5, b rGO, c V2O5@rGO-1.0, and d V2O5@rGO-2.0.

Supplementary Fig. 4 a HRTEM image and SAED pattern of V2O5@rGO-1.5.

Supplementary Fig. 5 Raman spectra of V2O5, rGO, and V2O5@rGO-1.5.

Supplementary Fig. 6 TGA curve of V2O5@rGO-1.5.

Supplementary Fig. 7 a XPS survey of V2O5, rGO, and V2O5@rGO-1.5. High-resolution XPS spectra of b O 1s and c V 2p for V2O5 and V2O5@rGO-1.5.

Supplementary Fig. 8 Output voltage under various temperature differences for V2O5@rGO-x.

Supplementary Fig. 9 (a) Output voltage under various temperature differences, and (b) Seebeck coefficient for V2O5 and rGO.

Supplementary Fig. 10 Self-charging curves of various systems.

Supplementary Fig. 11 Temperature dependence of the open-circuit voltage for various systems.

Supplementary Fig. 12 CV curve with capacitance dominating contribution at 1.0 mV s−1 of V2O5@rGO-1.5.

Supplementary Fig. 13 GITT curves of V2O5@rGO-1.5.

Supplementary Fig. 14 a Rate capability of V2O5@rGO-1.5 based ZIB. b Performances comparation with other reported results. c Cyclic stability under 10 A g−1.

Supplementary Table 1. Thermoelectrochemical performances comparison of V2O5@rGO-1.5 based solid-state ZTEC with other systems.

| System | ΔTa | ¦S¦b | Pmax/(A×ΔT2)c | Ref. |
| --- | --- | --- | --- | --- |
| Zn-G//V2O5@rGO-1.5 | 7.5 | 11.1 | 2.7 | This work |
| PAAm based TC | 10 | ~3 | 0.66 | Adv. Energy Mater. 12, 2201542 (2022) |
| UGdmCl based TGC | 10 | 4.2 | 1.1 | Nat. Commun. 9, 5146 (2018) |
| 3D Au/Cu based i-TE | 10 | 17 | 0.16 | Adv. Energy Mater. 12, 2103666 (2022) |
| Au/Cu based i-TE | ~10 | 12.7 | 0.66 | Science 368, 1091-1098 (2020) |
| i-PVA based TC | 40 | - | 0.22 | ACS Nano 16, 8347-8357 (2022) |
| BST/FeCN3-/4- based TC | 30.7 | 4.11 | 0.96 | Nano Energy 103, 107826 (2022) |
| BC-based TEC | 10 | ~4.5 | 0.024 | Chem. Eng. J. 433, 134550 (2022) |
| a Temperature difference (K). b Seebeck coefficient (mV K−1). c Normalized power density (mW m−2 K−2). |  |  |  |  |