Table 1. Optimization of depolymerization conditions of LMC 1a.

| Entry | Catalyst | Solvent （2mL） |  | Yield 1b % | Yield 1c % |
| --- | --- | --- | --- | --- | --- |
| 1 | FeCl3 | CH3CN |  | 87 | 71 |
| 2 | FeCl2 | acetone |  | 76 | 80 |
| 3 | FeCl2·4H2O | acetone |  | 62 | 72 |
| 4 | Fe(OTf)3 | acetone |  | 43 | 38 |
| 5 | CuCl2 | acetone |  | 38 | 27 |
| 6 | CeCl3 | acetone |  | 50 | 42 |
| 7 | NaCl | acetone |  | 20 | 15 |
| 8 | FeCl3 | DCE |  | 69 | 48 |
| 9 | FeCl3 | MeOH |  | 24 | 18 |
| 10 | FeCl3 | acetone |  | 91 | 88 |
| 11 | FeCl3 | H2O |  | 0 | 0 |
| 12 | FeCl3 | Acetic acid |  | 68 | 31 |
| 13 | FeCl3 | acetone:H2O(2:1) |  | 35 | 16 |
| 14a | FeCl3 | acetone | 77 |  | 78 |
| 15b | FeCl3 | acetone | 35 |  | 18 |

Reaction conditions: substrate 1a (0.1 mmol), catalyst (0.2 eq), TBACl (0.2 eq) solvent (2 mL), O2 (1 atm), room temperature for 12 h and irradiated with blue LED (400-410 nm, 20W). aAir instead of O2, bN2 instead of O2. The yield was determined by GC with dodecane as the internal standard.

Table 2. Scope of lignin model substrates.

| Entry | Substrate, yield % | Entry | Substrate, yield % |
| --- | --- | --- | --- |
| 1 | 2b: 86 2c: 25 | 6 | 2b: 93 2c: 96 |
| 2 | 2b: 68 2c: 19 | 7 | 2b: 78 2c: 21 |
| 3 | 2b: 32 2c: 94 | 8 | 2b: 68 2c: 9 |
| 4 | 2b: 21 2c: 25 | 9 | 2b: 65 2c: 87 |
| 5 | 2b: 17 2c: 11 |  |  |

Standard condition: 0.1 mmol substrate 2a, 0.2 eq FeCl3, 0.2 eq TBACl, 2.0 mL acetone, O2 atmosphere, rt, 12 h, 20 W blue LED. The 2b was the yieldof benzoic acids, the 2c was the yield of phenols. The yields were measured by GC.