Supplementary Material #1

to the paper

Removal of Methylene Blue Dye Using Crushed Walnut Shell Adsorbent –Determining Comminution Energy and Optimal Operational Conditions

List of Tables:

Table S1. Band test worksheet, sample

Table S2. Design of Experiments

List of Figures:

Fig. S1. Resonance forms of Methylene Blue Cation (MB+)

Fig. S2. Hydrated (a) and Dimer (b) structures of MB

Fig. S3: Calibration curve of MB

Fig. S4: MB’s Spectrophotometry spectrum (10 mg/L)

Fig. S5: Walnut Shell’s Spectrophotometry spectrum (2.5 g/L), (a): type I; (b): type II; and (c): type III

Fig. S6: Non-linear Freundlich isotherm modeling of MB adsorption on Walnut Shell, (a): type I; (b): type II; and (c): type III

Fig. S7: Non-linear Langmuir isotherm modeling of MB adsorption on Walnut Shell, (a): type I; (b): type II; and (c): type III

Fig. S8. The results of the complete sieve analysis for fines produced in the last three replicates

Fig. S9. Mesh plot of MB removal efficiency for adsorbent type I with respect to adsorbent to dye ratio and WS dosage

Table S1. Band test worksheet, sample

Note: the user fills highlighted cells.

Table S2. Design of Experiments

Fig. S1. Resonance forms of Methylene Blue Cation (MB+) (Ovchinnikov et al. 2016)

(a)

(b)

Fig. S2. Hydrated (a) and Dimer (b) structures of MB (Ovchinnikov et al. 2016)

Fig. S3: Calibration curve of MB

Fig. S4: MB’s Spectrophotometry spectrum (10 mg/L)

(a)

(b)

(c)

Fig. S5: Walnut Shell’s Spectrophotometry spectrum (2.5 g/L), (a): type I; (b): type II; and (c): type III

|  |  | KF = 12.29 nF = 2.68 R2 = 0.9902 Significance F = 0.06 ARE = 0.19 EABS = 7.17 χ2 = 0.46 MSPD = 12.00 |
| --- | --- | --- |
| (a) |  |  |
|  |  | KF = 16.81 nF = 3.30 R2 = 0.8699 Significance F = 0.23 ARE = 0.61 EABS = 17.76 χ2 = 4.84 MSPD = 42.64 |
| (b) |  |  |
|  |  | KF = 33.74 nF = 2.43 R2 = 0.9998 Significance F = 0.01 ARE = 0.04 EABS = 2.19 χ2 = 0.03 MSPD = 2.53 |
| (c) |  |  |
| Notes: Non-linear Freundlich equation: qe= KF Ce 1nF Linearized equation: Lnqe = 1nF LnCe+ LnKF |  |  |

Fig. S6: Non-linear Freundlich isotherm modeling of MB adsorption on Walnut Shell, (a): type I; (b): type II; and (c): type III

|  |  | qm = 117.34 KL = 0.04 R2 = 0.9996 Significance F = 0.01 ARE = 0.25 EABS = 6.60 χ2 = 0.80 MSPD = 17.60 |
| --- | --- | --- |
| (a) |  |  |
|  |  | qm = 105.30 KL = 0.07 R2 = 0.9995 Significance F = 0.01 ARE = 0.51 EABS = 14.55 χ2 = 3.67 MSPD = 35.90 |
| (b) |  |  |
|  |  | qm = 232.66 KL = 0.20 R2 = 0.9991 Significance F = 0.02 ARE = 0.57 EABS = 17.07 χ2 = 4.79 MSPD = 40.61 |
| (c) |  |  |
| Notes: Non-linear Langmuir equation: qe= qm KL Ce1 + KL Ce Linearized equation: Ceqe = 1KLqm + Ceqm Average Relative Error (ARE): 100n i = 1nqe, measured - qe, calculatedqe, measured Sum of Absolute Error (EABS): i = 1nqe, measured - qe, calculated Chi-square test (χ2): i = 1nqe, measured - qe, calculated2qe, measured Marquardt’s Percent Standard Deviation: 1001n - pi = 1nqe, measured - qe, calculatedqe, measured2 Where qe, measured is the experimental value while qe, calculated is the calculated value, n is the number of data points in the experiment (here = 3), and p is the number of parameters of the model (here = 2). |  |  |

Fig. S7: Non-linear Langmuir isotherm modeling of MB adsorption on Walnut Shell, (a): type I; (b): type II; and (c): type III

Fig. S8. The results of the complete sieve analysis for fines produced in the last three replicates

Fig. S9. Mesh plot of MB removal efficiency for adsorbent type I with respect to adsorbent to dye ratio and WS dosage

References:

Ovchinnikov, O. V., Evtukhova, A. V., Kondratenko, T. S., Smirnov, M. S., Khokhlov, V. Y., & Erina, O. V. (2016). Manifestation of intermolecular interactions in FTIR spectra of methylene blue molecules. Vibrational Spectroscopy, 86, 181-189. https://doi.org/10.1016/j.vibspec.2016.06.016