Supplementary Information (SI) for

Role of iron species in the production of iron-modified hydrochar for arsenic removal via hydrothermal carbonization

Yiwei Zhang1,2, Dandan Chen2,*, Yutong Xing2, Bangwei Liu2, Yan Zhou2, Ping Lu2.

1. School of Environment, Nanjing Normal University, Nanjing 210023, China;

2. School of Energy and Mechanical Engineering, Nanjing Normal University, Nanjing 210023, China;

*Corresponding Author: Tel/Fax: +86–25–85481085; E-mail: dandanchen@njnu.edu.cn

The Supporting Information includes:

0 Texts

3 Tables

5 Figures

# References

Table S1. Preparation conditions of iron-modified hydrochar

| Iron species | Preparation Time (min) | Iron concentration in solution (mol/L) | the mass ratio of iron in the feed iron solution (%) |
| --- | --- | --- | --- |
| FeCl3·6H2O | 120 | 0.107 | 6 |
| FeSO4·7H2O | 120 | 0.107 | 6 |
| Fe(NO3)3·9H2O | 60, 120, 240, 480 | 0.0357, 0.0714, 0.107, 0.143 | 2,4,6,8 |

Table S2. Pore structure of modified hydrochar prepared under different conditions

| Sample | BET surface area /m2/g | Average pore diameter /nm | Pore volume/ 10-2cc/g |
| --- | --- | --- | --- |
| PWC | 0.91 | - | - |
| 6%FN@HC | 7.107 | 7.8 | 1.386 |
| 6%FS@SO4 | 2.445 | 6.3 | 0.386 |
| 6%FC@Cl3 | 1.726 | 3.1 | 0.133 |
| 2% FN@HC | 7.151 | 10.5 | 1.868 |
| 4% FN@HC | 5.653 | 9.2 | 1.293 |
| 6% FN@HC | 7.107 | 7.8 | 1.386 |
| 8% FN@HC | 10.335 | 7.5 | 1.941 |
| 6% FN@HC-60 | 6.995 | 8.5 | 1.480 |
| 6% FN@HC | 7.107 | 7.8 | 1.386 |
| 6% FN@HC-240 | 17.898 | 10.7 | 4.767 |
| 6% FN@HC-480 | 29.825 | 9.57 | 7.139 |

Table S3. Kinetic parameters of As (Ⅲ) and As (Ⅴ) adsorption by iron-modified hydrochars

| Heavy metal | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Qe(mg/g) | k1(1/h) | R2 | Qe(mg/g) | k1(g/mg h) | R2 |
| As(Ⅲ) | 2.385 | 6.24 | 0.905 | 2.568 | 0.39 | 0.958 |
| As(Ⅴ) | 7.03 | 0.176 | 0.974 | 8.5 | 0.02316 | 0.982 |

Table S4. Isotherm model parameters of As (Ⅲ) and As (Ⅴ) adsorption by iron-modified hydrochars

| Heavy metal | Qm(mg/g) | Langmuir |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | KL(L/mg) | R2 | n | KF | R2 |
| As(Ⅲ) | 5.15 | 0.055 | 0.981 | 2.568 | 0.39 | 0.985 |
| As(Ⅴ) | 11.19 | 0.045 | 0.957 | 8.5 | 0.02316 | 0.983 |

Fig. S1. FTIR spectra of modified hydrochar prepared with the (a)different iron salts, (b) preparation time and (c) iron dosage on the FTIR spectrum of iron modified hydrochars

| Fig. S2. XPS Spectra of hydrochars modified by different iron specie |  |
| --- | --- |

| Fig. S3. N2 adsorption isotherms (a) (c) (e) and the pore size distribution (b) (d) (f) of different iron species, different iron dosage, and different preparation time |  |
| --- | --- |

Fig. S4. Adsorption kinetics curves of As (Ⅲ) and As (Ⅴ) by using 8%FN@HC. As (Ⅲ) concentration is 20mg/L; PH, 9± 0.2; Temperature, 25±1°C. As (Ⅴ) concentration is 40mg/L; PH 7±0.2; Temperature, 25± 1 °C

Fig. S5. Adsorption isotherms of As (Ⅲ) and As (Ⅴ) by using 8%FN@HC. (a) As (Ⅲ) concentration is 20 mg/L; PH, 9± 0.2; Temperature, 25±1°C. (b) As (Ⅴ) concentration is 40 mg/L; PH 7±0.2; Temperature, 25± 1 °C