Preparation of ZnGa2O4 Nanoflowers and Their Full-color Luminescence Properties

Yan Liu1,*, Xinhuan Wan1,*, Tingting Zheng1,*, Xiuyun Zhang1,*, Chen Chen2,*

1Department of Pharmacy, Shandong University of Traditional Chinese Medicine, Jinan, 250355, Shandong, China.

2Key Laboratory of New Material Research Institute, Department of Acupuncture-Moxibustion and Tuina, Shandong University of Traditional Chinese Medicine, Jinan ,250355, China.

*corresponding author: Tingting Zheng(ttz10_10@163.com), Xiuyun Zhang(zhangxiuyunsh@163.com) and Chen Chen(21129008@zju.edu.cn)

Table S1 Coordination numbers (CN) of Zn2+, Ga3+, Mn2+ and Cr3+ and corresponding effective ion radius and the effective compensation factors (φ).

| Ions | CN = 4 |  | CN = 6 |  |
| --- | --- | --- | --- | --- |
|  | Ion radius (Å) | φ | Ion radius (Å) | φ |
| Zn2+ | 0.60 | 3.33 | / | / |
| Ga3+ | / | / | 0.62 | 4.83 |
| Mn2+ | 0.66 | 3.03 | 0.83 | 2.41 |
| Cr3+ | / | / | 0.62 | 4.83 |

Figure S1 Mapping of elements in (a)-(b) ZnGa2O4:Mn2+ and (c)-(d) ZnGa2O4:Cr3+.

Figure S2 The FT-IR spectra of ZnGa2O4, ZnGa2O4:Mn2+ and ZnGa2O4: Cr3+.

Figure S3 The UV-Vis spectra of ZnGa2O4, ZnGa2O4:Mn2+ and ZnGa2O4: Cr3+.

Figure S4 The enlarged photoluminescence excitation spectrum of ZnGa2O4:Mn2+ at 300-500 nm.

Table S2 Fitting parameters obtained from bi-exponential fittings of PL dacays.

| Samples | τ1 [ms] | τ2 [ms] | I1 | I1 | τavg [ms] |
| --- | --- | --- | --- | --- | --- |
| ZnGa2O4 | 0.13 | 1.47 | 77.76 | 18.02 | 1.10 |
| ZnGa2O4:Mn2+ | 1.70 | 8.59 | 22.24 | 47.35 | 8.00 |
| ZnGa2O4:Cr3+ | 0.97 | 6.73 | 31.84 | 18.90 | 5.60 |

τavg is the average life span.