Table 1 Optimization of reaction conditionsa

| Entry | Catalyst | Solvent | Catalyst (g) | Temperature (օC) | Time (min) | Yield (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | - | Solvent-free | - | R.T. | 15 | - |
| 2 | MNPs | Solvent-free | 0.02 | 70 | 15 | 35 |
| 3 | Carr | Solvent-free | 0.02 | 70 | 15 | 40 |
| 4 | Carr-Met | Solvent-free | 0.02 | 70 | 15 | 50 |
| 5 | Carr-Met-MNPs | Solvent-free | 0.02 | 70 | 15 | 60 |
| 6 | Carr-Met-MNPs | EtOH | 0.02 | 70 | 15 | 75 |
| 7 | Carr-Met-MNPs | H2O | 0.02 | 70 | 15 | 55 |
| 8 | Carr-Met-MNPs | EtOH : H2O | 0.02 | 70 | 15 | 85 |
| 9 | Carr-Met-MNPs | CH3CN | 0.02 | 70 | 15 | 60 |
| 10 | Carr-Met-MNPs | CH2Cl2 | 0.02 | 70 | 15 | 30 |
| 11 | Carr-Met-MNPs | THF | 0.02 | 70 | 15 | 35 |
| 12 | Carr-Met-MNPs | Toluene | 0.02 | 70 | 15 | 30 |
| 13 | Carr-Met-MNPs | EtOH : H2O | 0.03 | 70 | 15 | 94 |
| 14 | Carr-Met-MNPs | EtOH : H2O | 0.04 | 70 | 15 | 94 |
| 15 | Carr-Met-MNPs | EtOH : H2O | 0.03 | 80 | 15 | 94 |
| 16 | Carr-Met-MNPs | EtOH : H2O | 0.03 | 70 | 60 | 94 |

a Reaction conditions: benzaldehyde (2j, 1 mmol), malonitrile (3, 1 mmol), hydrazine (4, 1 mmol), and ethyl acetoacetate (5, 1 mmol), 2 mL of solvents.

b Isolated yield.

Table 2 Synthesis of dihydropyrano [2, 3-c]pyrazole derivatives using Carr-Met-MNPsa

| Entry | R-CHO | Product | Time (min) | Yieldb (%) | TOFc | M.p (°C) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Observed (Literature) [Ref.] |  |
| 1 | 2a | 6a | 15 | 88 | 370.05 |  | 207–209(208–210)[16] |  |
| 2 | 2b | 6b | 17 | 92 | 342.2 |  | 214–216(216–218)[16] |  |
| 3 | 2c | 6c | 18 | 89 | 312.3 |  | 220–226(218–224)[16] |  |
| 4 | 2d | 6d | 3 | 90 | 1895 |  | 232–236(238–240)[16] |  |
| 5 | 2e | 6e | 9 | 89 | 642.5 |  | 242–2244(242–244)[21] |  |
| 6 | 2f | 6f | 8 | 92 | 728.1 |  | 246–249(244–246)[23] |  |
| 7 | 2g | 6g | 10 | 91 | 577 |  | 244–245(244–246)[16] |  |
| 8 | 2h | 6h | 15 | 92 | 387.36 |  | 218-220 |  |
| 9 | 2i | 6i | 10 | 91 | 577 |  | 240-242 |  |
| 10 | 2j | 6j | 15 | 94 | 395.8 |  | 244-2247(244-246)[17] |  |

a Reaction conditions: aldehyde (2a-2j, 1 mmol), malonitrile (3, 1 mmol), hydrazine (4, 1 mmol), ethyl acetoacetate (5, 1 mmol), in the EtOH : H2O (2 mL) as solvent, and  70 °C.

a Isolated yield.

cTurnover frequency (h-1).