Electronic Supplementary Information (ESI)

Dielectronic properties and photocatalytic activities of two novel cobalt(II) meso-tetraphenylporphyrin-based coordination complexes.

Nesrine Amiri a ¥, Mouhieddinne Guergueb a, Marwa Bourguiba b,c and Habib Nasri a

a Laboratory of Physico-Chemistry of Materials, University of Monastir, Avenue of the Environment, 5019 Monastir, Tunisia.

b Applied Mechanics and Systems Research Laboratory (LASMAP-EPT), polytechnic school, La Marsa, University of carthage, Tunisia.

c Faculty of science of Tunis, University of Tunis el manar, Tunisia.

¥ Corresponding author: E-mail: nesamiri@gmail.com

Tel: (+216) 28256432

Table of contents

| No. | Contents | Pg No. |
| --- | --- | --- |
| 1 | Scheme S1. Molecular structures of [CoII(Porph))(DMAP)2]. | 2 |
| 2 | Table S1. UV/Vis data of several free base meso-porphyrins, complex 1, complex 2 and a selection of cobalt meso-metalloporphyrins in dichloromethane. | 3 |
| 3 | Table S2. Emission data for complexes 1-2 and some related cobaltous metalloporphyrins. | 4 |
| 4 | Fig. S1. 1H NMR spectra of 1 (CDCl3, 500 MHz, 298 K). | 5 |
| 5 | Fig. S2. 1H NMR spectra of 2 (CDCl3, 500 MHz, 298 K). | 5 |
| 6 | Fig. S3. High resolution ESI mass spectrum of 1 in CH2Cl2. | 6 |
| 7 | Fig. S4. High resolution ESI mass spectrum of 2 in CH2Cl2. | 6 |
| 9 | references | 7 |

Scheme S1. Molecular structures of [CoII(Porph))(DMAP)2].

Table S1 UV/Vis data of several free base meso-porphyrins, complexe 1, complex 2 and a selection of cobalt meso-metalloporphyrins in dichloromethane.

| Compound |  | Soret band λ [nm] (log ε) |  |  |  | Q bands λ [nm] (log ε) |  |  |  | [ref] |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Free base meso-porphyrins |  |  |  |  |  |  |  |  |  |  |  |
| H2TPPa | 416 (6.10) |  | 513 (5.70) | 550 (4.36) |  |  | 590 (4.24) |  | 646 (4.19) |  | [1] |
| H2TTPa | 420 (5.95) |  | 515 (5.82) | 555 (4.28) |  |  | 595 (4.17) |  | 650 (4.10) |  | [1] |
| H2TPBPb | 419 (5.90) |  | 515 (4.46) | 551 (4.13) |  |  | 590 (3.94) |  | 646 (3.84) |  | [2] |
| H2Ppc | 421 |  | 517 | 553 |  |  | 592 |  | 648 |  | [3] |
| H2TMAPPd | 425 (5.92) |  | 522(5.67) | 550 (4.32) |  |  | 597 (4.15) |  | 653 (3.98) |  | [4] |
| H2TMPPe | 423(5.53) |  | 521(4.38) | 558(4.30) |  |  | 597(4.20) |  | 650(4.17) |  | [5] |
| H2TBrPP | 419 (6.58) |  | 515 (5.24) | 549 (4.93) |  |  | 590 (4.77) |  | 648 (4.68) |  | this work |
| H2TClPP | 417(5.50) |  | 515(4.93) | 548(4.55) |  |  | 590(4.46) |  | 646(4.41) |  | this work |
| Tetracoordinated cobalt(II) meso-metalloporhyrins |  |  |  |  |  |  |  |  |  |  |  |
| [CoII(TPP)]a | 412 |  | 528 |  | — |  |  |  |  |  | [6] |
| [CoII(TpivPP)]f | 412 |  | 524 |  | — |  |  |  |  |  | [7] |
| [CoII(Pp)]c | 414 |  | 531 |  | — |  |  |  |  |  | [3] |
| [CoII(TMAPP)]d | 415 (5.85) |  | 539 (5.49) |  | — |  |  |  |  |  | [4] |
| [CoII(TPBP)]b | 412 (6.07) |  | 528 (5.58) |  | — |  |  |  |  |  | [2] |
| [Co(TMPP)]e | 414(5.65) |  | 535(4.36) |  | — |  |  |  |  |  | [5] |
| [CoII(TBrPP)] | 412(5.58) |  | 528(4.62) |  | — |  |  |  |  |  | this work |
| [CoII(TClPP)] | 412(5.58) |  | 529(4.80) |  | — |  |  |  |  |  | this work |
| Pentacoordinated and hexacoordinated cobalt(II) meso-porphyrins |  |  |  |  |  |  |  |  |  |  |  |
| [CoII(TPBP)(4,4’-bpy)2]b,g(1) | 435 (5.75) |  | 552 (4.49) |  |  |  |  |  |  |  | this work |
| [CoII(TpîvPP)(4,4’-bpy)2]f,g | 439 (5.40) |  | 550 (4.25) |  | — |  |  |  |  |  | [7] |
| [CoII(TPP)(4,4′-bpy)2]a,g | 438 (5.39) |  | 549 (4.21) |  | — |  |  |  |  |  | [3] |
| [Co(TPP)(Hon)2]a,h | 434 (4.46) |  | 521 (3.54) |  | 555 (3.41) |  |  |  |  |  | [8] |
| [CoII(TMPP)(4-CNpy)]e,i | 437(5.62) |  | 558(4.60) |  | 600(4.54) |  |  |  |  |  | [5] |
| [CoII(TClPP)(4-CNpy)]i | 436(5.65) |  | 556(4.69) |  | 598(4.64) |  |  |  |  |  | [5] |
| [CoII(TMPP)(py)]e | — |  | 535 |  | — |  |  |  |  |  | [8] |
| [CoII(TMPP)(pip)]e,j | — |  | 532 |  | — |  |  |  |  |  | [9] |
| [CoII(TClPP)(pipz)]k | 436(5.60) |  | 553(4.63) |  | 592(4.49) |  |  |  |  |  | [10] |
| [{CoII(TMPP)2(2-pipz]e,k | 438(5.60) |  | 556(4.67) |  | 597(4.55) |  |  |  |  |  | [10] |
| [CoII(TBrPP)(DMAP)2] | 435(5.62) |  | 556(4.65) |  | — |  |  |  |  |  | this work |
| [CoII(TClPP)(DMAP)2] | 436(5.66) |  | 557(4.67) |  | — |  |  |  |  |  | this work |

a TPP = meso-[tetraphenyl]porphyrinato. b TPBP = meso-[tetrakis-[4-(benzoyloxy)phenyl]porphyrinato. c H2Pp = meso-tetrakis(4-N-pyrazolyl)phenyl porphyrinato. d TMAPP = meso-tetrakis {4-[((4-methoxyphenyl)acetyl)oxy]phenyl}porphyrinato. e TMPP = meso-tetra[para-methoxyphenyl]porphyrinato. f TpîvPP = α,α,α,α-tetrakis(o-pivalamidophenyl)porphyrinato. g 4,4’-bpy = 4,4’-bipyridine. h Hon = 2-aminopheno. i 4-CNpy = 4-cyanopyridine. j pip = piperidine. k pipz = µ-piperazine.

Table S2 Emission data for complexes 1-2 and some related cobaltous metalloporphyrins.

| Compound | excia | max (nm) |  |  | Φfb | τfc (ns) |  | Solvent |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Q(0,0)[nm] | Q(0,1)[nm] |  |  |  |  |  |  |  |
| Free base meso-porphyrins |  |  |  |  |  |  |  |  |  |  |
| H2TPPd | — | 653 | 722 |  | 0.12 | 9.6 | DMF |  | [11] |  |
| H2TPPd | — | 654 | 712 |  | 0.110 | - | CH2Cl2 |  | [12,13] |  |
| H2TPPd | — | 656 | 717 |  | 0.09 | - | CH2Cl2 |  | [14] |  |
| H2TPBPe | 420 | 651 | 719 |  | 0.054 | - | CH2Cl2 |  | [15] |  |
| H2TMPPf | 424 | 656 | 719 |  | 0.082 | 7.16 | CH2Cl2 |  | [5] |  |
| H2TMAPPg | 522 | 655 | 719 |  | 0.050 | 5.93 | CH2Cl2 |  | [4] |  |
| H2TBrPP | 549 | 654 | 720 |  | 0.054 | 7.23 | CH2Cl2 |  | this work |  |
| H2TClPP | 548 | 651 | 714 |  | 0.081 | 7.16 | CH2Cl2 |  | this work |  |
| Tetracoordinated cobalt(II) meso-metalloporhyrins |  |  |  |  |  |  |  |  |  |  |
| [CoII(TPBP)]e | 552 | 653 |  | 719 | 0.032 | - | CH2Cl2 |  | [2] |  |
| [CoII(TMPP)]f | 414 | 655 |  | 719 | 0.035 | 6.02 | CH2Cl2 |  | [5] |  |
| [CoII(TMAPP)]g | 540 | 653 |  | 718 | 0.028 | 1.5 | CH2Cl2 |  | [4] |  |
| [CoII(TBrPP)] | 528 | 654 |  | 719 | 0.036 | 6.17 | CH2Cl2 |  | this work |  |
| [CoII(TClPP)] | 529 | 652 |  | 713 | 0.04 | 6.10 | CH2Cl2 |  | this work |  |
| Pentacoordinated and hexacoordinated cobalt(II) meso-porphyrins |  |  |  |  |  |  |  |  |  |  |
| [CoII(TMPP)(4-CNpy)]f,h | 437 | 652 |  | 717 | 0.054 | 1.97 | CH2Cl2 |  | [5] |  |
| [CoII(TClPP)(4-CNpy)]h | 439 | 653 |  | 714 | 0.06 | 1.997 | CH2Cl2 |  | [5] |  |
| [CoII(TPBP)(4,4’-bipy)2]e,i | 550 | 652 |  | 718 | 0.036 | — | CH2Cl2 |  | [2] |  |
| [{CoII(TMPP)}2(2-pipz)]g,j | — | 653 |  | 719 | 0.026 | 1.57 | CH2Cl2 |  | [10] |  |
|  | — | 648 |  | 710 | — | 6.10 | Ethanol |  |  |  |
| [CoII(TClPP)(pipz)]g | — | 651 |  | 717 | 0.042 | 1.51 | CH2Cl2 |  | [10] |  |
|  | — | 640 |  | 711 | — | 5.90 | Ethanol |  |  |  |
| [CoII(TBrPP)(DMAP)2] | 556 | 654 |  | 719 | 0.058 | 1.731 | CH2Cl2 |  | this work |  |
| [CoII(TClPP)(DMAP)2] | 557 | 652 |  | 713 | 0.063 | 1.981 | CH2Cl2 |  | this work |  |

a exci = wavelength value of excitation. b Φf = fluorescence quantum yields. c τf = fluorescent lifetime. d TPP = meso-[tetraphenyl]porphyrinato. e TPBP = meso-[tetrakis-[4-(benzoyloxy)phenyl]porphyrinato. f TMPP = meso-tetra[para-methoxyphenyl]porphyrinato. g TMAPP = meso-tetrakis {4-[((4-methoxyphenyl)acetyl)oxy]phenyl}porphyrinato. h 4-CNpy = 4-cyanopyridine. i 4,4’-bipy = 4,4’-bipyridine. j pipz = µ-piperazine.

Fig. S1. 1H NMR spectra of 1 (CDCl3, 500 MHz, 298 K).

Fig. S2. 1H NMR spectra of 2 (CDCl3, 500 MHz, 298 K).

Fig. S3. High resolution ESI mass spectrum of 1 in CH2Cl2

Fig. S4. High resolution ESI mass spectrum of 2 in CH2Cl2

References

- Z. Denden, K. Ezzayani, E. Saint-Aman, F. Loiseau, S. Najmudin, C. Bonifácio, J.-C. Daran and H. Nasri, Insights on the UV/Vis, fluorescence, and cyclic Voltammetry properties and the molecular structures of ZnII tetraphenylporphyrin complexes with pseudohalide axial azido, cyanato‐N, thiocyanato‐N, and cyanido ligands, Eur. J. Inorg. Chem. 15 (2015) 2596-2610.

- N. Amiri, S. Nouir, M. Hajji, T. Roisnel, T. Guerfel, G. Simonneaux, H. Nasri, Synthesis, structure, photophysical properties and biological activity of a cobalt(II) coordination complex with 4,4’-bipyridine and porphyrin chelating ligands, J. Saudi Chem. Soc. 23 (2019), 781–794.

- Y. X. Du, Z. Q. Zhang, Y. H. Yao and J. Li, Inorg. Chem. Commun. 64 (2016) 19–22.

- N. Amiri, M. Guergueb, M. S. Al-Fakeh, M. Bourguiba, H. Nasri, A new cobalt(II) meso-porphyrin: synthesis,characterization, electric properties and application in the catalytic degradation of dyes, RSC Adv. 10 (2020) 44920.

- M. Guergueb, S. Nasri, J. Brahmi, F. Loiseau, F. Molton, T. Roisnel, V. Guerineau, I. Turowska-Tyrk, K. Aouadi, H. Nasri, Eﬀect of the coordination of p-acceptor 4cyanopyridine ligand on the structural and electronic properties of meso-tetra(para-methoxy) and meso-tetra(para-chlorophenyl) porphyrin cobalt(II) coordination compounds. Application in the catalytic degradation of methylene blue dye, RSC Adv. 10 (2020) 6900.

- Y. Belghith, A. Mansour, J.-C. Daran, H.Nasri. Spectroscopic and molecular structure characterization of the bis(2-aminophenol)(5,10,15,20-tetraphenylporphyrinato) cobalt(II) complex, Open J Inorg Chem. 2 (2012) 81-87.

- A. Mansour, Y. Belghith, M. S. Belkhiria, A. Bujaczb, V. Guérineau, H. Nasri, Synthesis, crystal structures and spectroscopic characterization of Co(II) bis(4,4′-bipyridine) with meso-porphyrins α,β,α,β-tetrakis(o-pivalamidophenyl) porphyrin (α,β,α,β-TpivPP) and tetraphenylporphyrin (TPP), J. Porphyrins Phthalocyanines 17 (2013) 1094-1103.

- F. A. Walker, J. Am. Chem. Soc., 95 (1973) 1154–9115.

- X. Q. Lin, B. Boisselier-Cocolios and K. M. Kadish, Inorg. Chem., 25 (1986) 3242–3248.

- M. Guergueb, S. Nasri, J. Brahmi, Y. O. Al-Ghamdi, F. Loiseau, F. Molton, T. Roisnel, V, Guerineau, H, Nasri, Spectroscopic characteri-zation, X-ray molecular structures and cyclic voltammetry study of two (piperazine) cobalt(II) meso-arylporphyin complexes. Application as a catalyst for the degradation of 4-nitrophenol, Polyhedron 209 (2021) 115468.

- J. W. Owens, R. Smith, R. Robinson and M. Robins, Inorg. Chim. Acta, 279 (1998) 226–231.

- H. J. Giraudeau, M. Callot and M. Gross, Inorg. Chem. 18 (1979) 201–206.

- S. Fortier, G. Wu and T. W. Hayton, Dalton Trans. 39 (2010) 352–354. 64 65

- A. Altomare, G. Casacarano, C. Giacovazzo, A. Guagliardi, M. C. Burla, G. Polidori and M. Camalli, J. Appl. Crystallogr. 27 (1994) 435–436.

- N. Amiri, M. Hajji, T. Roisnel, G. Simonneaux, H. Nasri, Synthesis, molecular structure, photophysical properties and spectroscopic characterization of new 1D-magnesium(II) porphyrin-based coordination polymer, Research on Chemical Intermediates  44 (2018) 5583–5595.