Supplementary Material for:

SYNTHESIS, STRUCTURAL CHARACTERIZATION AND PHOTOPHYSICAL PROPERTIES OF BIS(4'-CHLORO-2,2':6',2''- TERPYRIDYL)NICKEL(II)CHLORIDE DIHYDRATE

Basavaraja Thippeswamy 1,2, Parameshwar A. Suchetan1, Kittappa M. Mahadevan3, H. Nagabhushana4, Giriyapura R. Vijayakumar1,*

1Department of Chemistry, University College of Science, Tumkur University, Tumakuru-572 103, India

2Department of Chemistry, Maharani’s Science College for Women, Mysuru, 570012, India.

3Department of Chemistry, Kuvempu University, P. G. Centre, Kadur-577548, India

4Prof. C.N.R Rao Centre for Advanced Materials Research, Tumkur University, Tumkur-572 103, India

*Corresponding author E-mail: vijaykumargr18@gmail.com

Figure S1: FT-IR spectrum of bis(4'-chloro-2,2':6',2''-terpyridyl)nickel(II)chloride dihydrate.

Figure S2: TG-DTA of bis(4'-chloro-2,2':6',2''-terpyridyl)nickel(II)chloride dihydrate.

Table S1: Geometric parameters (Å, º) of Ni(Cltpy)2(Cl2).2H2O

| NI1—N5 | 2.009 (3) | C20—C19 | 1.382 (7) |
| --- | --- | --- | --- |
| NI1—N2 | 2.012 (3) | C20—C21 | 1.486 (7) |
| NI1—N3 | 2.109 (4) | C25—C24 | 1.398 (6) |
| NI1—N4 | 2.111 (5) | C27—C28 | 1.381 (8) |
| NI1—N6 | 2.116 (4) | C8—C7 | 1.378 (7) |
| NI1—N1 | 2.113 (4) | C8—C9 | 1.381 (7) |
| CL1—C8 | 1.731 (4) | C14—C13 | 1.368 (7) |
| CL2—C23 | 1.738 (5) | C14—C15 | 1.390 (8) |
| N2—C6 | 1.334 (6) | C29—C28 | 1.360 (7) |
| N2—C10 | 1.347 (6) | C16—C17 | 1.379 (8) |
| N5—C25 | 1.342 (6) | C12—C13 | 1.381 (7) |
| N5—C21 | 1.346 (6) | C19—C18 | 1.384 (7) |
| N1—C5 | 1.342 (7) | C3—C2 | 1.390 (7) |
| N1—C1 | 1.350 (5) | C18—C17 | 1.368 (7) |
| N3—C15 | 1.336 (7) | C24—C23 | 1.387 (7) |
| N3—C11 | 1.359 (6) | C22—C23 | 1.381 (7) |
| N4—C16 | 1.332 (6) | C22—C21 | 1.380 (7) |
| N4—C20 | 1.365 (6) | C1—C2 | 1.387 (6) |
| N6—C30 | 1.325 (7) | C10—C9 | 1.399 (6) |
| N6—C26 | 1.356 (5) | C26—C27 | 1.385 (7) |
| C6—C7 | 1.387 (6) | C26—C25 | 1.471 (7) |
| C6—C1 | 1.493 (6) | C4—C3 | 1.373 (7) |
| C11—C12 | 1.382 (7) | C4—C5 | 1.384 (8) |
| C11—C10 | 1.477 (7) | C30—C29 | 1.386 (8) |
| N5—NI1—N2 | 178.92 (19) | C7—C8—C9 | 121.7 (4) |
| N5—NI1—N3 | 102.25 (15) | C7—C8—CL1 | 118.8 (4) |
| N2—NI1—N3 | 77.72 (16) | C9—C8—CL1 | 119.5 (4) |
| N5—NI1—N4 | 77.73 (16) | C13—C14—C15 | 118.0 (5) |
| N2—NI1—N4 | 101.20 (16) | N5—NI1—N6 | 77.97 (16) |
| N3—NI1—N4 | 93.18 (13) | N2—NI1—N6 | 103.11 (15) |
| N3—NI1—N6 | 93.67 (16) | C28—C29—C30 | 118.4 (5) |
| N4—NI1—N6 | 155.63 (14) | N4—C16—C17 | 123.2 (5) |
| N5—NI1—N1 | 102.49 (15) | C13—C12—C11 | 119.5 (5) |
| N2—NI1—N1 | 77.57 (16) | C20—C19—C18 | 118.9 (5) |
| N3—NI1—N1 | 155.22 (14) | C4—C3—C2 | 119.7 (5) |
| N4—NI1—N1 | 93.24 (16) | C1—C2—C3 | 118.4 (5) |
| N6—NI1—N1 | 90.26 (13) | N3—C15—C14 | 123.5 (5) |
| C6—N2—C10 | 121.7 (3) | C29—C28—C27 | 119.8 (6) |
| C6—N2—NI1 | 119.4 (3) | C15—N3—C11 | 117.9 (5) |
| C10—N2—NI1 | 118.9 (3) | C15—N3—NI1 | 127.1 (3) |
| C25—N5—C21 | 122.0 (4) | C11—N3—NI1 | 115.0 (3) |
| C25—N5—NI1 | 118.6 (3) | C16—N4—C20 | 117.5 (5) |
| C21—N5—NI1 | 119.4 (3) | C16—N4—NI1 | 127.7 (4) |
| C5—N1—C1 | 118.0 (5) | C20—N4—NI1 | 114.8 (3) |
| C5—N1—NI1 | 127.0 (4) | C30—N6—C26 | 118.4 (5) |
| C1—N1—NI1 | 114.9 (3) | C30—N6—NI1 | 127.2 (4) |
| C26—N6—NI1 | 114.0 (3) | C14—C13—C12 | 119.7 (5) |
| N2—C6—C7 | 120.8 (4) | C17—C18—C19 | 119.0 (5) |
| N2—C6—C1 | 113.6 (4) | C7—C6—C1 | 125.6 (4) |
| N3—C11—C12 | 121.4 (5) | C23—C24—C25 | 117.4 (5) |
| N3—C11—C10 | 114.3 (4) | C8—C7—C6 | 118.0 (5) |
| C12—C11—C10 | 124.2 (4) | C18—C17—C16 | 119.3 (5) |
| N1—C1—C2 | 122.3 (4) | N2—C10—C9 | 120.3 (4) |
| N1—C1—C6 | 114.4 (4) | N2—C10—C11 | 114.1 (4) |
| C2—C1—C6 | 123.2 (4) | C9—C10—C11 | 125.6 (5) |
| N6—C26—C27 | 121.3 (5) | C23—C22—C21 | 117.7 (5) |
| N6—C26—C25 | 114.8 (4) | C22—C23—C24 | 122.0 (5) |
| C27—C26—C25 | 123.9 (4) | C22—C23—CL2 | 119.8 (4) |
| C3—C4—C5 | 118.5 (5) | C24—C23—CL2 | 118.2 (4) |
| N6—C30—C29 | 123.1 (5) | N5—C21—C22 | 120.7 (5) |
| N5—C21—C20 | 113.7 (4) | C22—C21—C20 | 125.5 (5) |
| N4—C20—C19 | 122.1 (5) | C8—C9—C10 | 117.6 (5) |
| N4—C20—C21 | 114.2 (4) | N1—C5—C4 | 122.9 (5) |
| C19—C20—C21 | 123.7 (4) | C28—C27—C26 | 118.9 (5) |
| N5—C25—C24 | 120.1 (5) | C24—C25—C26 | 125.5 (5) |
| N5—C25—C26 | 114.4 (4) |  |  |
| C10—N2—C6—C7 | -1.4 (7) | NI1—N4—C16—C17 | -177.9 (4) |
| NI1—N2—C6—C7 | 177.0 (3) | N3—C11—C12—C13 | 0.2 (8) |
| C10—N2—C6—C1 | 177.6 (4) | C10—C11—C12—C13 | 179.9 (5) |
| NI1—N2—C6—C1 | -4.0 (5) | N4—C20—C19—C18 | 0.3 (7) |
| C15—N3—C11—C12 | -0.6 (7) | C21—C20—C19—C18 | -179.2 (5) |
| NI1—N3—C11—C12 | 179.6 (4) | C5—C4—C3—C2 | 0.9 (9) |
| C15—N3—C11—C10 | 179.7 (4) | N1—C1—C2—C3 | -0.5 (7) |
| NI1—N3—C11—C10 | -0.1 (5) | C6—C1—C2—C3 | 176.7 (5) |
| C5—N1—C1—C2 | -1.2 (7) | C4—C3—C2—C1 | 0.6 (8) |
| NI1—N1—C1—C2 | 176.5 (4) | C11—N3—C15—C14 | 0.8 (8) |
| C5—N1—C1—C6 | -178.6 (4) | NI1—N3—C15—C14 | -179.5 (4) |
| NI1—N1—C1—C6 | -1.0 (5) | C13—C14—C15—N3 | -0.6 (8) |
| N2—C6—C1—N1 | 3.1 (6) | C30—C29—C28—C27 | 0.1 (9) |
| C7—C6—C1—N1 | -178.0 (4) | C26—C27—C28—C29 | 1.1 (8) |
| N2—C6—C1—C2 | -174.3 (4) | C15—C14—C13—C12 | 0.2 (8) |
| C7—C6—C1—C2 | 4.6 (7) | C11—C12—C13—C14 | 0.0 (8) |
| C6—N2—C10—C9 | -0.1 (7) | C20—C19—C18—C17 | 1.1 (8) |
| NI1—N2—C10—C9 | -178.6 (3) | N5—C25—C24—C23 | 1.3 (7) |
| C6—N2—C10—C11 | 179.1 (4) | C26—C25—C24—C23 | -177.8 (5) |
| NI1—N2—C10—C11 | 0.6 (5) | C9—C8—C7—C6 | 0.3 (7) |
| N3—C11—C10—N2 | -0.3 (6) | CL1—C8—C7—C6 | 179.8 (3) |
| C12—C11—C10—N2 | 180.0 (5) | N2—C6—C7—C8 | 1.3 (7) |
| N3—C11—C10—C9 | 178.8 (4) | C1—C6—C7—C8 | -177.6 (4) |
| C12—C11—C10—C9 | -0.9 (8) | C19—C18—C17—C16 | -2.0 (8) |
| C30—N6—C26—C27 | -0.5 (7) | N4—C16—C17—C18 | 1.6 (8) |
| NI1—N6—C26—C27 | 173.1 (4) | C21—C22—C23—C24 | -1.2 (7) |
| C30—N6—C26—C25 | -179.0 (4) | C21—C22—C23—CL2 | 179.3 (3) |
| NI1—N6—C26—C25 | -5.4 (5) | C25—C24—C23—C22 | -0.5 (7) |
| C26—N6—C30—C29 | 1.8 (8) | C25—C24—C23—CL2 | 179.0 (3) |
| NI1—N6—C30—C29 | -170.8 (4) | C25—N5—C21—C22 | -1.4 (7) |
| C16—N4—C20—C19 | -0.8 (7) | NI1—N5—C21—C22 | 180.0 (3) |
| NI1—N4—C20—C19 | 177.2 (4) | C25—N5—C21—C20 | -178.8 (4) |
| C16—N4—C20—C21 | 178.8 (4) | NI1—N5—C21—C20 | 2.6 (5) |
| NI1—N4—C20—C21 | -3.3 (5) | C23—C22—C21—N5 | 2.1 (7) |
| C21—N5—C25—C24 | -0.4 (7) | C23—C22—C21—C20 | 179.2 (5) |
| NI1—N5—C25—C24 | 178.2 (3) | N4—C20—C21—N5 | 0.6 (6) |
| C21—N5—C25—C26 | 178.8 (4) | C19—C20—C21—N5 | -179.9 (4) |
| NI1—N5—C25—C26 | -2.6 (5) | N4—C20—C21—C22 | -176.7 (4) |
| N6—C26—C25—N5 | 5.3 (6) | C19—C20—C21—C22 | 2.9 (7) |
| C27—C26—C25—N5 | -173.2 (5) | C7—C8—C9—C10 | -1.7 (7) |
| N6—C26—C25—C24 | -175.5 (4) | CL1—C8—C9—C10 | 178.8 (4) |
| C27—C26—C25—C24 | 6.0 (8) | N2—C10—C9—C8 | 1.6 (7) |
| N6—C26—C27—C28 | -1.0 (8) | C11—C10—C9—C8 | -177.5 (5) |
| C25—C26—C27—C28 | 177.4 (5) | C1—N1—C5—C4 | 2.8 (8) |
| N6—C30—C29—C28 | -1.7 (9) | NI1—N1—C5—C4 | -174.5 (5) |
| C20—N4—C16—C17 | -0.2 (8) | C3—C4—C5—N1 | -2.7 (9) |

| Table S2. Geometric parameters for hydrogen bonds and other intermolecular contacts (Å, º) operating in the crystal structure of Ni(Cltpy)2(Cl2).2H2O. |  |  |  |  |
| --- | --- | --- | --- | --- |
| D-H…A | D-H | H…A | D…A | D-H…A |
| O1 -H2O1...Cl3i | 0.82 | 2.44 | 3.2587 | 174 |
| O1 -H1O1...Cl3ii | 0.83 | 2.44 | 3.2079 | 154 |
| O2-H2O2...Cl4 | 0.83 | 2.38 | 3.1875 | 165 |
| O2-H1O2...Cl4iii | 0.81 | 2.42 | 3.2204 | 170 |
| C5-H5...Cl3iv | 0.93 | 2.82 | 3.5266 | 134 |
| C12-H12...O1v | 0.93 | 2.58 | 3.4549 | 156 |
| C13-H13...Cl3vi | 0.93 | 2.81 | 3.6784 | 156 |
| C15-H15...O2vii | 0.93 | 2.58 | 3.2459 | 129 |
| C19-H19...Cl3viii | 0.93 | 2.67 | 3.5859 | 167 |
| C30-H30...O1iv | 0.93 | 2.54 | 3.2677 | 135 |

i: 1/2-x,-1/2+y,1/2+z; ii: -x,1-y,1/2+z; iii: -1/2+x,1/2-y,z; iv: 1/2+x,1/2-y,z; v: 1+x,y,z; vi: 3/2-x,-1/2+y,1/2+z; vii: 1-x,-y,1/2+z; viii: 1+x,-1+y,z.