Supporting Information

Comparing life cycle environmental impacts of batch and flow synthesis of early-stage polymer development

Or Galanta, Charles E. Diesendruckb, Sabrina Spataria*

aFaculty of Civil and Environmental Engineering, Technion - Israel Institute of Technology, Haifa 32000 Israel

bSchulich Faculty of Chemistry, Technion - Israel Institute of Technology, Haifa 32000 Israel

*Corresponding author, E-mail: ssabrina@technion.ac.il

Contents

Scale-up calculations and assumptions for LCI based on experimental lab-scale study	2

Solvent separation and recovery calculations	2

Table S1. Energy demands calculations and sources for LCI	3

Table S2. Chemicals input and output sources	4

Table S3. LCI for scenario 1	5

Table S4. LCI for scenario 2 and 3	6

References	7

Number of pages: 7

Number of tables: 4

# Scale-up calculations and assumptions for LCI based on experimental lab-scale study

Based on previous study,[1] at lab-scale, intramolecular cross-linking (CL) occurs through anthracene photodimerization upon irradiation with UV light (366 nm) in dilute solutions (0.5 mgmL-1) of polymer in THF. The amount of SCNPs generated in the lab-scale is 200 mg, where 400 mL solvent is used. To reach 4.5 mol% CL, the reaction time for batch process is 44 min. In the flow process, the reaction time to collect the same amount of SCNPs and 4.5 % mol CL (reactor volume ca. 100 mL, UV lamp length 50 cm) at flow rate 15 mLmin-1 is 27 min (400 mL divided by 15 mLmin-1).

For scale-up calculations, to create a life cycle inventory (LCI), in batch process we assume a reactor volume of 0.002 m3 (2000 mL) for the production of 1 g SCNPs. For the scale-up system design, the time of reaction assumed to remain 44 min (0.7 h). In flow process, with the current experimental conditions, the reaction will take a significantly long time to produce 1 g SCNPs, thereof, we first linearly scaled up the system assuming the reactor volume to be ca. 0.0002 m3 (200 mL), with a longer lamp of 100 cm. To keep desired intramolecular CL density of 4.5 mol% SCNPs, the flow rate will be 30 mlmin-1. With this system design, the time of reaction takes 67 min (1.1 h) to produce 1 g SCNPs.

# Solvent separation and recovery calculations

For scenario 1, where solvent is not recovered, the quantity of solvent for batch and flow processes is 0.002 m3 for 1 g SCNPs. Once solvent is recovered, as considered in scenarios 2 and 3, the quantity of solvent for flow process is 0.0002 m3 as reactor system design, however we take into account an excess of 0.0002 m3 (0.0004 m3 in total) for LCI calculations to consider a continuous flow process where reaction occurs in parallel to solvent recovery. For batch, the quantity of solvent remains 0.002 m3 due to reactor system design. Once solvent is recovered, only ‘make-up’ solvent is required to supply to the reaction due to solvent losses.[2]

Vacuum distillation is considered for product separation from solvent for product purification (scenario 1) or for solvent recovery (scenario). Solvent is recovered through distillation by pressure drop where solvent is heated to 40 ˚C.[3] Solvent condensation for recovery is done by using a chiller which is assumed to contain circulated cooling liquid, thereof the energy demands for condensation are taken from typical chiller specifications.[4] Solvent recovery through distillation for scenario 3 is calculated based on statistical analysis of empirical data from 150 waste solvent distillation.[2]

Equations for energy demands and their sources are detailed in Table 1. Chemicals input and output sources are detailed in Table 2. LCI for chemicals and energy demands are summarized in Table 2 for scenario 1 (batch and flow processes with no solvent recovery) and Table 3 for scenario 2 and 3 (batch and flow with solvent recovery) where results are linearly scaled to obtain a functional unit of 1 kg SCNPs, as expected in an industrial scale.

# Table S1. Energy demands calculations and sources for LCI

| Energy requirement | Equation | Parameters | units | LCI data | Source |
| --- | --- | --- | --- | --- | --- |
| Estir stirring solution[5] | 0.018∙m5∙s-3ρmix∙t | t – reaction time [s] - density [kgm-3] | [J] | Electricity, medium voltage {IL}¦ market for electricity, medium voltage ¦ APOS, U | Ecoinvent 3.0[6] |
| EUV UV operation[7] | 0.015kW∙t | t – reaction time [h] | [kWh] | Electricity, medium voltage {IL}¦ market for electricity, medium voltage ¦ APOS, U | Ecoinvent 3.0[6] |
| Epump Liquid pumping[5] | 1.53∙10-5kWhkg∙m | m – solution mass[kg] | [kWh] | Electricity, medium voltage {IL}¦ market for electricity, medium voltage ¦ APOS, U | Ecoinvent 3.0[6] |
| Evacuum Vacuum (drying/solvent separation)[3] | 4.2kW∙t | t – reaction time [h] | [kWh] | Electricity, medium voltage {IL}¦ market for electricity, medium voltage ¦ APOS, U | Ecoinvent 3.0[6] |
| Qcond Electricity for condensation[4] | 0.73kW∙t | t – reaction time [h] | [MJ] | Electricity, medium voltage {IL}¦ market for electricity, medium voltage ¦ APOS, U | Ecoinvent 3.0[6] |
| Qsolv heat Solvent heating[5] | Cp∙Tb-T0∙ρsolv∙V1000KJMJ∙ηheat | V – solvent volume [m3] | [MJ] | Heat, from steam, in chemical industry {RER}¦ market for heat, from steam, in chemical industry ¦ APOS, U | Ecoinvent 3.0[6] |
| Edist Electricity for distillation[2] | 0.033kW∙m | m – solvent [kg] | [kWh] | Electricity, medium voltage {IL}¦ market for electricity, medium voltage ¦ APOS, U | Ecoinvent 3.0[6] |
| Qdis Energy for distillation[2] | 1.21kg steamkg solvent∙2.8∙MJkg steam∙m | m – solvent [kg] | [MJ] | Heat, from steam, in chemical industry {RER}¦ market for heat, from steam, in chemical industry ¦ APOS, U | Ecoinvent 3.0[6] |
| msolv. rec. Solvent recovery for batch process[2] | 0.68kgkg solvent∙m | m – solvent [kg] | [kg] | - | - |
| msolv. rec. Solvent recovery for flow process[2] | 0.76kgkg solvent∙m | m – solvent [kg] | [kg] | - | - |
| msolv. res. Solvent residues for batch process[2] | 0.3kgkg solvent∙m | m – solvent [kg] | [kg] | - | - |
| msolv. res. Solvent residues for flow process[2] | 0.22kgkg solvent∙m | m – solvent [kg] | [kg] | - | - |

| Chemical | LCI data | Source |
| --- | --- | --- |
| PMMA | DE: Polymethylmethacrylate granulate (PMMA) mix ts | GaBi[8] |
| THF | Tetrahydrofuran {GLO}¦ market for ¦ APOS, U | Ecoinvent 3.0[6] |
| Benzene | Benzene {GLO}¦ market for ¦ APOS, U | Ecoinvent 3.0[6] |
| DCM | Dichloromethane {RoW}¦ market for dichloromethane ¦ APOS, U | Ecoinvent 3.0[6] |
| TCM | Trichloromethane {RoW}¦ market for trichloromethane ¦ APOS, U | Ecoinvent 3.0[6] |
| Toluene | Toluene, liquid {GLO}¦ market for ¦ APOS, S | Ecoinvent 3.0[6] |
| Incineration | Spent solvent mixture {RoW}¦ treatment of hazardous waste incineration ¦ APOS, U | Ecoinvent 3.0[6] |

# Table S2. Chemicals input and output sources

# Table S3. LCI for scenario 1

|  |  | Flow process |  |  |  |  |  | Batch process |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | THF | Benzene |  |  |  | Toluene | THF |  | Benzene |  | Toluene |
| Conditions |  |  |  |  |  |  |  |  |  |  |  |  |
|  | SCNPs [%mol CL] | 4.5 |  | 4.5 |  | 4.5 |  | 4.5 | 4.5 |  | 4.5 |  |
|  | Solvent for reaction [m3] | 0.4 |  | 0.4 |  | 0.4 |  | 2 | 2 |  | 2 |  |
|  | Flow rate [mLmin-1] | 30 |  | 30 |  | 30 |  | - | - |  | - |  |
|  | Time of reaction [h] | 1.1 |  | 1.1 |  | 1.1 |  | 0.7 | 0.7 |  | 0.7 |  |
| Materials |  |  |  |  |  |  |  |  |  |  |  |  |
| Physical properties | Density @ 25 ⁰C [kg·m3] | 889 | 876 |  |  |  | 867 | 889 |  | 876 |  | 867 |
|  | Cp @ 25 ⁰C [kJ/kg·K] | 1.7 | 1.8 |  |  |  | 1.7 | 1.7 |  | 1.8 |  | 1.7 |
| Materials inputs | Polymer precursor [kg] | 1 |  | 1 |  | 1 |  | 1 |  | 1 |  | 1 |
|  | Solvent [m3] | 2 |  | 2 |  | 2 |  | 2 |  | 2 |  | 2 |
| Materials outputs | Solvent waste for incineratione,g [m3] | 2 |  | 2 |  | 2 |  | 2 |  | 2 |  | 2 |
| Steps/Energy demands |  |  |  |  |  |  |  |  |  |  |  |  |
| Electricity [kWh] | Stirringh | 18 |  |  | 18 |  | 17 | 12 |  | 12 |  | 11 |
|  | UV lampi | 17 |  | 17 |  | 17 |  | 11 |  | 11 |  | 11 |
|  | Solvent pumping to reactor | 2.7E-03 |  | 2.7E-03 |  | 2.7E-03 |  | - |  | - |  | - |
|  | Concentrated polymer inject | 1.5E-05 |  | 1.5E-05 |  | 1.5E-05 |  | - |  | - |  | - |
|  | Water cooling pumping to UV lamp | 1.0E-03 |  | 1.0E-03 |  | 1.0E-03 |  | 6.7E-04 |  | 6.7E-04 |  | 6.7E-04 |
|  | Vacuum distillation | 2100 |  | 2100 |  | 2100 |  | 2100 | 2100 |  | 2100 |  |
|  | Solvent condensation | 365 |  | 365 |  | 365 |  | 365 | 365 |  | 365 |  |
| Heat [MJ] | Solvent heating to 40 ⁰C | 46 | 49 |  |  |  | 44 | 46 |  | 49 |  | 44 |
| Total |  |  |  |  |  |  |  |  |  |  |  |  |
| Total electricity [kWh] |  | 2500 |  | 2500 |  | 2500 |  | 2490 | 2490 |  | 2490 |  |
| Total heat [MJ] |  | 46 | 49 |  |  |  | 44 | 46 |  | 49 |  | 44 |

# Table S4. LCI for scenario 2 and 3

|  |  | Flow process |  |  |  | Batch process |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | THF | Benzene |  | Toluene | THF | Benzene |  |  | Toluene |
| Conditions |  |  |  |  |  |  |  |  |  |  |
|  | SCNPs [%mol CL] | 4.5 |  | 4.5 | 4.5 | 4.4 | 4.4 |  |  | 4.4 |
|  | Solvent for reaction [m3] | 0.4 |  | 0.4 | 0.4 | 2 | 2 |  |  | 2 |
|  | Solvent recoveredd,e [m3] | 0.3 |  | 0.3 | 0.3 | 1.4 | 1.4 |  |  | 1.4 |
|  | Flow rate [mLmin-1] | 30 |  | 30 | 30 | - | - |  |  | - |
|  | Time of reaction [h] | 1.1 |  | 1.1 | 1.1 | 0.7 | 0.7 |  |  | 0.7 |
| Materials |  |  |  |  |  |  |  |  |  |  |
| Physical properties | Density @ 25 ⁰C [kg·m3] | 889 | 876 |  | 867 | 889 | 876 |  |  | 867 |
|  | Cp @ 25 ⁰C [kJ/kg·K] | 1.7 | 1.8 |  | 1.7 | 1.7 | 1.8 |  |  | 1.7 |
| Materials inputs | Polymer precursor [kg] | 1 |  | 1 | 1 | 1 | 1 |  |  | 1 |
|  | ‘Make up’ Solvente,f [m3] | 0.1 |  | 0.1 | 0.1 | 0.6 | 0.6 |  |  | 0.6 |
| Materials outputs | Solvent waste for incineratione,g [m3] | 0.1 |  | 0.1 | 0.1 | 0.6 | 0.6 |  |  | 0.6 |
| Steps/Energy demands |  |  |  |  |  |  |  |  |  |  |
| Electricity [kWh] | Stirring | 18 |  | 18 | 17 | 12 |  | 12 |  | 11 |
|  | UV lamp | 17 |  | 17 | 17 | 11 | 11 |  |  | 11 |
|  | Solvent pumping to reactor | 2.7E-03 |  | 2.7E-03 | 2.7E-03 | - | - |  |  | - |
|  | Concentrated Polymer inject | 1.5E-05 |  | 1.5E-05 | 1.5E-05 | - | - |  |  | - |
|  | Water cooling pumping to UV lamp | 1.0E-03 |  | 1.0E-03 | 1.0E-03 | 6.7E-04 | 6.7E-04 |  |  | 6.7E-04 |
|  | Vacuum distillation (scenario 2) | 4670 |  | 4670 | 4670 | 3080 | 3080 |  |  | 3080 |
|  | Solvent condensation (scenario 2) | 540 |  | 540 | 540 | 810 | 810 |  |  | 810 |
|  | Atmospheric distillation (scenario 3) | 59 | 58 |  | 57 | 59 | 58 |  |  | 57 |
| Heat [MJ] | Solvent heating to 40 ⁰C (scenario 2) | 46 | 49 |  | 44 | 46 | 49 |  |  | 44 |
|  | Steam (distillation, scenario 3) | 916 | 902 |  | 893 | 4100 | 4040 |  |  | 3990 |
| Total |  |  |  |  |  |  |  |  |  |  |
| Total Electricity [kWh] | Scenario 2 | 5512 |  | 5512 | 5512 | 3638 | 3638 |  |  | 3638 |
|  | Scenario 3 | 93 | 92 |  | 91 | 81 | 80 |  |  | 80 |
| Total Heat [MJ] | Scenario 2 | 46 | 49 |  | 44 | 46 | 49 |  |  | 44 |
|  | Scenario 3 | 916 | 902 |  | 893 | 4100 | 4040 |  |  | 3995 |

# References

1. 	Galant O, Donmez HB, Barner‐Kowollik C, Diesendruck CE. Flow Photochemistry for Single‐Chain Polymer Nanoparticle Synthesis. Angewandte Chemie International Edition. 2021;60(4):2042-2046. doi:10.1002/anie.202010429

2. 	Capello C, Hellweg S, Badertscher B, Hungerbühler K. Life-Cycle Inventory of Waste Solvent Distillation: Statistical Analysis of Empirical Data. Environ Sci Technol. 2005;39(15):5885-5892. doi:10.1021/ES048114O

3. 	Parvatker AG, Tunceroglu H, Sherman JD, et al. Cradle-to-Gate Greenhouse Gas Emissions for Twenty Anesthetic Active Pharmaceutical Ingredients Based on Process Scale-Up and Process Design Calculations. ACS Sustain Chem Eng. 2019;7(7):6580-6591. doi:10.1021/acssuschemeng.8b05473

4. 	Lab chiller specs,.Average of cooling capacities of 0.25 to 1.2 kW. https://bit.ly/3h9Sr6X%22

5. 	Piccinno F, Hischier R, Seeger S, Som C. From laboratory to industrial scale: a scale-up framework for chemical processes in life cycle assessment studies. J Clean Prod. 2016;135:1085-1097. doi:10.1016/j.jclepro.2016.06.164

6. 	Pre Consultants SimaPro 9.0.0.49, The Netherlands, 2018.

7. 	Low pressure mercury vapour lamp, purchased from Helios Quartz America INC, operated at 15W with peak emission at 366 nm.

8. 	Sphera GaBi 9: The Software System for Life Cycle Assessment, Stuttgart, 2020.