Supplementary Materials for

Evidence of Polariton-Version Quantum Cherenkov Radiations

Lei Wang et al.

*Corresponding author. Email: lei_wang@jlu.edu.cn, liuxueqing@jlu.edu.cn, and haiyu_wang@jlu.edu.cn

This PDF file includes:

Note S1 to S3

Figs. S1 to S15

References (1 to 8)

Note S1. Low-frequency cutoffs in quantum Cherenkov radiation theory and polariton-version quantum Cherenkov radiation model

For non-point charges like relativistic electron beams described by quantum wave packets in cylindrical coordinates, it predicts the typical rates (such as  or ) of photon emission in the cases with/without electron spin flipping obey the following equations, due to total angular momentum and energy conservations in both azimuthal and radial polarizations1,

(S1)

(S2)

(S3)

(S4)

Ei and Ef are the energies for initial and final states of single-electron beam, respectively; i is the spread angle for initial state of single-electron beam;  is the fine-structure constant (1/137); m is the rest mass of electron; n is the refractive index; vp is the phase velocity of light; ħ is reduced Planck constant;  is the angular frequency of photons. Those equations for the calculations of emission rates always work, no matter if there is a plane-wave basis or a cylindrical basis for the final state.

It definitely shows a spectral discontinuity at the frequency cutoff for Eq. S1 and Eq. S2, where CR = 0 and electron spin flip occurs. If no spin flip in this theory,  would provide a negligible value near the spectrally low-frequency cutoff in the azimuthal polarization (Eq. S3), and would not give this spectral discontinuity in the radial polarization (Eq. S4, which is dominant and also the only possibility in conventional Cherenkov radiation theory). More importantly, except Eq. S4, the other are quadratic functions of photon energy (ħ or hvprobe, where h is Planck constant, and v is the frequency of probe photons). For example, it could be the quadratic expression for Eq. S1 and Eq. S2 as following,  for simplification. Sketch for the emission rate of this single-electron-beam-version quantum Cherenkov photons with electron spin flip are presented in Fig. 1b in the main text.

For the polariton-version quantum Cherenkov radiation model from the time-resolved experiment point of view, similar predictions could be used here for double-cone polariton emissions arising from transient non-point electron wave packets, and various PhPs could be involved experimentally, too. Then, we mainly consider the theoretical expectations of radial/azimuthal polariton emission rate with spin flips. The resulting emission rate of polaritons here could be similar to the Eq. S1/S2 in the form of quadratic function of probe photon energy, and should contain the corrections from the contributions of other types of PhPs. In experiments, we find the amplitudes (, half of peak-to-peak value for pulse-like signals) of Cherenkov-type PhPs are presented as quadratic functions for the probe photon energy (Fig. 1d in the main text). Since  is proportional to the emitted photon number (Nph) in single-electron-beam-version quantum Cherenkov photons, and here assuming  is proportional to the emitted PhP number (NPhP) as presented in Fig. S6, we could obtain a quadratic expression as follow,  (, ). It is experimentally found that  decays in the form of  at first, covering the ‘region I’ in Fig. 3c in the main text. While for the lower probe photon energy window corresponding to the ‘region II’ in Fig. 3c in the main text,  gradually enhances as  further decreases. This deviation from the expectation of single-electron-beam-version quantum Cherenkov theory is likely due to the superposition with other types of PhPs in crystals, including near-infrared PhPs (discussed in Fig. S7) and displacive-type PhPs (shown in BaTiO3 (110) crystals in Supplementary Note 2, too). Thus, the quadratic fitting results of  in Fig. 1d in the main text suggest a blue-shifted center cutoff frequency (  2.4 eV for Cone-1, and   2.6 eV for cone-2), in comparison with the true low-frequency cutoff for Cherenkov-type PhPs in the lower probe photon energy range. Fortunately, we can directly observe the suppression of PhPs around this low-frequency cutoff in THz domain (Fig. 1e in the main text), showing a ~20-meV-width gap with the center of  at ~1.83 eV, corresponding to the true low-frequency cutoff for Cherenkov-type PhPs. It also acts as a boundary separating the region II from the region III (Fig. 3c in the main text). It suggests that the resulting spectral discontinuity could affect other types of PhPs in vicinity, too, in the polariton-version quantum Cherenkov radiation model. It in turn means if no spin flip in the polariton-version quantum Cherenkov radiation, it would not be a sharp dip around the low-frequency cutoff in THz domain, since the other types of PhPs could fill in this spectral region immediately.

In a word, those evidence verify the existence of electron spin flips in the radial/azimuthal polarization case. Namely, ultrashort-pulse-stimulated bound electrons are initial non-point charges described by quantum wave packets (i.e., populated in a metastable state labelled by the number  in Fig. 1c in the main text, with se = –1/2 for assumption), then they have to return to the ground state by experiencing twice electron-spin flip transitions (referring to Fig. 3f in the main text, it may become se = 1/2 state for the first spin flip, and finally returns to a ground state, labelled by the number  in Fig. 1c in the main text, with se = –1/2 again after the second spin flip) and emitting double-cone Cherenkov-type PhPs (Cone-1 and Cone-2 in Fig. 1d in the main text). Such twice electron-spin flip transitions are further demonstrated by the time-resolved circular polarization dynamics in fig. S10, suggesting that there are opposite phases for observed polaritons (the inner and outer cones), respectively. This is also a relativistic phenomenon, since it emits double-cone polaritons almost instantaneously in the local coordinate, and this instantaneous process should have a duration for the observers in the laboratory coordinate.

In addition, averaged temporal durations of 126  35 fs for Cherenkov-type PhPs in LN crystals are longer than the best instrument response function of ~35 fs, and the first temporal duration of Cherenkov-type PhP (139  33 fs for Cone-1) is longer than the second one (112  32 fs for Cone-2), taken the restored dynamic curves in Fig. 3f in the main text for example. It indicates a varied coherent momentum uncertainty of ultrashort-pulse-stimulated bound electrons during twice electron-spin flip transitions, since the strong similarities to a quantized charged-particle beam model2, where the smaller coherent momentum uncertainty of the relativistic particle is, the longer the shock wave (Cherenkov radiation) becomes.

Note S2. Material-specific low-frequency cutoff for quantum Cherenkov radiations

Fig. S9d presents the TA data of BaTiO3 (110) crystal under 1.55-eV excitation. Its longest transient response is up to ~6 ps for the blue side of probe window. There are stronger positive signals in BaTiO3 (110) crystals, compared to that in pristine LN crystals. Impressively, honeycomb-like structures are still clearly observed in THz domain of BaTiO3 (110) crystals, but appear in a relatively lower frequency range (from ~0.4 THz to ~3 THz, Fig. S9e). Steady-state absorption and TA data analysis of BaTiO3 (110) crystals under 3.1-eV excitation also support electronic responses are not contributed to the observed periodic structures in THz domain (Fig. S9a-c). So, this THz feature in Fig. S9e reveals Cherenkov-type PhPs in BaTiO3 (110) crystals, and the underlying position of spectral discontinuity is at ~655 nm, different from that of pristine LN crystals. Thus, a material-specific low-frequency cutoff for quantum Cherenkov radiations in ferroelectric crystals is further demonstrated.

Note S3. Component analysis of the term of  in graphene

The term of  for graphene is obtained in the following steps. First, we get a curve by subtracting the contributions of other terms from the original curve probed at 410 nm for graphene. Then, we fit this remaining curve by a two-exponential function. The fitting results for the obtained term of  in the graphene sample are related to two kinds of signals: one is a positive decay signal with a relatively longer lifetime of ~1.4 ps in this delay time window of Fig. 3k in the main text (probably from free carriers beyond the Dirac cone of graphene), and the other is a negative bleaching decay signal with a relatively shorter lifetime of ~135 fs. Since this negative bleaching decay signal probed at 410 nm is corresponding to the hot Dirac fermions at higher energy levels of the graphene sample, its lifetime is of course shorter than that (~250 fs) probed at 800 nm (Fig. S10).

Noting that the term of  at 410 nm in graphene just follows the initial polariton dynamics processes after relativistic corrections shown in Fig. 3l in the main text, it implies ultrashort-pulse-accelerated hot-Dirac fermions could not directly return to the ground state by quickly experiencing twice electron-spin flip transitions and emitting two hybrid polaritons almost synchronously. In other words, if ultrashort-pulse-accelerated hot-Dirac fermions are synchronous with this term of  at 410 nm like in LN crystals, it should have an earlier initial time for  in graphene. Instead, it starts just after the finish of initial polariton dynamics. This suggests ultrashort-pulse-accelerated hot-Dirac fermions in graphene could lose a part of energy in the form of double-cone Cherenkov-type polariton emissions, and then turn to free carriers and hot Dirac fermions at relatively high energy levels, thanks to the zero-gap nature of graphene.

Figure S1. a, Schematic of 35-fs TA experiments under 1.55-eV excitation. The pump pulse energy is ~120 nJ/pulse for LN crystals in a reflective focusing case with a focal length of 250 mm in this work, unless there are specific statements on the pump pulse energy. Ultrashort 35-fs pulses with photon energy of 1.55 eV (800 nm) or 3.1 eV (400 nm) are loosely focused into a crystal as pump lights, in order to generate Cherenkov radiations. Super-continuum (SC) white lights with similar pulse widths of pump lights are probe lights, recording all transient responses at the focal point of pump lights. b, Typical TA dynamics (for example, probed at 450 nm) of x-cut LN crystals under 1.55-eV excitation with paralleled and perpendicular cases. We find the influence of scattering of pump lights on the TA data around 800 nm for perpendicular case is much larger than that for paralleled case. So, we prefer to present those TA data in the paralleled case in this paper. c, Normalized TA dynamics (for example, probed at 400 nm) of z-cut/x-cut LN crystals under 1.55-eV excitation with different thicknesses. It is found that the time intervals of double-cone Cherenkov-type PhPs for the two z-cut LN crystals are almost thickness-independent, and both are longer than that in the x-cut LN crystal with 0.5 mm thickness. In this work, the x-cut LN crystal with 0.5 mm thickness is mainly used, if without specific statements on the category of LN crystals. On the other hand, if we estimate the distance in the laboratory coordinate between double-cone Cherenkov-type PhPs based on those time intervals and group velocity (vg) shown in Fig. S4, it will be much shorter than the thickness of LN samples. Thus, it rules out the possibility of two pulse-like signals (named Cone-1 and Cone-2) for Cherenkov-type PhPs with opposite phases to each other is originated from the two regions near the front and back interfaces of LN crystals, due to the bulk optical rectification effect3.

Figure S2. a, Chirped TA data for quartz substrates under 1.55-eV excitation. b, FFT amplitude spectrum for the TA data of quartz substrates under 1.55-eV excitation. c, Chirped TA data for quartz substrates under 3.1-eV excitation, where the pump pulse energy is much larger than that used for LN crystals. d, FFT amplitude spectrum for the TA data of quartz substrates under 3.1-eV excitation.

Figure S3. a, Steady-state absorption spectrum for pristine LN crystals. b, TA data for pristine LN crystals under 3.1-eV excitation. It indicates that for pristine LN crystals in 1.55-eV and 3.1-eV excitation conditions, the energy of single pump photon is not large enough for directly pumping the electrons in the valence band to the conduction band by single-photon absorption (SPA). So, the multiple-photon absorption (MPA) exists in both cases, indicating the contribution of the imaginary part of complex refractive index. This electronic response in excited states for 3.1-eV excitation TA experiments is overwhelming, in contrast to that for 1.55-eV excitation TA experiments.

Figure S4. Calculated group velocity (vg) based on the group refractive index (ng) of LN crystals4,5, where ng = c/vg shows a continuous curve and is much larger than 1 in the probe window (c is the speed of light in vacuum and vg is group velocity of light in solids). Thus, in conventional Cherenkov radiation theory, it would not give a discontinuity in the observed spectral dispersion of Cherenkov-type PhPs.

Figure S5. The influence of overlapping in space between pump lights and SC white-light probe lights focused inside LN crystals on the transient signal amplitudes in TA experiments. a, paralleled case under 1.55-eV excitation. b, perpendicular case under 1.55-eV excitation. Herein, the overlapping in space between pump pulses and SC white-light probe pulses focused inside LN crystals in the following TA experiments are chosen to obtain the similar transient signal amplitudes for both Cherenkov-type PhPs.

Figure S6. a, Input power dependent kinetics for pristine LN crystals under 1.55-eV excitation (probed at 410 nm). b, Amplitudes () of double-cone Cherenkov-type PhPs (Cone-1 and Cone-2) as a quadratic function of input pump power, which is consistent with the report for nonlinear Cherenkov radiations6. Hence, it is reasonable to estimate the proportional relation between  and the emitted PhP number (NPhP).

Figure S7. FFT amplitude spectrum for pristine LN crystals under 1.55-eV excitation at the probe wavelength of a, 605 nm; b, 660 nm; c, 700 nm and d, 830 nm. Inset in panel a are the dynamics curves for the four corresponding probe wavelengths, which shows the shorter probe wavelength has the smaller influence of coherent oscillation arisen from near-infrared PhPs. The coherent oscillation dynamics in region III are more sensitive to the coherence of output laser pulses.

Figure S8. FFT amplitude spectrum for the TA data of pristine LN crystals under 3.1-eV excitation.

Figure S9. a, Steady-state absorption spectrum for BaTiO3 (110) crystals. b, TA data for pristine BaTiO3 (110) crystals under 3.1-eV excitation. c, FFT amplitude spectrum for the TA data of BaTiO3 (110) crystals under 3.1-eV excitation. d, TA data of BaTiO3 (110) crystal under 1.55-eV excitation. e, FFT amplitude spectrum for the TA data of BaTiO3 (110) crystals under 1.55-eV excitation. The blue dashed line indicates one of displacive-type PhPs in BaTiO3 crystals.

Figure S10. a, The same (SCP, σ++ for both pump and probe lights with left circular polarization) and opposite (OCP, σ+− for the pump light with left circular polarization and the probe light with right circular polarization) circularly polarized dynamics for pristine LN crystals under 1.55-eV excitation (probed at 400 nm), and b, corresponding time-resolved circular polarization (P) dynamics, where the horizontal line in the panel b indicates the zero-point line. The definition of P is 7. Since pump pulses are σ+, it will selectively stimulate the electron spin state of se = –1/2, which will give a positive circular polarization at the initial time. But in fig. S10d, there are negative P values within the first 150 fs (a negative peak value of P  –1 appears at ~100 fs), indicating the first electron-spin flip transition for the emission of Cone-1. Then, the P value becomes positive again at the apparent delay time between ~0.5 ps and ~1.5 ps, covering the time of Cone-2 emitting. This indicates the second electron-spin flip transition.

Figure S11. Normalized relaxation dynamics of hot Dirac fermions probed at 800 nm in graphene on quartz substrates under 3.1-eV excitation. Solid red line is the single-exponential fitting result. It indicates the relaxation lifetime of ~250 fs, which is consistent with previous report8.

Figure S12. Raman spectra of quartz substrate and graphene on quartz under 532 nm excitation. The blue curve (graphene-quartz) for pure Raman signals of graphene is obtained by subtracting the Raman signals of quartz from that of graphene on quartz. The typical Raman signals at G peak (1583 cm-1) and 2D peak (2673 cm-1) for graphene indicate the good quality of monolayer sample, and the additional enhancement in the range of 50-500 cm-1 covers the main Raman signals of quartz, implying the substrate modulation effect.

Figure S13. a, FFT amplitude spectrum and b, corresponding 3D representation for TA data of FsLDW-LN under 1.55-eV excitation. FFT amplitude spectrum for FsLDW-LN crystals under 1.55-eV excitation at the probe wavelength of c, 605 nm; d, 660 nm; e, 700 nm and f, 830 nm. Inset in panel c are the dynamics curves for the four corresponding probe wavelengths.

Figure S14. The photographs of FsLDW-LN squares. Sample #1, Epulse = 0.2 J/pulse. Sample #2, Epulse = 0.3 J/pulse. Sample #3, Epulse = 0.55 J/pulse. Sample #4, Epulse = 0.8 J/pulse. Sample #5, Epulse = 0.1 J/pulse. Sample #6, Epulse = 0.14 J/pulse. Sample #7, Epulse = 0.15 J/pulse. Sample #8, Epulse = 0.95 J/pulse. The size of each modification area is 1 mm (length)  1 mm (width)  0.1 mm (thickness). The fabrication depths for FsLDW-LN samples are controllable. When the value of Epulse bellows the threshold condition, the fabricated squares are ‘invisible’ by naked eyes (i.e., Sample #5 and Sample #6 indicated by dotted squares). The glass substrates are removed in TA experiments.

Figure S15. AFM images of the surface of LN crystals with (a) no treatment, (b) femtosecond laser ablation, (c) after thermal annealing of original LN and (d) after thermal annealing of samples with hybrid laser fabrication process. In the condition close to the fabrication threshold, a smooth surface after femtosecond laser ablation is expected. So, thermal annealing can restore the surface roughness after femtosecond laser ablation to the idea case, which is close to that of original LN crystals with a thermal annealing treatment.

References

- I. Kaminer, M. Mutzafi, A. Levy, G. Harari, H. H. Sheinfux, S. Skirlo, J. Nemirovsky, J. D. Joannopoulos, M. Segev, M. Soljačić, Quantum Čerenkov radiation: spectral cutoffs and the role of spin and orbital angular momentum. Phys. Rev. X 6, 011006 (2016).

2.	A. Karnieli, N. River, A. Arie, I. Kaminer, The coherence of light is fundamentally tied to the quantum conherence of the emitting particle. Sci. Adv. 7, eabf8096 (2021).

3.	L. Xu, X. C. Zhang, D. H. Auston, Terahertz beam generation by femtosecond optical pulses in electro-optic materials. Appl. Phys. Lett. 61, 17841786 (1992).

4.	D. E. Zelmon, D. L. Small, D. Jundt, Infrared corrected Sellmeier coefficients for congruently grown lithium niobate and 5 mol.% magnesium oxide-doped lithium niobate. J. Opt. Soc. Am. B 14, 33193322 (1997).

5.	Q. R. Xing, K. M. Yoo, R. R. Alfano, Conical emission by four-photon parameteric generation by using femtosecond laser pulses. Appl. Opt. 32, 20872089 (1993).

6.	Y. Zhang, Z. D. Gao, Z. Qi, S. N. Zhu, N. B. Ming, Nonlinear Čerenkov radiation in nonlinear photonic crystal waveguides. Phys. Rev. Lett. 100, 163904 (2008).

7.	Y. Y. Yue, H. Y. Wang, L. Wang, L. Y. Zhao, H. Wang, B. R. Gao, H. B. Sun, Direct observation of room-temperature intravalley coherent coupling processes in monolayer MoS2. Laser Photonics Rev. 16, 2100343 (2022).

8.	L. B. Huang, G. V. Hartland, L. Q. Chu, Luxmi, R. M. Feenstra, C. X. Lian, K. Tahy, H. L. Xing, Ultrafast transient absorption microscopy studies of carrier dynamics in epitaxial graphene. Nano Lett. 10, 13081313 (2010).a