Supplementary Materials for

Atomically-precise engineering of spin-orbit polarons

in a kagome magnetic Weyl semimetal

Hui Chen1,2,3†, Yuqing Xing1,2†, Hengxin Tan4, Li Huang1,2, Qi Zheng1,2, Zihao Huang1,2, Xianghe Han1,2, Bin Hu1,2, Yuhan Ye1,2, Yan Li1,2, Yao Xiao1,2, Hechang Lei5, Xianggang Qiu1, Enke Liu1, Haitao Yang1,2,3, Ziqiang Wang6, Binghai Yan4 and Hong-Jun Gao1,2,3*

Corresponding author: hjgao@iphy.ac.cn,

Fig. S1.

Fig. S1. Demonstration of the single vacancy with nc-AFM. a, STM image of the single S vacancy, showing a hole-like feature (Vs= -4 mV, It=10 pA). b, Constant-height AFM images by using a CO tip in the same region of (a) with the scanning height of -190 pm (left) and -70 pm (right), respectively, showing the missing S atom at the vacancy site. Scanning height: -190 pm, Vs= -4 mV, It=10 pA. Scanning amplitude = 50 pm.

Fig. S2.

Fig. S2. Typical large-scale STM image of S-terminated surface, showing randomly-distributed S vacancies with different size and shape.

Fig. S3.

Fig. S3. Demonstration of the single vacancy repairing with nc-AFM. a,b STM images showing the topography before (a) and after (b) vacancy repairing (Vs= -4 mV, It=10 pA). c, Constant-height AFM images at the same region of (b), showing the filling of an additional S atom at the vacancy site as marked by the red spot in (a). Scanning height: -190 pm, Vs= -4 mV, It=10 pA. Scanning amplitude = 50 pm.

Fig. S4.

Fig. S4. Topography and dI/dV spectra of S vacancies before and after vacancy repairing. a,b STM images before (a) and after (b) STM manipulations, showing that a single S vacancy is repaired (Vs = −400 mV, It = 500 pA). c, Typical dI/dV spectra obtained at the blue, red and green spots, respectively, showing the similar density of state at the as-repaired vacancy with vacancy-free S surface region (Vs = −400 mV, It = 500 pA, Vmod = 0.5 mV).

Fig. S5.

Fig. S5. Transition barrier of a S atom from the bulk to the single vacancy site on the S-surface. Four intermediate structures in the Nudged Elastic Band (NEB) calculations are considered as #2 ~#5, where #1 and #6 show the surface S vacancy and bulk S vacancy respectively (only the three top-most layers are shown for simplicity). The S (green) moves in out-of-plane direction from #1 to #3 (barrier ~ 0.74 eV), and moves in the surface plane from #3 to #6 (barrier ~ 0.73 eV). Notice that structures #3 and #4 are very close but not the same. The medium energy barrier indicates that pulling one S from the bulk to occupy the surface vacancy site is possible. Spin-orbit coupling is not included.

Fig. S6.

Fig. S6. Step-by-step atomic manipulation of S vacancy aggregates: from irregular to regular vacancy shape. a, Consecutive STM images of a large vacancy being repaired and transformed into a quasi-triangular vacancy highlighted by the dotted blue triangle (Vs = −100 mV, It = 500 pA). b, Consecutive STM images of another large vacancy being repaired and transformed into a quasi-hexagonal vacancy highlighted by the dotted green hexagon (Vs = −100 mV, It = 500 pA). The scale bars in all figures correspond to 1 nm.

Fig. S7.

Fig. S7. Localized quantum states around a dimer S-vacancy at the S-terminated surface. a, dI/dV spectra at a dimer S-vacancy, showing several peaks corresponding to the bound states induced by the vacancy. b, STM image of a dimer-vacancy and dI/dV maps at different energies: -254 meV, -265 meV, -277 meV, -292 meV, and -360 meV, respectively.

Fig. S8.

Fig. S8. STM images and spectra of five-, six-, and seven- atomic vacancies on S terminated surfaces. a, STM images showing five-, six-, and seven- atomic vacancies on S-terminated surfaces. b, dI/dV spectra on the positions (marked by light blue, blue and green cross in (a), respectively) of the five-, six-, and seven- atomic vacancies, respectively, showing the sharp peak around -240 mV. The scale bar is 1 nm in (a) and (b).

Fig. S9.

Fig. S9. The dI/dV linecut along the edge of linear atomic S vacancies. a-e STM topography of linear atomic vacancies and dI/dV linecut along the red arrow, showing the spatial decay of the bound states with the atomic shift. The scale bar is 1 nm.

Fig. S10.

Fig. S10. Energy evolution of anti-bonding states for different vacancies. a, The model with a single hopping parameter, t, is considered in for simulation of the inter-vacancy interaction.  by a In the vacancy number, energy levels saturate to corresponding infinite size cases, 2t, 4t and 6t for linear, bilayer and triangular (also hexagonal) configurations. b, Energy evolution of the anti-bonding states for different vacancies based on the model in (a).

Fig. S11.

Fig. S11. Analysis of the lattice distortion around S vacancies. The antisymmetric strain map U(r)≡uaa(r)-ubb(r)(a) are derived from STM topography (b), showing that the relatively-larger lattice distortion is localized at the triangular vacancies.