Analysis of the substrate nature on the strength of a single-lap joint

A. Houaria, K. Madanib, M. El Ajramib, M. Belhouarib, R.D.S.G. Campilhoc,d

a Mechanical Engineering Department, Faculty of Technology, University M'Hamed Bougara of Boumerdes, Algeria

b Department of Mechanical Engineering, LMSS, University of Djillali Liabes, Sidi Bel Abbes, Algeria

c ISEP-School of Engineering, Polytechnic of Porto, R. Dr. António Bernardino de Almeida, 431, 4200-072 Porto, Portugal

d INEGI-Institute of Science and Innovation in Mechanical and Industrial Engineering, Pólo FEUP, Rua Dr. Roberto Frias, 400, 4200-465 Porto, Portugal

Table.1: Mechanical properties of the Adekit®A-140 adhesive

| Material | E (MPa) | ν | τII,τIII (MPa) | GIC kJ/m2 | GIIC,GIIIC kJ/m2 | σPL (MPa) | σY (MPa) | η | n | σYTS (MPa) | A % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adekit®A-140 | 2692 | 0.3 | 24.1 | 0.5 | 2.41 | 12.64 | 14.64 | 1.45 | 3.56 | 32 | 5 |

Table 2: Mechanical properties of Aluminum 2024-T3

| Material | E (MPa) | ν | σPL (MPa) | σY (MPa) | σUTS(MPa) | n | A % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Aluminium 2024- T3 | 74700 | 0.33 | 219 | 303 | 462 | 9.52 | 14 |

Table 3: Mechanical properties of fiber and matrix.

| Mechanical characteristic of carbon fiber |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E1 (MPa) | E2 (MPa) | E3 (MPa) | 12 | 13 | 23 | G12 (MPa) | G13 (MPa) | G23 (MPa) |
| 235000 | 12900 | 12900 | 0.27 | 0.27 | 0.27 | 8050 | 8050 | 8050 |
| Mechanical characteristic of the matrix |  |  |  |  |  |  |  |  |
| E1 (MPa) | E2 (MPa) | E3 (MPa) | 12 | 13 | 23 | G12 (MPa) | G13 (MPa) | G23 (MPa) |
| 3700 | - | - | 0.33 | - | - | 1380 | - | - |

Table 4: Mechanical properties of the composite.

| E1 (MPa) | E2 (MPa) | E3 (MPa) | 12 | 13 | 23 | G12 (MPa) | G13 (MPa) | G23 (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 77135 | 4200 | 4200 | 0.336 | 0.336 | 0.58 | 3058.9 | 3058.9 | 2500 |

| Properties | Units | Metal Al2024-T3 | Ceramic SiC [29] |
| --- | --- | --- | --- |
| Young’s modulus, E | [MPa] | 74700 | 302000 |
| Poisson coefficient, ν | - | 0.33 | 0.17 |
| Elastic limit, σY | [MPa] | 303 | - |
| Maximum stress, σUTS | [MPa] | 462 | 1400 |
| fracture energy, GIc | [kJ/m2] | 24 | 0.065 |
| Hardening modulus, H | [MPa] | 1000 | - |
| Stress-strain transfer ratio, “q” | [MPa] | 91600 [29] |  |

Table 5: Material properties of the metal (Al2024-T3) and FGM substrates [29].

Table.6: Mechanical and fracture properties of the Araldite A138 and Adiket®A-140 adhesives [26].

| Property | Adekit® A-124 (C1) [26] | Araldite AV138 (C2) [32] |
| --- | --- | --- |
| Young modulus E [Gpa] | 2692 | 4890 |
| Poisson’s ratio v | 0.35 | 0.33 |
| Tensile yield stress [Gpa] | 14.36 | 36.49 |
| Tensile strength [Gpa] | 32 | 40 |
| Shear modulus G[Gpa] | 846 | 1560 |
| Shear strength [Gpa] | 24.1 | 30.2 |
| Toughness in tension [N/mm] | 0.5 | 0.2 |
| Toughness in shear [N/mm] | 2.41 | 0.38 |
| Tensile failure strain % | 4.35 | 1.21 |

| Configuration |  | FGA (AdekitA-140/ Araldite AV138) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Radius UMM By row | Radius USDFLD By coordinate | n=0.5 (Rich Araldite AV138) |  | n=1.0 |  | n=2.0 (Rich AdekitA-140) |  |
|  |  | KnnUMM | KnnUSDFD | KnnUMM | KnnUSDFD | KnnUMM | KnnUSDFD |
| 0 | 0 | 13300 | 13300 | 13300 | 13300 | 13300 | 13300 |
| 2.21 | 2,82843 | 13743 | 13831,1 | 14450 | 15048 | 15925 | 16875 |
| 4.42 | 4,24264 | 14540 | 14382,7 | 15875 | 16244 | 18200 | 18282 |
| 6.63 | 7,07107 | 15410 | 16476,2 | 17312 | 17937 | 20125 | 20775 |
| 8.84 | 8,48528 | 16368 | 16338,3 | 18750 | 19133 | 21700 | 21715 |
| 11.04 | 11,3137 | 17450 | 17792,8 | 20187 | 20626 | 22935 | 23173 |
| 13.25 | 12,7279 | 18750 | 18785,2 | 21587 | 21522 | 23800 | 23790 |
| 15.46 | 15,5563 | 20432 | 20800,7 | 22925 | 23315 | 24325 | 24275 |
| 17.67 | 17,67 | 24500 | 24500 | 24500 | 24500 | 24500 | 24500 |