Supplementary Information

Highly conductive and stretchable hydrogel using a percolated network of whiskered gold nanosheets

Chaehong Lim1,2,⊥, Seunghwan Lee1,2,⊥, Chansul Park1,2, Jeong Hyun Kim1, Dae-Hyeong Kim1,2,3,*, and Taeghwan Hyeon1,2,*

1Center for Nanoparticle Research, Institute for Basic Science (IBS), Seoul 08826, Republic of Korea

2School of Chemical and Biological Engineering, and Institute of Chemical Processes, Seoul National University, Seoul 08826, Republic of Korea

3Department of Materials Science and Engineering, Seoul National University, Seoul 08826, Republic of Korea

⊥These authors contributed equally to this work.

*To whom correspondences should be addressed.

E-mail: dkim98@snu.ac.kr and thyeon@snu.ac.kr

| Ref. No. and Journal title | Conductive component | Conductivity (S/cm) | Stretchability (%) |
| --- | --- | --- | --- |
| This work | W-AuNS | 3300 | 100 (with substrate) |
| 37, Nat. Nanotechnol. (2021) | Graphene flake, CNT | 0.35 |  |
| 38, J. Mater. Chem. A (2020) | CNT | 0.005 |  |
| 39, ACS Appl. Mater. Interfaces (2019) | CNT | 0.002 | 1000 (mechanical) |
| 40, Nat. Commun. (2018) | PEDOT: PSS | 0.231 | 121 |
| 41, Proc. Natl. Acad. Sci. U. S. A. (2012) | PANI | 0.11 |  |
| 42, Adv. Funct. Mater. (2018) | PEDOT:PSS | 0.0035 |  |
| 43, Mater. Chem. Front. (2018) | PANI | 0.0064 | 80 (mechanical) |
| 44, Adv. Mater. (2020) | PEDOT:PSS | 0.1 |  |
| 45, Adv. Funct. Mater. (2020) | PEDOT:PSS | 0.002 |  |
| 46, ACS Nano (2014) | PPy | 0.195 | 30 |
| 47, Mater. Lett. (2018) | PPy | 0.0088 |  |
| 48, Chem. Mater. (2018) | CNT, PPY | 0.3493 | 515 (mechanical) |
| 49, Eur. Polym. J. (2007) | Silver particle | 0.0006 |  |
| 50, Mater. Lett. (2014) | Silver nanoparticle | 0.572 |  |
| 51, Macromol. Rapid Commun. (2005) | Gold nanoparticle | 0.0095 |  |
| 52, Mater. Sci. Eng. C. (2016) | Gold nanoparticle | 0.0013 |  |
| 53, Adv. Mater. (2022) | PEDOT:PSS | 306 | 31 |
| 18, Adv. Mater. (2022) | PEDOT:PSS | 10 | 150 |
| 54, Nat. Commun. (2019) | PEDOT:PSS | 40 | 35 |
| 19, Nat. Biomed. Eng. (2019) | PEDOT:PSS | 47.4 | 20 |
| 55, Adv. Mater. (2022) | PEDOT PSS, MXENE | 55.17 | 7 |
| 56, Sci. adv. (2022) | PEDOT PSS, AuNP | 670 | 15 |
| 32, Nat. Electron. (2021) | Silver flake | 350 (partially dried) | 250 (partially dried) |
| 57, J. Mater. Chem. A (2022) | Silver flake | 12.31 | 535 |
| 58, Nat. Commun. (2023) | PPy | 80 | 36 |
| 59, Nat. Mater. (2022) | PEDOT:PSS | 11 | 400 |
| 60, Macromol. Rapid Commun. (2022) | PEDOT:PSS, ionic liquid | 38 | 45 |
| 61, Nat. Commun. (2020) | PEDOT:PSS | 28 | 20 |
| 62, Adv. Funct. Mater. (2021) | Silver nanowire | 166 | 90 |

Supplementary Table 1. Conductivities and stretchabilities of conductive and stretchable hydrogels. PANI (polyaniline), CNT (carbon nanotube), PPy (polypyrrole), and PEDOT:PSS (poly(3,4-ethylenedioxythiophene) polystyrene sulfonate).

|  | PAAm (hydrogel) | PAA (hydrogel) | PVA (hydrogel) | PBA (organogel) |
| --- | --- | --- | --- | --- |
| Hydrogel or organogel solutions | 120, 180, 240, and 300 mg of AAm (Acrylamide, Sigma Aldrich, A8887) was dissolved in 1 ml of water to prepare PAAm12, PAAm18, PAAm24, and PAAm30, respectively. Proper amount of 65 mM MBAA (N,N′-Methylenebis(acrylamide), Sigma Aldrich, 146072) solution was added to the AAm solution to make the ratio between MBAA and AAm 600:1. Then, the solution was degassed in vacuum for 3 hours. | 2.4 ml of AA (Acrylic acid, Sigma Aldrich, 147230), 1.23 ml of 0.3 M FeCl3 (Iron(III) chloride, Sigma Aldrich, 157740) solution, 0.9 ml of 65 mM MBAA solution, and 5.47 ml of water was mixed to prepare PAA hydrogel solution. The solution was purged with argon for 30 minutes. | 150 mg of PVA (Poly(vinyl alcohol), Sigma Aldrich, 341584; Mw 89,000 – 98,000) was dissolved in 1 ml of water by vigorous stirring at 90 ℃ for 4 hours. | 0.7 ml of butyl acrylate (Sigma Aldrich, 234923), 0.3 ml of paraffin oil (Sigma Aldrich, 18512), and 35 μl of 0.6 M EGDA (Ethylene glycol diacrylate, Sigma Aldrich, 480797) solution was mixed to prepare PBA organogel solution. |
| Initiator solutions | 25 μl of 77 mM APS (Ammonium persulfate, Sigma Aldrich, 248614) solution and 25 μl of TEMED (N,N,N′,N′-Tetramethylethylenediamine, Sigma Aldrich, T22500) solution (20 μl of TEMED per 1 ml of water) were used as initiator and accelerator for 1.5 ml of the hydrogel solution. | 25 μl of 19 mM APS solution was used as initiator for 1.5 ml of the hydrogel solution. | (Freeze-thaw) | 20 μl of AIBN solution (2,2′-Azobis(2-methylpropionitrile) solution, Sigma Aldrich, 714887) was used as an initiator for 1.5 ml of the organogel solution. |

Supplementary Table 2. Preparation of hydrogels and an organogels. Acrylic acid, butyl acrylate, and ethylene glycol diacrylate were used after removing inhibitors.

References

1.	Liang, Q. et al. Electron Conductive and Transparent Hydrogels for Recording Brain Neural Signals and Neuromodulation. Adv. Mater. 35, 2211159 (2022).

2.	Tringides, C. M. et al. Viscoelastic surface electrode arrays to interface with viscoelastic tissues. Nat. Nanotechnol. 16, 1019-1029 (2021).

3.	Jiang, Y. et al. Topological supramolecular network enabled high-conductivity, stretchable organic bioelectronics. Science 375, 1411-1417 (2022).

4.	Jiang, Z. et al. A 1.3-micrometre-thick elastic conductor for seamless on-skin and implantable sensors. Nat. Electron. 5, 784-793 (2022).

5.	Miyamoto, A. et al. Inflammation-free, gas-permeable, lightweight, stretchable on-skin electronics with nanomeshes. Nat. Nanotechnol. 12, 907-913 (2017).

6.	Stoyanov, H., Kollosche, M., Risse, S., Waché, R. & Kofod, G. Soft Conductive Elastomer Materials for Stretchable Electronics and Voltage Controlled Artificial Muscles. Adv. Mater. 25, 578–583 (2013).

7.	Dong, R., Ma, P. X. & Guo, B. Conductive biomaterials for muscle tissue engineering. Biomaterials 229, 119584 (2020).

8.	Choi, Y. S. et al. Stretchable, dynamic covalent polymers for soft, long-lived bioresorbable electronic stimulators designed to facilitate neuromuscular regeneration. Nat. Commun. 11, 5990 (2020).

9.	Choi, S., Han, S. I., Kim, D., Hyeon, T. & Kim, D.-H. High-performance stretchable conductive nanocomposites: materials, processes, and device applications. Chem. Soc. Rev. 48, 1566-1595 (2019).

10.	Yuk, H., Lu, B. & Zhao, X. Hydrogel bioelectronics. Chem. Soc. Rev. 48, 1642-1667 (2019).

11.	Choi, S. et al. Highly conductive, stretchable and biocompatible Ag-Au core-sheath nanowire composite for wearable and implantable bioelectronics. Nat. Nanotechnol. 13, 1048-1056 (2018).

12.	Gu, M. et al. Stretchable batteries with gradient multilayer conductors. Sci. Adv. 5, eaaw1879 (2019).

13.	Jang, K.-I. et al. Rugged and breathable forms of stretchable electronics with adherent composite substrates for transcutaneous monitoring. Nat. Commun. 5, 4779 (2014).

14.	Xie, Z., Avila, R., Huang, Y. & Rogers, J. A. Flexible and Stretchable Antennas for Biointegrated Electronics. Adv. Mater. 32, 1902767 (2020).

15.	Afanasenkau, D. et al. Rapid prototyping of soft bioelectronic implants for use as neuromuscular interfaces. Nat. Biomed. Eng. 4, 1010-1022 (2020).

16.	Feig, V. R., Tran, H., Lee, M. & Bao, Z. Mechanically tunable conductive interpenetrating network hydrogels that mimic the elastic moduli of biological tissue. Nat. Commun. 9, 2740 (2018).

17.	Yuk, H., Wu, J. & Zhao, X. Hydrogel interfaces for merging humans and machines. Nat. Rev. Mater. 7, 935-952 (2022).

18.	Li, G. et al. Highly Conducting and Stretchable Double-Network Hydrogel for Soft Bioelectronics. Adv. Mater. 34, 2200261 (2022).

19.	Liu, Y. et al. Soft and elastic hydrogel-based microelectronics for localized low-voltage neuromodulation. Nat. Biomed. Eng. 3, 58-68 (2019).

20.	Dvir, T. et al. Nanowired three-dimensional cardiac patches. Nat. Nanotechnol. 6, 720-725 (2011).

21.	Hu, L. et al. Hydrogel-Based Flexible Electronics. Adv. Mater., 2205326 (2023).

22.	Deng, J. et al. Electrical bioadhesive interface for bioelectronics. Nat. Mater. 20, 229-236 (2021).

23.	Li, G. et al. Development of Conductive Hydrogels for Fabricating Flexible Strain Sensors. Small 18, 2101518 (2022).

24.	Matsuhisa, N., Chen, X., Bao, Z. & Someya, T. Materials and structural designs of stretchable conductors. Chem. Soc. Rev. 48, 2946-2966 (2019).

25.	Wang, W. et al. Tough and stretchable ionogels by in situ phase separation. Nat. Mater. 21, 359-365 (2022).

26.	Jung, D. et al. Highly conductive and elastic nanomembrane for skin electronics. Science 373, 1022-1026 (2021).

27.	Zhao, Y. et al. Soft strain-insensitive bioelectronics featuring brittle materials. Science 378, 1222-1227 (2022).

28.	Feig, V. R. et al. An Electrochemical Gelation Method for Patterning Conductive PEDOT:PSS Hydrogels. Adv. Mater. 31, 1902869 (2019).

29.	Jung, D. et al. Adaptive Self-Organization of Nanomaterials Enables Strain-Insensitive Resistance of Stretchable Metallic Nanocomposites. Adv. Mater. 34, 2200980 (2022).

30.	Kim, J.-Y. & Kotov, N. A. Charge Transport Dilemma of Solution-Processed Nanomaterials. Chem. Mater. 26, 134-152 (2013).

31.	Wang, L. & Daoud, W. A. Hybrid conductive hydrogels for washable human motion energy harvester and self-powered temperature-stress dual sensor. Nano Energy 66, 104080 (2019).

32.	Ohm, Y. et al. An electrically conductive silver–polyacrylamide–alginate hydrogel composite for soft electronics. Nat. Electron. 4, 185-192 (2021).

33.	Zhao, Y. et al. A self-healing electrically conductive organogel composite. Nat. Electron. 6, 206-215 (2023).

34.	Lim, C. et al. Facile and Scalable Synthesis of Whiskered Gold Nanosheets for Stretchable, Conductive, and Biocompatible Nanocomposites. ACS Nano 16, 10431-10442 (2022).

35.	Guan, Q.-F. et al. Bio-Inspired Lotus-Fiber-like Spiral Hydrogel Bacterial Cellulose Fibers. Nano Lett. 21, 952-958 (2021).

36.	Yan, J. A Review of Sintering-Bonding Technology Using Ag Nanoparticles for Electronic Packaging. Nanomaterials 11, 927 (2021).

37.	Tringides, C. M. et al. Viscoelastic surface electrode arrays to interface with viscoelastic tissues. Nat. Nanotechnol. 16, 1019-1029 (2021).

38.	He, P. et al. Anti-freezing and moisturizing conductive hydrogels for strain sensing and moist-electric generation applications. J. Mater. Chem. A 8, 3109-3118 (2020).

39.	Deng, Z. et al. Stimuli-Responsive Conductive Nanocomposite Hydrogels with High Stretchability, Self-Healing, Adhesiveness, and 3D Printability for Human Motion Sensing. ACS Appl. Mater. Interfaces 11, 6796-6808 (2019).

40.	Feig, V. R., Tran, H., Lee, M. & Bao, Z. Mechanically tunable conductive interpenetrating network hydrogels that mimic the elastic moduli of biological tissue. Nat. Commun. 9, 2740 (2018).

41.	Pan, L. et al. Hierarchical nanostructured conducting polymer hydrogel with high electrochemical activity. Proc. Natl. Acad. Sci. U. S. A. 109, 9287-9292 (2012).

42.	Roshanbinfar, K. et al. Electroconductive Biohybrid Hydrogel for Enhanced Maturation and Beating Properties of Engineered Cardiac Tissues. Adv. Funct. Mater. 28, 1803951 (2018).

43.	Zhu, Y., Liu, S., Shi, X., Han, D. & Liang, F. A thermally responsive host–guest conductive hydrogel with self-healing properties. Mater. Chem. Front. 2, 2212-2219 (2018).

44.	Zhang, S. et al. Room-Temperature-Formed PEDOT:PSS Hydrogels Enable Injectable, Soft, and Healable Organic Bioelectronics. Adv. Mater. 32, 1904752 (2020).

45.	Li, S., Wang, L., Zheng, W., Yang, G. & Jiang, X. Rapid Fabrication of Self‐Healing, Conductive, and Injectable Gel as Dressings for Healing Wounds in Stretchable Parts of the Body. Adv. Funct. Mater. 30 (2020).

46.	Hur, J. et al. Polypyrrole/Agarose-Based Electronically Conductive and Reversibly Restorable Hydrogel. ACS Nano 8, 10066-10076 (2014).

47.	Li, Y., Zhang, H., Ni, S. & Xiao, H. In situ synthesis of conductive nanocrystal cellulose/polypyrrole composite hydrogel based on semi-interpenetrating network. Mater. Lett. 232, 175-178 (2018).

48.	Deng, Z., Guo, Y., Zhao, X., Ma, P. X. & Guo, B. Multifunctional Stimuli-Responsive Hydrogels with Self-Healing, High Conductivity, and Rapid Recovery through Host–Guest Interactions. Chem. Mater. 30, 1729-1742 (2018).

49.	Xiang, Y. & Chen, D. Preparation of a novel pH-responsive silver nanoparticle/poly(HEMA–PEGMA–MAA) composite hydrogel. Eur. Polym. J. 43, 4178-4187 (2007).

50.	Devaki, S. J., Narayanan, R. K. & Sarojam, S. Electrically conducting silver nanoparticle–polyacrylic acid hydrogel by in situ reduction and polymerization approach. Mater. Lett. 116, 135-138 (2014).

51.	Zhao, X. et al. Thermoswitchable Electronic Properties of a Gold Nanoparticle/Hydrogel Composite. Macromol. Rapid Commun. 26, 1784-1787 (2005).

52.	Baei, P. et al. Electrically conductive gold nanoparticle-chitosan thermosensitive hydrogels for cardiac tissue engineering. Mater. Sci. Eng. C. 63, 131-141 (2016).

53.	Wang, J. et al. Ultra-High Electrical Conductivity in Filler-Free Polymeric Hydrogels Toward Thermoelectrics and Electromagnetic Interference Shielding. Adv. Mater. 34, 2109904 (2022).

54.	Lu, B. et al. Pure PEDOT:PSS hydrogels. Nat. Commun. 10, 1043 (2019).

55.	Liu, J. et al. Additive Manufacturing of Ti3C2-MXene-Functionalized Conductive Polymer Hydrogels for Electromagnetic-Interference Shielding. Adv. Mater. 34, 2106253 (2022).

56.	Won, D. et al. Digital selective transformation and patterning of highly conductive hydrogel bioelectronics by laser-induced phase separation. Sci. adv. 8, eabo3209 (2022).

57.	Liu, H. et al. Multifunctional gradient hydrogel with ultrafast thermo-responsive actuation and ultrahigh conductivity. J. Mater. Chem. A 10, 21874-21883 (2022).

58.	He, H. et al. Hybrid assembly of polymeric nanofiber network for robust and electronically conductive hydrogels. Nat. Commun. 14, 759 (2023).

59.	Zhou, T. et al. 3D Printable High Performance Conducting Polymer Hydrogel for All-Hydrogel Bioelectronics. Preprint at https://www.biorxiv.org/content/10.1101/2022.01.29.478311v1 (2022).

60.	Yang, J., Chang, L., Ma, C., Cao, Z. & Liu, H. Highly Electrically Conductive Flexible Ionogels by Drop-Casting Ionic Liquid/PEDOT:PSS Composite Liquids onto Hydrogel Networks. Macromol. Rapid Commun. 43, 2100557 (2022).

61.	Yuk, H. et al. 3D printing of conducting polymers. Nat. Commun. 11, 1604 (2020).

62.	Zhou, Q. et al. Mechanically Strong and Multifunctional Hybrid Hydrogels with Ultrahigh Electrical Conductivity. Adv. Funct. Mater. 31, 2104536 (2021).