Facile Synthesis of Z-Scheme Fe-nPPy/BiOI Nanocomposite for Enhanced Visible Light Driven Photocatalytic Activity

Rajesh Kumara,b, Rituporn Gogoia, Kajal Sharmaa, Astha Singha, Prem Felix Sirila*

a School of Basic Sciences, Indian Institute of Technology Mandi, Mandi, Himachal Pradesh-175005, India

b Govt. College Kullu, Himachal Pradesh- 175001, India

*Corresponding author: prem@iitmandi.ac.in

Table of Content:

| Sr. No. | Contents | Page |
| --- | --- | --- |
| 1 | Fig. S1: XRD patterns (a) and FTIR spectra (b) of the synthesized nanocomposites | S-2 |
| 2 | Fig. S2: XPS survey spectra of (a) BiOI, Fe-nPPy and Fe-nPPy/BiOI-3 and (b) other synthesized nanocomposites. | S-2 |
| 3 | Fig. S3: Deconvoluted Fe2p XPS spectra of (a) Fe-nPPy and (b) Fe-nPPy/BiOI-3 | S-3 |
| 4 | Fig. S4: Variation in the UV-Vis absorbance spectra with time of: (a) CV dye and (b) Tetracycline, showing the photocatalytic degradation using Fe-nPPy/BiOI-3 nanocomposite as the photocatalyst under visible light irradiation. | S-3 |
| 5 | Fig. S5: XRD patterns of fresh and after three cycles of photocatalysis of Fe-nPPy/BiOI-3 | S-4 |
| 6 | Table S1: XPS Peak table showing % composition of different elements in Fe-nPPy/BiOI-3 | S-4 |
| 7 | Fig. S6: UPS spectra of (a) Fe-nPPy and (b) BiOI | S-5 |

Fig. S1: XRD patterns (a) and FTIR spectra (b) of the synthesized nanocomposites.

Fig. S2: XPS survey spectra of (a) BiOI, Fe-nPPy and Fe-nPPy/BiOI-3 and (b) other synthesized nanocomposites.

Fig. S3: Deconvoluted Fe2p XPS spectra of (a) Fe-nPPy and (b) Fe-nPPy/BiOI-3.

Fig. S4: Variation in the UV-Vis absorbance spectra with time of: (a) CV dye and (b) Tetracycline, showing the photocatalytic degradation using Fe-nPPy/BiOI-3 nanocomposite as the photocatalyst under visible light irradiation.

Fig. S5: Fig. S5: XRD patterns of fresh and after three cycles of photocatalysis of Fe-nPPy/BiOI-3.

Table S1: Surface elemental composition of Fe-nPPy/BiOI-3 as per survey spectra.

| Name | Peak BE | FWHM eV | Area (P) CPS.eV | Atomic % | Q | SF |
| --- | --- | --- | --- | --- | --- | --- |
| I3d | 619.75 | 1.58 | 2755213.41 | 7.27 | 1 | 42.416 |
| Bi4f | 159.88 | 2.52 | 5469514.21 | 11.55 | 1 | 38.304 |
| C1s | 285.87 | 3.08 | 608732.95 | 53.19 | 1 | 1 |
| O1s | 531.23 | 4.23 | 596396.4 | 21.53 | 1 | 2.881 |
| N1s | 400.79 | 3.3 | 110187.25 | 6.2 | 1 | 1.676 |
| Fe2p | 720.08 | 0.56 | 29798.18 | 0.25 | 1 | 14.353 |

Fig. S6: UPS spectra of (a) Fe-nPPy and (b) BiOI