Enhancement of the Electronic and Optical Properties of Superalkali Metal Adsorbed Al10N10 Nanocage

Shradha Lakhera1, Meenakshi Rana1*, Kamal Devlal1, Vivek Dhuliya2, Diwakar Padalia3

1Department of Physics, School of Sciences, Uttarakhand Open University,

Haldwani, 263139, Uttarakhand, India

2Department of Physics, Gurukula Kangri (Deemed to be University), Haridwar, 249404, Uttarakhand, India

3Department of Physics, School of Basic & Applied Sciences, K. R. Mangalam University, Gurugram 122103, Haryana, India

SD 1. Computed values of frontier molecular orbital parameters for Al10N10, Al10N10+Li4N, and Al10N10+Li4O.

| Molecular property | Al10N10 | Li4N | Li4O | Al10N10+Li4N | Al10N10+Li4O |
| --- | --- | --- | --- | --- | --- |
| ELUMO | -0.859 | -1.583 | -1.483 | -2.586 | -2.58 |
| EHOMO | -6.829 | -4.788 | -3.01 | -3.458 | -3.458 |
| Bandgap (ΔE) | 5.98 | 3.20 | 1.527 | 0.872 | 0.878 |
| Ionization potential (IP) | 6.829 | 4.788 | 3.01 | 3.458 | 3.458 |
| Electron affinity (EA) | 0.859 | 1.583 | 1.483 | 2.586 | 2.58 |
| Chemical potential (CP) | -3.844 | -3.185 | -2.246 | -3.022 | -3.019 |
| Electronegativity (χ) | 3.844 | 3.185 | 2.246 | 3.022 | 3.019 |
| Hardness (η) | 2.99 | 1.6 | 0.763 | 0.436 | 0.439 |
| Softness (S) | 0.33 | 0.625 | 1.310 | 1.14 | 1.13 |
| Electrophilicity index (ω) | 2.47 | 3.17 | 3.305 | 10.472 | 10.38 |
| Electron accepting power (ω+) | 1.3 | 1.773 | 2.277 | 9.016 | 8.926 |
| Electron donating power (ω-) | 6.69 | 4.959 | 4.523 | 12.038 | 11.945 |

SD 2. Charge distribution of Al10N10, Al10N10+Li4N, and Al10N10+Li4O.

| Al10N10 |  |  | Al10N10+Li4N |  |  | Al10N10+Li4O |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | Mulliken | Natural | Atom | Mulliken | Natural | Atom | Mulliken | Natural |
| 1N | -0.6237 | -1.24285 | 1N | -0.29405 | -1.1868 | 1N | -0.61919 | -1.235 |
| 2N | -0.6625 | -1.27116 | 2N | -0.0865 | -1.2541 | 2N | -0.66574 | -1.2611 |
| 3N | -0.6341 | -1.22278 | 3N | -0.19237 | -1.2204 | 3N | -0.63411 | -1.2253 |
| 4N | -0.6426 | -1.22788 | 4N | -0.13295 | -1.2191 | 4N | -0.64088 | -1.2309 |
| 5N | -0.9447 | -1.90638 | 5N | -0.07043 | -1.9328 | 5N | -0.96995 | -1.9322 |
| 6N | -0.651 | -1.24621 | 6N | -0.26852 | -1.9819 | 6N | -0.75672 | -1.2704 |
| 7N | -0.9302 | -1.88918 | 7N | 0.04627 | -1.9551 | 7N | -0.93866 | -1.8939 |
| 8N | -0.639 | -1.24541 | 8N | 0.00564 | -1.9798 | 8N | -0.75414 | -1.3327 |
| 9N | -0.9641 | -1.92796 | 9N | -0.29822 | -1.9882 | 9N | -1.07233 | -1.962 |
| 10N | -0.9423 | -1.91024 | 10N | 0.07314 | -1.9708 | 10N | -0.94946 | -1.9047 |
| 11Al | 0.6693 | 1.25362 | 11Al | 0.20691 | 1.3559 | 11Al | 0.59124 | 1.2269 |
| 12Al | 0.945 | 1.89639 | 12Al | -0.25876 | 1.8012 | 12Al | 0.95766 | 1.8899 |
| 13Al | 0.6351 | 1.2581 | 13Al | 0.20792 | 1.5596 | 13Al | 0.70294 | 1.2435 |
| 14Al | 1.0157 | 1.88436 | 14Al | 0.38625 | 1.8689 | 14Al | 1.03 | 1.8763 |
| 15Al | 0.5738 | 1.22568 | 15Al | 0.33225 | 1.1578 | 15Al | 0.52337 | 1.2477 |
| 16Al | 0.9356 | 1.88943 | 16Al | 0.09996 | 1.8704 | 16Al | 0.93076 | 1.8764 |
| 17Al | 0.6747 | 1.31779 | 17Al | 0.19429 | 1.3716 | 17Al | 0.63417 | 1.296 |
| 18Al | 0.9722 | 1.92476 | 18Al | 0.33666 | 1.9025 | 18Al | 0.71361 | 0.9875 |
| 19Al | 0.6256 | 1.25104 | 19Al | -1.14555 | 1.5927 | 19Al | 0.43978 | 1.2149 |
| 20Al | 0.5872 | 1.1889 | 20Al | 0.328 | 1.1499 | 20Al | 0.5534 | 1.2086 |
|  |  |  | 21Li | -0.25793 | 0.7812 | 21O | -0.89086 | -1.5055 |
|  |  |  | 22Li | -0.23074 | 0.831 | 22Li | 0.64441 | 0.6686 |
|  |  |  | 23Li | 0.01557 | 0.6775 | 23Li | -0.01208 | 0.5458 |
|  |  |  | 24Li | -0.3287 | 0.8277 | 24Li | 0.50081 | 0.9102 |
|  |  |  | 25N | -0.28594 | -2.0586 | 25Li | 0.68196 | 0.5611 |

SD 3. Computed Raman and FT-IR data for Al10N10, Al10N10+Li4N, and Al10N10+Li4O (Symmetric stretching-ν, asymmetric stretching-α, torsional bending in plane (scissoring)-δ, twisting-τ, rocking-ρ, and wagging-ω).

| Mode | Frequency | Infrared | Raman activity | Raman intensity |
| --- | --- | --- | --- | --- |
| Al10N10 |  |  |  |  |
| δN-Al | 939.05 | 110.2480 | 30.7926 | 3730.53 |
| αN-N | 816.53 | 91.9515 | 33.2537 | 5627.05 |
| αAl-Al | 392.65 | 26.5559 | 85.3043 | 74921.03 |
| δN-Al | 378.40 | 20.7184 | 111.9406 | 106493.88 |
| ρN-Al | 922.21 | 52.6197 | 147.0823 | 18615.68 |
| ωN-Al | 900.91 | 40.2275 | 235.7481 | 31564.466 |
| Al10N10+Li4N |  |  |  |  |
| ωN-Al | 226.09 | 1.8246 | 258.1683 | 732908.4229 |
| αN-Li | 565.54 | 87.4078 | 267.6186 | 105291.6903 |
| δN-Li | 247.99 | 1.2557 | 279.7280 | 654119.7673 |
| νN-Li | 536.28 | 131.6795 | 299.7464 | 132803.6603 |
| δN-Li | 419.67 | 21.3554 | 308.5051 | 234507.9193 |
| δN-Al | 546.31 | 1.2215 | 320.2344 | 136134.4709 |
| ωAl-Li | 234.39 | 6.5481 | 325.4654 | 856745.3315 |
| νAl-Al | 597.42 | 11.3414 | 370.4899 | 128848.1155 |
| νAl-Al | 517.61 | 24.6676 | 480.7147 | 230451.3295 |
| δN-Li | 302.60 | 17.6277 | 584.4910 | 897452.5464 |
| ωN-Al | 635.62 | 28.6479 | 621.1076 | 187707.3783 |
| ωLi-Al | 98.01 | 29.0553 | 1144.8880 | 18224635.88 |
| δN-Al | 619.75 | 10.0699 | 1395.7798 | 446754.1058 |
| νN-Al | 773.18 | 152.5462 | 1721.8904 | 331225.6743 |
| δN-Al | 823.43 | 172.8667 | 1775.0076 | 294447.6551 |
| Al10N10+Li4O |  |  |  |  |
| νN-Al | 316.90 | 38.2484 | 168.6000 | 234640.6733 |
| ωLi-Al | 882.66 | 73.2357 | 180.6977 | 25410.47099 |
| αO-Li | 451.81 | 132.6184 | 188.2530 | 121801.575 |
| αN-Al | 812.60 | 155.6839 | 191.4038 | 32759.42004 |
| δN-Li | 610.56 | 15.7927 | 210.6384 | 69740.61646 |
| ωN-Al | 794.52 | 41.9528 | 230.0789 | 41521.14983 |
| δAl-Li | 231.85 | 4.0754 | 362.0037 | 974940.9449 |
| δN-Al | 548.62 | 36.2575 | 415.5063 | 174978.1742 |
| δO-Li | 391.25 | 22.0650 | 569.3363 | 503917.4141 |
| αN-Al | 782.64 | 81.3065 | 588.7981 | 110081.8741 |
| δO-Li | 438.63 | 5.2133 | 848.0514 | 585417.3599 |
| αO-Li | 841.79 | 227.5721 | 1160.2674 | 182676.4638 |

SD 4. Simulated absorption transitions of Al10N10, Al10N10+Li4N, and Al10N10+Li4O.

| Structure | Excited state | Absorption (excitation energy, wavelength, oscillator strength) |
| --- | --- | --- |
| Al10N10 | S0→S1 | 2.4053 eV,515.45 nm, f=0.0093 |
|  | S0→S2 | 2.6394 eV,469.74 nm, f=0.0097 |
|  | S0→S3 | 2.7025 eV, 458.77 nm, f=0.0129 |
|  | S0→S4 | 2.8119 eV,440.92 nm, f=0.0146 |
|  | S0→S5 | 2.8260 eV,438.73 nm, f=0.0251 |
|  | S0→S6 | 2.9516 eV,420.06 nm, f=0.0311 |
|  | S0→S7 | 3.1300 eV,396.11 nm, f=0.0223 |
|  | S0→S8 | 3.1961 eV,387.92 nm, f=0.0301 |
|  | S0→S9 | 3.2998 eV, 375.74 nm, f=0.0117 |
| Al10N10+Li4N | S0→S1 | 0.8289 eV, 1495.69 nm, f=0.0006 |
|  | S0→S2 | 0.9178 eV,1350.83 nm, f=0.0258 |
|  | S0→S3 | 1.0019 eV, 1237.55 nm, f=0.0006 |
|  | S0→S4 | 1.1308 eV, 1096.45 nm, f=0.0113 |
|  | S0→S5 | 1.1707 eV, 1059.08 nm, f=0.0018 |
|  | S0→S6 | 1.2035 eV, 1030.21 nm, f=0.0173 |
|  | S0→S7 | 1.3195 eV, 939.67 nm, f=0.0120 |
|  | S0→S8 | 1.3325 eV, 930.45 nm, f=0.0038 |
|  | S0→S9 | 1.3523 eV, 916.87 nm, f=0.0298 |
| Al10N10+Li4O | S0→S1 | 1.5547 eV, 797.48 nm, f=0.0364 |
|  | S0→S2 | 1.9053 eV, 650.73 nm, f=0.0372 |
|  | S0→S3 | 2.1330 eV, 581.26 nm, f=0.0657 |
|  | S0→S4 | 2.3808 eV, 520.77 nm, f=0.0799 |
|  | S0→S5 | 2.4887 eV, 498.19 nm, f=0.0222 |
|  | S0→S6 | 2.5412 eV, 487.89 nm, f=0.1435 |
|  | S0→S7 | 2.6554 eV, 466.91 nm, f=0.0213 |
|  | S0→S8 | 2.7542 eV, 450.16 nm, f=0.0672 |
|  | S0→S9 | 2.8039 eV, 442.19 nm, f=0.0112 |