SUPPLEMENTARY MATERIAL

Environmental Science and Pollution research

5 years of leaching experiments to evaluate a modified bauxite residue. Part 1: transformation into a soil and storage of immobilized heavy metals from acid mine drainage

Patricia Merdy1, Alexandre Parker1,2, Chen Chen1,2, Pierre Hennebert2,3

1 Université de  Toulon, Aix Marseille Univ., CNRS, IM2NP, F-83041 TOULON CEDEX 9, France

2 Formerly Ineris (French National Institute for Industrial Environment and Risks), BP 2, F-60550 Verneuil-en-Halatte, France

3 Consultant, Quartier Les Roux, F-13590 Meyreuil, France.

Corresponding author : patricia.merdy@univ-tln.fr

List of appendixes:

- Appendix 1: Average concentrations (mg/l) of the drains per year and per lysimeter

- Appendix 2: Quantities (mg/kg) of elements in the drains per year and per lysimeter

Appendix 1 : Average concentrations (mg/l) of drains per year and per lysimeter

Physico-chemical parameters

| Paramètre/Lysimètre | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 16 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| pH |  |  |  |  |  |  |  |  |  |
| year1 | 8.4 | 7.6 | 8.5 | 7.6 | 8.9 | 7.7 | 8.0 | 7.9 |  |
| year2 | 7.7 | 7.5 | 7.7 | 7.5 | 7.7 | 8.0 | 8.3 | 8.2 | 9.1 |
| year3 | 7.8 | 7.5 | 8.2 | 7.7 | 8.1 | 8.2 | 8.2 | 8.2 | 8.4 |
| year4 | 7.4 | 7.2 | 7.2 | 7.6 | 8.1 | 8.2 | 8.2 | 8.2 | 8.2 |
| year5 | 7.0 | 7.2 | 7.1 | 7.4 | 7.8 | 7.8 | 8.0 | 8.1 | 8.1 |
| EC (mS/cm) |  |  |  |  |  |  |  |  |  |
| year1 | 7.7 | 3.6 | 9.9 | 6.3 | 17.4 | 8.5 | 13.8 | 5.9 |  |
| year2 | 3.5 | 3.1 | 6.7 | 6.0 | 11.4 | 9.7 | 9.0 | 6.4 | 26.1 |
| year3 | 3.5 | 3.0 | 5.8 | 5.2 | 7.1 | 6.4 | 6.0 | 5.2 | 12.8 |
| year4 | 3.0 | 2.7 | 5.5 | 4.7 | 8.6 | 7.3 | 6.7 | 4.5 | 16.0 |
| year5 | 2.5 | 2.3 | 3.8 | 3.3 | 4.8 | 4.3 | 5.1 | 3.8 | 15.0 |
| pe |  |  |  |  |  |  |  |  |  |
| year1 | 3.3 | 3.4 | 3.3 | 3.3 | 3.2 | 3.3 | 3.6 | 4.0 |  |
| year2 | 4.0 | 4.0 | 3.8 | 3.7 | 3.8 | 3.8 | 4.5 | 4.6 | 3.4 |
| year3 | 5.5 | 5.7 | 5.4 | 5.7 | 5.5 | 5.5 | 5.4 | 5.5 | 4.4 |
| year4 | 5.4 | 5.2 | 5.2 | 5.2 | 5.1 | 5.1 | 5.1 | 5.1 | 5.9 |
| year5 | 6.0 | 5.9 | 5.8 | 5.8 | 5.6 | 5.6 | 5.5 | 5.6 | 6.8 |

Concentrations (if values >LQ are considered equal to 0)

| Elements (mg/l) / Lysimeter | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 16 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al | 1.24 | 0.17 | 1.46 | 0.11 | 1.41 | 0.12 | 0.12 | 2.29 |
| year1 | 1.42 | 0.19 | 1.56 | 0.13 | 1.81 | 0.14 | 0.13 |  |
| year2 | 1.00 | 0.08 | 1.54 | 0.08 | 0.14 | 0.08 |  | 2.46 |
| year3 | 0.85 | 0.48 | 1.86 | 0.27 |  |  |  | 1.42 |
| year4 | 0.63 | 0.05 | 0.53 | 0.04 | 0.02 | 0.03 | 0.01 | 0.79 |
| year5 | 0.24 |  | 0.29 | 0.03 |  |  | 0.20 | 0.73 |
| Si | 0.21 | 0.99 | 0.17 | 0.86 | 0.64 | 1.12 | 1.80 | 0.17 |
| year1 | 0.17 | 1.00 | 0.11 | 0.81 | 0.14 | 0.90 | 1.34 |  |
| year2 | 0.33 | 0.86 | 0.27 | 0.78 | 0.92 | 1.31 | 2.73 |  |
| year3 | 0.17 | 0.97 | 0.14 | 0.95 | 1.52 | 1.72 | 2.15 |  |
| year4 | 0.30 | 1.14 | 0.31 | 1.28 | 1.83 | 1.66 | 2.43 | 0.29 |
| year5 | 0.11 | 1.26 | 0.21 | 1.37 | 2.45 | 2.25 | 3.15 | 0.04 |
| Fe | 0.02 | 0.05 | 0.04 | 0.06 | 0.04 | 0.03 | 0.00 | 0.21 |
| year1 |  | 0.08 |  |  |  |  |  |  |
| year2 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 |  |  |
| year3 | 0.03 | 0.06 | 0.09 | 0.13 | 0.09 | 0.04 |  | 0.33 |
| year4 | 0.00 | 0.00 | 0.01 | 0.01 | 0.00 | 0.00 | 0.00 | 0.08 |
| year5 |  |  |  |  |  |  |  |  |
| Ca | 401 | 426 | 332 | 363 | 322 | 343 | 361 | 274 |
| year1 | 332 | 398 | 298 | 333 | 268 | 302 | 271 |  |
| year2 | 531 | 364 | 330 | 340 | 352 | 349 | 531 | 265 |
| year3 | 790 | 820 | 609 | 628 | 544 | 585 | 607 | 258 |
| year4 | 483 | 464 | 406 | 427 | 392 | 400 | 407 | 392 |
| year5 | 577 | 594 | 501 | 543 | 512 | 524 | 522 | 359 |
| Mn | 0.02 | 0.01 | 0.02 | 0.01 | 0.02 | 0.02 | 0.02 | 0.00 |
| year1 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 |  |
| year2 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |  |  |
| year3 | 0.00 | 0.00 |  | 0.00 |  |  |  | 0.00 |
| year4 |  | 0.00 |  | 0.00 |  |  |  | 0.00 |
| year5 |  |  |  |  |  |  |  |  |
| Mg | 0.5 | 41.7 | 0.7 | 41.5 | 5.0 | 49.0 | 17.1 | 0.2 |
| year1 | 0.3 | 49.7 | 0.2 | 44.2 | 0.3 | 35.5 | 14.5 |  |
| year2 | 0.2 | 29.6 | 0.1 | 35.2 | 3.7 | 107.2 | 25.7 |  |
| year3 | 0.8 | 18.6 | 0.4 | 31.8 | 19.3 | 67.7 | 18.4 | 0.1 |
| year4 | 1.8 | 13.4 | 1.8 | 41.9 | 20.2 | 79.4 | 17.5 | 0.4 |
| year5 | 1.9 | 9.6 | 4.4 | 28.5 | 24.8 | 44.9 | 25.5 |  |
| Na | 1393 | 486 | 2039 | 1291 | 2326 | 1853 | 2152 | 8202 |
| year1 | 1736 | 560 | 2302 | 1367 | 2294 | 1905 | 2474 |  |
| year2 | 710 | 373 | 1620 | 1346 | 3285 | 2276 | 2210 | 8595 |
| year3 | 497 | 315 | 1640 | 1222 | 2344 | 1702 | 1611 | 7331 |
| year4 | 294 | 178 | 921 | 701 | 1782 | 1312 | 1137 | 3835 |
| year5 | 283 | 205 | 870 | 640 | 1255 | 1079 | 1400 | 4409 |
| K | 31.1 | 7.7 | 37.5 | 20.4 | 64.3 | 41.7 | 45.1 | 66.0 |
| year1 | 40.1 | 8.8 | 45.0 | 20.8 | 80.8 | 44.2 | 58.8 |  |
| year2 | 12.0 | 4.1 | 14.1 | 14.8 | 34.8 | 39.9 | 19.7 | 44.0 |
| year3 | 9.7 | 8.9 | 43.4 | 42.8 | 57.6 | 67.5 | 40.0 | 395.9 |
| year4 | 2.3 | 2.5 | 7.5 | 8.4 | 10.1 | 12.0 | 7.2 | 61.0 |
| year5 | 4.7 | 5.8 | 19.2 | 20.8 | 19.8 | 18.5 | 17.5 | 136.6 |
| P | 0.02 | 0.02 | 0.01 | 0.01 | 0.01 | 0.01 | 0.02 | 0.02 |
| year1 |  |  | 0.01 | 0.01 |  |  |  |  |
| year2 | 0.02 | 0.02 |  | 0.01 | 0.02 | 0.02 |  | 0.02 |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  | 0.01 | 0.01 | 0.02 | 0.02 |
| year5 |  |  |  |  |  |  |  |  |
| S | 1545 | 812 | 1758 | 1557 | 2381 | 1635 | 2284 | 3724 |
| year1 | 1897 | 955 | 2114 | 1770 | 2848 | 1850 | 2993 |  |
| year2 | 1000 | 616 | 1121 | 1094 | 2334 | 1704 | 2241 | 3974 |
| year3 | 74 | 68 | 140 |  | 178 | 160 | 143 | 332 |
| year4 | 658 | 548 | 1319 | 958 | 1981 | 1627 | 1336 | 3830 |
| year5 | 270 | 264 | 382 | 356 | 412 | 403 | 450 | 1259 |
| As | 0.021 | 0.029 | 0.022 | 0.029 | 0.002 | 0.010 | 0.013 | 0.012 |
| year1 |  |  | 0.014 | 0.013 |  | 0.013 | 0.023 |  |
| year2 | 0.041 | 0.043 | 0.036 | 0.072 |  | 0.016 |  | 0.014 |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.001 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.006 |
| year5 |  |  |  |  |  |  |  |  |
| Cd |  | 0.008 | 0.008 | 0.009 | 0.005 | 0.003 | 0.009 | 0.000 |
| year1 |  | 0.008 | 0.008 | 0.009 | 0.005 | 0.005 | 0.009 |  |
| year2 |  | 0.008 |  | 0.010 |  |  |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  |  | 0.000 |  | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| Co | 0.004 | 0.005 | 0.007 | 0.004 | 0.002 | 0.003 | 0.004 | 0.005 |
| year1 | 0.005 | 0.006 | 0.007 | 0.003 | 0.004 | 0.004 | 0.004 |  |
| year2 | 0.003 | 0.003 |  | 0.004 | 0.002 | 0.004 |  | 0.005 |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  | 0.000 | 0.000 |  |  |
| year5 |  |  |  |  |  |  |  |  |
| Cr | 0.30 | 0.04 | 0.30 | 0.13 | 1.08 | 0.42 | 0.25 | 1.52 |
| year1 | 0.383 | 0.045 | 0.365 | 0.157 | 1.455 | 0.584 | 0.354 |  |
| year2 | 0.076 | 0.028 | 0.202 | 0.063 | 0.241 | 0.035 | 0.010 | 1.543 |
| year3 | 0.049 | 0.018 | 0.129 | 0.039 | 0.041 | 0.038 | 0.015 | 1.167 |
| year4 | 0.027 | 0.005 | 0.096 | 0.012 | 0.041 | 0.006 | 0.004 | 1.620 |
| year5 |  |  | 0.041 |  |  | 0.022 |  | 1.207 |
| Cu | 0.004 | 0.003 | 0.004 | 0.005 | 0.007 | 0.005 | 0.005 | 0.009 |
| year1 | 0.005 | 0.005 | 0.007 | 0.006 | 0.007 | 0.006 | 0.005 |  |
| year2 | 0.004 | 0.004 |  |  | 0.006 | 0.005 |  | 0.009 |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.001 | 0.001 | 0.002 | 0.005 | 0.005 | 0.005 | 0.003 | 0.003 |
| year5 |  |  |  |  |  |  |  |  |
| Mo | 0.133 | 0.045 | 0.178 | 0.096 | 0.291 | 0.091 | 0.067 | 0.812 |
| year1 | 0.180 | 0.051 | 0.225 | 0.098 | 0.424 | 0.113 | 0.073 |  |
| year2 | 0.023 | 0.041 | 0.089 | 0.124 | 0.043 | 0.029 | 0.061 | 0.879 |
| year3 | 0.012 | 0.021 | 0.035 | 0.063 | 0.009 | 0.030 | 0.040 | 0.424 |
| year4 | 0.007 | 0.017 | 0.024 | 0.055 | 0.016 | 0.047 | 0.050 | 0.273 |
| year5 | 0.011 | 0.014 | 0.032 | 0.051 | 0.016 | 0.051 | 0.068 | 0.190 |
| Ni | 0.000 | 0.005 | 0.000 | 0.003 | 0.004 | 0.005 | 0.006 | 0.000 |
| year1 |  | 0.010 |  | 0.006 | 0.008 | 0.009 | 0.010 |  |
| year2 |  |  |  |  |  |  |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.001 | 0.001 | 0.001 | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| Pb | 0.109 | 0.113 | 0.117 | 0.116 | 0.117 | 0.116 | 0.137 | 0.000 |
| year1 | 0.134 | 0.139 | 0.144 | 0.143 | 0.145 | 0.143 | 0.137 |  |
| year2 | 0.035 | 0.035 | 0.035 | 0.035 | 0.035 | 0.035 |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  |  |  |  | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| V | 0.070 | 0.036 | 0.104 | 0.039 | 0.066 | 0.035 | 0.019 | 0.075 |
| year1 | 0.069 | 0.028 | 0.104 | 0.034 | 0.078 | 0.035 | 0.014 |  |
| year2 | 0.064 | 0.061 | 0.123 | 0.064 | 0.067 | 0.031 | 0.020 | 0.074 |
| year3 | 0.052 | 0.034 | 0.078 | 0.029 | 0.013 | 0.023 | 0.018 | 0.049 |
| year4 | 0.088 | 0.052 | 0.103 | 0.042 | 0.025 | 0.038 | 0.032 | 0.089 |
| year5 | 0.090 | 0.069 | 0.074 | 0.054 | 0.038 | 0.052 | 0.039 | 0.108 |
| Sb | 0.000 |  | 0.000 | 0.000 | 0.001 | 0.000 | 0.000 |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.000 |  | 0.000 | 0.000 | 0.001 | 0.000 | 0.000 |  |
| year5 |  |  |  |  |  |  |  |  |
| Se | 0.015 | 0.009 | 0.053 | 0.040 | 0.062 | 0.043 | 0.035 | 0.444 |
| year3 |  |  |  |  | 0.052 |  |  | 0.264 |
| year4 | 0.015 | 0.009 | 0.053 | 0.040 | 0.073 | 0.043 | 0.035 | 0.480 |
| year5 |  |  |  |  | 0.061 |  |  | 0.588 |
| Zn | 0.571 | 0.537 | 0.614 | 0.541 | 0.404 | 0.050 | 0.025 | 0.003 |
| year1 | 0.779 | 0.715 | 0.775 | 0.718 | 0.505 | 0.071 | 0.049 |  |
| year2 | 0.095 | 0.078 | 0.116 | 0.078 |  |  |  |  |
| year3 | 0.011 |  |  |  |  |  |  |  |
| year4 | 0.002 | 0.024 | 0.002 | 0.063 | 0.003 | 0.015 | 0.002 | 0.003 |
| year5 |  | 0.010 |  | 0.008 |  | 0.019 |  |  |
| Ce |  |  |  |  |  |  |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  |  |  |  |  |
| year5 |  |  |  |  |  |  |  |  |

Concentrations (if values >LQ are considered equal to LQ)

| Elements (mg/l) / Lysimeter | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 16 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al | 1.24 | 0.11 | 1.46 | 0.10 | 1.23 | 0.09 | 0.09 | 2.29 |
| year1 | 1.42 | 0.10 | 1.56 | 0.10 | 1.81 | 0.11 | 0.09 |  |
| year2 | 1.00 | 0.08 | 1.54 | 0.08 | 0.14 | 0.08 | 0.08 | 2.46 |
| year3 | 0.85 | 0.48 | 1.86 | 0.27 | 0.03 | 0.03 | 0.03 | 1.42 |
| year4 | 0.63 | 0.05 | 0.53 | 0.04 | 0.02 | 0.03 | 0.01 | 0.79 |
| year5 | 0.24 | 0.02 | 0.29 | 0.03 | 0.02 | 0.02 | 0.20 | 0.73 |
| Si | 0.11 | 0.99 | 0.11 | 0.86 | 0.59 | 1.12 | 1.80 | 0.03 |
| year1 | 0.08 | 1.00 | 0.06 | 0.81 | 0.13 | 0.90 | 1.34 |  |
| year2 | 0.23 | 0.86 | 0.27 | 0.78 | 0.92 | 1.31 | 2.73 | 0.01 |
| year3 | 0.17 | 0.97 | 0.14 | 0.95 | 1.52 | 1.72 | 2.15 | 0.09 |
| year4 | 0.30 | 1.14 | 0.31 | 1.28 | 1.83 | 1.66 | 2.43 | 0.29 |
| year5 | 0.11 | 1.26 | 0.21 | 1.37 | 2.45 | 2.25 | 3.15 | 0.04 |
| Fe | 0.03 | 0.04 | 0.04 | 0.04 | 0.04 | 0.03 | 0.03 | 0.05 |
| year1 | 0.03 | 0.04 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 |  |
| year2 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 |
| year3 | 0.03 | 0.06 | 0.09 | 0.13 | 0.09 | 0.04 | 0.01 | 0.33 |
| year4 | 0.00 | 0.00 | 0.01 | 0.01 | 0.00 | 0.00 | 0.00 | 0.08 |
| year5 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 |
| Ca | 401 | 426 | 332 | 363 | 322 | 343 | 361 | 274 |
| year1 | 332 | 398 | 298 | 333 | 268 | 302 | 271 |  |
| year2 | 531 | 364 | 330 | 340 | 352 | 349 | 531 | 265 |
| year3 | 790 | 820 | 609 | 628 | 544 | 585 | 607 | 258 |
| year4 | 483 | 464 | 406 | 427 | 392 | 400 | 407 | 392 |
| year5 | 577 | 594 | 501 | 543 | 512 | 524 | 522 | 359 |
| Mn | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.00 |
| year1 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 |  |
| year2 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| year3 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| year4 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| year5 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| Mg | 0.3 | 41.7 | 0.4 | 41.5 | 5.0 | 49.0 | 17.1 | 0.0 |
| year1 | 0.1 | 49.7 | 0.1 | 44.2 | 0.3 | 35.5 | 14.5 |  |
| year2 | 0.1 | 29.6 | 0.1 | 35.2 | 3.7 | 107.2 | 25.7 | 0.0 |
| year3 | 0.8 | 18.6 | 0.4 | 31.8 | 19.3 | 67.7 | 18.4 | 0.1 |
| year4 | 1.8 | 13.4 | 1.8 | 41.9 | 20.2 | 79.4 | 17.5 | 0.4 |
| year5 | 1.9 | 9.6 | 4.4 | 28.5 | 24.8 | 44.9 | 25.5 | 0.0 |
| Na | 1393 | 486 | 2039 | 1291 | 2326 | 1853 | 2152 | 8202 |
| year1 | 1736 | 560 | 2302 | 1367 | 2294 | 1905 | 2474 |  |
| year2 | 710 | 373 | 1620 | 1346 | 3285 | 2276 | 2210 | 8595 |
| year3 | 497 | 315 | 1640 | 1222 | 2344 | 1702 | 1611 | 7331 |
| year4 | 294 | 178 | 921 | 701 | 1782 | 1312 | 1137 | 3835 |
| year5 | 283 | 205 | 870 | 640 | 1255 | 1079 | 1400 | 4409 |
| K | 31.1 | 7.7 | 37.5 | 20.4 | 64.3 | 41.7 | 45.1 | 53.4 |
| year1 | 40.1 | 8.8 | 45.0 | 20.8 | 80.8 | 44.2 | 58.8 |  |
| year2 | 12.0 | 4.1 | 14.1 | 14.8 | 34.8 | 39.9 | 19.7 | 34.6 |
| year3 | 9.7 | 8.9 | 43.4 | 42.8 | 57.6 | 67.5 | 40.0 | 395.9 |
| year4 | 2.3 | 2.5 | 7.5 | 8.4 | 10.1 | 12.0 | 7.2 | 61.0 |
| year5 | 4.7 | 5.8 | 19.2 | 20.8 | 19.8 | 18.5 | 17.5 | 136.6 |
| P | 0.02 | 0.02 | 0.01 | 0.01 | 0.02 | 0.02 | 0.02 | 0.02 |
| year1 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 |  |
| year2 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.02 |
| year3 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 |
| year4 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.02 | 0.02 |
| year5 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 |
| S | 1545 | 812 | 1758 | 1483 | 2381 | 1635 | 2284 | 3724 |
| year1 | 1897 | 955 | 2114 | 1770 | 2848 | 1850 | 2993 |  |
| year2 | 1000 | 616 | 1121 | 1094 | 2334 | 1704 | 2241 | 3974 |
| year3 | 74 | 68 | 140 | 0 | 178 | 160 | 143 | 332 |
| year4 | 658 | 548 | 1319 | 958 | 1981 | 1627 | 1336 | 3830 |
| year5 | 270 | 264 | 382 | 356 | 412 | 403 | 450 | 1259 |
| As | 0.014 | 0.015 | 0.015 | 0.015 | 0.012 | 0.012 | 0.013 | 0.013 |
| year1 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.014 |  |
| year2 | 0.022 | 0.033 | 0.028 | 0.032 | 0.012 | 0.014 | 0.012 | 0.013 |
| year3 | 0.015 | 0.015 | 0.015 | 0.015 | 0.015 | 0.015 | 0.015 | 0.015 |
| year4 | 0.001 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.006 |
| year5 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 |
| Cd | 0.004 | 0.004 | 0.004 | 0.005 | 0.004 | 0.004 | 0.004 | 0.004 |
| year1 | 0.004 | 0.004 | 0.004 | 0.004 | 0.004 | 0.004 | 0.005 |  |
| year2 | 0.004 | 0.005 | 0.004 | 0.006 | 0.004 | 0.004 | 0.004 | 0.004 |
| year3 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.009 | 0.009 | 0.009 | 0.009 | 0.009 | 0.009 | 0.009 | 0.009 |
| Co | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.004 |
| year1 | 0.002 | 0.002 | 0.003 | 0.002 | 0.002 | 0.002 | 0.003 |  |
| year2 | 0.002 | 0.002 | 0.002 | 0.004 | 0.002 | 0.003 | 0.002 | 0.004 |
| year3 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 | 0.002 |
| Cr | 0.29 | 0.04 | 0.30 | 0.12 | 1.01 | 0.42 | 0.23 | 1.52 |
| year1 | 0.383 | 0.045 | 0.365 | 0.157 | 1.455 | 0.584 | 0.354 |  |
| year2 | 0.076 | 0.020 | 0.202 | 0.063 | 0.241 | 0.035 | 0.010 | 1.543 |
| year3 | 0.049 | 0.018 | 0.129 | 0.039 | 0.041 | 0.038 | 0.015 | 1.167 |
| year4 | 0.027 | 0.005 | 0.096 | 0.012 | 0.041 | 0.006 | 0.004 | 1.620 |
| year5 | 0.011 | 0.011 | 0.041 | 0.011 | 0.011 | 0.022 | 0.011 | 1.207 |
| Cu | 0.004 | 0.004 | 0.004 | 0.004 | 0.005 | 0.004 | 0.004 | 0.009 |
| year1 | 0.004 | 0.004 | 0.004 | 0.004 | 0.005 | 0.004 | 0.004 |  |
| year2 | 0.004 | 0.004 | 0.003 | 0.003 | 0.005 | 0.004 | 0.003 | 0.009 |
| year3 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 |
| year4 | 0.001 | 0.001 | 0.002 | 0.005 | 0.005 | 0.005 | 0.003 | 0.003 |
| year5 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 | 0.003 |
| Mo | 0.133 | 0.045 | 0.178 | 0.096 | 0.291 | 0.091 | 0.067 | 0.812 |
| year1 | 0.180 | 0.051 | 0.225 | 0.098 | 0.424 | 0.113 | 0.073 |  |
| year2 | 0.023 | 0.041 | 0.089 | 0.124 | 0.043 | 0.029 | 0.061 | 0.879 |
| year3 | 0.012 | 0.021 | 0.035 | 0.063 | 0.009 | 0.030 | 0.040 | 0.424 |
| year4 | 0.007 | 0.017 | 0.024 | 0.055 | 0.016 | 0.047 | 0.050 | 0.273 |
| year5 | 0.011 | 0.014 | 0.032 | 0.051 | 0.016 | 0.051 | 0.068 | 0.190 |
| Ni | 0.006 | 0.006 | 0.006 | 0.006 | 0.007 | 0.006 | 0.007 | 0.006 |
| year1 | 0.005 | 0.006 | 0.005 | 0.005 | 0.006 | 0.006 | 0.006 |  |
| year2 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 |
| year3 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.001 | 0.001 | 0.001 | 0.000 |
| year5 | 0.011 | 0.011 | 0.011 | 0.011 | 0.011 | 0.011 | 0.011 | 0.011 |
| Pb | 0.046 | 0.047 | 0.048 | 0.048 | 0.053 | 0.051 | 0.058 | 0.033 |
| year1 | 0.054 | 0.055 | 0.056 | 0.056 | 0.068 | 0.062 | 0.078 |  |
| year2 | 0.035 | 0.035 | 0.035 | 0.035 | 0.035 | 0.035 | 0.035 | 0.035 |
| year3 | 0.033 | 0.033 | 0.033 | 0.033 | 0.033 | 0.033 | 0.033 | 0.033 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.019 | 0.019 | 0.019 | 0.019 | 0.019 | 0.019 | 0.019 | 0.019 |
| V | 0.070 | 0.036 | 0.104 | 0.039 | 0.066 | 0.035 | 0.019 | 0.075 |
| year1 | 0.069 | 0.028 | 0.104 | 0.034 | 0.078 | 0.035 | 0.014 |  |
| year2 | 0.064 | 0.061 | 0.123 | 0.064 | 0.067 | 0.031 | 0.020 | 0.074 |
| year3 | 0.052 | 0.034 | 0.078 | 0.029 | 0.013 | 0.023 | 0.018 | 0.049 |
| year4 | 0.088 | 0.052 | 0.103 | 0.042 | 0.025 | 0.038 | 0.032 | 0.089 |
| year5 | 0.090 | 0.069 | 0.074 | 0.054 | 0.038 | 0.052 | 0.039 | 0.108 |
| Sb | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 |
| year3 | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.001 | 0.000 | 0.000 | 0.000 |
| year5 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 |
| Se | 0.037 | 0.035 | 0.050 | 0.045 | 0.062 | 0.046 | 0.044 | 0.444 |
| year3 | 0.049 | 0.049 | 0.049 | 0.049 | 0.052 | 0.049 | 0.049 | 0.264 |
| year4 | 0.015 | 0.009 | 0.053 | 0.040 | 0.073 | 0.043 | 0.035 | 0.480 |
| year5 | 0.046 | 0.046 | 0.046 | 0.046 | 0.061 | 0.046 | 0.046 | 0.588 |
| Zn | 0.391 | 0.393 | 0.391 | 0.396 | 0.156 | 0.039 | 0.030 | 0.034 |
| year1 | 0.531 | 0.534 | 0.529 | 0.536 | 0.224 | 0.046 | 0.039 |  |
| year2 | 0.076 | 0.065 | 0.090 | 0.064 | 0.037 | 0.037 | 0.037 | 0.037 |
| year3 | 0.011 | 0.006 | 0.006 | 0.006 | 0.006 | 0.006 | 0.006 | 0.006 |
| year4 | 0.002 | 0.024 | 0.002 | 0.063 | 0.003 | 0.015 | 0.002 | 0.003 |
| year5 | 0.008 | 0.010 | 0.008 | 0.008 | 0.008 | 0.019 | 0.008 | 0.008 |
| Ce | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 | 0.023 |
| year3 | 0.052 | 0.052 | 0.052 | 0.052 | 0.052 | 0.052 | 0.052 | 0.052 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 | 0.018 |

Appendix 2 : Quantities (mg/kg) of elements in the drains per year and per lysimeter

Mass used: 24 kg (of MBR or UMBR) for lysimeters 1 to 8 ;  45.49 kg of mining residue for lysimeters 9, 10 and 11 ; 37.44 kg of mining residue for lysimeters 12, 13 and 14 ; 50.23 kg for the lysimeter 15 and 1087 kg for the lysimeter 16.

In bold: cumulative quantity over 5 or 4 years

Quantity (if values > LQ are considered equal to 0)

| Elements (mg/l) / Lysimeter | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 16 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Métaux |  |  |  |  |  |  |  |  |
| Al | 8.0 | 1.0 | 6.8 | 0.5 | 3.4 | 0.2 | 0.2 | 0.7 |
| year1 | 4.1 | 0.2 | 3.7 | 0.2 | 3.4 | 0.2 | 0.1 |  |
| year2 | 1.3 | 0.1 | 0.8 | 0.0 | 0.0 | 0.0 |  | 0.3 |
| year3 | 1.1 | 0.6 | 1.5 | 0.2 |  |  |  | 0.2 |
| year4 | 1.0 | 0.1 | 0.4 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year5 | 0.5 |  | 0.4 | 0.0 |  |  | 0.1 | 0.1 |
| Si | 1.4 | 8.8 | 1.1 | 6.3 | 6.2 | 6.6 | 5.2 | 0.0 |
| year1 | 0.3 | 2.4 | 0.2 | 1.9 | 0.3 | 1.6 | 1.2 |  |
| year2 | 0.2 | 1.0 | 0.2 | 0.4 | 0.3 | 0.4 | 0.2 |  |
| year3 | 0.2 | 1.2 | 0.1 | 0.7 | 1.0 | 1.1 | 1.1 |  |
| year4 | 0.5 | 1.6 | 0.2 | 1.0 | 0.5 | 0.3 | 0.3 | 0.0 |
| year5 | 0.2 | 2.5 | 0.3 | 2.2 | 4.2 | 3.1 | 2.4 | 0.0 |
| Fe | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.0 | 0.0 | 0.1 |
| year1 |  | 0.0 |  |  |  |  |  |  |
| year2 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |  |  |
| year3 | 0.0 | 0.1 | 0.1 | 0.1 | 0.1 | 0.0 |  | 0.1 |
| year4 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year5 |  |  |  |  |  |  |  |  |
| Ca | 4538 | 4321 | 2479 | 2674 | 1968 | 2008 | 1097 | 138 |
| year1 | 931 | 1021 | 711 | 792 | 537 | 707 | 300 |  |
| year2 | 575 | 406 | 188 | 199 | 101 | 116 | 32 | 25 |
| year3 | 1002 | 1037 | 500 | 469 | 345 | 385 | 321 | 44 |
| year4 | 754 | 663 | 303 | 347 | 99 | 74 | 47 | 13 |
| year5 | 1277 | 1194 | 777 | 867 | 885 | 726 | 397 | 57 |
| Mn | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year1 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |  |
| year2 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |  |  |
| year3 | 0.0 | 0.0 |  | 0.0 |  |  |  | 0.0 |
| year4 |  | 0.0 |  | 0.0 |  |  |  | 0.0 |
| year5 |  |  |  |  |  |  |  |  |
| Mg | 8.6 | 202.3 | 8.9 | 217.2 | 61.9 | 225.5 | 49.9 | 0.0 |
| year1 | 0.5 | 107.3 | 0.4 | 92.0 | 0.5 | 68.5 | 17.2 |  |
| year2 | 0.2 | 33.2 | 0.0 | 21.8 | 1.1 | 35.4 | 1.5 |  |
| year3 | 1.0 | 23.5 | 0.3 | 23.8 | 12.2 | 44.6 | 9.7 | 0.0 |
| year4 | 2.8 | 19.1 | 1.4 | 34.1 | 5.1 | 14.8 | 2.0 | 0.0 |
| year5 | 4.2 | 19.3 | 6.8 | 45.5 | 42.9 | 62.2 | 19.4 |  |
| Na | 5822 | 2599 | 9596 | 6876 | 8519 | 6898 | 4518 | 2903 |
| year1 | 3266 | 1087 | 5264 | 3553 | 3479 | 3290 | 2336 |  |
| year2 | 840 | 447 | 948 | 817 | 930 | 749 | 133 | 827 |
| year3 | 631 | 398 | 1347 | 913 | 1489 | 1120 | 853 | 1253 |
| year4 | 459 | 254 | 687 | 570 | 452 | 244 | 132 | 127 |
| year5 | 626 | 412 | 1350 | 1022 | 2168 | 1494 | 1065 | 696 |
| K | 104 | 47 | 179 | 136 | 163 | 145 | 73 | 94 |
| year1 | 65.1 | 15.6 | 99.1 | 54.9 | 79.3 | 59.6 | 36.9 |  |
| year2 | 12.4 | 4.5 | 8.8 | 9.5 | 10.0 | 13.2 | 1.2 | 2.9 |
| year3 | 12.2 | 11.2 | 35.7 | 32.0 | 36.6 | 44.4 | 21.2 | 67.7 |
| year4 | 3.6 | 3.6 | 5.6 | 6.8 | 2.6 | 2.2 | 0.8 | 2.0 |
| year5 | 10.4 | 11.7 | 29.8 | 33.3 | 34.3 | 25.6 | 13.3 | 21.6 |
| P | 0.01 | 0.00 | 0.00 | 0.01 | 0.00 | 0.00 | 0.00 | 0.00 |
| year1 |  |  | 0.00 | 0.00 |  |  |  |  |
| year2 | 0.01 | 0.00 |  | 0.00 | 0.00 | 0.00 |  | 0.00 |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  | 0.00 | 0.00 | 0.00 | 0.00 |
| year5 |  |  |  |  |  |  |  |  |
| S | 7133 | 4333 | 7434 | 6282 | 6449 | 5361 | 3799 | 756 |
| year1 | 4254 | 2240 | 5096 | 4282 | 4451 | 3831 | 3092 |  |
| year2 | 1163 | 694 | 647 | 652 | 670 | 564 | 134 | 374 |
| year3 | 94 | 86 | 115 |  | 113 | 106 | 76 | 57 |
| year4 | 1025 | 783 | 983 | 778 | 503 | 302 | 155 | 127 |
| year5 | 598 | 530 | 593 | 569 | 712 | 558 | 342 | 199 |
| As | 0.023 | 0.040 | 0.017 | 0.014 | 0.001 | 0.008 | 0.001 | 0.000 |
| year1 |  |  | 0.005 | 0.003 |  | 0.005 | 0.001 |  |
| year2 | 0.021 | 0.038 | 0.011 | 0.010 |  | 0.003 |  | 0.000 |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.002 | 0.002 | 0.001 | 0.001 | 0.001 | 0.000 | 0.000 | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| Cd |  | 0.009 | 0.002 | 0.003 | 0.001 | 0.002 | 0.000 | 0.000 |
| year1 |  | 0.005 | 0.002 | 0.002 | 0.001 | 0.002 | 0.000 |  |
| year2 |  | 0.004 |  | 0.001 |  |  |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  |  | 0.000 |  | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| Co | 0.003 | 0.007 | 0.003 | 0.003 | 0.003 | 0.002 | 0.001 | 0.000 |
| year1 | 0.002 | 0.006 | 0.003 | 0.001 | 0.002 | 0.001 | 0.001 |  |
| year2 | 0.001 | 0.001 |  | 0.002 | 0.000 | 0.001 |  | 0.000 |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  | 0.000 | 0.000 |  |  |
| year5 |  |  |  |  |  |  |  |  |
| Cr | 0.833 | 0.153 | 1.129 | 0.477 | 1.605 | 0.910 | 0.247 | 0.590 |
| year1 | 0.633 | 0.098 | 0.774 | 0.401 | 1.500 | 0.842 | 0.238 |  |
| year2 | 0.096 | 0.024 | 0.113 | 0.037 | 0.069 | 0.011 | 0.001 | 0.146 |
| year3 | 0.062 | 0.023 | 0.106 | 0.029 | 0.026 | 0.025 | 0.008 | 0.199 |
| year4 | 0.042 | 0.008 | 0.072 | 0.010 | 0.011 | 0.001 | 0.000 | 0.054 |
| year5 |  |  | 0.064 |  |  | 0.031 |  | 0.190 |
| Cu | 0.008 | 0.007 | 0.003 | 0.005 | 0.006 | 0.003 | 0.002 | 0.001 |
| year1 | 0.005 | 0.003 | 0.002 | 0.001 | 0.004 | 0.002 | 0.002 |  |
| year2 | 0.002 | 0.002 |  |  | 0.001 | 0.001 |  | 0.001 |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.002 | 0.002 | 0.001 | 0.004 | 0.001 | 0.001 | 0.000 | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| Mo | 0.403 | 0.252 | 0.618 | 0.491 | 0.399 | 0.295 | 0.128 | 0.195 |
| year1 | 0.323 | 0.123 | 0.473 | 0.247 | 0.349 | 0.186 | 0.046 |  |
| year2 | 0.029 | 0.051 | 0.050 | 0.071 | 0.012 | 0.010 | 0.004 | 0.083 |
| year3 | 0.016 | 0.027 | 0.028 | 0.047 | 0.006 | 0.020 | 0.021 | 0.073 |
| year4 | 0.010 | 0.024 | 0.018 | 0.045 | 0.004 | 0.009 | 0.006 | 0.009 |
| year5 | 0.025 | 0.028 | 0.049 | 0.081 | 0.028 | 0.071 | 0.052 | 0.030 |
| Ni | 0.000 | 0.006 | 0.000 | 0.002 | 0.002 | 0.003 | 0.001 | 0.000 |
| year1 |  | 0.006 |  | 0.001 | 0.002 | 0.003 | 0.000 |  |
| year2 |  |  |  |  |  |  |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| Pb | 0.189 | 0.188 | 0.137 | 0.136 | 0.139 | 0.154 | 0.080 | 0.000 |
| year1 | 0.177 | 0.177 | 0.127 | 0.125 | 0.134 | 0.148 | 0.080 |  |
| year2 | 0.012 | 0.010 | 0.010 | 0.010 | 0.005 | 0.006 |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  |  |  |  | 0.000 |
| year5 |  |  |  |  |  |  |  |  |
| V | 0.654 | 0.399 | 0.570 | 0.266 | 0.240 | 0.179 | 0.057 | 0.036 |
| year1 | 0.169 | 0.072 | 0.245 | 0.083 | 0.143 | 0.074 | 0.013 |  |
| year2 | 0.081 | 0.070 | 0.070 | 0.040 | 0.018 | 0.010 | 0.001 | 0.007 |
| year3 | 0.066 | 0.044 | 0.064 | 0.021 | 0.008 | 0.015 | 0.009 | 0.008 |
| year4 | 0.137 | 0.074 | 0.077 | 0.034 | 0.006 | 0.007 | 0.004 | 0.003 |
| year5 | 0.200 | 0.139 | 0.114 | 0.087 | 0.065 | 0.072 | 0.030 | 0.017 |
| Sb | 0.000 |  | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 | 0.000 |  | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |  |
| year5 |  |  |  |  |  |  |  |  |
| Se | 0.024 | 0.012 | 0.040 | 0.032 | 0.157 | 0.008 | 0.004 | 0.154 |
| year3 |  |  |  |  | 0.033 |  |  | 0.045 |
| year4 | 0.024 | 0.012 | 0.040 | 0.032 | 0.019 | 0.008 | 0.004 | 0.016 |
| year5 |  |  |  |  | 0.106 |  |  | 0.093 |
| Zn | 0.898 | 0.877 | 0.803 | 0.904 | 0.086 | 0.087 | 0.014 | 0.000 |
| year1 | 0.797 | 0.752 | 0.755 | 0.813 | 0.085 | 0.059 | 0.014 |  |
| year2 | 0.084 | 0.071 | 0.047 | 0.027 |  |  |  |  |
| year3 | 0.014 |  |  |  |  |  |  |  |
| year4 | 0.003 | 0.034 | 0.002 | 0.051 | 0.001 | 0.003 | 0.000 | 0.000 |
| year5 |  | 0.021 |  | 0.013 |  | 0.026 |  |  |
| Ce |  |  |  |  |  |  |  |  |
| year3 |  |  |  |  |  |  |  |  |
| year4 |  |  |  |  |  |  |  |  |
| year5 |  |  |  |  |  |  |  |  |

Quantity (if values > LQ are considered equal to LQ)

| Element (mg/kg) / Lysimeter | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 16 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Element |  |  |  |  |  |  |  |  |
| Al | 8.0 | 1.2 | 6.8 | 0.6 | 3.5 | 0.4 | 0.3 | 0.7 |
| year1 | 4.1 | 0.3 | 3.7 | 0.3 | 3.4 | 0.3 | 0.1 |  |
| year2 | 1.3 | 0.1 | 0.8 | 0.0 | 0.0 | 0.0 | 0.0 | 0.3 |
| year3 | 1.1 | 0.6 | 1.5 | 0.2 | 0.0 | 0.0 | 0.0 | 0.2 |
| year4 | 1.0 | 0.1 | 0.4 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year5 | 0.5 | 0.0 | 0.4 | 0.0 | 0.0 | 0.0 | 0.1 | 0.1 |
| Si | 1.4 | 8.8 | 1.1 | 6.3 | 6.2 | 6.6 | 5.2 | 0.0 |
| year1 | 0.3 | 2.4 | 0.2 | 1.9 | 0.3 | 1.6 | 1.2 |  |
| year2 | 0.2 | 1.0 | 0.2 | 0.4 | 0.3 | 0.4 | 0.2 | 0.0 |
| year3 | 0.2 | 1.2 | 0.1 | 0.7 | 1.0 | 1.1 | 1.1 | 0.0 |
| year4 | 0.5 | 1.6 | 0.2 | 1.0 | 0.5 | 0.3 | 0.3 | 0.0 |
| year5 | 0.2 | 2.5 | 0.3 | 2.2 | 4.2 | 3.1 | 2.4 | 0.0 |
| Fe | 0.2 | 0.3 | 0.2 | 0.2 | 0.2 | 0.1 | 0.1 | 0.1 |
| year1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.0 |  |
| year2 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year3 | 0.0 | 0.1 | 0.1 | 0.1 | 0.1 | 0.0 | 0.0 | 0.1 |
| year4 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year5 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| Ca | 4538 | 4321 | 2479 | 2674 | 1968 | 2008 | 1097 | 138 |
| year1 | 931 | 1021 | 711 | 792 | 537 | 707 | 300 |  |
| year2 | 575 | 406 | 188 | 199 | 101 | 116 | 32 | 25 |
| year3 | 1002 | 1037 | 500 | 469 | 345 | 385 | 321 | 44 |
| year4 | 754 | 663 | 303 | 347 | 99 | 74 | 47 | 13 |
| year5 | 1277 | 1194 | 777 | 867 | 885 | 726 | 397 | 57 |
| Mn | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year1 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |  |
| year2 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year3 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year4 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| year5 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
| Mg | 8.6 | 202.3 | 8.9 | 217.2 | 61.9 | 225.5 | 49.9 | 0.0 |
| year1 | 0.5 | 107.3 | 0.4 | 92.0 | 0.5 | 68.5 | 17.2 |  |
| year2 | 0.2 | 33.2 | 0.0 | 21.8 | 1.1 | 35.4 | 1.5 | 0.0 |
| year3 | 1.0 | 23.5 | 0.3 | 23.8 | 12.2 | 44.6 | 9.7 | 0.0 |
| year4 | 2.8 | 19.1 | 1.4 | 34.1 | 5.1 | 14.8 | 2.0 | 0.0 |
| year5 | 4.2 | 19.3 | 6.8 | 45.5 | 42.9 | 62.2 | 19.4 | 0.0 |
| Na | 5822 | 2599 | 9596 | 6876 | 8519 | 6898 | 4518 | 2903 |
| year1 | 3266 | 1087 | 5264 | 3553 | 3479 | 3290 | 2336 |  |
| year2 | 840 | 447 | 948 | 817 | 930 | 749 | 133 | 827 |
| year3 | 631 | 398 | 1347 | 913 | 1489 | 1120 | 853 | 1253 |
| year4 | 459 | 254 | 687 | 570 | 452 | 244 | 132 | 127 |
| year5 | 626 | 412 | 1350 | 1022 | 2168 | 1494 | 1065 | 696 |
| K | 104 | 47 | 179 | 136 | 163 | 145 | 73 | 94 |
| year1 | 65.1 | 15.6 | 99.1 | 54.9 | 79.3 | 59.6 | 36.9 |  |
| year2 | 12.4 | 4.5 | 8.8 | 9.5 | 10.0 | 13.2 | 1.2 | 2.9 |
| year3 | 12.2 | 11.2 | 35.7 | 32.0 | 36.6 | 44.4 | 21.2 | 67.7 |
| year4 | 3.6 | 3.6 | 5.6 | 6.8 | 2.6 | 2.2 | 0.8 | 2.0 |
| year5 | 10.4 | 11.7 | 29.8 | 33.3 | 34.3 | 25.6 | 13.3 | 21.6 |
| P | 0.14 | 0.13 | 0.09 | 0.09 | 0.09 | 0.08 | 0.05 | 0.01 |
| year1 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 | 0.00 |  |
| year2 | 0.01 | 0.01 | 0.01 | 0.01 | 0.00 | 0.00 | 0.00 | 0.00 |
| year3 | 0.03 | 0.03 | 0.02 | 0.02 | 0.02 | 0.02 | 0.01 | 0.00 |
| year4 | 0.01 | 0.01 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| year5 | 0.07 | 0.07 | 0.05 | 0.05 | 0.06 | 0.05 | 0.03 | 0.01 |
| S | 7133 | 4333 | 7434 | 6282 | 6449 | 5361 | 3799 | 756 |
| year1 | 4254 | 2240 | 5096 | 4282 | 4451 | 3831 | 3092 |  |
| year2 | 1163 | 694 | 647 | 652 | 670 | 564 | 134 | 374 |
| year3 | 94 | 86 | 115 | 0 | 113 | 106 | 76 | 57 |
| year4 | 1025 | 783 | 983 | 778 | 503 | 302 | 155 | 127 |
| year5 | 598 | 530 | 593 | 569 | 712 | 558 | 342 | 199 |
| As | 0.123 | 0.131 | 0.084 | 0.087 | 0.066 | 0.067 | 0.036 | 0.007 |
| year1 | 0.033 | 0.032 | 0.030 | 0.030 | 0.022 | 0.027 | 0.013 |  |
| year2 | 0.029 | 0.042 | 0.013 | 0.016 | 0.004 | 0.005 | 0.001 | 0.001 |
| year3 | 0.019 | 0.019 | 0.012 | 0.011 | 0.009 | 0.010 | 0.008 | 0.003 |
| year4 | 0.002 | 0.002 | 0.001 | 0.001 | 0.001 | 0.000 | 0.000 | 0.000 |
| year5 | 0.040 | 0.036 | 0.028 | 0.029 | 0.031 | 0.025 | 0.014 | 0.003 |
| Cd | 0.040 | 0.041 | 0.029 | 0.031 | 0.026 | 0.025 | 0.013 | 0.002 |
| year1 | 0.011 | 0.013 | 0.010 | 0.011 | 0.007 | 0.009 | 0.004 |  |
| year2 | 0.005 | 0.006 | 0.002 | 0.003 | 0.001 | 0.001 | 0.000 | 0.000 |
| year3 | 0.003 | 0.003 | 0.002 | 0.002 | 0.002 | 0.002 | 0.001 | 0.000 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.021 | 0.019 | 0.014 | 0.015 | 0.016 | 0.013 | 0.007 | 0.001 |
| Co | 0.017 | 0.019 | 0.013 | 0.012 | 0.010 | 0.010 | 0.006 | 0.001 |
| year1 | 0.006 | 0.009 | 0.007 | 0.005 | 0.005 | 0.005 | 0.003 |  |
| year2 | 0.003 | 0.003 | 0.001 | 0.002 | 0.001 | 0.001 | 0.000 | 0.000 |
| year3 | 0.004 | 0.004 | 0.002 | 0.002 | 0.002 | 0.002 | 0.001 | 0.000 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.004 | 0.003 | 0.003 | 0.003 | 0.003 | 0.002 | 0.001 | 0.000 |
| Cr | 0.858 | 0.177 | 1.129 | 0.495 | 1.624 | 0.910 | 0.256 | 0.590 |
| year1 | 0.633 | 0.098 | 0.774 | 0.401 | 1.500 | 0.842 | 0.238 |  |
| year2 | 0.096 | 0.025 | 0.113 | 0.037 | 0.069 | 0.011 | 0.001 | 0.146 |
| year3 | 0.062 | 0.023 | 0.106 | 0.029 | 0.026 | 0.025 | 0.008 | 0.199 |
| year4 | 0.042 | 0.008 | 0.072 | 0.010 | 0.011 | 0.001 | 0.000 | 0.054 |
| year5 | 0.025 | 0.022 | 0.064 | 0.018 | 0.019 | 0.031 | 0.008 | 0.190 |
| Cu | 0.029 | 0.028 | 0.021 | 0.023 | 0.020 | 0.018 | 0.009 | 0.002 |
| year1 | 0.011 | 0.010 | 0.009 | 0.009 | 0.009 | 0.008 | 0.004 |  |
| year2 | 0.004 | 0.004 | 0.002 | 0.002 | 0.001 | 0.001 | 0.000 | 0.001 |
| year3 | 0.006 | 0.006 | 0.004 | 0.004 | 0.003 | 0.003 | 0.003 | 0.001 |
| year4 | 0.002 | 0.002 | 0.001 | 0.004 | 0.001 | 0.001 | 0.000 | 0.000 |
| year5 | 0.006 | 0.006 | 0.004 | 0.005 | 0.005 | 0.004 | 0.002 | 0.000 |
| Mo | 0.403 | 0.252 | 0.618 | 0.491 | 0.399 | 0.295 | 0.128 | 0.195 |
| year1 | 0.323 | 0.123 | 0.473 | 0.247 | 0.349 | 0.186 | 0.046 |  |
| year2 | 0.029 | 0.051 | 0.050 | 0.071 | 0.012 | 0.010 | 0.004 | 0.083 |
| year3 | 0.016 | 0.027 | 0.028 | 0.047 | 0.006 | 0.020 | 0.021 | 0.073 |
| year4 | 0.010 | 0.024 | 0.018 | 0.045 | 0.004 | 0.009 | 0.006 | 0.009 |
| year5 | 0.025 | 0.028 | 0.049 | 0.081 | 0.028 | 0.071 | 0.052 | 0.030 |
| Ni | 0.070 | 0.069 | 0.049 | 0.048 | 0.043 | 0.043 | 0.024 | 0.005 |
| year1 | 0.015 | 0.017 | 0.013 | 0.013 | 0.010 | 0.013 | 0.006 |  |
| year2 | 0.006 | 0.006 | 0.003 | 0.003 | 0.002 | 0.002 | 0.000 | 0.001 |
| year3 | 0.023 | 0.023 | 0.015 | 0.014 | 0.012 | 0.012 | 0.010 | 0.003 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.025 | 0.023 | 0.018 | 0.018 | 0.020 | 0.016 | 0.009 | 0.002 |
| Pb | 0.351 | 0.342 | 0.255 | 0.254 | 0.227 | 0.248 | 0.128 | 0.012 |
| year1 | 0.226 | 0.222 | 0.177 | 0.177 | 0.163 | 0.188 | 0.094 |  |
| year2 | 0.040 | 0.039 | 0.020 | 0.021 | 0.010 | 0.011 | 0.002 | 0.003 |
| year3 | 0.042 | 0.042 | 0.027 | 0.025 | 0.021 | 0.022 | 0.018 | 0.006 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.042 | 0.038 | 0.030 | 0.031 | 0.033 | 0.026 | 0.015 | 0.003 |
| V | 0.654 | 0.399 | 0.570 | 0.266 | 0.240 | 0.179 | 0.057 | 0.036 |
| year1 | 0.169 | 0.072 | 0.245 | 0.083 | 0.143 | 0.074 | 0.013 |  |
| year2 | 0.081 | 0.070 | 0.070 | 0.040 | 0.018 | 0.010 | 0.001 | 0.007 |
| year3 | 0.066 | 0.044 | 0.064 | 0.021 | 0.008 | 0.015 | 0.009 | 0.008 |
| year4 | 0.137 | 0.074 | 0.077 | 0.034 | 0.006 | 0.007 | 0.004 | 0.003 |
| year5 | 0.200 | 0.139 | 0.114 | 0.087 | 0.065 | 0.072 | 0.030 | 0.017 |
| Sb | 0.057 | 0.055 | 0.038 | 0.037 | 0.036 | 0.032 | 0.022 | 0.006 |
| year3 | 0.030 | 0.030 | 0.019 | 0.018 | 0.015 | 0.015 | 0.012 | 0.004 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.027 | 0.025 | 0.019 | 0.019 | 0.021 | 0.017 | 0.009 | 0.002 |
| Se | 0.189 | 0.168 | 0.152 | 0.143 | 0.157 | 0.104 | 0.065 | 0.154 |
| year3 | 0.063 | 0.063 | 0.041 | 0.037 | 0.033 | 0.033 | 0.026 | 0.045 |
| year4 | 0.024 | 0.012 | 0.040 | 0.032 | 0.019 | 0.008 | 0.004 | 0.016 |
| year5 | 0.102 | 0.093 | 0.071 | 0.074 | 0.106 | 0.064 | 0.035 | 0.093 |
| Zn | 0.965 | 0.924 | 0.866 | 0.951 | 0.157 | 0.156 | 0.053 | 0.006 |
| year1 | 0.835 | 0.778 | 0.793 | 0.848 | 0.128 | 0.111 | 0.041 |  |
| year2 | 0.096 | 0.083 | 0.053 | 0.034 | 0.011 | 0.012 | 0.002 | 0.003 |
| year3 | 0.014 | 0.008 | 0.005 | 0.005 | 0.004 | 0.004 | 0.003 | 0.001 |
| year4 | 0.003 | 0.034 | 0.002 | 0.051 | 0.001 | 0.003 | 0.000 | 0.000 |
| year5 | 0.017 | 0.021 | 0.012 | 0.013 | 0.013 | 0.026 | 0.006 | 0.001 |
| Ce | 0.106 | 0.103 | 0.071 | 0.068 | 0.064 | 0.059 | 0.041 | 0.012 |
| year3 | 0.066 | 0.066 | 0.043 | 0.039 | 0.033 | 0.034 | 0.028 | 0.009 |
| year4 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| year5 | 0.040 | 0.036 | 0.028 | 0.029 | 0.031 | 0.025 | 0.014 | 0.003 |

[Dos de couverture, ne pas mettre de texte sur cette page, ni la supprimer]