SUPPLEMENTARY MATERIAL

Environmental Science and Pollution research

5 years leaching experiments to evaluate a modified bauxite residue. Part 2: Remediation of sulfidic mine tailings

Patricia Merdy1, Alexandre Parker1,2, Chen Chen1,2, Pierre Hennebert2, 3

1 Université de Toulon, Aix Marseille Univ., CNRS, IM2NP, 83041 TOULON CEDEX 9, France

2Formerly Ineris (French National Institute for Industrial Environment and Risks), BP 2, F-60550 Verneuil-en-

Halatte, France.

3Consultant, Quartier Les Roux, F-13590 Meyreuil, France

Corresponding author : patricia.merdy@univ-tln.fr

List of appendixes:

- Appendix 1: Average concentrations (mg/l) of the drains per year and per lysimeter

- Appendix 2: Quantities (mg/kg) of elements in the drains per year and per lysimeter

Appendix 1 : Average concentrations (mg/l) of drains per year and per lysimeter

Physico-chemical parameters

| Parameter/Lysimeter | 8 | 9 | 10 | 11 | 12 | 13 | 14 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| pH |  |  |  |  |  |  |  |
| year1 | 7.9 | 3.8 | 7.4 |  |  |  |  |
| year2 | 8.2 | 4.1 | 7.6 | 7.5 | 1.7 | 5.5 | 7.1 |
| year3 | 8.2 | 3.7 | 7.3 | 7.3 | 1.9 | 8.1 | 7.9 |
| year4 | 8.2 | 3.7 | 7.6 | 7.5 | 2.0 | 8.6 | 7.4 |
| year5 | 8.1 | 3.6 | 7.5 | 7.5 | 2.1 | 8.1 | 4.8 |
| EC (mS/cm) |  |  |  |  |  |  |  |
| year1 | 5.9 | 1.8 | 4.8 |  |  |  |  |
| year2 | 6.4 | 1.1 | 3.3 | 3.2 | 45.7 | 11.9 | 23.0 |
| year3 | 5.2 | 1.4 | 3.4 | 2.4 | 17.5 | 8.1 | 2.6 |
| year4 | 4.5 | 1.4 | 3.7 | 2.5 | 31.1 | 10.1 | 2.5 |
| year5 | 3.8 | 0.7 | 2.9 | 2.1 | 11.2 | 6.9 | 3.7 |
| pe |  |  |  |  |  |  |  |
| year1 | 4.0 | 6.9 | 4.9 |  |  |  |  |
| year2 | 4.6 | 6.1 | 4.4 | 4.5 | 6.9 | 2.3 | 2.5 |
| year3 | 5.5 | 8.2 | 6.1 | 6.0 | 8.1 | 5.6 | 5.5 |
| year4 | 5.1 | 9.2 | 8.1 | 6.9 | 10.3 | 6.5 | 8.1 |
| year5 | 5.6 | 9.4 | 7.8 | 7.5 | 13.8 | 4.5 | 11.0 |

Concentrations (if values >LQ are considered equal to 0)

| Elements (mg/l) / Lysimeter | 8 | 9 | 10 | 11 | 12 | 13 | 14 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al | 0.19 | 10.21 | 0.08 | 0.09 | 944.01 | 0.84 | 71.27 |
| year1 | 0.16 | 11.59 | 0.12 |  |  |  |  |
| year2 |  | 5.72 | 0.08 | 0.09 | 3397 | 0.18 | 0.08 |
| year3 |  | 9.55 | 0.08 |  | 750 | 0.07 | 0.59 |
| year4 |  | 12.20 | 0.01 |  | 1330 | 0.06 | 0.02 |
| year5 | 0.22 | 5.67 |  |  | 405 | 2.28 | 99.70 |
| Si | 5.41 | 31.31 | 28.44 | 31.18 | 46 | 14.23 | 37.67 |
| year1 | 7.24 | 33.22 | 28.03 |  |  |  |  |
| year2 | 3.10 | 20.13 | 21.91 | 23.98 | 56 | 8.81 | 11.61 |
| year3 | 2.25 | 28.22 | 27.50 | 30.77 | 31 | 11.45 | 13.40 |
| year4 | 2.79 | 39.62 | 31.95 | 34.50 | 44 | 13.68 | 12.57 |
| year5 | 4.34 | 36.66 | 47.84 | 49.87 | 46 | 15.52 | 46.90 |
| Fe | 0.03 | 0.10 | 0.04 | 0.04 | 5634 | 0.57 | 141.37 |
| year1 |  | 0.11 | 0.08 |  |  |  |  |
| year2 |  | 0.10 | 0.05 | 0.05 | 21832 | 0.70 | 0.10 |
| year3 | 0.06 | 0.06 | 0.02 | 0.04 | 6125 | 1.07 | 0.46 |
| year4 | 0.01 | 0.08 | 0.01 | 0.01 | 8600 | 0.51 | 0.13 |
| year5 |  |  |  |  | 1917 | 0.22 | 197.84 |
| Ca | 445 | 297 | 453 | 622 | 350 | 489 | 729 |
| year1 | 363 | 349 | 374 |  |  |  |  |
| year2 | 465 | 203 | 375 | 472 | 345 | 637 | 1053 |
| year3 | 669 | 212 | 741 | 846 | 282 | 466 | 798 |
| year4 | 481 | 229 | 699 | 758 | 401 | 720 | 608 |
| year5 | 569 | 113 | 625 | 710 | 352 | 443 | 675 |
| Mn | 0.03 | 0.52 | 0.01 | 0.01 | 0.96 | 0.15 | 2.31 |
| year1 | 0.02 | 0.73 | 0.02 |  |  |  |  |
| year2 |  | 0.33 | 0.00 | 0.01 | 1.72 | 0.20 | 0.86 |
| year3 |  | 0.29 | 0.00 | 0.00 | 2.55 | 0.12 | 0.09 |
| year4 |  | 0.31 | 0.00 | 0.00 | 2.39 | 0.08 | 0.23 |
| year5 | 0.09 | 0.18 |  |  | 0.59 | 0.15 | 2.97 |
| Mg | 87.4 | 8.8 | 8.6 | 9.0 | 26 | 106.8 | 116.5 |
| year1 | 106.5 | 9.7 | 10.1 |  |  |  |  |
| year2 | 74.4 | 6.3 | 5.8 | 8.6 | 69 | 90.6 | 119.8 |
| year3 | 62.6 | 8.6 | 5.2 | 5.0 | 46 | 74.5 | 79.9 |
| year4 | 57.8 | 7.9 | 8.4 | 7.7 | 53 | 169.0 | 118.9 |
| year5 | 58.9 | 6.7 | 12.1 | 15.6 | 14 | 107.0 | 119.0 |
| Na | 928 | 39 | 634 | 76 | 8 | 1632 | 74 |
| year1 | 963 | 51 | 855 |  |  |  |  |
| year2 | 1060 | 17 | 338 | 106 | 22 | 2 | 7 |
| year3 | 1110 | 16 | 510 | 14 | 8 | 2738 | 17 |
| year4 | 605 | 12 | 469 | 56 | 11 | 1846 | 24 |
| year5 | 758 | 10 | 486 | 69 | 5 | 1808 | 96 |
| K | 12.9 | 14.7 | 3.5 | 3.1 | 552 | 3.9 | 2.8 |
| year1 | 9.0 | 11.2 | 3.5 |  |  |  |  |
| year2 | 13.5 | 9.9 | 1.8 | 1.7 | 1273 | 2.3 | 1.0 |
| year3 | 38.3 | 39.3 | 9.6 | 7.1 | 31 | 12.4 | 4.0 |
| year4 | 6.9 | 29.6 | 1.7 | 0.6 | 6 | 1.3 | 0.7 |
| year5 | 12.1 | 31.1 | 4.5 | 5.9 | 3 | 3.7 | 3.2 |
| P | 0.02 | 0.45 | 0.02 | 0.03 | 347.63 | 0.06 | 0.46 |
| year1 | 0.02 | 0.02 |  |  |  |  |  |
| year2 |  | 1.04 | 0.01 | 0.02 | 2913 | 0.09 | 0.09 |
| year3 |  | 0.05 |  |  | 92 |  |  |
| year4 | 0.02 | 0.07 | 0.05 | 0.04 | 88 | 0.04 | 0.02 |
| year5 |  | 0.36 |  |  | 18 | 0.06 | 0.59 |
| S | 1027 | 352 | 845 | 390 | 2044 | 985 | 738 |
| year1 | 1369 | 455 | 1143 |  |  |  |  |
| year2 | 1000 | 187 | 679 | 487 | 2000 | 2000 | 2000 |
| year3 | 123 | 24 | 77 | 52 | 1322 | 210 | 60 |
| year4 | 870 | 253 | 848 | 571 | 11993 | 2317 | 582 |
| year5 | 400 | 44 | 319 | 259 | 1395 | 749 | 585 |
| As | 0.009 | 0.027 | 0.035 | 0.030 | 15.301 | 0.039 | 0.040 |
| year1 | 0.016 | 0.015 | 0.017 |  |  |  |  |
| year2 |  | 0.078 | 0.060 | 0.044 | 72.63 | 0.069 | 0.037 |
| year3 |  |  |  |  | 13.76 |  |  |
| year4 | 0.002 | 0.002 | 0.004 | 0.001 | 11.70 | 0.008 | 0.003 |
| year5 |  |  |  |  | 3.38 |  | 0.054 |
| Cd |  | 0.289 | 0.005 | 0.003 | 0.29 |  | 0.015 |
| year1 |  | 0.322 |  |  |  |  |  |
| year2 |  | 0.239 | 0.007 | 0.005 | 0.37 |  |  |
| year3 |  | 0.235 | 0.003 |  | 0.98 |  | 0.010 |
| year4 |  | 0.231 | 0.001 | 0.001 | 0.14 |  |  |
| year5 |  | 0.154 |  |  | 0.23 |  | 0.018 |
| Co | 0.004 | 0.012 | 0.003 | 0.012 | 1.21 | 0.035 | 1.029 |
| year1 | 0.004 | 0.008 | 0.004 |  |  |  |  |
| year2 |  | 0.069 | 0.006 | 0.017 | 5.98 | 0.023 | 0.180 |
| year3 |  | 0.004 |  |  | 1.04 | 0.007 | 0.057 |
| year4 |  | 0.004 | 0.000 | 0.000 | 1.57 | 0.007 | 0.024 |
| year5 |  |  |  |  | 0.51 | 0.042 | 1.363 |
| Cr | 0.05 | 0.01 | 0.01 | 0.01 | 1.12 | 0.05 | 0.11 |
| year1 | 0.073 | 0.010 | 0.010 |  |  |  |  |
| year2 |  | 0.008 | 0.012 | 0.014 | 5.67 | 0.031 | 0.043 |
| year3 | 0.035 | 0.009 |  |  | 1.06 | 0.037 | 0.044 |
| year4 | 0.002 | 0.002 |  |  | 0.47 | 0.000 |  |
| year5 | 0.021 |  |  |  | 0.52 | 0.055 | 0.125 |
| Cu | 0.006 | 0.012 | 0.006 | 0.006 | 333.20 | 0.644 | 15.275 |
| year1 | 0.010 | 0.011 | 0.005 |  |  |  |  |
| year2 |  | 0.015 | 0.007 | 0.008 | 2710 | 0.153 | 0.138 |
| year3 |  | 0.012 |  |  | 24 | 0.038 | 0.056 |
| year4 | 0.003 | 0.014 | 0.006 | 0.003 | 187 | 0.053 | 0.015 |
| year5 |  |  |  |  | 26 | 1.080 | 20.799 |
| Mo | 0.036 | 0.004 | 0.005 |  | 0.61 | 0.015 | 0.004 |
| year1 | 0.032 |  | 0.012 |  |  |  |  |
| year2 | 0.053 | 0.005 | 0.003 |  | 3.11 | 0.025 | 0.007 |
| year3 | 0.037 | 0.003 |  |  | 0.61 | 0.005 |  |
| year4 | 0.034 |  | 0.001 |  | 0.82 | 0.004 | 0.001 |
| year5 | 0.035 |  |  |  | 0.23 |  |  |
| Ni | 0.001 | 0.052 | 0.007 | 0.008 | 0.894 | 0.024 | 0.559 |
| year1 |  | 0.060 |  |  |  |  |  |
| year2 |  | 0.030 | 0.013 | 0.015 | 6.07 | 0.021 | 0.117 |
| year3 |  |  |  |  | 0.41 |  | 0.020 |
| year4 | 0.001 | 0.030 | 0.001 | 0.001 | 0.75 | 0.004 | 0.010 |
| year5 |  |  |  |  | 0.20 | 0.032 | 0.738 |
| Pb | 0.126 | 3.050 | 0.104 | 0.140 | 0.61 | 0.019 | 0.030 |
| year1 | 0.126 | 2.18 | 0.142 |  |  |  |  |
| year2 |  | 5.69 | 0.047 | 0.076 | 1.96 | 0.035 | 0.035 |
| year3 |  | 3.20 | 0.059 | 0.081 | 0.95 |  |  |
| year4 |  | 2.81 | 0.049 | 0.162 | 0.65 | 0.004 | 0.000 |
| year5 |  | 5.67 | 0.091 | 0.368 | 0.29 |  | 0.038 |
| V | 0.034 | 0.005 | 0.004 | 0.004 | 0.42 | 0.006 | 0.015 |
| year1 | 0.023 | 0.005 |  |  |  |  |  |
| year2 | 0.039 |  | 0.006 | 0.006 | 1.35 | 0.012 | 0.017 |
| year3 | 0.031 |  |  |  |  |  |  |
| year4 | 0.047 |  | 0.001 | 0.001 | 0.37 | 0.003 | 0.002 |
| year5 | 0.064 |  |  |  | 0.22 | 0.005 | 0.018 |
| Sb | 0.000 | 0.003 | 0.033 | 0.024 | 0.34 | 0.003 | 0.001 |
| year3 |  |  | 0.031 |  |  |  |  |
| year4 | 0.000 | 0.003 | 0.022 | 0.019 | 0.34 | 0.003 | 0.001 |
| year5 |  |  | 0.046 | 0.029 |  |  |  |
| Se | 0.016 | 0.033 | 0.002 | 0.005 | 1.102 | 0.497 | 0.224 |
| year3 |  | 0.065 |  |  | 2.03 | 0.498 | 0.131 |
| year4 | 0.016 | 0.002 | 0.002 | 0.005 | 0.14 | 0.863 | 0.360 |
| year5 |  |  |  |  | 1.10 | 0.464 | 0.220 |
| Zn | 0.051 | 34.438 | 0.062 | 0.082 | 12.05 | 0.099 | 1.453 |
| year1 | 0.070 | 37.5 | 0.095 |  |  |  |  |
| year2 |  | 24.0 | 0.122 | 0.157 | 93.39 |  | 0.063 |
| year3 | 0.007 | 29.5 | 0.010 |  | 3.58 |  |  |
| year4 | 0.013 | 47.7 | 0.015 | 0.006 | 4.27 | 0.102 | 0.308 |
| year5 | 0.053 | 20.7 | 0.036 |  | 1.60 | 0.098 | 1.683 |
| Ce |  | 0.055 |  |  | 0.399 | 0.011 | 0.069 |
| year3 |  |  |  |  | 0.425 |  |  |
| year4 |  | 0.055 |  |  | 0.253 | 0.002 |  |
| year5 |  |  |  |  | 0.408 | 0.021 | 0.069 |

Concentrations (if values >LQ are considered equal to LQ)

| Elements (mg/l) / Lysimeter | 8 | 9 | 10 | 11 | 12 | 13 | 14 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al | 0.09 | 10.21 | 0.07 | 0.05 | 944.01 | 0.35 | 66.52 |
| year1 | 0.09 | 11.59 | 0.09 |  |  |  |  |
| year2 | 0.08 | 5.72 | 0.08 | 0.08 | 3397 | 0.18 | 0.08 |
| year3 | 0.03 | 9.55 | 0.08 | 0.03 | 750 | 0.07 | 0.59 |
| year4 | 0.01 | 12.20 | 0.01 | 0.01 | 1330 | 0.06 | 0.02 |
| year5 | 0.22 | 5.67 | 0.02 | 0.02 | 405 | 0.43 | 90.64 |
| Si | 5.41 | 31.31 | 28.44 | 31.18 | 44 | 14.23 | 37.67 |
| year1 | 7.24 | 33.22 | 28.03 |  |  |  |  |
| year2 | 3.10 | 20.13 | 21.91 | 23.98 | 37 | 8.81 | 11.61 |
| year3 | 2.25 | 28.22 | 27.50 | 30.77 | 31 | 11.45 | 13.40 |
| year4 | 2.79 | 39.62 | 31.95 | 34.50 | 44 | 13.68 | 12.57 |
| year5 | 4.34 | 36.66 | 47.84 | 49.87 | 46 | 15.52 | 46.90 |
| Fe | 0.03 | 0.08 | 0.04 | 0.03 | 5634 | 0.24 | 131.95 |
| year1 | 0.03 | 0.09 | 0.04 |  |  |  |  |
| year2 | 0.03 | 0.08 | 0.05 | 0.04 | 21832 | 0.70 | 0.10 |
| year3 | 0.06 | 0.06 | 0.02 | 0.04 | 6125 | 1.07 | 0.46 |
| year4 | 0.01 | 0.08 | 0.01 | 0.01 | 8600 | 0.51 | 0.13 |
| year5 | 0.02 | 0.02 | 0.02 | 0.02 | 1917 | 0.05 | 179.86 |
| Ca | 445 | 297 | 453 | 622 | 350 | 489 | 729 |
| year1 | 363 | 349 | 374 |  |  |  |  |
| year2 | 465 | 203 | 375 | 472 | 345 | 637 | 1053 |
| year3 | 669 | 212 | 741 | 846 | 282 | 466 | 798 |
| year4 | 481 | 229 | 699 | 758 | 401 | 720 | 608 |
| year5 | 569 | 113 | 625 | 710 | 352 | 443 | 675 |
| Mn | 0.02 | 0.52 | 0.01 | 0.01 | 0.96 | 0.13 | 2.31 |
| year1 | 0.02 | 0.73 | 0.02 |  |  |  |  |
| year2 | 0.00 | 0.33 | 0.00 | 0.01 | 1.72 | 0.20 | 0.86 |
| year3 | 0.00 | 0.29 | 0.00 | 0.00 | 2.55 | 0.12 | 0.09 |
| year4 | 0.00 | 0.31 | 0.00 | 0.00 | 2.39 | 0.08 | 0.23 |
| year5 | 0.09 | 0.18 | 0.00 | 0.00 | 0.59 | 0.13 | 2.97 |
| Mg | 87.4 | 8.8 | 8.6 | 9.0 | 26 | 106.8 | 116.5 |
| year1 | 106.5 | 9.7 | 10.1 |  |  |  |  |
| year2 | 74.4 | 6.3 | 5.8 | 8.6 | 69 | 90.6 | 119.8 |
| year3 | 62.6 | 8.6 | 5.2 | 5.0 | 46 | 74.5 | 79.9 |
| year4 | 57.8 | 7.9 | 8.4 | 7.7 | 53 | 169.0 | 118.9 |
| year5 | 58.9 | 6.7 | 12.1 | 15.6 | 14 | 107.0 | 119.0 |
| Na | 928 | 39 | 634 | 76 | 8 | 1632 | 74 |
| year1 | 963 | 51 | 855 |  |  |  |  |
| year2 | 1060 | 17 | 338 | 106 | 22 | 2 | 7 |
| year3 | 1110 | 16 | 510 | 14 | 8 | 2738 | 17 |
| year4 | 605 | 12 | 469 | 56 | 11 | 1846 | 24 |
| year5 | 758 | 10 | 486 | 69 | 5 | 1808 | 96 |
| K | 12.9 | 14.7 | 3.3 | 3.1 | 203 | 3.9 | 2.8 |
| year1 | 9.0 | 11.2 | 3.0 |  |  |  |  |
| year2 | 13.5 | 9.9 | 1.8 | 1.7 | 1273 | 2.3 | 1.0 |
| year3 | 38.3 | 39.3 | 9.6 | 7.1 | 31 | 12.4 | 4.0 |
| year4 | 6.9 | 29.6 | 1.7 | 0.6 | 6 | 1.3 | 0.7 |
| year5 | 12.1 | 31.1 | 4.5 | 5.9 | 1 | 3.7 | 3.2 |
| P | 0.02 | 0.45 | 0.02 | 0.03 | 329.34 | 0.04 | 0.37 |
| year1 | 0.01 | 0.02 | 0.01 |  |  |  |  |
| year2 | 0.01 | 1.04 | 0.01 | 0.02 | 1942 | 0.05 | 0.09 |
| year3 | 0.03 | 0.05 | 0.03 | 0.03 | 92 | 0.03 | 0.03 |
| year4 | 0.02 | 0.07 | 0.05 | 0.04 | 88 | 0.04 | 0.02 |
| year5 | 0.03 | 0.36 | 0.03 | 0.03 | 18 | 0.04 | 0.49 |
| S | 1027 | 352 | 845 | 390 | 2044 | 985 | 738 |
| year1 | 1369 | 455 | 1143 |  |  |  |  |
| year2 | 1000 | 187 | 679 | 487 | 2000 | 2000 | 2000 |
| year3 | 123 | 24 | 77 | 52 | 1322 | 210 | 60 |
| year4 | 870 | 253 | 848 | 571 | 11993 | 2317 | 582 |
| year5 | 400 | 44 | 319 | 259 | 1395 | 749 | 585 |
| As | 0.012 | 0.016 | 0.021 | 0.023 | 15.301 | 0.020 | 0.025 |
| year1 | 0.013 | 0.013 | 0.013 |  |  |  |  |
| year2 | 0.012 | 0.034 | 0.044 | 0.034 | 72.63 | 0.041 | 0.025 |
| year3 | 0.015 | 0.015 | 0.015 | 0.015 | 13.76 | 0.015 | 0.015 |
| year4 | 0.002 | 0.002 | 0.004 | 0.001 | 11.70 | 0.008 | 0.003 |
| year5 | 0.018 | 0.018 | 0.018 | 0.018 | 3.38 | 0.018 | 0.028 |
| Cd | 0.004 | 0.289 | 0.005 | 0.004 | 0.27 | 0.008 | 0.009 |
| year1 | 0.004 | 0.322 | 0.004 |  |  |  |  |
| year2 | 0.004 | 0.239 | 0.006 | 0.004 | 0.25 | 0.004 | 0.004 |
| year3 | 0.002 | 0.235 | 0.003 | 0.002 | 0.98 | 0.002 | 0.010 |
| year4 | 0.000 | 0.231 | 0.001 | 0.001 | 0.14 | 0.000 | 0.000 |
| year5 | 0.009 | 0.154 | 0.009 | 0.009 | 0.23 | 0.009 | 0.011 |
| Co | 0.002 | 0.010 | 0.002 | 0.007 | 1.15 | 0.035 | 1.029 |
| year1 | 0.002 | 0.008 | 0.002 |  |  |  |  |
| year2 | 0.002 | 0.024 | 0.003 | 0.012 | 3.99 | 0.023 | 0.180 |
| year3 | 0.003 | 0.004 | 0.003 | 0.003 | 1.04 | 0.007 | 0.057 |
| year4 | 0.000 | 0.004 | 0.000 | 0.000 | 1.57 | 0.007 | 0.024 |
| year5 | 0.002 | 0.002 | 0.002 | 0.002 | 0.51 | 0.042 | 1.363 |
| Cr | 0.04 | 0.01 | 0.01 | 0.01 | 1.06 | 0.05 | 0.10 |
| year1 | 0.059 | 0.010 | 0.010 |  |  |  |  |
| year2 | 0.003 | 0.005 | 0.006 | 0.007 | 3.78 | 0.017 | 0.023 |
| year3 | 0.035 | 0.009 | 0.008 | 0.008 | 1.06 | 0.037 | 0.044 |
| year4 | 0.002 | 0.002 | 0.000 | 0.000 | 0.47 | 0.000 | 0.000 |
| year5 | 0.021 | 0.011 | 0.011 | 0.011 | 0.52 | 0.055 | 0.125 |
| Cu | 0.004 | 0.011 | 0.004 | 0.005 | 315.66 | 0.388 | 15.275 |
| year1 | 0.005 | 0.011 | 0.004 |  |  |  |  |
| year2 | 0.003 | 0.011 | 0.005 | 0.006 | 1807 | 0.153 | 0.138 |
| year3 | 0.005 | 0.012 | 0.005 | 0.005 | 24 | 0.038 | 0.056 |
| year4 | 0.003 | 0.014 | 0.006 | 0.003 | 187 | 0.053 | 0.015 |
| year5 | 0.003 | 0.003 | 0.003 | 0.003 | 26 | 0.493 | 20.799 |
| Mo | 0.032 | 0.003 | 0.004 | 0.003 | 0.57 | 0.006 | 0.003 |
| year1 | 0.027 | 0.003 | 0.005 |  |  |  |  |
| year2 | 0.053 | 0.004 | 0.003 | 0.003 | 2.08 | 0.025 | 0.005 |
| year3 | 0.037 | 0.003 | 0.002 | 0.002 | 0.61 | 0.005 | 0.002 |
| year4 | 0.034 | 0.000 | 0.001 | 0.000 | 0.82 | 0.004 | 0.001 |
| year5 | 0.035 | 0.003 | 0.003 | 0.003 | 0.23 | 0.003 | 0.003 |
| Ni | 0.007 | 0.048 | 0.007 | 0.009 | 0.847 | 0.017 | 0.559 |
| year1 | 0.005 | 0.060 | 0.005 |  |  |  |  |
| year2 | 0.005 | 0.030 | 0.008 | 0.009 | 4.05 | 0.021 | 0.117 |
| year3 | 0.018 | 0.018 | 0.018 | 0.018 | 0.41 | 0.018 | 0.020 |
| year4 | 0.001 | 0.030 | 0.001 | 0.001 | 0.75 | 0.004 | 0.010 |
| year5 | 0.011 | 0.011 | 0.011 | 0.011 | 0.20 | 0.017 | 0.738 |
| Pb | 0.059 | 3.050 | 0.098 | 0.140 | 0.61 | 0.021 | 0.025 |
| year1 | 0.090 | 2.18 | 0.142 |  |  |  |  |
| year2 | 0.035 | 5.69 | 0.043 | 0.076 | 1.96 | 0.035 | 0.035 |
| year3 | 0.033 | 3.20 | 0.059 | 0.081 | 0.95 | 0.033 | 0.033 |
| year4 | 0.000 | 2.81 | 0.049 | 0.162 | 0.65 | 0.004 | 0.000 |
| year5 | 0.019 | 5.67 | 0.091 | 0.368 | 0.29 | 0.019 | 0.024 |
| V | 0.031 | 0.004 | 0.004 | 0.005 | 0.39 | 0.005 | 0.009 |
| year1 | 0.019 | 0.004 | 0.004 |  |  |  |  |
| year2 | 0.039 | 0.004 | 0.005 | 0.005 | 1.35 | 0.008 | 0.010 |
| year3 | 0.031 | 0.007 | 0.007 | 0.007 | 0.01 | 0.007 | 0.007 |
| year4 | 0.047 | 0.000 | 0.001 | 0.001 | 0.37 | 0.003 | 0.002 |
| year5 | 0.064 | 0.004 | 0.004 | 0.004 | 0.22 | 0.004 | 0.009 |
| Sb | 0.012 | 0.013 | 0.033 | 0.024 | 0.03 | 0.012 | 0.012 |
| year3 | 0.023 | 0.023 | 0.031 | 0.023 | 0.02 | 0.023 | 0.023 |
| year4 | 0.000 | 0.003 | 0.022 | 0.019 | 0.34 | 0.003 | 0.001 |
| year5 | 0.012 | 0.012 | 0.046 | 0.029 | 0.012 | 0.012 | 0.012 |
| Se | 0.037 | 0.038 | 0.033 | 0.034 | 1.102 | 0.497 | 0.210 |
| year3 | 0.049 | 0.065 | 0.049 | 0.049 | 2.03 | 0.498 | 0.131 |
| year4 | 0.016 | 0.002 | 0.002 | 0.005 | 0.14 | 0.863 | 0.360 |
| year5 | 0.046 | 0.046 | 0.046 | 0.046 | 1.10 | 0.464 | 0.204 |
| Zn | 0.048 | 34.438 | 0.050 | 0.042 | 11.42 | 0.042 | 1.262 |
| year1 | 0.063 | 37.5 | 0.056 |  |  |  |  |
| year2 | 0.037 | 24.0 | 0.065 | 0.077 | 62.27 | 0.037 | 0.050 |
| year3 | 0.007 | 29.5 | 0.010 | 0.006 | 3.58 | 0.006 | 0.006 |
| year4 | 0.013 | 47.7 | 0.015 | 0.006 | 4.27 | 0.102 | 0.308 |
| year5 | 0.053 | 20.7 | 0.036 | 0.008 | 1.60 | 0.041 | 1.683 |
| Ce | 0.023 | 0.042 | 0.023 | 0.023 | 0.399 | 0.020 | 0.043 |
| year3 | 0.052 | 0.052 | 0.052 | 0.052 | 0.425 | 0.052 | 0.052 |
| year4 | 0.000 | 0.055 | 0.000 | 0.000 | 0.253 | 0.002 | 0.000 |
| year5 | 0.018 | 0.018 | 0.018 | 0.018 | 0.408 | 0.018 | 0.046 |

Appendix 2 : Quantities (mg/kg) of elements in the drains per year and per lysimeter

Mass used: 24 kg (of MBR or UMBR) for lysimeters 1 to 8 ;  45.49 kg of mining residue for lysimeters 9, 10 and 11 ; 37.44 kg of mining residue for lysimeters 12, 13 and 14 ; 50.23 kg for the lysimeter 15 and 1087 kg for the lysimeter 16.

In bold: cumulative quantity over 5 or 4 years

Quantity (if value < LQ = 0)

| Elements (mg/kg) / Lysimeter | 8 | 9 | 10 | 11 | 12 | 13 | 14 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Element |  |  |  |  |  |  |  |
| Al | 0.3 | 23.6 | 0.1 | 0.0 | 2727 | 0.2 | 74.9 |
| year1 | 0.0 | 8.2 | 0.0 |  |  |  |  |
| year2 |  | 1.6 | 0.0 | 0.0 | 934 | 0.0 | 0.0 |
| year3 |  | 4.0 | 0.0 |  | 364 | 0.0 | 0.0 |
| year4 |  | 5.2 | 0.0 |  | 765 | 0.0 | 0.0 |
| year5 | 0.2 | 4.6 |  |  | 663 | 0.2 | 74.9 |
| Si | 8.1 | 93.6 | 66.6 | 48.9 | 105 | 12.1 | 49.8 |
| year1 | 2.1 | 31.1 | 18.5 |  |  |  |  |
| year2 | 0.1 | 3.8 | 3.0 | 1.8 | 8 | 0.9 | 1.4 |
| year3 | 1.2 | 11.7 | 8.1 | 9.0 | 15 | 0.6 | 0.5 |
| year4 | 0.3 | 17.0 | 1.7 | 2.2 | 25 | 0.0 | 0.1 |
| year5 | 4.5 | 29.9 | 35.4 | 35.9 | 57 | 10.7 | 47.7 |
| Fe | 0.0 | 0.1 | 0.0 | 0.0 | 16749 | 0.2 | 156.8 |
| year1 |  | 0.1 | 0.0 |  |  |  |  |
| year2 |  | 0.0 | 0.0 | 0.0 | 6051 | 0.1 | 0.0 |
| year3 | 0.0 | 0.0 | 0.0 | 0.0 | 2969 | 0.1 | 0.0 |
| year4 | 0.0 | 0.0 | 0.0 | 0.0 | 4948 | 0.0 | 0.0 |
| year5 |  |  |  |  | 2781 | 0.0 | 156.8 |
| Ca | 1326 | 611 | 1031 | 856 | 917 | 392 | 1055 |
| year1 | 325 | 281 | 263 |  |  |  |  |
| year2 | 16 | 51 | 52 | 49 | 80 | 67 | 138 |
| year3 | 346 | 88 | 217 | 247 | 137 | 24 | 31 |
| year4 | 53 | 98 | 37 | 48 | 231 | 1 | 7 |
| year5 | 586 | 92 | 462 | 512 | 470 | 300 | 879 |
| Mn | 0.1 | 0.8 | 0.0 | 0.0 | 4.1 | 0.1 | 2.6 |
| year1 | 0.0 | 0.3 | 0.0 |  |  |  |  |
| year2 |  | 0.1 | 0.0 | 0.0 | 0.5 | 0.0 | 0.1 |
| year3 |  | 0.1 | 0.0 | 0.0 | 1.2 | 0.0 | 0.0 |
| year4 |  | 0.1 | 0.0 | 0.0 | 1.4 | 0.0 | 0.0 |
| year5 | 0.1 | 0.1 |  |  | 1.0 | 0.1 | 2.5 |
| Mg | 217.6 | 22.1 | 15.9 | 14.1 | 94.5 | 86.3 | 172.8 |
| year1 | 115.6 | 7.9 | 4.4 |  |  |  |  |
| year2 | 2.6 | 1.8 | 0.6 | 0.9 | 18.3 | 10.4 | 18.4 |
| year3 | 32.3 | 3.6 | 1.5 | 1.5 | 22.5 | 3.9 | 3.1 |
| year4 | 6.4 | 3.4 | 0.4 | 0.5 | 30.7 | 0.1 | 1.4 |
| year5 | 60.6 | 5.5 | 8.9 | 11.3 | 23.0 | 71.9 | 149.9 |
| Na | 2310 | 63 | 1105 | 78 | 23 | 1354 | 104 |
| year1 | 852 | 38 | 540 |  |  |  |  |
| year2 | 38 | 6 | 32 | 20 | 5 | 0 | 1 |
| year3 | 573 | 7 | 150 | 4 | 4 | 143 | 1 |
| year4 | 67 | 5 | 25 | 4 | 6 | 1 | 0 |
| year5 | 780 | 8 | 359 | 50 | 8 | 1209 | 102 |
| K | 43 | 67 | 8 | 7 | 381 | 3 | 5 |
| year1 | 9.9 | 9.7 | 1.6 |  |  |  |  |
| year2 | 0.5 | 3.1 | 0.2 | 0.2 | 361.6 | 0.2 | 0.1 |
| year3 | 19.8 | 16.3 | 2.8 | 2.1 | 15.0 | 0.6 | 0.2 |
| year4 | 0.8 | 12.7 | 0.1 | 0.0 | 3.4 | 0.0 | 0.0 |
| year5 | 12.4 | 25.4 | 3.3 | 4.3 | 1.3 | 2.6 | 4.4 |
| P | 0.01 | 0.63 | 0.00 | 0.00 | 683 | 0.01 | 0.40 |
| year1 | 0.01 | 0.01 |  |  |  |  |  |
| year2 |  | 0.28 | 0.00 | 0.00 | 551.69 | 0.01 | 0.02 |
| year3 |  | 0.02 |  |  | 44.69 |  |  |
| year4 | 0.00 | 0.03 | 0.00 | 0.00 | 50.74 | 0.00 | 0.00 |
| year5 |  | 0.30 |  |  | 35.45 | 0.01 | 0.38 |
| S | 1899 | 622 | 1158 | 293 | 10029 | 750 | 1000 |
| year1 | 1293 | 414 | 787 |  |  |  |  |
| year2 | 35 | 54 | 68 | 55 | 446 | 235 | 318 |
| year3 | 63 | 10 | 23 | 15 | 641 | 11 | 2 |
| year4 | 96 | 108 | 45 | 36 | 6900 | 2 | 7 |
| year5 | 412 | 36 | 236 | 187 | 2043 | 502 | 672 |
| As | 0.004 | 0.009 | 0.002 | 0.003 | 39.821 | 0.005 | 0.016 |
| year1 | 0.004 | 0.005 | 0.001 |  |  |  |  |
| year2 |  | 0.003 | 0.001 | 0.003 | 19.926 | 0.005 | 0.004 |
| year3 |  |  |  |  | 6.669 |  |  |
| year4 | 0.000 | 0.001 | 0.000 | 0.000 | 6.731 | 0.000 | 0.000 |
| year5 |  |  |  |  | 6.495 |  | 0.013 |
| Cd |  | 0.646 | 0.001 | 0.000 | 1.061 |  | 0.003 |
| year1 |  | 0.258 |  |  |  |  |  |
| year2 |  | 0.065 | 0.000 | 0.000 | 0.069 |  |  |
| year3 |  | 0.098 | 0.001 |  | 0.476 |  | 0.000 |
| year4 |  | 0.099 | 0.000 | 0.000 | 0.079 |  |  |
| year5 |  | 0.126 |  |  | 0.437 |  | 0.003 |
| Co | 0.001 | 0.012 | 0.001 | 0.001 | 3.367 | 0.029 | 1.135 |
| year1 | 0.001 | 0.006 | 0.001 |  |  |  |  |
| year2 |  | 0.002 | 0.000 | 0.001 | 1.124 | 0.003 | 0.027 |
| year3 |  | 0.002 |  |  | 0.504 | 0.000 | 0.002 |
| year4 |  | 0.002 | 0.000 | 0.000 | 0.901 | 0.000 | 0.000 |
| year5 |  |  |  |  | 0.837 | 0.026 | 1.105 |
| Cr | 0.103 | 0.013 | 0.005 | 0.000 | 2.722 | 0.040 | 0.132 |
| year1 | 0.062 | 0.009 | 0.005 |  |  |  |  |
| year2 |  | 0.000 | 0.000 | 0.000 | 1.063 | 0.002 | 0.004 |
| year3 | 0.018 | 0.004 |  |  | 0.515 | 0.002 | 0.002 |
| year4 | 0.000 | 0.001 |  |  | 0.273 | 0.000 |  |
| year5 | 0.022 |  |  |  | 0.871 | 0.036 | 0.127 |
| Cu | 0.001 | 0.022 | 0.002 | 0.001 | 651 | 0.302 | 13.607 |
| year1 | 0.000 | 0.009 | 0.001 |  |  |  |  |
| year2 |  | 0.002 | 0.000 | 0.001 | 497 | 0.017 | 0.020 |
| year3 |  | 0.005 |  |  | 12 | 0.002 | 0.002 |
| year4 | 0.000 | 0.006 | 0.000 | 0.000 | 108 | 0.000 | 0.000 |
| year5 |  |  |  |  | 35 | 0.283 | 13.584 |
| Mo | 0.088 | 0.002 | 0.001 |  | 1.787 | 0.003 | 0.001 |
| year1 | 0.028 |  | 0.001 |  |  |  |  |
| year2 | 0.002 | 0.001 | 0.000 |  | 0.581 | 0.003 | 0.001 |
| year3 | 0.019 | 0.001 |  |  | 0.297 | 0.000 |  |
| year4 | 0.004 |  | 0.000 |  | 0.471 | 0.000 | 0.000 |
| year5 | 0.036 |  |  |  | 0.438 |  |  |
| Ni | 0.000 | 0.066 | 0.000 | 0.000 | 2.070 | 0.007 | 0.626 |
| year1 |  | 0.046 |  |  |  |  |  |
| year2 |  | 0.008 | 0.000 | 0.000 | 1.117 | 0.002 | 0.018 |
| year3 |  |  |  |  | 0.199 |  | 0.001 |
| year4 | 0.000 | 0.013 | 0.000 | 0.000 | 0.433 | 0.000 | 0.000 |
| year5 |  |  |  |  | 0.322 | 0.005 | 0.607 |
| Pb | 0.069 | 10.762 | 0.200 | 0.305 | 1.807 | 0.002 | 0.014 |
| year1 | 0.069 | 2.355 | 0.107 |  |  |  |  |
| year2 |  | 1.245 | 0.006 | 0.006 | 0.535 | 0.002 | 0.003 |
| year3 |  | 1.331 | 0.017 | 0.024 | 0.462 |  |  |
| year4 |  | 1.203 | 0.003 | 0.010 | 0.374 | 0.000 | 0.000 |
| year5 |  | 4.627 | 0.068 | 0.265 | 0.436 |  | 0.010 |
| V | 0.107 | 0.001 | 0.000 | 0.001 | 0.942 | 0.002 | 0.008 |
| year1 | 0.018 | 0.001 |  |  |  |  |  |
| year2 | 0.001 |  | 0.000 | 0.001 | 0.379 | 0.001 | 0.002 |
| year3 | 0.016 |  |  |  |  |  |  |
| year4 | 0.005 |  | 0.000 | 0.000 | 0.214 | 0.000 | 0.000 |
| year5 | 0.066 |  |  |  | 0.349 | 0.001 | 0.006 |
| Sb | 0.000 | 0.001 | 0.044 | 0.022 | 0.198 | 0.000 | 0.000 |
| year3 |  |  | 0.009 |  |  |  |  |
| year4 | 0.000 | 0.001 | 0.001 | 0.001 | 0.198 | 0.000 | 0.000 |
| year5 |  |  | 0.034 | 0.021 |  |  |  |
| Se | 0.002 | 0.028 | 0.000 | 0.000 | 2.943 | 0.342 | 0.164 |
| year3 |  | 0.027 |  |  | 0.985 | 0.026 | 0.005 |
| year4 | 0.002 | 0.001 | 0.000 | 0.000 | 0.079 | 0.001 | 0.004 |
| year5 |  |  |  |  | 1.879 | 0.315 | 0.155 |
| Zn | 0.095 | 86.9 | 0.049 | 0.003 | 24.4 | 0.021 | 1.257 |
| year1 | 0.034 | 30.4 | 0.019 |  |  |  |  |
| year2 |  | 6.9 | 0.001 | 0.003 | 17.6 |  | 0.004 |
| year3 | 0.004 | 12.3 | 0.003 |  | 1.7 |  |  |
| year4 | 0.001 | 20.4 | 0.001 | 0.000 | 2.5 | 0.000 | 0.004 |
| year5 | 0.055 | 16.9 | 0.027 |  | 2.6 | 0.021 | 1.249 |
| Ce |  | 0.023 |  |  | 1.046 | 0.001 | 0.032 |
| year3 |  |  |  |  | 0.206 |  |  |
| year4 |  | 0.023 |  |  | 0.146 | 0.000 |  |
| year5 |  |  |  |  | 0.694 | 0.001 | 0.032 |